## Slide 1
Itaru Nakagawa, RIKEN
March 2, 2021
Final Design and Safety Review of the INTT Ladder and Barrels
WBS: 3.01
Ladder Electronic Components

## Slide 2: Ladder Electric Components Overview
Tracking System: MVTX+INTT+TPC
Type-A
Type-B
2. FPHX Chips
HDI
Wirebonding
(silicon-FPHX)
FPHX Chip
Type-A
Type-B
1. Silicon strip sensors
INTT Full Ladder
3. HDI Readout Cable
Wirebonding
(FPHX-HDI)

## Slide 3: Silicon Strip Sensors (Hamamatsu)
Tracking System: MVTX+INTT+TPC
Type-A
Type-B
A: 16 mm (B:20 mm)
9.984mm
Single cell
f-direction
Single cell geometry (active region):
128 strips (better resolution in f-direction)
Strip width = 78 mm
f-length = 78 mm x 128 strips x 2 cells =19.97 mm
z-length = A: 16 mmx 8=128 mm
B: 20 mm x5=100 mm
128mm
Type-A (8 x 2 cells)
Type-B (5 x 2 cells)
100mm
19.97mm

## Slide 4: Silicon Strip Sensors (Hamamatsu)
Tracking System: MVTX+INTT+TPC
Type-A
AC readout pads
probe trace
40 % of pad
60 % of pad are secured for wirebonding
Type-B
Strip orientation
Read out orientation

## Slide 5: Silicon Quality Assurance (HPK/NCU)
Chart: 16×8 VI
| 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85 | 90 | 95 | 100 | 105 | 110 | 115 | 120 | 125 | 130 | 135 | 140 | 145 | 150 | 155 | 160 | 165 | 170 | 175 | 180 | 185 | 190 | 195 | 200 | 205 | 210 | 215 | 220 | 225 | 230 | 235 | 240 | 245 | 250
W7-1 | 71.46 | 107.7 | 127.9 | 140.5 | 149.8 | 157.4 | 164.3 | 170.5 | 176.1 | 182.3 | 186.7 | 191.6 | 196.2 | 200.6 | 204.8 | 208.8 | 212.6 | 216.3 | 219.9 | 223.3 | 226.6 | 229.8 | 232.9 | 235.8 | 238.7 | 241.4 | 244.1 | 246.7 | 249.2 | 251.6 | 254 | 256.3 | 258.5 | 260.7 | 262.7 | 264.8 | 266.9 | 268.8 | 270.8 | 272.6 | 274.5 | 276.2 | 278 | 279.6 | 281.4 | 283.1 | 284.7 | 286.3 | 287.9 | 289.5
W7-2 | 73.67 | 109.9 | 130.6 | 143.5 | 153.1 | 160.9 | 167.8 | 174.1 | 180.6 | 185.3 | 190.4 | 195.4 | 200 | 204.5 | 208.8 | 212.8 | 216.7 | 220.5 | 224.2 | 227.6 | 230.9 | 234 | 237 | 239.9 | 242.7 | 245.6 | 248.3 | 250.9 | 253.4 | 255.9 | 258.3 | 260.7 | 262.9 | 265.1 | 267.3 | 269.5 | 271.5 | 273.5 | 275.5 | 277.4 | 279.2 | 281.1 | 282.9 | 284.6 | 286.3 | 288 | 289.7 | 291.3 | 293 | 294.4
W8-2 | 82.55 | 100.5 | 122.4 | 135.4 | 146 | 151.3 | 158.9 | 166.9 | 171.9 | 177 | 182.1 | 186 | 191.4 | 195.6 | 200.8 | 203.3 | 207.1 | 209.2 | 214.9 | 217.6 | 220.5 | 220.9 | 227.3 | 229.7 | 233.5 | 237.7 | 238.5 | 239.9 | 243.4 | 247.8 | 249 | 253.3 | 253.1 | 255 | 257.7 | 259.7 | 262.1 | 264.3 | 266 | 268 | 269.6 | 271.7 | 273.4 | 275.2 | 277.3 | 277.8 | 280.3 | 282.2 | 283.4 | 284.9
W9-2 | 86.53 | 100.9 | 121.1 | 133.3 | 141.8 | 149.5 | 155.1 | 162.3 | 167.4 | 174.5 | 175.9 | 181.9 | 190.9 | 195.1 | 191.8 | 198.9 | 202.2 | 205.6 | 209.4 | 212.7 | 215.4 | 218.5 | 221.6 | 224.4 | 227.3 | 230.2 | 232.8 | 235.3 | 237.8 | 239.9 | 242.5 | 244.8 | 238.9 | 247.7 | 250.1 | 252.4 | 255.2 | 257.5 | 258.8 | 261.1 | 262.3 | 263.9 | 265.6 | 268.1 | 269.9 | 270.8 | 273.2 | 274.5 | 275.2 | 276.9
STEP1 Sensor by sensor performances (IV, CV) are measured Hamamatsu co. before delivery.
STEP2 Strip by strip performances are further evaluated in Taiwan for 20% fraction of silicon sensors
STEP3 QA results are kept in DB to be referred to rank ladder performance. So far most of silicons are confirmed to be good quality.
Silicon QA in Taiwan
Hamamatsu’s QA
nA

## Slide 6: FPHX Chip/Produced by FNAL
Tracking System: MVTX+INTT+TPC
Specification | FPHX
ADC/channel | 3 bits
Operation Voltage | 2.5V
Power Consumption | 64 mW
Number of channels | 128
Data Transmission | 200Mbps
Developed for Forward Vertex Detector for PHENIX at Fermi Lab.
Each FPHX chip integrates and shapes (CR-RC) signals, digitizes and sparsifies the hit channels each beam crossing (106ns beam clock), and serially pushes out the digitized data.
Front end
(Analog section)
Production 13k FPHX Chips in 2018&2019 while 3k needed for 56 ladders.

## Slide 7: FPHX Chip (Analog Section)
Tracking System: MVTX+INTT+TPC
+
_
Vref
Shaper
Integrator
Input
Comp
Vth0
Comp
Vth1
Comp
Vth7
Programmable Thresholds
Disc outputs
3-bit ADC
T-peak ~ 60 ns (programmable)
Program gain and Vref
128 channel
46, 50, 60, 67, 85, 100, 150, or 200 mV/fC
60 ns peak time (rt- pgmbl)
3—bit ADC (th-pgmbl)
Optimized to 1 to 2.5 pf input
115e + 134e/pf
~ 70 to 140 mW/ch (dep. gain)
At max. input transistor bias of 38uA: 115e + 134e/pF
Silicon strip + readout line capacitance ~ 6pF
Predicted noise ~ 115e + 134e/pF * 6pF ~ 1,000e
Signal ~ 20,000e
Expected S/N ~ 20/1

## Slide 8: FPHX Chip (Digital Section)
Tracking System: MVTX+INTT+TPC
Analog
Data Processing
Data Output
20 bit Serial data word structure

## Slide 9: High Density Interconnect (HDI) Cable
Tracking System: MVTX+INTT+TPC
INTT HDI (Manufactured by Yamashita co., Japan)
Digital GND pad
 | FVTX | INTT
# Layers | 7 | 7
Length [cm] | ~20 | 40
Pitch [mm] | 40 | 60
M20-7910342R
2 Thermistats 3pin readout
Analog GND pad
Analog and digital pads are used for grounding in case we need them.
The design is based on HDI’s of FVTX. The cable length is longer, but the pitch of the signal line is somewhat relaxed 60 [mm] instead of 40 [mm].
FVTX HDI
Dedicated Bias connectors each side
Hirose DF18 connector
Data, slow control, FPHX power
Thermistats
Notes: Conservative copy of FVTX HDI.
Length, pitch are difference.
New themostat readout.
2 bias lines is new feature. Even one line dies, the other one can survive.

## Slide 10: High Density Interconnect (HDI) Cable
Tracking System: MVTX+INTT+TPC
7 cupper layers
High signal line density in 2 layers
Solid ground outer layers to shield signal layers
L1
L2
L3
L4
L5
L6
L7
Analog GND
Clock Signal
Bias
Power
Signal
Digital GND
Thermistats & RF
Cross Section of HDI

## Slide 11: High Density Interconnect (HDI) Cable
Tracking System: MVTX+INTT+TPC
7 cupper layers
High signal line density in 2 layers
Solid ground outer layers to shield signal layers
L1
L2
L3
L4
L5
L6
L7
Analog GND
Clock Signal
Bias
Power
Signal
Digital GND
Thermistats & RF
71.3%
93.5%
6.50%
94.0%
7.2%
93.2%
4.7%
Copper Fraction

## Slide 12: High Density Interconnect (HDI) Cable
Tracking System: MVTX+INTT+TPC
Major contribution to the radiation length comes from 7 copper layers
Signal layers are effectively thin.
Total radiation length is 0.40%.
HDI | Thickness [mm] | X/X0 [%]
Copper | 38 | 0.26
Polymide | 380 | 0.14
Total | 432 | 0.40
Copper Fraction
Effective Thickness
[mm]
Material Budget of HDI Cable

## Slide 13: Successful Performance
INTT Ladders have been tested extensively in NWU/BNL/NTU test benches and beam tests at FNAL in 2018 and 2019.
Calibration responses are confirmed to be very similar to those of FVTX’s. We understood by now minor difference in response from the design difference between FVTX and INTT.
Overall satisfactory performance was confirmed from INTT ladders.

## Slide 14: Summary
• The INTT Ladder consisted of Silicon strip sensors, FPHX chips, HDIs and stave.
• The INTT Silicon strip sensors are manufactured by Hamamatsu photonics. Basic design is based on FVTX silicon strip sensors. The primary difference is the dimension of the strip and sensors. The thickness is standard 320mm. → Ready
• The HDI cable is also designed based on the one of FVTX and manufactured in Yamashita co in Japan. The cable consisted of 7 layers and signal layers are kept inner layers to be shielded by ground or bias layers. The radiation length is kept to be as low as 0.40%. Demonstrated good performance through two beam tests in 2018 and 2019. → Ready
• FPHX chips are developed by Fermi lab for FVTX detector for PHENIX. Sufficient enough FPHX chips are produced for INTT needs. Some programmable parameters will be uniquely optimized for INTT. → Ready
We are ready for the ladder mass production.

## Slide 15: Back Up

## Slide 16
The CV Measurement Circuit of INTT Sensor Testing
Measure the capacitance of single channel from AC readout pad to check the status of each channels.
Supply bias voltage to the backside of sensor. The AC signal also send to backside and measure current variety form AC pad on front side. To sure we only measure the single channel capacitance, relay matrix will ground all channels except target channel. The system and circuit are showed in right plots.
Ground the DC pad to sure the sensors are full depletion, because grounding bias ring are difficult during all chips measurement. The bottom left plot shows the difference between grounding bias ring and DC pads. The value of DC pad situation is little higher, but the trend are the same, so ground some DC pads to supply same voltage is expedient method.
AC readout
AC readout
AC readout
…
Backside
-
+
A

## Slide 17: Scratch by Probing Pads

## Slide 18
The Measurement Result of INTT Sensor Testing
Because the layout of sensor, each module is divided into four parts in the measurement. The left plot show one part result of sensor 1133-1159. All capacitance of channels are gaussian distribution, so we can identify the broken and functional channels from measurement. The left plot obviously show there are two different distributions. These differences could match to measuring period that be showed in middle plot.
The capacitance of signal channel showed in left plots is about 0.5pF, so total capacitance is about 1000pF. Compared with total sensor from HAMAMATSU’s inspection only has 7% difference. Therefore, this method could measure the capacitance of single channel.
To check why capacitances are different in periods, we analyze the relation between environment and measurement. The right plots shows the variety of capacitance with humidity at same temperature. The result shows the measurement is not obviously affected by humidity, so maybe this effect come from the status of sensor or measure system.
Two chips are remeasured in period II
Period I
Period II
Broken

## Slide 19
Summary
Even if can’t ground bias ring during whole measurement, grounding from the DC pads also could get single channel capacitance to check status od each channels.
However, the capacitance of single channel is too fine (<1.5pF), so the value could be affected by environment. From humidity study, the humidity didn’t has obvious effect, so maybe this effect come from the status of sensor or measure system.
If the capacitance are measured in short period, the values is stable. The RMS of gaussian distribution in same channel is about 0.05. Therefore, we still can use data that come from same measurement period to identify character of channels.
In first branch, all channels in sensor 1131-1159 are good. We don’t see any channel has very strange value.
The secondary branch check had started.
19

## Slide 20: HDI Material Budget
HDI | Thickness [mm] | X/X0 [%]
Copper* | 38 | 0.26
Polymide | 380 | 0.14
Total** | 432 | 0.40
*Copper thickness is not physical thickness, but average thickness.
**Total thickness is not 473μm, because of the copper average thickness.
Radiation length of each layer.

## Slide 21: Ladder Material Budget
Material | Thickness [mm] | X/X0 [%]
Silicon Sensor | 320 | 0.34
HDI | 473 | 0.39
Stave | 600 | 0.33
Total |  | 1.06
HDI | Thickness [mm] | X/X0 [%]
Copper* | 38 | 0.26
Polymide | 380 | 0.14
Total** | 432 | 0.40
*Copper thickness is not physical thickness, but average thickness.
**Total thickness is not 473μm, because of copper average thickness.

## Slide 22: High Density Interconnect (HDI) Cable
Tracking System: MVTX+INTT+TPC
~1cm
100×2MHz BCLK
Cu Layer-7
Cu Layer-1
Due to spatial limit of signal layers, some part of signal lines have to run unshielded layer-7 for a few cm.
The corresponding frequency is 10 – 30GHz, which is at least an order of magnitude higher frequency than the highest frequency (100×2MHz BCLK) signal transmits layer-7.
No problem has found in the past 2 beam test.

## Slide 23: Voltage Drop for FPHX Power
 | V@ROC | HDI [mW] | Bus Extender [mW] | Conversion Cable [mW] | DV [V] | V@FPHX
INTT | 2.5V | 135 ~ 185 | 145 | 185 | 0.20~0.25 | 2.30~2.25V
FVTX | 2.5V | 70 | 70 | N/A | ~0.1 | 2.4V
DV
Due to the long readout cable chain of INTT, the voltage drop for FPHX power line is rather severe compared to FVTX. The FPHX is designed to be operated at 2.5V.
Bus extender
Conversion cable

## Slide 24: DV for FPHX Power Solution
 | V@ROC | DV [V] | V@FPHX
INTT | 3.0V | 0.20~0.25 | 2.80~2.75V
FVTX | 2.5V | ~0.1 | 2.4V
The plan is to replace all 2.5V regulators by 3.0V ones on the backplane of the ROC. Further voltage drop is expected due to higher LVDS current operation (To be discussed by Takashi).
FPHX regulators
(total 32/ROC)