## Slide 1: sPhenix Solenoid Magnet History and Design
May 22, 2015
M. Anerella

## Slide 2: Conductor Specifications
Heavily stabilized
~ 300% margin

## Slide 3: Solenoid Coil Specifications
Pasquale Fabbricatore, April 15, 2015 email*:
the external layer is done with 188 (thin)+159 (thick) + 189 (thin) =536 turns The inner layer: 184 (thin)+164 (thick) + 183 (thin) =531 turns
* And also “as-built” notes on coil drawing
MIITS rating:??
How much will it heat without dump resistor 160K?
Peak temperature in conductor: 450K?
How much will it heat with dump resistor working, 50K?

## Slide 4: Magnet Specifications
Coil Mandrel
  Aluminum 5083
  Wall: mm
  OD Diameter: 3060mm
  Cooling tubes welded
  11 parallel tubes
  20 mm ID, 30 mm OD
Tie Rods
  Supports the cold mass
  Inconel 718
  6 x Axial Tie-rods
  16 x radial Tie-rods
Cryostat Vacuum Vessel
  Wall: Aluminum 5083, 35 mm/50mm
  OuterWall: OD 3.540 m, L=3.790m
  InnerWall: ID 2.840 m, L=3.790m
  Annular End Flanges: Al-5083, 50mm
  Tie-rods attachments
Copper Tubing
Stainless tubing
Thermal Shields, Aluminum
  8 x panels
  Inner diameter
  Outer diameter
Needs work

## Slide 5: Coil Construction
Coils wound into an external aluminum support cylinder
Internal splices: 1.5 m weld of aluminum edges + 0.2 m gap then 0.3 m solder of aluminum faces on both sides of weld
Coils epoxy impregnated into support cylinder after winding
Exiting leads: aluminum removed and NbTi soldered to heavy copper stabilizer leads (overlapping aluminum)

## Slide 6: Coil Cooling
Aluminum Cooling tubes
Ø30 mm x 5mm thick, flattened to 22 mm
Stitch welded to Aluminum mandrel
11 parallel circuits
Manifolds top & bottom
Coils are in insulating vacuum
Conductively cooled via external support cylinder

## Slide 7: Outer Heat Shield (similar construction for Inner Heat Shield)

## Slide 8: Coil Mechanical Support
Inconel Tie Rods:
8 tangential, 3 axial, at each end
Upper tangential rods (8 total) loose at 300K
Lead End axial rods (3) loose at 300K
Thermal contraction of Al at 4K tightens rods, shifts coil
Motion accommodated by spherical, belleville washers

## Slide 9: Support Loading
horizontal
vertical

## Slide 10: Valve box
Vacuum vessel+
  Design pressure:
  internal 1 barg [psia], external 1 atm
  Design Temperature: 300K
  Diameter: 970 mm, 38.25inch
  Length: 860 mm, 33.85 inch
  Wall: 10 mm, 0.393 inch
  End plate: wall 20mm,
  Volume: 635Liters
  Stainless Steel 304
Chimney
  Diameter: 273 mm, 10.75inch
  Length: 1065 mm, 42 inch
  wall 9.3 mm, ”
  Volume: 63 Liters
  Stainless Steel 304
Needs work

## Slide 11: Back-up slides

## Slide 12: Tie rod strain gauge installations

## Slide 13: Strain Gauge Info
SC Solenoid Magnet is at SLAC
  BNL heat shield shipping restraints are fabricated & received at SLAC
  SLAC has:
    Installed BNL restraints
    Tightened coil supports
  SLAC will:
    Rig magnet onto truck

## Slide 14: Incoming inspections & tests
300K Coil Electrical Testing:
R, L and Q
Impulse test
520V Hypot
Instrumentation inspections; voltage taps, strain gauges, etc.
Mechanical Inspections:
Visual (damage or other shipping incidents)
Helium circuit vacuum leak check
Cryostat vacuum leak check
Coil position alignment (by re-tightening tie rods by prescribed amounts)