## Slide 1
Ladder from Taiwan
Test & Inspection
Rachid Nouicer, Milan Stojanovic

## Slide 2
Bench Test South Side

## Slide 3
South Side (Modul 51) – Bias = 100V at BNL
Calibration
Amplitude vs Channel
Number o entries
Current A = 140 nA Current B = 110 nA

## Slide 4
Bench Test North Side

## Slide 5
North Side (Module 264) – Bias = 100V at BNL
Calibration
Amplitude vs Channel
Number o entries
Current A = 220 nA Current B = 2.3 μA

## Slide 6
South Side (Module 51) – Bias = 100V at Taiwan

## Slide 7
North Side (Module 264) – Bias = 100V at Taiwan

## Slide 8
Visual Inspection at BNL

## Slide 9
Visual Inspection
The ladder safely arrived at BNL
No damages during transportation observed

## Slide 10
Visual Inspection
Dust on the ladders observed

## Slide 11
Visual Inspection
Dust on the ladders observed

## Slide 12
Visual Inspection
Wire bonding issues

## Slide 13
Visual Inspection
Encapsulation issue

## Slide 14
Visual Inspection
Gluing issue
  There is no glue between the HDIs
Taiwan Ladder
BNL Ladder

## Slide 15
Visual Inspection