## Slide 1
27th OCTOBER 2021
EIC Solenoidal Magnet Design
Progress
V.Calvelli
Contributors
CEA : V. Calvelli, C. Berriaud, C.Mayri, M. Segreti, F. Stacchi, L. Quettier
JLAB : R. Rajput-Ghoshal, R. Fair, G.Probir, E. Sun, R. Ent BNL : E. Aschenauer, A. Kiselev
Notes: Saisir les champs « Titre », « P. Nom » et « Date.
Laisser ou retirer le bandeau.

## Slide 2: Open questions from summer 2021
CS
BS
FS
ATHENA Proposal Committee-detector concept&integration sub-group – October, 27 2021
DIRC
SOLENOID
FS
BS
Open questions:
Which magnet design? - Solenoidal Configuration - Helmholtz Configuration
What kind of conductor? - NbTi Rutherford with Al stabilizer - NbTi Rutherford with Cu stabilizer
What is the impact of the calorimeters?
How to reduce the asymmetrical forces (1.3 MN)?
Parameter | Values
BIP (T) | 3.15
Bpeak (T) | 4.35
Coil thickness (mm) | 200
Energy (MJ) | 183.9
H TCP 2 (%) | 6.61
H FLAT 1 (%) | 25.12
Projectivity (T/Amm²) | 14.82
Parameter | Values
BIP (T) | 2.97
Bpeak (T) | 4.84
Coil thickness (mm) | 200
Energy (MJ) | 235.7
H TCP 2 (%) | 4.83
H FLAT 1 (%) | 16.37
Projectivity (T/Amm²) | 17.51
Magnetic field map released 28/05/2021
Magnetic field map released 07/05/2021
25.3 tons
73.1 tons
Easier to wind
Lighter & more transparent
Few producers in the world
Solenoidal configuration
Helmholtz configuration

## Slide 3: ANSWERS
CS
BS
FS
ATHENA Proposal Committee-detector concept&integration sub-group – October, 27 2021
DIRC
SOLENOID
Parameter | Values
BIP (T) | 3.15
Bpeak (T) | 4.35
Coil thickness (mm) | 200
Energy (MJ) | 183.9
H TCP 2 (%) | 6.61
H FLAT 1 (%) | 25.12
Projectivity (T/Amm²) | 14.82
Solenoidal configuration
Re-arrangement of the calorimeters material composition
Adjustment of the magnet position
Adjustment of the calorimeters position
To balance the forces between the calorimeters and the magnet

## Slide 4: SOCRATE
ATHENA Proposal Committee-detector concept&integration sub-group – October, 27 2021
DIRC
SOLENOID
SOlenoidal Coils with Rutherford cAble in nbTi for the EIC

## Slide 5: THE ENVIRONMENT OF SOCRATE – THE CALORIMETERS
ATHENA Proposal Committee-detector concept&integration sub-group – October, 27 2021
DIRC
SOLENOID
Respect to the version of July
Magnet is shifted
of Z = -25 cm respect to IP
to give more space to the RICH
Barrel Hcal is:
Symmetric respect to the IP
50 cm longer
Total length is now 9500 mm

## Slide 6: THE ENVIRONMENT OF SOCRATE – THE CALORIMETERS
Endcaps Hcal are made of:
51 layers of 2 cm steel and 50 x 3.5 mm gap,
the gaps are 3 mm scintillator and 0.5 mm air
Layers can be made in:
Iron  impact on the fringe field / forces
Stainless steel  no magnetic interaction
ATHENA Proposal Committee-detector concept&integration sub-group – October, 27 2021
Respect to the version of July
Barrel Hcal has:
2 different structure (Inner / Outer)
83 %
70 %
85 %
85 %
IRON / Volume fraction
85 %
85 %
83 % / 70 %
83 %
Starting point
Optimization of the iron in the endcaps to balance the axial forces

## Slide 7: THE ENVIRONMENT OF SOCRATE – THE CALORIMETERS
ATHENA Proposal Committee-detector concept&integration sub-group – October, 27 2021
Flux Plate
(100% iron)
Lepton Hcal
(SS)
Outer Barrel
Inner Barrel
Filler
Hadron Hcal
Outer Barrel
Inner Barrel
25 cm
Hadron Hcal
Flux Plate
(25 cm)
Lepton Hcal (70 cm)
Filler
2D model
3D model
Only ferromagnetic parts are shown

## Slide 8: Preliminary MAGNETIC RESULTS & DESIGN
ATHENA Proposal Committee-detector concept&integration sub-group – October, 27 2021
Parameter | Value | Old version | Units
B0 | 3.02 | 3.13 | T
B peak | 4.19+0.27 | 4.35+0.27 | T
Energy | 175.5 | 183.9 | MJ
B @ Z = -5.6 m | 10.5 | - | mT
B @ Z = 7.2 m | 5.2 | - | mT
B @ R = 3.4 m | 24.8 | - | mT
H TPC 1 | 16.2 | 6.61 | %
H FLAT 1 | 27.5 | 25.12 | %
Proj | 10.4 | 14.8 | T/Amm²
Fz | 37 | 13500 | kN
4.45 T

## Slide 9: Iron saturation & fringe field
ATHENA Proposal Committee-detector concept&integration sub-group – October, 27 2021
Barrel is saturating  fringe field outside the magnet comes from here
No more margins in dimensions 
Check with the other equipment / experiments possible solutions

## Slide 10: Preliminary CONDUCTOR DESIGN
ATHENA Proposal Committee-detector concept&integration sub-group – October, 27 2021
JE=Iop/Acond = 24.7 A/mm2
Acond = 389 mm2
Yield strength @ 4.2K → 110 MPa
(Atlas, Mu2e conductor Al stabilizer)
Easier to fabricate and wind respect to the old version
4 layers in the solenoids

## Slide 11: Preliminary CONDUCTOR DESIGN
ATHENA Proposal Committee-detector concept&integration sub-group – October, 27 2021
Design input |  | 
Temperature | 4.5 | K
Max field (+ self field) | 4.18+0.3 | T
Margin of load line | 35% | 
Dump voltage | 1000 | V
Cable input |  | 
Jc(T,B) | Bottura fit* | 
N° strands | 40 | 
Cu/Sc ratio | 1.3 | 
RRR Cu | 100 | 
Conductor output |  | 
Iop | 9.6 | kA
Jc | 987 | A/mm2
Øst | 0.84 | mm
Temperature Margin | 1.96 | K
Aspect ratio | 1.6 | 
Hot spot temperature | 50.5 | K
Stabilizer input |  | 
5N AlNi0.1% | Micro-alloying CW 20% | 
Current density | 24.7 | A/mm²
Nb layers | 4 | 
RRR Al | 500 | 
Insulation thickness | 0.5 | mm
*parameters for the fit (C.R. Spencer)
Bc20 | 14.5 [T] | α | 0.57
Tc0 | 9.2 [K] | β | 0.9
n | 1.7 | γ | 1.9
C0 | 73000 [TA/mm²] |  | 
Chart: Load line
| 4.4571999999999994
Working point | 986.7994
Jc @ 4.2 K | 9220.1055 | 6203.7886 | 4667.3998 | 3637.4662 | 2855.6636 | 2217.77 | 1671.4499 | 1185.9851 | 740.0191 | 312.5152 | 0 | 0 | 0
Jc @ 4.5 K | 8640.0242 | 5782.2852 | 4320.6809 | 3337.249 | 2588.0771 | 1974.5336 | 1446.8071 | 975.1303 | 537.3593 | 102.687 | 0 | 0 | 0
Jc @ 6.46 K | 4523.1252 | 2806.8668 | 1884.9914 | 1235.748 | 715.9774 | 258.3934 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Load line | 0 | 986.7994 | 1516.7579 | 3099.5226
35% margin is the same of CMS  good for operating safely

## Slide 12: Preliminary MECHANICAL DESIGN
ATHENA Proposal Committee-detector concept&integration sub-group – October, 27 2021
2D axisymmetric mechanical model
In red: coils In blue: support structure
(thickness = 50 mm)
Boundary condition:
Top of the support structure is blocked in z
Contact conditions:
coils/support structure  sliding contact with possible separation

## Slide 13: Preliminary MECHANICAL DESIGN
ATHENA Proposal Committee-detector concept&integration sub-group – October, 27 2021
Cool down + Energization (via magnetic forces at each of the conductor nodes) + orthotropic conductor are taken into account for calculations
Materials | Young’s modulus (GPa) | Poisson’s ratio n | Integrated thermal shrinkage from 293 K to 4 K | 2/3 of the Yield stress for security margin (MPa)
Al (conductor stabilizer) | 78 | 0.34 | 4.15 10-3 | 70
Reinforced Al (support structure) | 78 | 0.34 | 4.15 10-3 | 135
Main material properties at 4K
x
y
z
Cartesian coordinate system
Materials | Young’s modulus (GPa) | Poisson’s ratio n | Integrated thermal shrinkage
Cu/NbTi composite | 128 | 0.35 | 2.65 10-3
Al | 78 | 0.34 | 4.15 10-3
Glass epoxy (G-10) | 42 (warp) 20 (normal) | 0.25 0.34 | 2.41 10-3 7.06 10-3
Conductor material properties at 4K
Young’s moduli Ex, Ey, Ez (GPa) | Poisson’s ratios nxy, nxz, nyx, nyz, nzx, nzy | Shear moduli Gxy, Gyz, Gxz (GPa) | Integrated thermal shrinkage
72, 73, 78 | 0.34, 0.33, 0.33, 0.32, 0.35, 0.35 | 18, 26, 25 | 4.11 10-3

## Slide 14: Preliminary MECHANICAL DESIGN
ATHENA Proposal Committee-detector concept&integration sub-group – October, 27 2021
Cool down
Peak Von Mises stress at 4K
= 10 MPa in coils
(< spec of 70 MPa)
= 8 MPa in Al support structure
(< spec of 135 MPa)
Peak Von Mises stress at energization
= 63 MPa in coils
(< spec of 70 MPa)
= 73 MPa in Al support structure
(< spec of 135 MPa)
Energization
50 mm thick reinforced Al support structure

## Slide 15: PRELIMINARY CRYOGENICS DESIGN SCHEME
ATHENA Proposal Committee-detector concept&integration sub-group – October, 27 2021
1680
2100
3000
4000
Magnet + insulation
Rint : 1680 mm
Rext :2100 mm
L : 3720 mm
Chimney
R : 50 mm
L : 1100 m
Reservoir
1000 * 500 * 2000 mm3
S=7 m²
S=0.35 m²
S=98 m²
Surfaces
 | 4.5 K Level Static / Dynamics | 45 K – 80 K Level Static / Dynamics
Radiative Losses |  | 
Radiation on the cold mass (0.3 W/m²) | 30 | 
Radiation on the reservoir (0.1 W/m²) | 0.7 | 
Radiation on he screens (3 W/m²) |  | 300
Conductive Losses |  | 
Cold mass support | 0.4 | 5
Screen support |  | 20
Piping |  | Tbd
Cryogenics valves | 2 | 20
Instrumentation | Tbd | 
Current leads | Tbd | 
Electric Losses |  | 
Joints | 3 | 
Foucault currents on the mandrel | Tbd | 
Foucault currents on the screens |  | Tbd
TOT | 36.1 | 345

## Slide 16: COLD MASS THERMOSIPHON
ATHENA Proposal Committee-detector concept&integration sub-group – October, 27 2021
2 times 10 pipes over ½ perimeter
Space between pipes : 400 mm
DT in the mandrel (Al 5083) (200 mm) : 16 mK
Collector diameter: F = 21.3 x 1.6 mm
Inner diameter : 8 mm
Tank riser : 500 mm
Flux in every pipe: ~0,6 g/s

## Slide 17: SCREEN CIRCUIT – EXTERNAL PANELS + FLOOR
ATHENA Proposal Committee-detector concept&integration sub-group – October, 27 2021
5 loops spaced by 1.4 m
DT inside a 3 mm panel of (Al3003) : ~2.5 K
insulators
260 W to extract between 45 et 80 K (15 b)
 ~1 g/s

## Slide 18: SCREEN CIRCUIT – INTERNAL PANEL
ATHENA Proposal Committee-detector concept&integration sub-group – October, 27 2021
Cooling by conduction from the ends
DT inside a 5 mm (Al1050) panel : ~2 K
insulators
85 W to extract between 45 et 80 K (15 b)
 0.35 g/s

## Slide 19: PRELIMINARY MASS BUDGET AND ASSEMBLY
H Cal
coils
Coil former & mechanical support
Cryostat with
MLI
Thermal shields
Solenoidal Configuration | Volume (m3)
SS* | 3.214
Cu (thermal shield) | 0.970
MLI | 3.183
Al | 2.632
Coil NbTi | 0.2161
Coil Insulation | 0.8719
Conductor Stabilizer (Al) | 7.2621
ATHENA Proposal Committee-detector concept&integration sub-group – October, 27 2021

## Slide 20: CONCLUSIONS
Preliminary Conceptual Designs are OK
No major issues
Fringe field  understand what are the margins respect to the other equipment / experiments
Time to move towards a detailed design
ATHENA Proposal Committee-detector concept&integration sub-group – October, 27 2021

## Slide 21
Direction de la Recherche Fondamentale
Institut de recherche
sur les lois fondamentales de l’Univers
Commissariat à l’énergie atomique et aux énergies alternatives
Centre de Saclay | 91191 Gif-sur-Yvette Cedex
Etablissement public à caractère industriel et commercial | R.C.S Paris B 775 685 019
Notes: Saisir le champ « Service »