## Slide 1: New Sensor Wafer Production by BNL IO
8/3/2022
Gabriele Giacomini
https://indico.bnl.gov/event/16500/

## Slide 2
 |  |  |  |  | New Layout (July 2022) |  | 
 | 2x2 mm2 |  |  |  |  |  | 
 | pitch | gap |  |  |  |  | 
7x | 200 | 100 |  |  | 4x4 pixels, 500um pitch, for EICROC |  | 
 | 5x5 mm2 |  |  |  |  |  | 
 | pitch | gap |  |  | pitch | gap | 
7x | 500 | 300 |  |  | 500 | 300 | 
7x | 300,200,100 | 150,100,50 | multipitch |  | 500 | 400 | 
 | 5x10mm2 |  |  |  |  |  | 
 | pitch | gap |  |  | pitch | gap | 
6x | 500 | 300 |  | 4x | 500 | 350 | 
6x | 300,200,100 | 150,100,50 | multipitch | 6x | 500 | 400 | 
2x | 500 | 400 |  | 6x | 500 | 450 | 
2x | 500 | 200 |  |  |  |  | 
 | 5x25mm2 |  |  |  |  |  | 
 | pitch | gap |  |  | pitch | gap | 
2x | 500 | 300 |  | 5x | 700 | 500 | 2.5mm long pixels
2x | 300,200,100 | 150,100,50 | multipitch | 5x | 700 | 600 | 2.5mm long pixels
2x | 700 | 350 | 2.5mm long pixels |  |  |  | 
1x | 700 | 450 | 2.5mm long pixels |  |  |  | 
1x | 500,300 | 350,200 | 2.5mm long pixels, multipitch |  |  |  | 
2x | 500,300 | 250,150 | 2.5mm long pixels, multipitch |  |  |  | 
Layout #1
Old ACLGADstrip wafer,
Metal (and GLASS) to be modified
4 wafers in fabrication (2 50um + 2 20um)
Old layout

## Slide 3
AC-LGAD pro EIC ROC test (wire-bond)
500um pitch, metal width = 200um
Layout #1

## Slide 4
Layout #2
EICROC bump-bond compatible
1cm x 1cm
0.5cm x 0.5cm
0.2cm x 0.2cm
Compatible with EICROC
+ test structures
Metal not designed yet, but lithos can start with:
1- JTE
2- Nresistive
3- gain
4- contacts
Starting wafers: 50, 30, 20 um thick substrates

## Slide 5
Layout #2
EICROC bump-bond compatible - #1
EIC ROC pads
Guard Ring Bumps
N+ Bumps

## Slide 6
Layout #2
EICROC bump-bond compatible - #2
EIC ROC pads