## Slide 1
Lucas Brouwer
Lawrence Berkeley National Laboratory
Superconducting CCT Magnets: A Flexible Technology for Compact FFA’s
September 14th, 2023
2023 Workshop on Fixed Field Alternating Gradient Accelerators

## Slide 2: Outline
introduction to the Canted-Cosine-Theta (CCT) magnet design
incorporating alternating gradients into a continuous coil (AG-CCT)
Introduction to CCT
Background
Introduction to the AG-CCT
Alternating gradients for large ∆p/p with fixed-field
HEP high-field (straight), ARDAP project for proton therapy (curved)
The AG-CCT for fixed-field return arc design
A 2.4 T curved dipole magnet
Status
Plans
Flexible generation of combined function fields for curved and straight magnets
Nb3Sn + HTS magnets
Combined function CCT’s relevant to FFA’s

## Slide 3: Abbreviated History of the Concept (HEP focused)
1970, basic concept published
~2000-2015, revisited by industry and labs
Highlights: extension to combined function + curved magnets, low current demonstrators ~2-3 T
~2015-now, push for high field Nb3Sn magnets + CCT’s going into accelerators
Highlights: 8-10 T Nb3Sn dipoles at LBNL/PSI, NbTi orbit correctors for HiLumi LHC

## Slide 4: Canted-Cosine-Theta (CCT) SC Magnets
Advantages
excellent field quality (to large % of aperture)
stress management for high-field and/or large apertures
combined function fields (i.e. dipole + quadrupole)
Challenges
slightly more conductor (~15-20%)
tradeoff of longer ends vs. efficiency for very short magnets
D.I. Meyer, R. Flasck, 1970, doi.org/10.1016/0029-554X(70)90784-6

## Slide 5: The CCT is a Flexible Technology for Combined Function Fields
n=1, dipole
n=2, quadrupole
n=1, 2, 3, dipole+quad.+sext.

## Slide 6: Example: Combined Function Dipole + Quadrupole (40 mm ø)
-12 mm
12 mm
4.36 T
2.91 T

## Slide 7: The CCT Naturally Extends to Curved Magnets
Dipole Quadrupole Sextupole
Single winding combined function: dipole+quad.+sext.

## Slide 8: The alternating gradient CCT (AG-CCT) is a method for producing alternating gradient fields with continuous windings instead of separate magnets
Quadrupole fields along the bend, blue is produced by AG-CCT and dash-black is desired integral
Example: 5 section AG-CCT layer (FDFDF)
W. Wan, et al., PRAB, 2015, https://doi.org/10.1103/PhysRevSTAB.18.103501
Compact nesting of ends

## Slide 9: Magnetic design of curved CCTs: in toroidal (binormal) coordinates you can derive the relation between the winding path and the toroidal harmonics (but is it useful?)
Parametrization of winding path
Current density sheet (pitch averaged)
Field harmonics (arbitrary combinations allowed)

## Slide 10: Instead, parameterize the CCT geometry in the beam dynamics software COSY INFINITY
Initial Hard Edge Model
Motivation: analytic coil design in curved frame is difficult, but coil parameterization is straight-forward
Directly connects coil geometry to beam optimization (eliminates field parameterization in curved system)
Biot-Savart model includes all end effects and coil transitions
generate “seed” set of curved CCT winding coefficients approximating hard-edge solution
example: W. Wan et. al., 2015, doi.org/10.1103/PhysRevSTAB.18.103501
Biot-Savart Model from Coil Parameterization

## Slide 11: Outline
US-MDP program for Nb3Sn and HTS magnets
AG-CCT design for proton therapy
fabrication and test of curved dipole layers
Introduction to CCT
Background
Introduction to the AG-CCT
Alternating gradients for large ∆p/p with fixed-field
HEP high-field (straight), ARDAP project for proton therapy (curved)
The AG-CCT for fixed-field return arc design
A 2.4 T curved dipole magnet
Status
Plans
Flexible generation of combined function fields for curved and straight magnets
Nb3Sn + HTS magnets
Combined function CCT’s relevant to FFA’s

## Slide 12: Metallic Winding Mandrels Accurately Position the Conductor and Intercept Lorentz Forces for Stress Management
Force accumulation in traditional Cos(θ)
CCT ribs intercept force
Important for high field magnets with strain sensitive conductor (Nb3Sn/HTS)
Important for large aperture magnets

## Slide 13: Nb3Sn and HTS CCT Dipole Development at LBNL (within the HEP - US Magnet Development Program)
CCT3,4,5: 9.2 T, 90 ø (2015-2018)
CCT6: 13 T, 120 ø (2026)
Nb3Sn: 9 T demonstrated in a 90 mm bore, 13 T to be demonstrated in a 120 mm bore in ~3 years
D. Arbelaez et. al, 2022, doi.org/10.1109/TASC.2022.3155505
X. Wang et al., 2021, doi.org/10.1088/1361-6668/abc2a5
T. Shen et al., 2022, DOI: 10.1103/PhysRevAccelBeams.25.122401
HTS: demonstrated 1.5-3 T, future focus is hybrid ~15 T (HTS+Nb3Sn)
C2: 3 T, 60 ø (2021) - REBCO
BIN5c: 1.6 T, 31 ø (2021) – Bi2212
subscale: 5 T, 50 ø (now)

## Slide 14: ARDAP Accelerator Stewardship project to develop a large momentum acceptance SC gantry for proton therapy
L. Brouwer, et al., IEEE Trans. Appl. Supercond, 2017, https://doi.org/10.1109/TASC.2016.2628305
A single AG-CCT magnet provides 1:1 imaging from the degrader source to patient (with large momentum acceptance)

## Slide 15: Large momentum acceptance beam optics with a single, 5 T magnet for proton therapy gantries (70-250 MeV)
Four layers
Lay12: AG-CCT
Lay34: CCT dipole
Alt. Quadrupole (± 22.7 T/m)
Const. Dipole (2.3 T)
-6% dp/p
+11% dp/p

## Slide 16: A reduced bend prototype for a first test
Alternating Quadrupole (± 22.7 T/m)
Constant Dipole (2.3 T)
Four layer CCT design with large acceptance (20%)
2.4 T dipole in 290 mm aperture (reduced bend angle)
Fabrication and test of two dipole layers

## Slide 17: Baseline technology established for design, fabrication, and test of high-curvature CCT magnets with very large apertures

## Slide 18: A prototype magnet consisting of the two dipole layers reached the design field in a liquid helium bath (4.5 K)
The magnet reached nominal current after 17 quenches (60% of wire short-sample)
onset of electrical damage to outer layer which leads to end of testing
peak current of 1008 A
10 minute hold at nominal current
2.4 T dipole field in very large aperture (290 mm) with tight bend radius (ρ=0.9 m)
L. Brouwer et al., “Design and test of a curved superconducting dipole magnet for proton therapy,” NIM-A, vol. 957, p. 163414, Mar. 2020, https://doi.org/10.1016/j.nima.2020.163414
LBNL: L. Brouwer, S. Caspi, J. Herrera, J. Swanson, M Maruszewski, M. Marchevsky, K. Edwards, J. Taylor, W. Wan, S. Prestemon, X. Wang, C. Myers, S. Myers, R. Hafalia, M. Turqueti, C. Sun, D. Robin, M. Reynolds, A. Hodgkinson, T. Lipton
Varian Medical: A. Godeke, M. Schillo, A. Huggins, R. Nast
Paul Scherrer Institute: M. Schippers, A. Gerbershagen, C. Calzolaio, S. Sanfilippo

## Slide 19: Outline
new program to build and test combined function CCT magnets relevant to FFA’s
Introduction to CCT
Background
Introduction to the AG-CCT
Alternating gradients for large ∆p/p with fixed-field
HEP high-field (straight), ARDAP project for proton therapy (curved)
The AG-CCT for fixed-field return arc design
Combined function CCT’s relevant to FFA’s
A 2.4 T curved dipole magnet
Status
Plans
Flexible generation of combined function fields for curved and straight magnets
Nb3Sn + HTS magnets

## Slide 20: We have new R&D funding to develop combined function CCT magnets (relevant to FFA applications)
  Near term: solidify design parameters for the prototype magnet within 1 year.
  Combined function CCT’s map onto existing layouts
  New accelerator layouts leveraging the AG-CCT?
  Goals for five year program:
  develop the technology for combined function, superconducting CCT magnets
  build and test a prototype magnet to demonstrate performance in the 5-7 T range
  Question for this workshop - what do you see as the key aspects of SC magnet technology which needs to be demonstrated for future FFA’s?

## Slide 21: Summary
CCT is flexible design for combined function fields in straight and curved geometries
The AG-CCT integrates alternating gradients into a single magnet
8-10 T Nb3Sn dipoles for HEP (US-MDP)
2.4 T curved NbTi dipole for proton therapy
13 T, 120ø Nb3Sn dipole
plan to build and test ~5 T combined function CCT magnets relevant to FFA’s (now is an excellent time for community feedback)
Introduction to CCT
Background
Introduction to the AG-CCT
Alternating gradients for large ∆p/p with fixed-field
HEP high-field (straight), ARDAP project for proton therapy (curved)
The AG-CCT for fixed-field return arc design
A 2.4 T curved dipole magnet
Status
Plans
Flexible generation of combined function fields for curved and straight magnets
Nb3Sn + HTS magnets
Combined function CCT’s relevant to FFA’s

## Slide 22
Backup Slides

## Slide 23: Focus on scoping the AG-CCT design to 1.2, 2.4 GeV/c passes in collaboration with LBNL’s Accelerator Modeling Program (AMP)
K. M. Black et al., “Muon Collider Forum Report.”, 2023, http://arxiv.org/abs/2209.01318

## Slide 24: Focus on scoping the AG-CCT design to 1.2, 2.4 GeV/c passes in collaboration with LBNL’s Accelerator Modeling Program (AMP)
B0 = 1.725 T
G = 87.67 T/m
φtot = 30 deg
φsplit = 3.95, 6.0, 10.11, 6.0, 3.95
aperture = 100 mm
ρ = 3.02 m
For reference energy

## Slide 25: Harmonics along the length for coil design based on SCOFF model (at 30 mm reference radius – 60% of aperture)
B3 integrates to zero through ends
B4 integrates to zero through ends

## Slide 26: In plane fields for perfect sectioning + peak field on conductor
Quad Layers
Dipole only
Combined
Peak field on the conductor is 7.5 T, a 23% rise (from 6.11 T of dipole+gradient)
4.5 T
-4.5 T
1.76 T
6.25 T

## Slide 27: These fields are a bit high for Nb-Ti, but feasible with respect to conductor performance (the LHC NbTi cable is a good reference)
36 strands of 0.825 mm wire (15.1 mm thick)
Short-sample assuming LHC NbTi cable
Test winding into old AG-CCT mandrel

## Slide 28: Momentum Acceptance Addresses a Key Technical Risk (Fast Field Ramping)
Fast depth scanning with beam energy is desired during treatment
some tumors can be treated at fixed-field
order of magnitude reduction in magnet field ramping for worst-case scenario
3.73 cm
7.96 cm
15.75 cm
Magnetic rigidity settings
1.19
1.50
1.87
With a large momentum acceptance, each magnet setting covers a range of treatment energy (e.g. 20% dp/p)



## Slide 29: Hall probes verified the design field at nominal current, a more complicated measurement system is required for future field quality characterization determining the harmonic content
H1
H4
H5
At 4.5 K and nominal current of 922 A
probes/predicted agree within error on center axis: H1, H4, H5
probes/predicted fall slightly outside error off center axis: H2,H3
Measurements by C. Myers and X. Wang