## Slide 1
Multiatmopshere CO2 amplifier optically pumped by a 4.3 mm Fe:ZnSe laser
(AE85 funded by DoE Accelerator Stewardship grant)
Sergei Tochitsky, Dana Tovey, Jeremy Pigeon, Chan Joshi
Department of Electrical Engineering, UCLA
Igor Pogorelsky, Mikhail Polyanskiy
Brookhaven National Laboratory, USA
Sergei Mirov, V Fedorov
University of Alabama at Birmingham

## Slide 2
Motivation
Neptune Laboratory
Particle Acceleration using relativistic laser pulses
  Ponderomotive force scales as I2
    a0=1 I=1016W/cm2 (CO2) ≈ 1018W/cm2 (1µm)
Plasma Based Ion Accelerators
  Overdense plasma phenomena in range ne = 1-10ncr (ncr=1019 cm3) can be easily realized in an ionized gas .
Laser Wakefield Accelerators
  Need subpicosecond 0.3-0.5 ps multi-TW mid-IR pulses.
ATF -2023
Despite demonstrated 15 TW, 3 ps (UCLA) and 5 TW, 2 ps (BNL) CO2 lasers,
subpicosecond multi-TW laser-driver is yet to be developed. Both
bandwidth and repetition rate are limited by pulsed power technology.
Notes: 2

## Slide 3
10.4
10.6
10.8
11
0
0.2
0.4
0.6
0.8
1
Normalized Gain
1atm
10.4
10.6
10.8
11
Wavelength (
m
m)
CO
2
Gain Spectrum
10atm
10.4
10.6
10.8
11
20atm
Recipe for success: High-gain CO2 laser
Population of 001 level Maximized
Population of 100 level Minimized
Optically Pumped CO2 Laser
Normalized Ampl..
Wavelength (mm)
~1.2THz
CO2 Molecule
ATF -2023

## Slide 4
Modeling of Ultrafast Pulse Amplification
4.3 mm
Laser
10-15 atm
Isotope CO2
Amplifier
10 mm pulses
500 fs
10 GW
10 mm
<300 fs
OPA
Seed
Feasibility study of a compact GW class
CO2 amplifier and gain dynamics.
D. Tovey et al. Appl. Opt., 58, 5756, 2019,
0.5 ps seed
2 mJ, ~1.0 ps
(FWHM)
ATF -2023

## Slide 5
Z. Biglov, et al MSU, Bulletin of the Academy of Sciences of the USSR, 55, 135 (1991).
Multi-isotopic Mix at 15 atm can support
100 fs, 10 mm pulses
CO2 gain profile
ATF -2023
Optically pumped high-pressure mix of several stable isotopic CO2 + He can become a viable gain medium for 0.3-0.5 ps mid-IR pulses.
M. Polyanskiy, et al “High-peak-power long wave infrared lasers with CO2 amplifiers”, Photonics, 8, 101 (2021).
ATF Path to multi-TW, 0.5 ps pulses for LWFA requires a few mJ, 300 fs, 9.2 mm seed.
Gain Tailoring in Isotopic CO2 amplifier

## Slide 6
Group of Prof. S. Mirov
Tunable 3.9-5 mm Fe:ZnSe source for
Optical Pumping of the CO2 laser
ATF -2023

## Slide 7
Group of Prof. S. Mirov
Tunable 3.9-5 mm Fe:ZnSe source for
Optical Pumping of the CO2 laser
ATF -2023
D. Martyshkin, et al “Room temperature, nanosecond, 60 mJ/pulse
Fe:ZnSe master oscillator power amplifier system operating at
3.8-5.0 µm,” Opt. Express 29, 2387-2393 (2021).

## Slide 8
Fe:ZnSe
laser
Lens
NaCl
Optically pumped CO2 cell
DM
Calorimeter
Lens
HCT detector /
Calorimeter /
Pyrocamera
10 μm lasing
10 μm filter
DM
Diffraction grating
4.3 μm pump: 50 mJ, 150 ns
9.3 mm
4.3 μm pump
9.3 mm
10 μm lasing
15 atm
Optically Pumped 10-15 atm CO2 Laser
A 10-cm long high-pressure CO2 cell.
ATF -2023
Neptune Laboratory
Notes: Is it ok that we don’t show reflection off diffraction grating (when used as output coupler)?
Should I make FZS box smaller? Put on right maybe?
Got new beam profile for 15 atm lasing but using old beam profile for FZS pump beam (should I get new one?)

## Slide 9
With >35 mJ absorbed at 4.4 mm , up to 3.5 mJ at 10.3 mm lasing measured in a palm-size the CO2 cell.
Lasing and Gain Dynamics in OP CO2 cell
Achieving lasing at high pressures required greater amounts of CO2 and tuning pump wavelength to reduce absorption, D. Tovey et al, Optics Express, 29 (2021).
Neptune Laboratory
ATF -2023

## Slide 10
Repetition Rate Scaling in OP CO2 Laser
Visible He-Ne beam deflectometry shows fast heat dissipation in the multiatmosphere CO2 cell. Repetition rate ~1 kHz is durable.
  Measurements of lasing and gain of a high-pressure optically pumped CO2 laser
  >10% efficiency near 10 atm
  >10% small signal gain
  Can be scaled to 1 KHz – limited by gas dynamics
Neptune Laboratory
ATF -2023
Notes: - What pressure/mix should I show for absorption spectrum (a) ?

## Slide 11
Two-color 0.8 and 10 mm ultrafast laser system
Neptune Laboratory
12’ x 5’ optical table
Element
Spitfire Ace
Pulse Width: 1ps
Repetition Frequency: 1kHz
Ascend
Ascend
Spitfire Ace
Pulse Width: 35fs
Repetition Frequency: 1kHz
Ascend
External Compressor
Translation
PD
Element Seed Kit
BS
HE Topas
NDFG
TOPAS 800
ATF -2023
2022 Femtosecond/Picosecond Ti:sapphire system at the UCLA Neptune Laboratory

## Slide 12
Two-color 0.8 and 10 mm ultrafast laser system
Neptune Laboratory
E≥8 mJ
FWHM = 900 fs
PRF=1000 Hz
Measured ps Pulse profile using autocorrelator
ATF -2023
Measured fs Pulse profile using SPIDER
E≥7 mJ
FWHM = 35 fs
PRF=1000 Hz

## Slide 13
Mid-IR 4-16 mm ultrafast laser system
Neptune Laboratory
ATF -2023
DFG in GaSe
Mid-IR XFROG
Tunable 9-11 mm ultrashort seed pulses are available at UCLA.

## Slide 14
HR
LGS Q-switch
Sapphire
plate
Cr:Er:YSGG
4x100mm
OC 40%
2794 nm
Sapphire
plate
CaF2
f=500 mm
171 cm
Input vs Output, (triangles) free running regime,
(circles) Q-switched regime
Pulse duration, (triangles) long cavity 171cm,
(circles) short cavity 39 cm.
λ/4
Pulse duration at 39 J pump energy
and 146 mJ output energy.
70 cm
74 cm
EO Q-switched 2.8 mm Er:YSGG laser
ATF -2023

## Slide 15
2023-2026 mid-IR USP Program
Development of a compact, multiatmosphere CO2 amplifier for picosecond and sub-picosecond 10 mm pulses will require several steps.
At UCLA
  Step 1 Using a regular 12CO2-He mix demonstrate ~3 ps, 3 mJ pulses at 3-10Hz in the optically pumped regenerative amplifier.
  Step 2 Using a 12CO2+13CO2/He mix demonstrate 1 ps, 3 mJ pulses at 10.7 mm in a direct amplification regime.
  At ATF BNL
  Step 3 Amplification of 0.5 ps pulses to a few mJ (GWs) using the BNL isotopic mix 12C16O2-16O12C18O-12C18O2 mix in a CPA regime.
  Step 4 Study and develop a broadband isotopic amplifier suitable to support 0.3-0.5 ps bandwidth. Demonstrate amplification of subpicosecond 9-10 mm pulses.
ATF -2023

## Slide 16
Summary
We have made important and necessary steps in developing a compact, multiatmosphere CO2 amplifier but picosecond and sub-picosecond 10 mm pulses are yet to be amplified.
  Gain dynamics+lasing study in optically pumped CO2 active medium pumped by a ~50 mJ Fe:ZnSe laser indicates that a short ≤10 cm long cell-amplifier at >10 atm pressure is durable.
  Conversion efficiency from pump could reach 10%.
  Next steps in 2023 will be developing a 50 mJ 4.3 Fe:ZnSe synchronizable pump laser system (UAB), building an OP regenerative amplifier and demonstrating amplification of a subpicosecond pulse in isotope CO2 active medium (UCLA+BNL).
ATF -2023

## Slide 17: Activities & Impacts Associated with this Experiment – All Years
Invited Talks:
S. Tochitsky et al, “High-pressure CO2 laser optically pumped at 4.3 mm,” Directed Energy Annual Symposium, Albuquerque, NM, March 2021, (invited).
Manuscripts (books, conference and journal articles, other; please include works submitted by not yet accepted):
  S.Ya. Tochitsky and C. Joshi “Long-Wave Infrared filamentation in air: lasers and high-field phenomena” chapter in Light Filaments: Structures, challenges and applications, ed. J.C. Diels, IET, UK, 2021
  E. C. Welch, S.Ya. Tochitsky, J.J. Pigeon, and C. Joshi “ Long-wave infrared picosecond parametric amplifier based on Raman shifter technology,” Optical Express, 26, 5154-5163, 2018. DOI/10.1364/OE.26.005154
  D. Tovey, S. Ya Tochitsky, J. J. Pigeon, M. N. Polyanskiy, I. Ben-Zvi, and C. Joshi . “Multi-atmosphere picosecond CO2 amplifier optically pumped at 4.3 µm.” Applied Optics, 58, 5756-5763 (2019).
  J. J. Pigeon, D. Tovey, S. Ya Tochitsky, G. J. Louwrens, I. Ben-Zvi, D. Martyshkin, V. Fedorov, K. Karki, S. Mirov, and C. Joshi. “Resonant nonlinear refraction of 4.3-µm light in CO2 gas.” Physical Review A (R), 100, 011803 (2019).
  Dana Tovey, J. J. Pigeon, S. Ya Tochitsky, G. J. Louwrens, I. Ben-Zvi, C. Joshi, D. Martyshkin, V. Fedorov, K. Karki, and S. Mirov, “Gain dynamics in a CO2 active medium optically pumped at 4.3 m,” Journal of Applied Physics,128, 103103 (2020).
  D. Martyshkin, K. Karki, V. Fedorov, and S. Mirov, “Room temperature, nanosecond, 60 mJ/pulse Fe:ZnSe master oscillator power amplifier system operating at 3.8-5.0 µm,” Optics Express 29, 2387-2393 (2021).
  J. J. Pigeon, D. Tovey, S. Ya. Tochitsky, G. Louwrens, D. Maryshkin, V. Fedorov, K. Karki, S. Mirov, I. Ben-Zvi, and C. Joshi, “Resonant nonlinear refraction of mid-IR light in CO and CO2 gas” Phys. Rev. A 104, 043519 (2021).
  D. Tovey, J. J. Pigeon, S. Ya. Tochitsky, G. Louwrens, D. Maryshkin, V. Fedorov, K. Karki, S. Mirov, I. Ben-Zvi, and C. Joshi, “Lasing in 15 atm CO2 cell optically pumped by a Fe:ZnSe laser”Optics Express, 29, 31455-31464 (2021).
  Overall: 1 chapter in a book, 7 refereed papers, 8 + Conference papers
Theses awarded
  Dana T. Tovey, MSc. Thesis 2021
Patents and/or hardware delivered: A novel 4.3 um Fe:ZnSe MOPA laser system built by UAB and used at UCLA.
Other

## Slide 18
UCLA
MARS
10 Hz 4.3 mm
Fe:ZnSe Laser
10 Hz 4.3 mm
Fe:ZnSe amplifier
~mJ
0.5 ps
Mode-locked
15 atm OPCO2
Laser
15 atm
OPCO2
Preamp
15 atm
OPCO2
Amplifier
10 mJ
1 J
3 J
4 J
100 ns
0.5 J
0.5 ps
+++) Table-top electrical discharge-free compact TW LWIR
laser system is suitable for advanced accelerators and self-guiding in air over kms.
+++) Optical-to-optical conversion efficiency 0.1-0.4 is far above
any state-of-the-art LWIR OPA.
- - - ) Laser hysics of Optically Pumped high-pressure CO2 medium needs to be studied.
Optically pumped high-pressure CO2 lasers can be the game changer in LWIR USP:100 ns pump and 0.3-3 ps LWIR pulse
Compact OP CO2 TW Laser
AAC-2022