## Slide 1: TCAD Simulation for Deep Gain Layer
March 1st 2023
eRD112/LGAD Consortium Meeting
Gabriele Giacomini
https://indico.bnl.gov/event/18522/

## Slide 2
50-um thick DC-LGAD
Gain layer implanted at 380keV (current BNL tech) vs 1MeV
TCAD simulations – Breakdown Voltage
Chart: implantation dose (1e12 cm-2)
| 1.8 | 1.85 | 1.9000000000000001 | 1.9500000000000002 | 2
1MeV | 262 | 226 | 192 | 156 | 120
380keV | 220 | 185 | 150
Once the energy is decided, fine tune the dose to have a VBD ~ 200V

## Slide 3
TCAD simulations – Electric field
ae/ah (1 MeV) > ae/ah (380 MeV)
 Hence higher gain is expected
1/E = 3.125 cm/MV
1/E = 2.56 cm/MV
1MeV
380keV
E (V/cm)
Depth into substrate (um)

## Slide 4
Some measurements
Chart: Bias Voltage (V)
| 50 | 100 | 150 | 175 | 200
BNL new LGAD | 10 | 15 | 25 | 36 | 60
BNL old LGAD | 20.8 | 33 | 40.3
HPK | 11.5 | 15.1667 | 24.6667 | 32 | 68.5 | 135.6667
HPK
BNL new LGAD
Chart: Width [mm]
HPK UP
HPK UP
HPK UP
HPK UP
Low-noise charge measurements with charge sensitive preamplifier (shaping time ~ 1us)
Beta hitting the LGADs
Doping concentration of the gain layer (extracted from CV)

## Slide 5
EICROC
EICROC bump-bond compatible
2cm x 0.5cm
0.5cm x 0.5cm
0.2cm x 0.2cm
Compatible with EICROC
1 x 50, 30, 20 um thick substrates : passivation to be opened this week
Test on wafer and then dicing.

## Slide 6
Next: LGAD & AC-LGAD with higher gain
Test on small devices:
Single channel LGADs (1.3 mm x1.3mm)
EICROC for AC – LGAD
3 + 3 wafers, one per thickness
First litho done, out for first implant (JTE) next week
With present technology, max gain = 60 for mips
To have more gain, we need higher UNIFORM implantation energy (380keV  1Mev)