## Slide 1
J. L. Rudeiros Fernandez* D. Arbelaez, L. Brouwer, P. Ferracin, S. Prestemon
US Magnet Development Program
Lawrence Berkeley National Laboratory
CCT Fabrication Method Development: paraffin-wax based CCT subscale magnet
US-MDP Collaboration Meeting 2023

## Slide 2: Table of contents
01
Introduction and motivation
02
Development of the wax VPI for CCT
03
The wax CCT coil
J. L. Rudeiros Fernandez et al.
04
Conclusions and next steps

## Slide 3: 1. Introduction and motivation
J. L. Rudeiros Fernandez et al.
CCT subscale magnet has been demonstrated as an agile platform to investigate fundamental aspects of CCT magnets.
Fundamental iterations on the manufacturing of the coils and structural assemblies have a higher turn-around rate.
Aluminum shell
Smartshim
Nb3Sn individual turn
Strain gauge location
Rib
Spar
Layer 1
Layer 2
CCT subscale fundamental structure

## Slide 4: 1. Introduction and motivation
J. L. Rudeiros Fernandez et al.
CCT sub2
*Haight, A., Haynes, M. M., Krave, S. T., Rudeiros-Fernandez, J. L., & Shen, T. (2021). Characterization of Candidate Insulation Resins for Training Reduction in High Energy Physics Magnets. Submitted for Publication at the CEC-ICMC.
*Krave, S., Shen, T., & Haight, A. (2021). Exploring New Resin Systems for Nb3Sn Accelerator Magnets. IEEE Transactions on Applied Superconductivity, 31(5), 1-4.
Resins used for the subscale program
CCT sub2
CCT sub3
CCT sub4
Epoxy resin Mix61
CTD-701X*
Training might be related to interfacial mechanisms (heat dissipation due to frictional motion, debonding, crack propagation…) and therefore the change of resin might play a big role.

## Slide 5: 1. Introduction and motivation
J. L. Rudeiros Fernandez et al.
Mix 61
Stycast 2850 MT
Paraffin wax
CTD-101K
Interfacial mechanisms might play a key role, can we compare the apparent adhesion between different resin systems and a representative material?
Resin
Pull-out frame
*3LPo1A-05 [L5]: Interface characterization for superconducting magnets

## Slide 6: 1. Introduction and motivation
J. L. Rudeiros Fernandez et al.
Paraffin wax
Mix 61
Interface failure
Friction driven
Crack propagation
Interface failure
Friction driven
Characterization of the apparent interfacial shear strength

## Slide 7: 1. Introduction and motivation
J. L. Rudeiros Fernandez et al.
Characterization of the apparent interfacial shear strength
Energy release due to interfacial debonding, cracking and relative motion friction will be significantly reduced in the case of a paraffin wax system:
  Low energy dissipation during cracking.
  Low bonding strength (leading to low energy debonding events).
  Creation of low friction interfaces between main coil constituents (i.e. mandrel, cable strands and cable).
The paraffin wax systems has been proven successful in the box sample [1].
[1] Daly, Michael, et al. "Improved training in paraffin-wax impregnated Nb3Sn Rutherford cables demonstrated in BOX samples." Superconductor Science and Technology 35.5 (2022): 055014.

## Slide 8: Table of contents
01
Introduction and motivation
02
Development of the wax VPI for CCT
03
The wax CCT coil
J. L. Rudeiros Fernandez et al.
04
Conclusions and next steps

## Slide 9: 2. Development of the wax VPI for CCT
J. L. Rudeiros Fernandez et al.
Top reservoir
Coil
Vacuum chamber
Vacuum pump
Resin mixer
Compressed air
General sequence of CCT for vacuum pressure impregnation (VPI) using epoxy resins (e.g. Mix61, CTD-101K) or polyolefin-based resin (e.g. CTD-701X*)
Outgassing of the coil under vacuum.
Resin mixing and degassing.
Resin transfer to the coil until the reservoir is filled.
Vacuum open to atmospheric pressure.
Curing of the coils within a furnace.

## Slide 10: 2. Development of the wax VPI for CCT
J. L. Rudeiros Fernandez et al.
The paraffin-wax process implies additional challenges with respect to traditional resins:
  High uniform temperature is required in all parts of the system.
  High volumetric contraction during phase transformation.
Top reservoir
Coil
Vacuum chamber
Vacuum pump
Resin mixer
Compressed air

## Slide 11: 2. Development of the wax VPI for CCT
J. L. Rudeiros Fernandez et al.
Temperature
Time
Paraffin wax melting point
Cooling pipe
air
Diagram of the impregnation bag system
Mandrel
Mandrel ID
Mandrel OD
Glass fiber tape
Peel ply
Flow media
Cooling by convection
Vacuum bag
External heating elements
Cable

## Slide 12: 2. Development of the wax VPI for CCT
J. L. Rudeiros Fernandez et al.
Phase 1
Phase 2
Phase 3 (Final coil)
Aluminum
Aluminum
Aluminum-bronze
Development

## Slide 13: 2. Development of the wax VPI for CCT
J. L. Rudeiros Fernandez et al.
Successful filling of the grooves and cable.
No apparent cracking after the liquid nitrogen test.
The exhibited bonding strength between the filled cable and the aluminum mandrel was very low.
Liquid nitrogen test
Nb3Sn cable

## Slide 14: 2. Development of the wax VPI for CCT
J. L. Rudeiros Fernandez et al.
Aluminum (subscale outer-layer)
Phase 2 – Iteration 1
Main set-up
Vacuum chamber
Mixer
Vacuum pump

## Slide 15: Table of contents
01
Introduction and motivation
02
Development of the wax VPI for CCT
03
The wax CCT coil
J. L. Rudeiros Fernandez et al.
04
Conclusions and next steps

## Slide 16: 3. The wax CCT coil
J. L. Rudeiros Fernandez et al.
New features in the CCT wax coil
New heaters were installed directly in contact with the cable for quench studies. Heaters attached with Stycast 2850 (* Work by D. Arbelaez and R. Teyber).
New design of the G10 splice support pieces in order to minimize the volume of wax in the region and ensure mechanical protection of the splice.

## Slide 17: 3. The wax CCT coil
J. L. Rudeiros Fernandez et al.
Impregnation
Diagram of the impregnation bag system
Mandrel
Mandrel ID
Mandrel OD
Glass fiber tape
Peel ply
Flow media
Cooling by convection
Vacuum bag
External heating elements
Cable
Chart: CCT Wax Impregnation
Paraffin wax melting point

## Slide 18: 3. The wax CCT coil
J. L. Rudeiros Fernandez et al.
Impregnated coil - surface
Rotation
Coil
Support
Smartmotor
Linear translation stage
Microscope
PC
Axial rod
2.5 mm
0°
90°
180°
270°
360°
A microscope moves along a linear stage taking images of the outer surface of the coils, row by row. The angular displacement of the coil is provided by a smart-motor.
An algorithm reconstructs the full image which is planned to be used to search for differences between pristine and tested coils.
(CCT Sub5)
Paraffin wax
(CCT Sub2)
Mix 61

## Slide 19: 3. The wax CCT coil
J. L. Rudeiros Fernandez et al.
Developments for the wax-based CCT assembly: paraffin wax inner layer + mix61 outer layer (from Sub3)
*Courtesy of G. Vallone
CCT Sub2, 3, and 4
CCT Sub5 (wax)
Increase in the smartshims angle to increase conductor support during energization
Miniaturization of the elements for fabrication of the smartshims allows for a new 3D printed structure during assembly.
Compressed air
Smartshim left
Smartshim right
Vacuum pump
Resin mixer
Overflow
a
b
a
b
a
b
a
b

## Slide 20: Table of contents
01
Introduction and motivation
02
Development of the wax VPI for CCT
03
The wax CCT coil
J. L. Rudeiros Fernandez et al.
04
Conclusions and next steps

## Slide 21: 4. Conclusions and next steps
J. L. Rudeiros Fernandez et al.
A method to successfully impregnate CCT magnets based on the VPI method has been developed.
The paraffin wax interfacial strength with copper wire has been characterized, showing two orders of magnitude lower adhesion in relation to the epoxy resin used for previous CCT magnets (i.e. Mix61).
A low friction system has the potential to reduce some of the phenomena normally associated with training.
The test of magnet showed no training in the wax layer!
Towards a “full” wax subscale (inner + outer layer).

## Slide 22: Thanks!
J. L. Rudeiros Fernandez et al.

## Slide 23: Additional slides
J. L. Rudeiros Fernandez et al.
Iteration 1
Iteration 2
Iteration 3
The overall filling of the grooves and cable improved with each iteration.
The incremental improvements in the set-up lead to the complete filling of all the main cavities.
The higher temperature uniformity led to a uniform flow of wax along the outer surface of the mandrel.
Iterative progress on the wax VPI

## Slide 24: Additional slides
J. L. Rudeiros Fernandez et al.