## Slide 1: 2023 MDP Collaboration Meeting 20 T hybrid magnet and comparative analysis
P. Ferracin
US Magnet Development Program

## Slide 2: Introduction Working group
Members US MDP 20 T working group
  LBNL: D. Arbelaez, L. Brouwer, P. Ferracin, L. Garcia Fajardo, M. Juchno, G. Vallone
  FNAL: G. Ambrosio, E. Barzi, V. Kashikhin, V. Marinozzi, I. Novitski, A. Zlobin
  NHMFL: L. Cooley
  BNL: M. Anerella, J. Cozzolino, R. Gupta, F. Kurian, B. Yahia
Contributions from
  Etienne Rochepault (CEA)

## Slide 3: Introduction Bi-weekly meetings
47 meetings so far
  https://conferences.lbl.gov/category/100/

## Slide 4: Introduction Goals of working group
Conceptual design of a 20 T hybrid HTS-LTS magnet
  Comparative analysis of different design options for a 20 T hybrid
    Cos design and its stress-management options
    Block-type coil design (block with flared ends)
    Common-coil design (block with racetrack coils)
Review and follow-up of current work on hybrid magnets
  Collect and organize information to provide inputs for 20 T hybrid design
Design of a support structure for test HTS inserts in CCT6 and SMCT outserts
  Study the possibility of using the structure for hybrid magnets towards 20T

## Slide 5: Introduction Motivations: why 20 T hybrid?

## Slide 6: Introduction Goals of working group
Conceptual design of a 20 T hybrid HTS-LTS magnet
  Comparative analysis of different design options for a 20 T hybrid
    Cos design and its stress-management options
    Block-type coil design (block with flared ends)
    Common-coil design (block with racetrack coils)
Review and follow-up of current work on hybrid magnets
  Collect and organize information to provide inputs for 20 T hybrid design
Design of a support structure for test HTS inserts in CCT6 and SMCT outserts
  Study the possibility of using the structure for hybrid magnets towards 20T

## Slide 7: Design criteria
Coil and magnet parameters
  Free coil aperture (diameter) 50 mm
  Operational bore field 20 T
  load-line fraction @ 1.9K: Iop/Iss <= 87 %
  2D Geometrical harmonics bn<3 units for n<10 (at Rref=17 mm)
Quench protection
  All coils powered in series
  Maximum hot spot temperature 350 K
Mechanics
  Maximum Nb3Sn coil stress <180 (<150) MPa at 1.9 (293) K
  For the HTS <120 MPa

## Slide 8: Superconducting materials Wires and cables
Nb3Sn
  0.7 – 1.1 mm strands
    Typical properties of 127 or 169 (Bruker-OST) RRP stacks
  Rutherford cables: 8-26 mm wide, 1.3-2.0 mm thick
Bi2212
  Isotropic, round, multifilamentary
    Bruker-OST architecture 19 × 36, 37 × 18 or 55 × 18 for 0.8 mm diameter wires
  On paper, possible same strand and Rutherford cable dimensions as Nb3Sn
REBCO
  CORC (ATC LLC) and STAR (AMPeers) wires: tapes around Cu former
  Wire diameter from 1.3 to 3.6 mm
  Multi-wire cable for accelerator magnets not available yet (R&D in progress)

## Slide 9: The 20 T hybrid zoo* (First iteration, presented at 2021 MT Conference)
Mechanics
Next steps:

## Slide 10: …about a year later
LTS
HTS
LTS
HTS
LTS
HTS

## Slide 11: Cos-theta design Magnetic analysis
Coil inner diameter 60 mm
  Internal support structure
Design constraint: double-layer coils
6 layers, with cables 18 to 24 mm wide
  2 layer HTS, 4 layer LTS
HTS: CCT-like or “single turn” SMCT
LTS: SMCT design + CT
Field quality requirements met
Load-line % : 80% for HTS, 80% for LTS

## Slide 12: Cos-theta design Mechanical analysis
Assumptions:
  Infinitely rigid yoke, deformable SS coil support parts
  No pre-stress, no cool-down, only e.m. forces
  Coil turn allowed to slide and separate from structure
5 mm thick spars (mandrels)
Several iterations carried out
  Non need of force interception in the outermost layers
  But CCT-type of interception in inner most layers

## Slide 13: Cos-theta design Mechanical analysis
Significant deformation (large displ. scaling) of the coil support structure  induced stress on the coil blocks/turns

## Slide 14: Cos-theta design Mechanical analysis
In HTS, only small areas above 120 MPa of VM stress
In LTS, stress within the 180 MPa limits (except few corner effects)

## Slide 15: Cos-theta design Quench protection
Preliminary work done on CT
  See V. Marinozzi presentation
1 m long model studied
With CLIQ and dump resistor 
  400 K in the Nb3Sn
Very challenging (like everything else with 20 T hybrids), further work needed, but not a showstopper

## Slide 16: Block design Magnetic analysis
Coil inner diameter 70 mm
  Internal support structure
Design constraint
  double-layer coils
  HD2/FRESCA2 style coil
3 double-layer coils, with 15 mm wide cable
Field quality requirements met
Load-line %: 75% for HTS, 84% for LTS
Challenges: “insertion” of HTS coil inside LTS coils, grading and splicing

## Slide 17: Block design Mechanical
10 mm thick winding pole
Coils vertically separated by horizontal plates
HTS and LTS separated by vertical ribs
In HTS, stress within the 120 MPa of VM stress (except a corner effect)
In LTS, stress within the 180 MPa of VM stress

## Slide 18: Common-coil design Magnetic analysis
Coil inner diameter 50 mm
  No internal support structure
Single layer coils allowed : splice in the central pole
  So, vertical and horizontal flexibility
4 layers, with cables 13 mm to 18 mm wide
  1 layer HTS, 3 layer LTS
Field quality requirements met
Load-line %: 88% for HTS, 86% for LTS
Challenges: HTS field quality blocks close to the aperture

## Slide 19: Common-coil design Mechanical analysis
No internal structure in innermost layer
Stress management only horizontally
In HTS, stress within the 120 MPa of VM stress
In LTS, area with stress above 180 MPa of VM stress
  Work in progress to mitigate stress (see M. Anerella’s presentation)

## Slide 20: Conclusions 2D analysis and next steps
Three design options considered: cos-theta, block, common-coil
  Similar HTS conductor area in the 3 designs
  Smaller LTS area for common-coil vs cos-theta and block
    But lower margin (still in spec), higher stress
So far, on CT: no show stoppers but mechanics and QP challenging
Next steps
  QP and “rigid” stress analysis to fine tune cross-sections  complete the 2D comparison, with all 3 meeting specs (including QP)
  Move to 2D full mech analysis and 3D
Additional “stable and focused” resources would be highly beneficial

## Slide 21: Publications
MT27 (published) ASC 2022 (accepted)

## Slide 22: Introduction Goals of working group
Conceptual design of a 20 T hybrid HTS-LTS magnet
  Comparative analysis of different design options for a 20 T hybrid
    Cos design and its stress-management options
    Block-type coil design (block with flared ends)
    Common-coil design (block with racetrack coils)
Review and follow-up of current work on hybrid magnets
  Collect and organize information to provide inputs for 20 T hybrid design
Design of a support structure for test HTS inserts in CCT6 and SMCT outserts
  Study the possibility of using the structure for hybrid magnets towards 20T

## Slide 23: CCT Nb3Sn insert, CCT Bi2212 insert
LBNL hybrid (expected 2023)
  CCT5 as Nb3Sn outsert
    8-9 T in 90 mm aperture
  B12212 CCT inserts (Bin5)
    ~1 T in 30 mm aperture

## Slide 24: CC Nb3Sn outsert, CC REBCO insert
BNL hybrid (expected 2023/2024)
  10 T Nb3Sn CC outsert
  CORC CC MDP (1-2 T)
    To be tested in CC outsert in 2023/2024
  CORC CC STTR (3-5 T)
    To be tested in CC outsert in 2023/2024

## Slide 25: CT Nb3Sn outserts
Large aperture (120 mm) Nb3Sn outserts (2024/2025)
  FNAL SMCT
    ~11 T with 2 layers
  LBNL CCT
    15-16 T (80-85% at 1.9 K) with 4 layers

## Slide 26: How do the compare with the 20T CT outsert?
20 T outsert, 140 mm
CCT6, 120 mm
SMCT, 120 mm
16 T, 85% 1.9 K
11 T

## Slide 27: LBNL Bi2212 inserts and hybrids
LBNL Bi2212 CCT (3-5 T)
  2-layers, ID/OD: 50-77 mm
  To be tested in CCT6 in 2026
How high could we go with CCT6 and a Bi2212 insert (Je ~800 A/mm2 at 20 T?
  Bbore max (short sample) of about 20 T

## Slide 28: How does it compare to the 20 T CT design?
Powered in series
24 T Bbore at short sample
Powered indipendently
20 T Bbore at short sample

## Slide 29: FNAL Bi2212 inserts and hybrids
FNAL Bi2212 SMCT (1-2 T)
  2-layers, ID/OD: ~20-50 mm
  To be tested in SMCT+MDPCT1-inner in 2025
    16-18 T field range

## Slide 30: Bi2212 hybrids Beyond 16 T, and towards 20 T

## Slide 31: REBCO inserts
FNAL CORC COMB (~5 T, stand-alone with iron)
  2-layers, ID/OD: 100-120 mm
  To be tested in CCT6/SMCT in 2025
LBNL CORC CCT C3 (~5 T, stand-alone no iron)
  6-layers, ID/OD: 70-150 mm
  To be tested in stand-alone in 2024
LBNL STAR CCT S1 (~1-2 T)
  2-layers, ID/OD: 50-77 mm
  To be tested in CCT5 in 2024-2025

## Slide 32: Conclusions
Good progress with a 2D comparison between 20 T designs
  Still missing QP and mechanics in infinitely rigid iron for a full comparison
Next step: 2D analysis with support structure and 3D design
  Looking for dedicated student/post-doc
Hybrid activities
  Several 10-12 T hybrids coming up in the next 2 years
  120 mm Nb3Sn outserts with HTS inserts could bring us beyond 16 T and towards 20 T
    But designs should be done in a coherent way (diameter, lengths….)

## Slide 33: Appendix

## Slide 34: Introduction Timeline (2020 updated roadmap)

## Slide 35: Introduction Previous work
2005, P. McIntyre, et al., 24 T hybrid for LHC tripler (TAMU)
2011, 2014, E. Todesco, et al., 20 T hybrid for LHC upgrade (CERN)
2015, G. Sabbi, et al., 20 T hybrid for SPPC China and FCC (LBNL)
2016, Q. Xu, et al., 20 T hybrid for SPPC China (IHEP)
2018, J. van Nugteren, et al., 20+ T HTS for LHC upgrade or FCC (CERN)
2020, D. Martins Araujo , et al., towards 20 T FRESCA2+Feather (CERN)
2021, J.S. Rogers, et al., 18 T hybrid (TAMU)
2022, P. Ferracin, et al., 20 T hybrid demonstrator (US MDP)
2015, R. Gupta, et al., 20 T hybrid for LHC upgrade (BNL)

## Slide 36: Superconducting materials: Je and Jo
Assumptions for magnetic analysis
  Je = Strand current / strand area
    Je_LTS = 875 A/mm2 (1.9 K, 16 T, 5% degrad.)
      3000 A/mm2 Jc (4.2 K, 12 T, virgin)
    Je_HTS = 740 A/mm2 (20 T)
      Bi2212 value
  Jo = Cable current / Cableinsulated area
    Jo = Je  0.67 (typical Rutherford cable)
      Assumed also for HTS (Bi2212)
Nb3Sn and HTS cross at 16.5 T
CORC wire still lower in both Je (600 A/mm2, 20 T) and Jo / Je (0.54)

## Slide 37: Current activities: block
Test Facility Dipole (TFD)
  Collaboration LBNL/FNAL
  Funded by DoE FES and HEP
  Test cables and inserts in a high transverse background field
    15 T in 94 x 144 mm bore
First implementation of horizontal plates for vertical stress management
By J.L. Rudeiros Fernandez, et al., 2LOr2A-06