## Slide 1: NHMFL annual cable needs - Solenoids
Existing Conductor: 37 m cable left (JE>1000) for making solenoids 31 m (JE ~700) cable to be used for insulation demo
Strand and cable need for Solenoids and short sample:
1. 9-strand subscale magnet cable, with nominal dimensions, 4 mm x 1.44 mm.
2. Piece lengths: >10 m (Baby-Ruth size), (>30m, upon successful 10 m)
3. Strand identically with the following characteristics:
1) 0.8 mm
2) 37 x 18 architecture.
3) JE@4.2K,5T > 1000 A/mm2 after plateau OPHT;
4) Twisting: Untwisted ok.
4. We can use cables up to 10 kA, with a 12 T BG, but <7.2 kA will be more helium efficient.
9-strand (Ø 0.8 mm)
TiO2 coated
Mullite
Alumina coated
No TiO2

## Slide 2: NHMFL Collaborations
  On-going collaboration with PPPL towards compact fusion: spherical tokamak Ohmic heating central solenoids
  Conductor TBD
  Other proposals are looking at 6 around 1 cable for high field testing
~3m (barrel samples)
We can use cables up to 10 kA, with a 12 T BG, but <7.2 kA will be more helium efficient.
9-strand (Ø 0.8 mm)
TiO2 coated
Mullite
Alumina coated
No TiO2