## Slide 1
J. L. Rudeiros Fernandez* D. Arbelaez, C. Bird, J. F. Croteau, P. Ferracin, S. Prestemon, T. Shen, G. Vallone
US Magnet Development Program
Lawrence Berkeley National Laboratory
Impregnation of CCT with alternative Resins
US-MDP Collaboration Meeting 2023

## Slide 2: Table of contents
01
Characterization of adhesion
02
Development of the Stycast VPI for CCT
03
Conclusions and next steps
J. L. Rudeiros Fernandez et al.

## Slide 3: 1. Characterization of adhesion
J. L. Rudeiros Fernandez et al.
CCT sub2
*Haight, A., Haynes, M. M., Krave, S. T., Rudeiros-Fernandez, J. L., & Shen, T. (2021). Characterization of Candidate Insulation Resins for Training Reduction in High Energy Physics Magnets. Submitted for Publication at the CEC-ICMC.
*Krave, S., Shen, T., & Haight, A. (2021). Exploring New Resin Systems for Nb3Sn Accelerator Magnets. IEEE Transactions on Applied Superconductivity, 31(5), 1-4.
Resins used for the subscale program
CCT sub2
CCT sub3
CCT sub4
Epoxy resin Mix61
CTD-701X*
Training might be related to interfacial mechanisms (heat dissipation due to frictional motion, debonding, crack propagation…) and therefore the change of resin might play a big role.

## Slide 4: 1. Characterization of adhesion
J. L. Rudeiros Fernandez et al.
CCT sub2
Materials
Wire:
Resins:
110 Copper wire (mirror-like surface), 1 mm diameter.
Paraffin wax Polarit G 54/56
Stycast 2850 MT BL + CAT23LV
Mix 61
CTD-101K
Stycast 2850 FT BL + CAT24LV

## Slide 5: 1. Characterization of adhesion
J. L. Rudeiros Fernandez et al.
Sample preparation
Assembly
Resin transfer
The specific resin is transferred to the mold formed by the assembly.
PVC tube
a
b
c
d
Resin
Teflon disc
Silicone O-Ring
Copper wire
Precision machined aluminum plates
Copper wire
a
b
c
d

## Slide 6: 1. Characterization of adhesion
J. L. Rudeiros Fernandez et al.
Sample preparation
a
b
c
d
Resin

## Slide 7: 1. Characterization of adhesion
J. L. Rudeiros Fernandez et al.
Mix 61
Stycast 2850 MT
Paraffin wax
CTD-101K
Resin
Pull-out frame
Pull-out test

## Slide 8: 1. Characterization of adhesion
J. L. Rudeiros Fernandez et al.
Tensile tester adapter
Tensile tester configuration
Load cell
Tensile grips
Pull-out frame
Pull-out frame configuration
Copper wire
Resin block
Tensile grips
Pull-out frame

## Slide 9: 1. Characterization of adhesion
J. L. Rudeiros Fernandez et al.
Paraffin wax
Mix 61
Interface failure
Friction driven
Crack propagation
Interface failure
Friction driven
Characterization of the apparent interfacial shear strength

## Slide 10: 1. Characterization of adhesion
J. L. Rudeiros Fernandez et al.
Characterization of the apparent interfacial shear strength
For each individual test, and based on a few simplification assumptions, one could compute the apparent interfacial shear strength based on: where is the peak load, is the perimeter of the wire, and is the embedded length.

## Slide 11: 1. Characterization of adhesion
Copper wire
Resin block
Wire grips
Pull-out frame
J. L. Rudeiros Fernandez et al.
Characterization of the apparent interfacial shear strength @ 77 K
Load cell
Dewar
G10 bars
Liquid Nitrogen
Tensile tester adapter

## Slide 12: Table of contents
01
Characterization of adhesion
02
Development of the Stycast VPI for CCT
03
Conclusions and next steps
J. L. Rudeiros Fernandez et al.

## Slide 13: 2. Development of the Stycast VPI for CCT
J. L. Rudeiros Fernandez et al.
BOX sample, M. Daly, PSI
Main motivation

## Slide 14: 2. Development of the Stycast VPI for CCT
J. L. Rudeiros Fernandez et al.
Top reservoir
Coil
Vacuum chamber
Vacuum pump
Resin mixer
Compressed air
General sequence of CCT for vacuum pressure impregnation (VPI) using epoxy resins (e.g. Mix61, CTD-101K) or polyolefin-based resin (e.g. CTD-701X*)
Outgassing of the coil under vacuum.
Resin mixing and degassing.
Resin transfer to the coil until the reservoir is filled.
Vacuum open to atmospheric pressure.
Curing of the coils within a furnace.

## Slide 15: 2. Development of the Stycast VPI for CCT
J. L. Rudeiros Fernandez et al.
The Stycast 2850 FT process implies additional challenges with respect to traditional resins in terms of high viscosity:
  Water: ∼1 cP
  Paraffin used in CCT Sub5: ∼4 cP @ 100 °C
  CTD-101K: <100 cP @ 60 °C
  Stycast 2850FT: 250000 cP
The main strategies to enable the impregnation are:
  Slightly increase of temperature (i.e. 40 °C) during resin mixing, outgassing and resin transfer.
  Promote fast longitudinal flow and radial penetration with new flow media scheme.
  Reduce viscosity by using Catalyst 24 LV / 23 LV.
Top reservoir
Coil
Vacuum chamber
Vacuum pump
Resin mixer
Compressed air

## Slide 16: 2. Development of the Stycast VPI for CCT
J. L. Rudeiros Fernandez et al.
Diagram of the impregnation bag system for Stycast
Mandrel
Mandrel ID
Mandrel OD
Glass fiber tape
Peel ply
New expanded Flow media
Vacuum bag
External heating elements
Cable

## Slide 17: 2. Development of the Stycast VPI for CCT
J. L. Rudeiros Fernandez et al.
Phase 2
Phase 3
Phase 4 (Final coil)
Aluminum
Aluminum-bronze
Development
Vacuum Assisted Resin Transfer Molding (VARTM)
Phase 1
Vacuum Pressure Impregnation

## Slide 18: 2. Development of the Stycast VPI for CCT
J. L. Rudeiros Fernandez et al.
Vacuum Assisted Resin Transfer Molding (VARTM)
Phase 1
Nb3Sn cable
Diagram of the impregnation bag system for Stycast
Aluminum plate
Peel ply
New expanded Flow media
Vacuum bag
External heating elements
Cable

## Slide 19: 2. Development of the Stycast VPI for CCT
J. L. Rudeiros Fernandez et al.
Vacuum Assisted Resin Transfer Molding (VARTM)
Phase 1
Nb3Sn cable

## Slide 20: 2. Development of the Stycast VPI for CCT
J. L. Rudeiros Fernandez et al.
Vacuum Assisted Resin Transfer Molding (VARTM)
Diagram of the impregnation bag system for Stycast
Aluminum plate
Peel ply
New expanded Flow media
Vacuum bag
External heating elements
Cable
Stycast
Nylon fiber

## Slide 21: 2. Development of the Stycast VPI for CCT
J. L. Rudeiros Fernandez et al.
Vacuum Assisted Resin Transfer Molding (VARTM)
Diagram of the impregnation bag system for Stycast
Aluminum plate
Peel ply
New expanded Flow media
Vacuum bag
External heating elements
Cable
Aluminum
Nb3Sn Strand
Glass insulation
Stycast

## Slide 22: 2. Development of the Stycast VPI for CCT
J. L. Rudeiros Fernandez et al.
Vacuum Assisted Resin Transfer Molding (VARTM)
Diagram of the impregnation bag system for Stycast
Aluminum plate
Peel ply
New expanded Flow media
Vacuum bag
External heating elements
Cable
Aluminum
Nb3Sn Strand
Glass insulation
Stycast
100 µm

## Slide 23: 2. Development of the Stycast VPI for CCT
J. L. Rudeiros Fernandez et al.
Vacuum Assisted Resin Transfer Molding (VARTM)
Diagram of the impregnation bag system for Stycast
Aluminum plate
Peel ply
New expanded Flow media
Vacuum bag
External heating elements
Cable
Aluminum
Nb3Sn Strand
Glass insulation
Stycast
Aluminum
Nb3Sn Strand
Glass insulation
Stycast

## Slide 24: 2. Development of the Stycast VPI for CCT
Diagram of the impregnation bag system for Stycast
Aluminum plate
Peel ply
New expanded Flow media
Vacuum bag
External heating elements
Cable
J. L. Rudeiros Fernandez et al.
Vacuum Assisted Resin Transfer Molding (VARTM)
Aluminum
Nb3Sn Strand
Glass insulation
Stycast
Nb3Sn Strand
Nb3Sn Strand
Nb3Sn Strand

## Slide 25: 2. Development of the Stycast VPI for CCT
Diagram of the impregnation bag system for Stycast
Aluminum plate
Peel ply
New expanded Flow media
Vacuum bag
External heating elements
Cable
J. L. Rudeiros Fernandez et al.
Vacuum Assisted Resin Transfer Molding (VARTM)
Glass insulation

## Slide 26: Table of contents
01
Characterization of adhesion
02
Development of the Stycast VPI for CCT
03
Conclusions and next steps
J. L. Rudeiros Fernandez et al.

## Slide 27: 3. Conclusions and next steps
J. L. Rudeiros Fernandez et al.
A method to measure the adhesion between a copper wire and various resin systems at room temperature and 77 K has been developed.
The paraffin wax interfacial strength with copper wire has been characterized, showing two orders of magnitude lower adhesion in relation to the epoxy resin used for previous CCT magnets (i.e. Mix61).
Next steps include measuring adhesion properties at 77 K.
A method to successfully impregnate single layer magnets with Stycast 2850 ft based on the VPI method is being developed.
Initial results indicate that there is potential for impregnation of single layer coils in which radial impregnation is feasible but substantial challenged remain ahead.

## Slide 28: Thanks!
J. L. Rudeiros Fernandez et al.