## Slide 1
Bi-2212: a Routine Long-Length Predictable Conductor and Path to Improve its Properties
Eric Hellstrom, I. Hossain, S. Barua, J. Jiang, P. Lee, A. Oloye, F. Kametani, and D. Larbalestier,
Applied Superconductivity Center, National High Magnetic Field Laboratory
Florida State University
NSF-DMR 2128556, DOE-OHEP DE-SC0010421, DOE-MDP, and the State of Florida
MDP - Brookhaven National Laboratory – Mar. 21-24, 2023

## Slide 2: Overview
Presentation will be in two parts:
  Effect of filament geometry and architecture on filament bonding
  Characterize IC distribution in long length wires
Driving questions
    What influences how filaments bond during the overpressure heat treatment?
    How does this affect JC?
    Is the uniformity of long-length wires good enough to build large coils?

## Slide 3: Champion Bi-2212 powder and wire – LXB-52
Jiang et al., IEEE Trans. Appl. Supercond. 29, 6400405 (2019)
Powder: Engi-Mat LXB-52
Alkaline earth cuprate
Wire: PMM170123 (0.8 mm, 55x18)
Powder is a mixture of phases
Grain size is small, so it does not degrade wire drawing

## Slide 4: Outline 1
Observed three bundle shapes in 85x18 wires
Investigated and analyzed filament geometry and filament bonding for the three bundle shapes
  In as-received 85x18 wire
  In wires quenched from the melt state

## Slide 5: The filament geometry in the three bundle shapes in the 85x18 wires is different
100 µm
Tetragonal
Hexagonal
Pentagonal
50 bar overpressure
ImageJ used to do the analysis
Samples
85x18 architecture
1.3, 1.2, 1.0, & 0.8 mm diameter wires
Densified wires at 820 ˚C and 50 bar for 12 h to remove void space
Analyzed the three bundle shapes individually
Imam Hossain

## Slide 6: Different bundle shapes have different average filament area and filament separation
Measured filament area & calculated equivalent diameter
Average filament diameter (µm)
Bundle shape
1.3 mm
1.2 mm
1.0 mm
0.8 mm
Tetragonal bundles have the smallest average filament area
Tetragonal bundles have the smallest filament separation
1.3 mm
1.2 mm
1.0 mm
0.8 mm
tet
pent
hex
tet
pent
hex

## Slide 7: What happens to the filaments during the overpressure heat treatment?
Designed and built an overpressure (OP) quench furnace
OP quench furnace freezes-in filament microstructure from the melt state

## Slide 8: Study how the filament microstructure changes in the melt state – filament bonding occurs
Standard overpressure heat treatment
Bi-2212 melts at ≈ 884°C
Bi-2212 is in the melt state
Solidification starts at 872°C
Quench at 875 °C – before solidification starts

## Slide 9: Quench samples from the melt state to study how the filament microstructure evolves in the melt state
820 °C – 2h
RT
887 °C - 0.2 h
Quenching
880 °C
882 °C
2.5 °C/h
878 °C
10 °C/h
Quench from 875 °C
(Just before
solidification starts)
Quenched samples after 0.2, 2, 3 and 4 h in the melt state
Increasing time in the melt for the filaments to bond together
tquench 0.2 h
Bi-2212 melts at ≈ 884°C

## Slide 10: Maximum filament bonding occurs in tetragonal bundles, which have minimum filament separation
Tetragonal
Percent of bonded filaments
tquench (h)
Percent of bonded filaments
tquench (h)
Percent of bonded filaments
tquench (h)
Percent of bonded filaments
tquench (h)
60%

## Slide 11: Filament bonding causes thermally-induced area fluctuation and even pinch-off
tquench = 0.2 h
tquench = 4 h
Some filaments are getting smaller
Area fluctuation occurs because liquid moves to the larger bonded region to reduce interfacial energy.
1.3 mm - Avg. Separation 4.34 µm
0.8 mm - Avg. Separation 2.3 µm
Bonded filaments

## Slide 12: With increasing time in the melt (tmelt) Bonded regions increase in area Individual filaments decrease in area
Investigated how the area of the smallest 5% of filaments changed with increasing tquench
Bi-2212 less aligned in large regions
Small regions can pinch off
tquench = 0.2 h
tquench = 4 h
With increasing time in the melt (tmelt) Bonded regions increase in area Individual filaments decrease in area

## Slide 13: Jc decreases with increasing tmelt
Jc vs tmelt
Jc (4.2 K, 5 T) (A/mm2)
tmelt (h)
n value vs tmelt
0.8 mm
1.3 mm
tmelt (h)
n value (4.2 K, 5 T)
1.2 mm
1.0 mm
JC decreases fastest in 0.8 and 1.0 mm wires that have the smallest filament separation
Reduced Jc and n value with increasing tmelt point to possible degradation of filament continuity along the length of the wire.

## Slide 14: Summary – filament geometry/bonding
Filaments in tetragonal bundles have the smallest area and separation, and they develop the most bonding
JC may degrade more in tetragonal bundles than in the other two shape bundles
Wires with uniform filament size, shape, and controlled separation should increase JC

## Slide 15: Driving questions – JC distribution
Bi-2212 is delivered in single lengths > 1 km
  Some early coils made with Nexans powder wire exhibited some unforeseen damage that is not seen in recent coils made with Engi-Mat powder wire
  Are there serious defects in the present-day wire that would make a coil unusable?
  Are we ready to scale up to coils with 1000 m of wire?
Is there a test to evaluate the Jc distribution in Bi-2212 wires that could help answer these questions?
[1] Brown, M. D. et al. Prediction of the Jc(B) behavior of Bi-2212 wires at high field. IEEE Trans. Appl. Supercond. 29, 1–4 (2019).
Shaon Barua

## Slide 16: Double differentiation of the V-I signal to extract the Ic distribution
Proposed by Baixeras and Fournet [1] and used by Warnes ­et al. [2] to study filament-sausaging degradation of critical current density (Jc) in Nb-Ti.
Edelman for 2223 [3] showed that the model had an operational validity even if the strict assumptions of Baixeras and Fournet were not fulfilled – Edelman suggested it use for 2212 too.
[1] Baixeras, J. & Fournet, G. Vortex displacement losses in a non-ideal type II superconductor. Journal of Physics and Chemistry of Solids 28, 1541–1547 (1967).
[2] Warnes, W. H. & Larbalestier, D. C. Critical current distributions in superconducting composites. Cryogenics 26, 643–653 (1986).
[3] Edelman, H. S. & Larbalestier, D. C. Resistive transitions and the origin of the n value in superconductors with a Gaussian critical‐current distribution. Journal of Applied Physics 74, 3312–3315 (1993).

## Slide 17: Double differentiation of the V-I signal to extract the Ic distribution
Since the factors that affect local critical current are thought to be randomly distributed and uncorrelated, should be a Gaussian: Central limit theorem
Number of sections with
Voltage contribution of infinitesimally short length of wire
For a more detailed treatment:
[1] Warnes, W. H. & Larbalestier, D. C. Critical current distributions in superconducting composites. Cryogenics 26, 643–653 (1986).
[2] Plummer, C. & Evetts, J. Dependence of the shape of the resistive transition on composite inhomogeneity in multifilamentary wires. IEEE Trans. Magn. 23, 1179–1182 (1987).
Notes: 1. In this method V-I curves are measured on shunted brass barrel. Now if we double differentiate the VI signal we can extract the Ic distribution.
2. Since the factors that affect local critical current are thought to be randomly distributed and uncorrelated, 𝜙(𝐼) should be a Gaussian: Central limit theorem
3. From the fitted curve we extract mean and std. deviation

## Slide 18: Double differentiation of the V-I signal to extract the Ic distribution
  ↓ Connectivity ↑
  At 5T:
  of Nb-Ti ≈ 3-5%

## Slide 19
NbTi current distribution curves are narrow
Transverse
Longitudinal
d2V/dI2
Is wire uniformity in 1 km long wires a concern?

## Slide 20
NbTi current distribution curves are narrow
Transverse
Longitudinal
d2V/dI2
Ic of Bi-2212 RWs could be increased further if the filament quality is improved.
Is wire uniformity in 1 km long wires a concern?

## Slide 21: What is the quality of filaments in as-delivered wires?
Billet No.: PMM180410, 8518, Ø 1 mm
Pentagonal
Hexagonal
Tetragonal
Filament Area[mm2] Map

## Slide 22: Filament sausaging in as-delivered wires is significant
Billet No.: PMM180410, 8518, Ø 1 mm
Filament Area[mm2] Map
Area [mm2]

## Slide 23: Filament sausaging in as-delivered wires is significant
Billet No.: PMM180410, 8518, Ø 1 mm
Sausaging in as-delivered wire is considerably greater than for Nb-Ti and Nb3Sn wires

## Slide 24: Filament sausaging in as-delivered wires is significant
Billet No.: PMM180410, 8518, Ø 1 mm
Sausaging in as-delivered wire is considerably greater than for Nb-Ti and Nb3Sn wires
Merged Filaments

## Slide 25: There are clear trends that Jc rises as σ/μ declines Lower Jc for Tmax = 896 °C - correlates to higher non-uniformity
Tmax = Maximum temperature during over pressure heat treatment

## Slide 26: There are clear trends that Jc rises as σ/μ declines Lower Jc for Tmax = 896 °C - correlates to higher non-uniformity
Image Analysis
Filament Area Distribution (s/m):
Engi-Mat: 0.19
Nexans: 0.21
Nb47wt.%Ti: 0.05
Both the area and the critical current distributions are closely correlated
Wire Axis
Bi-2212 filaments
Ag-0.2wt.%Mg sheath
Reacted filaments

## Slide 27: How uniform is a ~1 km long Bi-2212 wire? A complete strand map of the whole 10 kg billet might be able to answer our queries on long length uniformity

## Slide 28: 1200 m lengths of wire do not exhibit significant difference in performance

## Slide 29: Takeaway messages
Conductors as presently made have highly irregular filaments, which means that sausaging is built in, not something that develops as in Nb-Ti by over-drawing
  Although these irregularities become much worse during OPHT wires have high JE that is usable for coils
Wires that have filaments with uniform size, shape, and controlled separation in transverse and longitudinal sections provide a great opportunity for higher Jc
Long length uniformity of Bi-2212 wire is sufficiently good to wind km-lengths into magnets

## Slide 30: Thoughts on developing a Bi-2212 powder specification
Specify
Overall composition
Maximum fraction of each of the non-superconducting phases in powder
Maximum particle size of non-superconducting phases in powder
Particle size of Bi-2212
Maximum C and H (H2O) contents