## Slide 1: Measurement of displacement cross section for high-energy protons and future plan for material damage using 400-MeV protons at J-PARC
(J-PARC/JAEA) Shin-ichiro Meigo
8th RaDIATE Collaboration Meeting
June 26 – 30, 2023

## Slide 2: Outlook
Introduction of displacement cross section
Measurement of displacement cross section
  J-PARC for 0.4 – 30 GeV
  FNAL for 120 GeV
  CERN for 430 GeV
New facility for irradiation facility at J-PARC
  Aim for irradiation facility
  Multipurpose use for new facility
Summary

## Slide 3: Thank you BNL (ASTE collaboration)
Before start building of SNS, J-PARC, we did experiment using mercury target and proton beam at AGS/BNL as AGS spallation target experiment (ASTE) collaboration.
Laser Doppler Vibrometer
(LDV)
Mercury target vessel
M. Futakawa, et al., NIM A439 1 (2000)
Beam instruments
AGS to RHIC
D 20 cm x L 1.3 m

## Slide 4: Contents
Introduction of displacement cross section
Measurement of displacement cross section
  J-PARC 0.4 – 30 GeV
  FNAL 120 GeV
  CERN 430 GeV
New facility for irradiation facility at J-PARC
  Aim for irradiation facility
  Multipurpose use for new facility
Summary
Neutron beam lines (23)
Bird’s eye photo
Transmutation
Facility (TEF)
(Phase II）
Hadron Experiment Facility
Neutrino Exp. Facility
(294km to Super KAMIOKANDE)
Materials & Life Science Facility (MLF)
3GeV Synchrotron
RCS (25Hz,1MW)
Linac
400MeV(50mA)
JRR-3M
800m to MLF
30GeV Synchrotron
MR (0.75MW)
J-PARC = Japan Proton Accelerator Research Complex
JFY2007 Beam
JFY2008 Beam
JFY2009 Beam

## Slide 5: Introduction
ADS proposed by JAEA
Beam power 30 MW
1.5 GeV, 20 mA
Pb-Bi target
Proton beam window： Al alloy
(J-PARC neutron source at MLF)
W target: J-PARC TS2 for neutron and muon (Planned)
Proton
3 GeV
Proton
30 GeV
Proton injection
Displacement of atom
Beam window： Ti alloy
(J-PARC Neutrino facility)
Damage estimation is crucial to structural materials such as beam windows and targets used in high-intensity proton acceleration facilities (ADS, spallation neutron source).
Window
Proton
1.5 GeV

## Slide 6: Neutron prod. target vessel
Mercury (Hg) target vessel has a pitting erosion due to the high-pressure wave.
Tentative radioactive storage getting narrower
  The vessel is going to be used for 2 years instead of 1 year.
Abrupt heating of mercury
Pressure wave
Thermal expansion
Mercury
Wall
Cavitation bubble
Bubble inflates by the mercury negative pressure.
Cavitation bubble shrinks rapidly.
Shrink energy concentrates to one point
Wall
Micro-jet
Mercury vessel
Beam window (2.5 mm-t)
Most vulnerable to cavitation damage

## Slide 7: Displacement cross section (X-sec)
dpa (displacement per atom)：
Widely used as damage index for fission
and fusion reactors, and accelerator fac.
dpa = Fluence x displacement X-sec
Lack of data above 20 MeV: Difficult validation of calculation models
⇒ Experiments started at J-PARC
σ(E): Displacement cross section [b]
Δρ： Change of resistivity [Ω/m]
Φ: Fluence of incident protons [/cm2]
ρf: Resistivity change by Frenkel pair [Ω/m]
Displacement cross section：
Following Matthiessen's low obtained by observation of electrical resistivity [Ω/m].
To sustain the damage in sample, cryocooling is required for T < 20 K.
N. Mokhov, HPTW2016

## Slide 8: Displacement cross section at J-PARC
Instruments equipped upstream of beam dump for 3GeV synchrotron (RCS Rapid Cycling Synchrotron) : available various kinetic energy of proton 0.4~3 GeV
  Precious beam turning and monitor (beam scanning made for alignment)
  Achieved ~4 K (but used ~8 K to maintain normal conducting at sample)
From 3GeV RCS
Beam dump
To MLF
Equipped vacuum chamber with GM cooler
1 m
Beam
V+
V-
I+
I-
Sample wire
To obtain precious resistance
4 electrodes applied
Nb wire (Φ 0.25 mm) 99.9%
Cryocooler and sample

## Slide 9: Experiment at FNAL
GM cooler RDK-408D2
Similar manner of J-PARC experiment was applied at Fermilab Beam Test Facility (FTBF) M03.
1 m
Al plate
Thermometer
V+
V-
I-
I+
Horizontal beam position and width were scanned by using motion table.

## Slide 10: Electrical resistance change
Electrical resistance changes of metals at 8 K under 120 GeV proton irradiation
68 nΩ for 6.4×1014 protons
165 nΩ for 6.4×1014 protons
1.2 μΩ for 6.4×1014 protons
7.3 μΩ for 6.4×1014 protons
Al
Cu
Nb
W
Thermal jump?

## Slide 11: Disp. X-sec calculation in PHITS
Cross section given by PHITS
  Widely utilized Norgett-Robinson-Torrens (NRT) model
  arc-dpa model
    Nordlund and Konobeyev’s parameter applied
Displace number by NRT model (Nd)
Displace number by arc-dpa model (Nd arcdpa)
For ramp region Td> 2Ed/0.8,
the difference between the two models is a factor of 1.5.
arc: Athermal Recombination Correction
Td: Displacement energy
arc-dpa: instantaneous recombination at cryogenic
Nb
Ed 78 eV
Displace number
i : particle species
Displacement energy Td [eV]
Displacement number
Nd [Number]
ramp
x 1.5

## Slide 12: Comparison with calculation
Similar tendency of NRT and arc-dpa calculation for Ep<120 GeV
Nb ??
Hopefully try to measure by another chance
H. Matsuda, JNST 57 1141 (2020)
S. Meigo, EPJ Web of conf 239 06006 (2020)

## Slide 13: Ep 430 GeV at HiRadMat in CERN (plan)
Experiment in 2024
Borrowing vac. chamber and cryocooler used at HiRadMat

## Slide 14
  New facility for beam irradiation at J-PARC

## Slide 15: J-PARC TEF/ADS Project Transmutation Experimental Facility
ADS Target Test Facility (TEF-T)
Investigate engineering characteristics of LBE spallation target
400MeV-250kW Proton Beam
LBE Temperature 500℃max
Oxygen Potential Controlled
Hot Cell for PIE samples preparation
LINAC
RCS
MLF
LINAC: Linear accelerator
RCS： Rapid Cycling Synchrotron 3 GeV synchrotron
MR: Main Ring
MLF： Material Life Science Experimental Facility
HD: Hadron experimental facility
NU: Neutrino experimental facility
HD
NU
MR
TEF-P
TEF-T
Notes: In the J-PARC, we are trying to build up the TEF, transmutation experimental facility to develop the ADS.
As you know already, the TEF is divided into two fields:
One is a target facility and another is Physics facility.
This facility is do the engineering experiments relating to target technologies and physics on subcritical core.

## Slide 16: Overview of TEF-T
Isotope separation on-Line (ISOL) and belonging 2nd target were planned. Those are eliminated in the new plan.
TEF-P beam transport is no needed.
ADS Target Test Facility : TEF-T

## Slide 17: J-PARC proton beam irradiation facility
Proton beam irradiation facility planned at J-PARC
  H- beam 0.4 GeV, Power >250 kW with 25 Hz
  Dose >20 dpa/year at the Pb-Bi (LBE) target
User communities established for multi-purpose
  Head of mat. irradiation: Makimura-san
ADS: accelerator driven system
TEF-T: ADS Target Test facility
(JAEA Tech 2017-3)
Proton for space env. use
Low int. H+ extracted by LASER
232Th(p,X)225Ac
Building Hot-lab is also planned for PIE
Multi-purpose use
1. Irradiation fac.
2. Neutron for soft error
3. RI medicine 225Ac
4. Space env. use
With 0.4 GeV proton, sample receives equivalent He/dpa for high energy region.

## Slide 18: Hot lab for PIE
For the PIE of the samples irradiated at new facility, a new hot lab is planned to be constructed adjacent to the new facility.
Due to difference of the law regarding to irradiation sample environment, PIE has not been performed at J-PARC.
  JAEA: Radio Isotope
  J-PARC: Activated materials
J-PARC needs hot lab for PIE not only for MLF, but also other facilities of T2K and hadron.
Allowing to dismount MLF’s target vessel for mercury
Cells for PIE
- With manipulators
Specimens placed at LBE target will be transferred to cells by the channel located at underground.
We will minimize the space of the hot lab to reduce the cost.

## Slide 20: Variate of irradiation circumstance
LBE target
High-energy accelerator and fusion users were excavated by attending their conference

## Slide 21: Soft errors and semiconductor
Hitachi web page
Neutron beam profile
Highest cosmic neutron can provide.
Neutron beam line
w/o moderation
Φ0.2 m

## Slide 22: dpa and Single Event Upset (SEU) at semiconductor
NIEL: Non Ionization Energy Loss
= SEU cross section
Very simulator behaviors for projectile energy
Displacement X-sec
Recoil of capture gamma (1/v behavior)

## Slide 23: RI medicine production
Production of RI for medicine for TAT
a-emitting nuclides such as 225Ac (T1/2 10 d) play important roles.
211As production was promoted at RCNP and RIKEN using 209Bi(a,2n)211At reaction.
232Th target
(Φ110 – 60 mm x L 5mm)
LBE
225Ac production from 226Ra
~ 0.1TBq/year

## Slide 24: Proton for space use
Japan Aerospace Exploration Agency (JAXA): MMX (MMX: Martian Moons Exploration) Launch 2024 and return to earth 2029
Interplanetary Radiation Environment Monitor (IREM)
J-PARC with JAXA and NICT conducted the experiment at 3NBT.
Laser charge exchanger in new facility make it possible more frequently
To enhance the construction of the new facility, we explore the multi-purpose use for use of proton with low intensity, as well.
CHARMS (Charging and Radiation Monitors for Space weather) by NICT
NICT: National Institute of Information and Communications Technology
Experiments made at RCS beam dump

## Slide 25: Summary
120-GeV proton displacement cross-section:
  Successfully obtained the experimental data
  arc-dpa : good agreement with experiment except for Nb (Hopefully, retry in the future)
  NRT: Overestimate similar to the results for Ep < 30 GeV.
New facility:
  User community was established not only for material irradiation but also soft error and RI medicine.
  Since their demand is important to build the new facility, we are going to stimulate the activate among the communities.
  User community established (member ~250 persons)
  Technical Advisory Committee requires international user community. Please join this community!

## Slide 26
Supplement

## Slide 27: Comparison of Nb X-sec for neutron incident
Neutron results similar to proton E>100 MeV：
proton incident （nuclear force + Coulomb force)
⇒ Showing applicability for high energy region neutrons
With similar manner, data for 14-MeV neutron was deduced from the LLNL experiment.
M.W. Guinan et al., JNM 108&109 95 (1982)
PHITS code
KIT evaluation
NRT and arc-dpa showing agreement with experiment within error
NRT： Overestimation 50%
arc-dpa： good agreement

## Slide 29: Workshop for Facility Planning
J-PARC 35
JAEA (non J-PARC) 19
KEK (non J-PARC) 7
University 14
Research institute 19
Industry 36
Others 3
Participants:
In-person 14
On-line 119
Total 133
Workshop on “J-PARC Proton Beam Irradiation Facility Plan and Launch of User Community”
Host: J-PARC Center
Date: July 28, 2022, 13:00−16:00
Style: in-person @J-PARC + on-line (hybrid)
Purpose
  To discuss status of the facility planning and the possibility for versatile needs
  To launch a user community for supporting the facility planning and clarifying versatile needs
Agenda
Opening H. Oigawa (JAEA director)
Nuclear transmutation K. Tsujimoto (JAEA)
Facility design update F. Maekawa (J-PARC)
Needs from materials irradiation S. Makimura (KEK)
Needs from proton beam applications K. Otsuji (NICT)
Needs from Medical RI production K. Nagatsu (QST)
Needs from soft error testing K. Kobayashi (Kyoto I. T.)
Discussion, Launch of user community all
Closing T. Kobayashi (J-PARC)
Findings
In addition to the nuclear transmutation research, it turned out that there were high expectations for the facility that could use the J-PARC’s high-intensity proton beam at J-PARC.
The user community for the experimental facility was launched.

## Slide 30: TEF-T specification
Already Technical Design Report has been published to JAEA report.

## Slide 31: Hot lab for PIE
For the PIE of the samples irradiated at new facility, a new hot lab is planned to be constructed adjacent to the new facility.
Due to difference of the law regarding to irradiation sample environment, PIE has not been performed at J-PARC.
  JAEA: Radio Isotope
  J-PARC: Activated materials
J-PARC needs hot lab for PIE not only for MLF, but also other facilities of neutrino and hadron.
Furthermore, MLF probably requires to dismount the large target vessel for mercury using laser, which will be one of option of dismount stratage.
Cells for PIE
- With manipulators
Specimens placed at LBE target will be transferred to cells by the channel located at underground.
We will minimize the space of the hot lab to reduce the cost.

## Slide 32: Soft errors and semiconductor
Hitachi web page
For soft error and semiconductor
For application of space environment

## Slide 33: Neutron beam line at new facility
Horizontal view
Vertical view
Neutron beam profile (calculation)
Φ200 mm (Plan to expand the beam
JAEA Tech. 2017-003
User wants low dose area by the irradiation samples to prevent from soft-error of their instruments for data acutorsion.
Low
dose

## Slide 34: Proton use
Japan Aerospace Exploration Agency (JAXA): MMX (MMX: Martian Moons Exploration) Launch 2024 and return to earth 2029
Interplanetary Radiation Environment Monitor (IREM)
JAXA and NICT asked to use the GeV protons with low intensity.
Primary beam usage is difficult to simultaneously provide the beam to other facilities. Method using secondary protons produced by scattering at the beam dump window was developed.
To enhance the construction of the new facility, we proceed to explore the multi-purpose use for use of proton with low intensity, as well.
CHARMS (Charging and Radiation Monitors for Space weather) by NICT
NICT: National Institute of Information and Communications Technology

## Slide 35: Examination use of protons at atmosphere
To boost up multipurpose activities, we continued the work at 3NBT dump.
Energy spectrum of protons emitted from the beam dump window (Al) was successfully obtained as function of response function of scintillator.
Obtained energy spectrum of secondary proton spectrum emitted to air at J-PARC 3NBT for the case of 0.4-GeV protons irradiation.
Spectrum of detector #4 for Ep 0.4 GeV
Al-window (0.3 mm-t)
3NBT Dump at RCS
Plastic scintillators □50 mm
14 m at 13-deg for beam direction
Proton band
E4 [channel]
dE3 [channel]
Total leng.
1.45 m
Obtained proton spectrum
Cherenkov counter response
NICT already made experiments. JAXA will do experiment in March.
They want to vary the energy less than 0.4 GeV. At the new facility, the degrader may permit us.
As for validation of nuclear data, the new facility will play the role.

## Slide 36
In Japan, no explicit plan of Ac-225 production so far
New facility has the capability to produce Ac-225 at a level of several hundred GBq by using the proton beam halo in front of the LBE target.
55.5GBq
48.1GBq
5.5GBq
11,285GBq
2,664GBq
3,145GBq
・Target: Th-232 ～8g
・Beam: ～70 μA, 480 MeV proton
・Irradiation： 25 mAh/target
・Product： Ac-225, Ra-225
444
GBq
225Ra (15 d) → β→ 225Ac (9.9d)
This slide is reproduced and slightly modified by the courtesy of Dr. P Schaffer and Prof. H Fukuda, and Prof. T Nakano

## Slide 37: Estimation of Ac-225 production at new facility
225Ac* ~2 GBq
from 225Ra
400 h (～2 weeks) enough
※J-PARC operation：5000 h/year
225Ra
225Ac : TRIUMF produced already
232Th target（1 mmt, Φ110 - 60 mm, 78 g)
Irradiation 25 kW beam(10% of overall)
232Th(p,x)226Ra exp
PHITS calc for 0.4 GeV
0.025 barn
⇒ ~10 μg
※ Law of small amount of nuclear fuel Th < 0.9 kg
※ Detail target design under consideration
5 mmt Th ~10 GBq/mon. ⇒ ~100 GBq/year
Note： Reactor (JOYO) 226Ra 2 g ⇔ 24 GBq/60d
Production estimation with 232Th 1-mmt target
232Th (p,x)225Ra cross section [mb] for Ep 438 MeV
Exp. | PHITS calc.
4.2 | 5.1
Available 226Ra production?
Insufficient production of 226Ra
Availability Tb production like CERN?

## Slide 38: Beam optics using nonlinear optics at MLF
Press release on July 21 2020
Development of High Intensity Proton Beam Control Technology at J-PARC
Beam shaping using nonlinear optics reduces target damage and contributes to safe operation
Octupole magnet
Optimization of the parameter for peak reduction and beam loss
S. Meigo et al., “Two-parameter model for optimizing target beam distribution with an octupole magnet”, PRAB (2020)

## Slide 39: Experimental results of displacement X-sec
Resistivity and temperature during irradiation
Tk [GeV] | Experimental result [b]
0.4 | 1920±455
0.8 | 2140±508
1.3 | 2390±568
2.2 | 2250±534
3.0 | 2550±606
Cross section for 0.4, 0.8, 1.3, 2.2 and 3.0 GeV protons were observed.
- Proton beam repetition rate ~ 1 Hz
Error is dominated by resistivity change for a Frankel pair creation.
ρf = 14 ± 3 Ωm
ΔR
4 μΩ
Resistance [Ω]
Temp. [K]
Δρ (resistivity): ΔR x L/A
L, A: sample geometry
Φ (proton fluence)：
observed by beam monitor
ρf : resistivity change by a Frankel pair

## Slide 40
Sample assembly
Sample assembly
Al plate
Thermometer
Source:6221
Nano-voltmeter
2182A Keithley Inc.
Four point technique
PC
Labview
V+
V-
I+
I-
±10-100 mA
V+
V-
I-
I+
Data taking system
Al, Cu, Nb, and W wires with 0.25 mm diameter and 40 mm length were fixed to aluminum plate.
Electrical resistance measurement using delta-mode 4-terminal method with suppressed thermoelectromotive force.

## Slide 41: Role of niobium (Nb) material in accelerator
Superconducting accelerator: Mainly used Nb
B. Yee-Rendon et al., Phys. Rev. Accel. Beams 24, 12010 (2021)
JAEA-ADS accelerator (1.5 GeV, 20 mA)
SC magnets:
Neutrino facility at J-PARC
Prototype for ADS: Nb
（Spoke: SSR)
J-PARC COMET
SC solenoid
Super conducting (SC)
Normal conducting
- Data of Nb for proton projectile are required.

## Slide 42: Equipment layout in FTBF M03
42
Beam height 51.5 cm
Top view of layout
About 1.8 x 1011 protons per minute

## Slide 43: Layout (cont’d)
J-PARC
Linac
35 m
Hot Lab.61 mx43 m
pRAD
Acc.
Same as T-TAC6
To avoid conflict at here, as the first step design, we skip to be shorten beam transport about 35 m.
Electricity yard
(prohibiting to use underground)

## Slide 44: Neutron for semiconductor and soft error
Spallation neutrons gives users similar ones with a terrestrial spectrum.
New facility gives the flux with ~10 and ~100 times of ISIS/ChipIR and RCNP, respectively.
New facility will provide the best circumstance for SC and soft research.
Solar neutron (En< 1GeV)
Terrestrial neutron spectrum has a peak ~150 MeV.
Required to be at least 150 MeV in power device semiconductor test procedure (JEP151).
N.B. Lethargy: divided by relative energy bin-width

## Slide 45: RCNP (Osaka univ.)
Neutron flux at RCNP WN
RCNP: Research Center Nuclear Physics

## Slide 46: Community for soft error
We joined QiSS (Quantum Innovation for Safety and Smart Society) organized by RCNP at Osaka Univ. The representative of the J-PARC center N. Saito was taken over by Meigo.
We will join general incorporated association QASS (Quantum beam Applications for Safe and Smart society)
To enhance the construction of the new facility, we proceed to explore the multi-purpose use such as study for soft error.

## Slide 47: Preparation use of protons at atmosphere
To boost up multipurpose activities, we successfully obtained an additional budget from the JAEA president's discretionary expenses for R&D space and soft-error.
For proton use at RCS, the energy spectrum of protons emitted from the beam dump window (Al) was successfully obtained as function of response function of scintillator.
Same technique can be applied at new facility to use protons for satellite.
Obtained energy spectrum of secondary proton spectrum emitted to air at J-PARC 3NBT for the case of 0.4-GeV protons irradiation.
Counter telescope of (dE1 – E5) plastic scintillators to apply calorimetric counting
Spectrum of detector #4 for Ep 0.4 GeV
Obtained proton spectrum
Al-window (0.3 mm-t)
3NBT Dump at RCS
Plastic scintillators □50 mm
14 m at 13-deg for beam direction
Preliminary
Proton band
E4 [channel]
dE3 [channel]
Total leng.
1.45 m

## Slide 48: High energy part accel. R&D
TEF-T
8kW
Dump
10W
Dump
Wall
10W
Dump
YAG ( 2J/pulse)
H-
H-
H+
H0
H0Foil
TEF-T BT: 130m
Already built
New
building
H- Beam
400 MeV 25Hz 250kW
Pulse width 0.5ms
Peak current 50mA
For ADS accelerator studies at high-energy region, SC cavities (Spoke, Elliptical) can be installed at beam transport

## Slide 50
LBE target

## Slide 51: Requirement of power semiconductors
Subject | Report | Year
Test Method for Real-Time Soft Error Rate | JESD89-1A | 2007
Test Method for Alpha Source Accelerated Soft Error Rate | JESD89-2A | 2007
Test Procedure for the Measurement of Terrestrial Cosmic Ray Induced Destructive Effects in Power Semiconductor Devices | JEP151 | 2015
Only RCNP and J-PARC/MLF can be applied to JEP151 in Japan.
So far, only two experiments made by Kyusyu-Univ. and a SC bender carried out at MLF/BL10 in J-PARC for SC and soft research.
Requirement of JEDEC (Joint Electron Device Engineering Council)

## Slide 52: TRIUMF implementation plan
De-risking technologies: (matching to JAEA 2050+)

## Slide 53: Neutron facility for SC and soft error
Osaka Univ. (RCNP: Research Center for Nuclear Physics)
ChipIr at ISIS TS-2 (RAL UK)
Users at WNS gradually increased since 2004
Worldwide use
Contributing self-driving cars and ADAS (Advanced Driver-Assistance Systems)

## Slide 54
AGS
CT
JAERI
CT
AGS
SEC
AGS
SWIC
JAERI
SPIC
Hg
Target
Window
AGS
Flag