## Slide 1: Development of High Entropy Alloys for Next-Generation Beam Windows
Nick Crnkovich1, Michael Moorehead3, Gaurav Arora1, Kavin Ammigan2, Frederique Pellemoine2, Izabela Szlufarska1, Sujit Bidhar2, Adrien Couet1
University of Wisconsin-Madison, Madison, Wisconsin, U.S.A
Fermi National Accelerator Laboratory, Batavia, Illinois, U.S.A
Idaho National Laboratory, Idaho Falls, ID, U.S.A
and the effects of nanocrystallinity on radiation tolerance of beryllium
Notes: What is an HEA
Radiation damage in metals
Radiation Tolerance
Design process for HEA

## Slide 2: What are High Entropy Alloys
AKA ‘multi-principle element’ or ‘compositionally complex’ alloys (MPEAs, CCAs)
  Typically no element exceeds 35 at. %
  Studied in solid solution – simple crystals
Promising properties observed…
  Exceptional mechanical properties
  High temperature stability/strength
  Increased fracture toughness
  Enhanced radiation tolerance
(a) Conventional alloy, (b) High-entropy alloy (Miracle, Senkov | 2017)
[1] D.B. Miracle, O.N. Senkov, “A critical review of high entropy alloys and related concepts”, Acta Materialia, Volume 122, 2017.

## Slide 3: Radiation Tolerance in HEAs
T = 500 °C
(Lu | 2016)
Enhanced radiation tolerance has been shown in modeling and experimentation
Numerous proposed mechanisms:
  Enhanced recombination due to
    Concentration of damage cascade/ thermal spike
    Preferential diffusion pathways
  Sluggish diffusion of defects
[2] K. Jin, C. Lu, et al., “Effects of compositional complexity on the ion-irradiation induced swelling and hardening in Ni-containing equiatomic alloys”, Scripta Materialia, Volume 119, 2016.
Notes: FULL CITATIONS

## Slide 4: Radiation Tolerant Microstructures
Typical approach to improving radiation tolerance: increase sink density
Can be unstable for different temperature/damage regimes
Oxide-dispersion strengthened (ODS) alloys
(Allen | 2008)
Nanocrystalline alloys
(Barr | 2018)
100 nm
Cold-worked alloys
(Alshater | 2018)

## Slide 5: Design Goals for HEA
Property
Response
Specific Heat
CTE
Density
Yield stress
Heat Deposition
Temperature Rise
Thermal Expansion
Plasticity
Desired Properties
Low density
High specific heat
Low coeff. of thermal expansion.
Good radiation tolerance
High yield strength
Notes: BORING

## Slide 6: High Entropy Alloy Element Selection
Low density/Z
  Light transition metals
Forms single phase alloy
  Desirable for easier analysis
  Cr-Mn-V ternary forms single phase
  Fe forms intermetallic compounds
Minimal activation under protons
  Co/Cu/Ni have activation concerns

## Slide 7: High Entropy Alloy Design
Activity (Bq) after 5 hr of irradiation (120 GeV protons, 5.2e13 p/s)

## Slide 8: High Entropy Alloy Design
Phase fraction diagram of Al15Co4Cr25Mn15Ti6V35
Region to Maximize
CrMnV (1)
AlCrMnTiV (3)
Lower density/higher specific heat
AlCoCrMnTiV (4)
CrMnTiV (2)
Equimolar BCC single phase
Impurity getter
Semi-coherent B2 phase
Initial (low throughput) attempt resulted in Al15Co4Cr25Mn15Ti6V35
Alloys 1-4 manufactured and studied

## Slide 9: HEA Design Refinement
Systematic search using high-throughput CALPHAD simulations
  >8500 compositions for optimization of
    B2 phase region
    Onset of embrittling secondary phases
    Density, specific heat, CTE
> 120,000 compositions searched by Gaurav Aurora (presenting next)
  New stable single-phase BCC alloys found
 | Al | Co | Ti | Cr | Mn | V
Min | 10 | 0 | 1 | 10 | 1 | 10
Max | 30 | 5 | 15 | 35 | 30 | 35
Step | 4 | 1 | 2 | 3 | Bal | 2
Compositional search space (at%)

## Slide 10: HEA Design Refinement
Al16Cr25Mn30Ti1V24Co4
Al10Cr25Mn26Ti3V34Co2
Al16Cr25Mn30Ti1V26Co2
Al10Cr25Mn28Ti1V34Co2
Increased solidus
Lower sec. phase onset

## Slide 11: HEA Beam Heating
Target case: FNAL’s NuMI beam line
120 GeV protons—1 MW
10 µs pulse @ 0.75 Hz repetition
3 cm diameter window, edge held at 300 K
Energy deposition
Beam Gaussian distribution
Proton flux
Bethe-Bohr electronic stopping power

## Slide 12: HEA Beam Heating
    Temperature profile from single pulse of NuMI beam (120 GeV p, 6.25e13 ppp, σ = 1.3 mm)
    Centerline temperature from pulsed of NuMI beam (10 us pulse, 0.752 Hz)
Tavg = 171 C
Tavg = 670 C
Tavg = 48 C

## Slide 13: HEA Beam Heating
    Centerline temperature from pulsed of NuMI beam (10 us pulse, 0.752 Hz)
Average operating temperature of Al15Co4Cr25Mn15Ti6V35 between 150-200 C
Desired microstructure isn’t thermodynamically stable
  How quickly will C14 Laves or intermetallics form?
Test kinetics via heat treatment at 450-500 C
  Potentially enhanced by irradiation, but pulsed beam might mitigate
Stable operating microstructure
Desired microstructure window

## Slide 14: HEA Initial Characterization
SEM/EDX of
Al15Co4Cr25Mn15Ti6V35
Ti(C-N)

## Slide 15: HEA Initial Characterization
Images taken this month
High volume of precipitates
  Two entirely different morphologies
  Still need confirmation via EDX
    Morphology resembles Laves C14
Heat treatment employed poor at promoting B2 phase
  Homogenized and held at 1200 C only
Notes: Which axis

## Slide 16: HEA Initial Characterization
STEM BF
HAADF
Images taken this month
High volume of precipitates
  Two entirely different morphologies
  Still need confirmation via EDX
    Morphology resembles Laves C14
Heat treatment employed poor at promoting B2 phase
  Homogenized and held at 1200 C only
Notes: High angle annular dark field
Is central precipitate an agglomeration of the small ones?? Are the small ones nucleations of the big ones

## Slide 17: HEA Indentation
Lower density of Ti-(CN)

## Slide 18: HEA Indentation
5 component alloy
6 component alloy
Dislocation pileup
No crack initiation

## Slide 19: HEA Indentation
5 component (top), 6 component (bottom)
Sample | Vicker’s Hardness (Hv) | Modulus of Elasticity (GPa)
CrMnV | 390.58 | 186.93
CrMnTiV | 499.80 | 222.06
AlCrMnTiV | 453.06 | 163.36
AlCoCrMnTiV | 608.19 | 177.29
Ti64 | 339 | 110
Significant hardness increase but with promising signs of ductility
Stiffness greater than but comparable to Ti64

## Slide 20: HEA Current/Future Work
Irradiation with protons and V2+ ions at UW
  At 50-100 dpa what are dominant irradiation effects?
  At low dpa are effects visible?
Differential Scanning Calorimetry at FNAL
Next round of alloys being manufactured
  8 alloys encompassing my work and Gaurav’s
  Efficiency of Ti gettering
  Effect of B2 phase fraction
  High V content alloy
Heat treatment to determine microstructure evolution at estimated operating temperature
  Hold at 500 C for 45 days
UW Ion Beam Lab is NSUF facility!
  Protons up to 3 MeV and heavy ions
  LN2 cooling recently developed

## Slide 21
Effects of Nanocrystallinity on Irradiation of Beryllium

## Slide 22: Beryllium XRD
Materion – highly textured to basal plane
FNAL- untextured
LiJing Be- less textured
[1010]
[0001]
[0001]
[0001]
[1010]
[1010]

## Slide 23: Preliminary TEM of Be
Materion Be
LiJing Be
BeO precipitates?
Columnar grains

## Slide 24: Beryllium Irradiation Campaign
2.0 MeV protons to 0.25 dpa
  Nanocrystalline/textured Be from Materion
  Untextured Be from FNAL
Nanograins typically improve radiation tolerance via increased sink density
  Effects of texturing?
In process of preparing for TEM
  Twin-jet electropolishing for thin sample proving challenging

## Slide 25
Questions?

## Slide 26: Radiation Damage in Metals
Primary Knock-on Atom (PKA)
Thermal Spike
Damage Cascade
Vacancies
Self-Interstitials
Incoming Particle (n, p+, etc.)
Primary Collision
Thermal Spike
Quench
t→∞
Primary Collision: Incident particle scatters off nucleus of atom in crystal lattice with sufficient energy to remove the atom from its lattice site. This atom is called the Primary Knock-on Atom (PKA).
Thermal Spike:
The PKA recoils and collides with nearby atoms which are knocked from their lattice sites and collide with other atoms forming a damage cascade. Over picoseconds, many atoms are displaced from their lattice sites and the temperature locally rises far above the melting point of the material forming a thermal spike.
Quench
Following the thermal spike, displaced atoms are mobile enough to quickly find new lattice sites. However, as heat from the thermal spike dissipates, the mobility of atoms plummets leaving several surviving point defects: self-interstitial atoms and vacancies.
Long-Term Defect Evolution:
As time progresses and more damage cascades are produced, the population of point defects increases.
As diffusion occurs (minutes, hours, days), point defects can diffuse towards free surfaces or interfaces (sinks) to be annihilated. Dissimilar point defects can annihilate with one another. Alternatively, similar point defects can cluster together, giving rise to voids and dislocations.