## Slide 1: Interaction with Nick
Met in 2018 and 2019
Extensive knowledge in material science, radiation damage, mechanical engineering
Eagerness to share his insights and knowledge with his peers and mentees
Full of energy and enthusiasm

## Slide 2: Irradiation Induced Failure Analysis of NuMI Target
Sujit Bidhar
June 27, 2023

## Slide 3: Background- NT02 Target Fin
95 cm
Segmented Fins- 47 pieces
Individual target fin
20mm x 15 mm x 6.6 mm
Material : POCO ZXF 5Q graphite
Isotropic

## Slide 4: Background- Fracture fin
y
z
x
z
Beam Parameters:
Energy :120 GeV
Beam sigma : 1.1mm
Spill duration : 10µsec, 4x1013 protons/pulse
Duty cycle :1.87sec
Peak fluence : 8.6x1021 protons/cm2
Bulk swelling of ~2%

## Slide 5
Graphite Swelling Fluence factor
Kelly, J. Vac. Sci. Technol. A 4 (3), 1986
C-axis expansion is more than a-axis contraction
Swelling f(fluence, temperature)
  More swelling at lower temperature
XRD – Pyrolytic carbon

## Slide 6
Graphite Swelling XRD- POCO ZXF5Q
150 C
150 C
C-axis expansion is more than a-axis contraction  net expansion
Interstitial  expansion
Vacancy contraction
c
a
a
N. Simos, PRAB 20, 071002 (2017)

## Slide 7
Swelling factor function
Local Swelling factor =f(fluence)*g(temperature)
sw(Ø,T)= f(Ø).g(T)
∂(sw)= g(T). ∂f(Ø) + f(Ø).{∂ g(T)/ ∂T}. {∂T/ ∂u }
At constant fluence swelling factor follows a polynomial function with temperature (next slide)
Fluence is Gaussian distribution with location
f(Ø)=exp{-b(u/σ)2}
u=u(x,y,z)
Steady state thermal analysis

## Slide 8
Swelling Temperature Factor
Pronounced swelling at lower temperatures
D. Schweitzer, Physical Review, Vol 128 (2), 1962, pp .556-559
1 MWD = 7e16 nvt
Chart: Temperature factor
| 20 | 30 | 38 | 42 | 57 | 65 | 75 | 90 | 120 | 160 | 190
normalized data | 1 | 1.0326 | 0.97826 | 0.94565 | 0.92391 | 0.86957 | 0.86957 | 0.73913 | 0.54348 | 0.3587 | 0.19565
∂g(T)=-7 T3 - -5 T2 + -3 T+1.0083
NTO2 steady state operating temperature range

## Slide 9
Steady State Thermal Analysis
Path-y
Beam direction
Path-x
(a)
Chart: Distance from beam center, mm
| 0 | 6.8750000000000006E-2 | 0.13750000000000001 | 0.20624999999999999 | 0.27500000000000002 | 0.34375 | 0.41249999999999998 | 0.48125000000000001 | 0.55000000000000004 | 0.61875000000000002 | 0.6875 | 0.75624999999999998 | 0.82499999999999996 | 0.89375000000000004 | 0.96250000000000002 | 1.0313000000000001 | 1.1000000000000001 | 1.1688000000000001 | 1.2375 | 1.3063 | 1.375 | 1.4438 | 1.5125 | 1.5812999999999999 | 1.65 | 1.7188000000000001 | 1.7875000000000001 | 1.8563000000000001 | 1.925 | 1.9938 | 2.0625 | 2.1313 | 2.2000000000000002 | 2.2686999999999999 | 2.3374999999999999 | 2.4062999999999999 | 2.4750000000000001 | 2.5436999999999999 | 2.6124999999999998 | 2.6812 | 2.75 | 2.8188 | 2.8875000000000002 | 2.9563000000000001 | 3.0249999999999999 | 3.0937999999999999 | 3.1625000000000001 | 3.2313000000000001 | 3.3
path x | 87.04 | 87.027 | 86.989 | 86.925 | 86.837 | 86.724 | 86.588 | 86.429 | 86.25 | 86.05 | 85.832 | 85.596 | 85.345 | 85.079 | 84.801 | 84.512 | 84.214 | 83.909 | 83.597 | 83.282 | 82.964 | 82.645 | 82.327 | 82.01 | 81.696 | 81.389 | 81.088 | 80.794 | 80.508 | 80.231 | 79.964 | 79.709 | 79.466 | 79.235 | 79.016 | 78.81 | 78.618 | 78.44 | 78.277 | 78.128 | 77.995 | 77.876 | 77.773 | 77.685 | 77.613 | 77.557 | 77.516 | 77.492 | 77.484
path y | 87.04 | 86.944 | 86.66 | 86.195 | 85.559 | 84.768 | 83.843 | 82.796 | 81.65 | 80.426 | 79.142 | 77.813 | 76.453 | 75.075 | 73.687 | 72.301 | 70.924 | 69.558 | 68.202 | 66.86 | 65.53 | 64.214 | 62.91 | 61.617 | 60.335 | 59.061 | 57.793 | 56.531 | 55.273 | 54.017 | 52.764 | 51.512 | 50.261 | 49.01 | 47.758 | 46.505 | 45.251 | 43.994 | 42.736 | 41.474 | 40.211 | 38.944 | 37.674 | 36.402 | 35.126 | 33.848 | 32.568 | 31.285 | 30
Chart: Time, sec
Transient Temp. at beam center
Steady state thermal
1/8th symmetry model
Average irradiation temperature 30C~87C

## Slide 10
Swelling factor combined function of fluence and temperature
sw(u,T)=}
Chart: Distance from beam centre (x), mm
g(T) is plotted as function of location , from steady state temperature distribution

## Slide 11
XRD data NTO2 From Nick
Assumption
Experimental swelling = ∂(d/d0)
3.37
3.621
d-spacing, A0
XRD scan spot size is 50µm x 50µm x 10mm
In FEA, element size is made ~ 50µm so that it would match to XRD scan volume
3.542
3.618

## Slide 12
Determining Swelling Coefficient
Equating sw(u,T) to ∂(d/d0)  C
U (mm) | Temperature | sw | d-spacing | ∂(d/d0) | C
0 | 88 | 0.779 | 3.621 | 0.074481 | 0.000894
1.1 | 84 | 0.686 | 3.618 | 0.073591 | 0.001073
2.2 | 81 | 0.442 | 3.542 | 0.051039 | 0.001211
3.3 | 78 | 0.210 | 3.45 | 0.023739 | 0.001245
Chart: 
| 0 | 1.1000000000000001 | 2.2000000000000002 | 3.3
C | 0.095604 | 0.1073 | 0.11541 | 0.11292
XRD
u
Multi-variate regression analysis:
Varying “b” and “σ”to get C curve as flat as possible
 b= 0.155, C = 0.00107, σ =1.11
sw(u,T)=}
sw(u,T)
=}

## Slide 13
Young’s Modulus variation with Fluence Ø
“E” varies with Ø
Ø varies with location.
This two relationship is used to map “E” as a function of location
Chart: Distance from beam centre(x-axis), mm
Chart: Fluence, x1020
Chart: Fluence, x1020
Analytical function fit f1
Ø = Ø0 exp{-0.5(u/1.1)2}
E=E0[1+f1(Ø) ]
Peak fluence 8 x1020 p/cm2

## Slide 14
Static Structural analysis – σyy Distribution
State just before beam pulse after number of years of exposure to neutrons
Path-x
Beam direction
2.45 mm
Compressive
Tensile
Path-x
Path-x
Beam direction
Path-x
Without Swelling
With Swelling

## Slide 15: Simulation validation- failure strength
N. Simos, PRAB 20, 071002 (2017)
Swelling formulation raised the stress level up to 150 Mpa
Nick’s experimental data provided validation of swelling formulation

## Slide 16: Simulation Validation- amount of swelling
Deformed location
From Simulation
(3.323-3.3)*100/3.3= 0.7 %
3.3 mm
Observed bulk swelling at that location ~ 2%
Difference of factor of 2 is not too bad…?
Measurement technique
Assumptions in empirical formulation

## Slide 17: Simulation Validation- Mohr-Coulumb’s factor of safety
Fracture plane
Beam
FS distribution
FS <1
79 MPa
175 MPa
Probable crack initiation sites
Fractography suggest crack starting from inside and propagating outward

## Slide 18: Result
Nick’s experimental data helped in development of an empirical formula for local swelling
Better understanding of material failure mode
Publication of scientific journal paper Nuclear Material and Energy 24(2000)

## Slide 19: XRD at NSLS-II (BNL)
65keV
Xray Spot : 2mm x 0.05mm elliptical
Nick initiated this work and tried to get XRD tomography
We are carrying forward this effort

## Slide 20: In-situ XRD tomography with loading

## Slide 21: Rest in Eternal Peace
Supportive and collaborative environment
Nurturing the next generation of scientists and engineers
Inspirational legacy of excellence and pushing boundaries