## Slide 1: Demonstration of Thermal Limit to Mean Transverse Energy from Cesium Antimonide Photocathode Alimohammed Kachwala Arizona State University

## Slide 2: Outline
Introduction
High QE Cs3Sb Photocathode
Measurements Using Photoemission Electron Microscope
Photoemission Electron Energy Spectra (PEES)
Mean Transverse Energy (MTE)
Quantum Efficiency (QE)
Conclusion
Future Work

## Slide 3: Introduction
At Threshold, MTE ~ kbT, ~25 meV at 300 K
Low Emittance/MTE
LOW QE
Fast Response Time
(<1 ps)
Long Operational Lifetime
Metal Photocathodes
Energy
Φeffective
Ef
Vacuum Level
ℏω > Φeffective
ℏω ~ Φeffective
Position
Cu
Non Linear Photoemission
Need High QE cathodes to beat Non-Linear Photoemission
Physical Review Accelerators and Beams 26.9 (2023): 093401
Physical review letters 125.5 (2020): 054801

## Slide 4: High QE Photocathodes
Low Electron Affinity Semiconductors
Alkali Antimonide Photocathodes
K2CsSb
Na2KSb
Cs3Sb

## Slide 5: Cs3Sb for High Brightness Applications
Operational
Lifetime
Response Time
Applied Physics Letters 102.3 (2013).
Sub pico-second response time with λ = 520 nm
Applied Physics Letters 99.15 (2011).

## Slide 6: Cs3Sb for High Brightness Applications
High QE
Orders of Magitude Higher than Metal Photocathode
Applied Physics Letters 120.19 (2022): 194102.
Low MTE
40 meV at 300K
(Expected 25 meV)
22 meV at 90K
(Expected 8 meV)
At λ=690 nm, QE=0.7E-4
Physical Review Special Topics-Accelerators and Beams 18.11 (2015): 113401.
MTE of ~40 meV (> 25 meV at 300 K)
Physical Surface Roughness
Work Function Variation (“Chemical Roughness”)
Knee at
ℏω = 2.1 eV

## Slide 7: MTE: Photocathode Roughness
J. Appl. Phys. 121, 044904 (2017).
Phys. Rev Applied, 4, 024015 (2015).
(Physical + chemical) roughness
Physical Roughness
Chemical Roughness
Surface Morphology
Phys. Rev. ST- Accel and Beams, 21, 093401 (2018)

## Slide 8: Cs3Sb: Efforts to Grow Smooth Films
Sequential Deposition
Co-Deposition
Sequential: RMS surface roughness = 2.5 nm
Average spacing b/w peaks = 100 nm.
Co-Deposition: RMS surface roughness = 0.6 nm
Average spacing b/w peaks = 40 nm
Journal of Applied Physics 121.4 (2017).
Epitaxial Growth
Physical Review Letters 128.11 (2022): 114801.

## Slide 9: Cs3Sb: Efforts to Grow Smooth Films
Co-Deposition on Lattice Matched Substrate
Thin STO: RMS surface roughness = 0.3 nm
Average spacing b/w peaks = 60 nm.
Thick STO: RMS surface roughness = 0.6 nm
Average spacing b/w peaks = 100 nm.
On Si: RMS surface roughness = 1.4 nm
Average spacing b/w peaks = 100 nm.
Applied Physics Letters 120.19 (2022): 194102.
Observe Knee at
ℏω = 2.1 eV (λ = 620 nm)
Thin (6.3 nm): STO
Thick (40 nm): STO
40 nm thick on Si

## Slide 10: Experiment
Growth
Thickness: ~40 nm
Substrates: Si and Nb doped STO
QE
3% - 4%
λ = 530 nm
Transfer
Via UHV transfer line in PEEM
Measured: PEES, MTE & QE
Measurements
ℏω: 1.45 – 2.33 eV
Repetition rate: 500 kHz
Pulse length: 150 fs
OPA Laser
PEEM
Growth Chamber

## Slide 11: Photoemission Electron Energy Spectra
Substrate: Doped Si
Maximum Ek = 1% of the maxima of the energy distribution curve
Φ
~0.75 eV

## Slide 12: Photoemission Electron Energy Spectra
Φ = 1.6 eV
Electron Scattering during transport
Doped Si
Φ = 4.4 eV
NO Electron Scattering during transport
Platinum
Metal Cathode

## Slide 13: Photoemission Electron Energy Spectra
Substrate: Doped Si
Substrate: Nb Doped STO

## Slide 14: Mean Transverse Energy
Physical Review Special Topics-Accelerators and Beams 18.11 (2015): 113401.
Applied Physics Letters 99.15 (2011).
At ℏω = 1.5 eV, MTE = 30 meV (~25 meV at 300 K)
At ℏω = 1.8 eV, MTE = 40 meV and at ℏω = 2.3 eV, MTE = 150 meV (comparable to previously reported values)
The dotted line is the plot for (excess energy)/3 considering Φ = 1.5 eV (green) and Φ = 1.9 eV (brown)
MTE doesn’t scale as 1/3rd of excess energy (Scattering before emission)
GT

## Slide 15: Quantum Efficiency
1) Applied Physics Letters 120.19 (2022): 194102.
QE at ℏω =1.5 eV is 7 orders of magnitude lower when compared with that at ℏω = 2.3 eV
A knee-like feature is also observed in the QE spectral response at ℏω = 2.1 eV
Unstable D03 cubic structure
Nangoi, J. K., et al. arXiv preprint arXiv:2205.14322 (2022)

## Slide 16: Conclusion
Measured Photoemission electron energy spectra (PEES), MTE, and QE of Cs3Sb photocathodes in the photon energy range of 1.45–2.33 eV
The PEES indicate that for Cs3Sb cathodes is Φ = 1.5 ± 0.1 eV, significantly lower than the 2.1 eV value that was previously reported based on the QE spectral response
The value of MTE at this work function of 1.5 eV was observed to be ~30 meV—very close to the 25 meV (thermal limit) at 300 K within instrumental error
QE of the order of 10-7 at threshold (comparable to metal cathodes).
At ℏω = ~1.9 eV , QE of the order of 10-3 and MTE ~40 meV (better than metal cathodes)

## Slide 17: Future Work
PEES and MTE measurements on epitaxial Cs3Sb/CsSb photocathodes
Photoemission studies of other alkali antimonide photocathodes such as K2CsSb and Na2KSb
Growth and photoemission studies of epitaxial alkali antimonide photocathodes such as K2CsSb and Na2KSb
Study the performance of Cs3Sb and other alkali antimonide photocathodes at cryogenic temperatures

## Slide 18: Acknowledgement
Northern Illinois University
Oksana Chubenko
Arizona State University
Pallavi Saha
Priyadarshini Bhattacharyya
Siddharth Karkare (PI)
Euclid Beamlabs
Eric Montgomery

## Slide 19: Thank You! Questions? Comments?

## Slide 20
Back Up Slides

## Slide 21: MTE Measurement
GB

## Slide 22: MTE
, ,
,

## Slide 23: Cs3Sb/CsSb
Acknowledgement: Elena Echeverria, Cornell University
QE spectral response profile comparison between Cs3Sb and CsSb photocathodes
Growth Procedure: Co-Deposition
Oxidation Response