## Slide 1: Development of Multialkali antimonides photocathodes for high-brightness photoinjectors
Event: P3 Photocathode Workshop, October 3rd – 5th, 2023, New York, USA
Contents:
Multi-alkali antimonides photocathodes development
Why the Optical properties are important?
Experimental results (Cathode 1 & 2)
Density Function Theory (DFT) study (K3Sb, K2CsSb)
Comparison with experimental results
Summary & Future plan
Co-authors:
M. Krasilnikov, A. Oppelt, F. Stephan
DESY, Zeuthen, Germany
D. Sertore, L. Monaco, G. Guerini Rocco
INFN LASA, Segrate, Italy and Università degli Studi di Milano
P3 Photocathode Workshop 2023 , October 3rd – 5th, 2023
Speaker:
Sandeep Kumar Mohanty

## Slide 2
Multi-alkali antimonides photocathodes development
Alkali based Photocathodes (K₂CsSb, Na₂KSb, Cs₃Sb,….) have shown great potential in low gradient guns (<20 MV/m)
  Cornell DC gun, BNL SRF gun
  >1 % QE at green wavelengths, 0.5 - 0.6 mm.mrad/mm thermal emittance
  High average current
  Improves cathode laser efficiency and shaping
DESY collaborates with INFN LASA to explore multi-alkali photocathode performance in high-gradient guns
  INFN LASA, Italy, develops cathode recipe and production
  Photoinjector test facility at DESY Zeuthen site (PITZ) tests cathodes in a high-gradient RF gun.
In the R&D stage (produced a total of 8 cathodes), a reproducible recipe has been achieved for the KCsSb compound with a maximum QE of ~ 9% @ 515 nm [1].
3 KCsSb photocathodes were prepared at INFN LASA in July 2021 and successfully tested at PITZ RF gun [2].
  High QE ( 4-8 % at 515 nm)
  Thermal emittance (0.6 mm.mrad/mm) (lower than Cs₂Te)
  Response time (preliminary results show < 100 fs )
Higher dark current than Cs₂Te
Short operational lifetime (~48 hours)
Thin cathodes: Sb 5 nm
Thick cathodes: Sb 10 nm
[1] Mohanty SK, Krasilnikov M, Oppelt A, Stephan F, Sertore D, Monaco L, Pagani C, Hillert W. Development and Characterization of Multi-Alkali Antimonide Photocathodes for High-Brightness RF Photoinjectors. Micromachines. 2023; 14(6):1182. https://doi.org/10.3390/mi14061182 .
[2] S. Mohanty, "Development and Test Results of Multi-Alkali Antimonide Photocathodes in the High Gradient RF Gun at PITZ", in Proc. FEL2022, Trieste. doi:10.18429/jacow-fel2022-tup04
112.1 (thin)
147.1 (thick)
123.1 (thin)
Produced cathodes
KCsSb film
Mo

## Slide 3
“Multi-wavelength” Optical Diagnostics
used during cathode deposition
Motorized filter wheel
(housing 8 optical filters with different wavelengths)
LDLS laser
Optical filters
Eg+Ea
Real-time QE at 8 different wavelengths
Continuous tracking of the Eg+Ea value in real time.
  Identify the formation of new compounds
(transition from Sb to KSb and then to KCsSb)
Reaction Kinetics
  revealing reaction rates and intermediate stages.
Real-time reflectivity at 8 different wavelengths
Optical Characterization
  provide insights into the energy band structure
and electronic transitions within the compound
To improve + optimize cathode recipe :
  Two new cathodes grown in the new “production” system.
    One thick (Sb = 10 nm) (#137.2)
    One thin (Sb = 5 nm) (#137.3)
  To understand the evolving photocathode structure during and after deposition, a "multi-wavelength" diagnostic setup is utilized.
Multi-alkali antimonides photocathodes development
K
KSb
Cs
5 or 10 nm
KCsSb
Sb
Sequential deposition method
Eg = band gap
Ea = electron affinity
Thickness
Deposition rate
Real-time spectral response
Peaks due to electronic transitions
Real-time spectral reflectivity

## Slide 4
Why the Optical properties are important?
Analyzing a material's electronic structure using optical measurements like spectral reflectivity and spectral response is an indirect approach, relying on interpretations and correlations rather than direct electronic state measurement.
Optical Properties
Spectral reflectivity
Z
E
Eg
Ea
Evac
Conduction Band (C.B)
Valance Band (V.B)
Eg = Band gap
Ea = Electron affinity
Et = Photoemission threshold
Et
Polarisation: P(ω) = ϵ0 χ̃(ω) E(ω)
Complex dielectric function: ϵ̃(ω) = 1+ χ̃(ω)
Real part: ϵ’(ω) = ϵ1 = 1+ χ̃’(ω)
Imaginary part: ϵ”(ω) = ϵ2 = χ̃"(ω) Absorption
Refractive index n(ω) =
Extinction coefficient k(ω) =
Reflectivity R(ω) =
Maxwell model [1]
Peaks due to electronic transitions
e⁻
Spectral reflectivity
Band structure
Dielectric function
[1] F. Wooten, “Chapter 1 - introduction,” in Optical Properties of Solids,F. Wooten, Ed. Academic Press, 1972, pp. 1–14.
C.B
V.B

## Slide 5
Why the Optical properties are important?
Analyzing a material's electronic structure using optical measurements like spectral reflectivity and spectral response is an indirect approach, relying on interpretations and correlations rather than direct electronic state measurement.
Optical Properties
Spectral reflectivity
Peaks due to electronic transitions
Z
E
Eg
Ea
Evac
Conduction band
Valance band
Et
e⁻
Not simplified
to interpret directly
Film thickness
Film
Mo (substrate)
Interference effects due to thickness or the presence of multiple layers (such as thin films and substrates)
Also, surface roughness, etc. can influence.
Interpretation of optical measurements requires theoretical models and assumptions about the underlying electronic structure.
The dielectric function (Kramer’s-Kronig equation) is used to calculate the optical properties of the material.
Quantum Espresso software package and its postprocessing code epsilon.x
Optical properties like reflectivity etc.
Experimental reflectivity
Refractive index n(ω) =
Extinction coefficient k(ω) =
Reflectivity R(ω) =
Our Model
Comparison

## Slide 6
Cathode 137.2 (K+Sb+Cs), Sb = 10 nm (Thick)
Cathode - 1
Power is used for 120 °C
K
KSb
0.4-0.6 nm/min
Cs
10 nm
KCsSb
Sb
Power is used for 140 °C
Power is used for 120 °C
0.6-0.8 nm/min
I
II
Experimental results

## Slide 7
“Real-time” QE & Reflectivity curve 137.2 (KSb – Thick, Cathode-1)
K
During Sb deposition, the reflectivity was increased (at 2 nm).
After 70 nm of K evaporation (transition point) [1,2], there is a change in slope in real-time QE (at all the wavelengths).
After 70 nm of K evaporation (transition point) [1,2], the reflectivity patterns at 365nm, 488 nm, 540 nm, and 515 nm differ from that observed at
632 nm and 690 nm.
The rate of QE increase at 365 nm was higher compared to 297 nm only after 70 nm of K evaporation (e-e scattering!, if hv ≥ 2Eg).
“Real-time” QE vs. evaporated thickness during Sb & K deposition
“Real-time” Reflectivity vs. evaporated thickness during Sb & K deposition
[1] Mohanty SK, Krasilnikov M, Oppelt A, Stephan F, Sertore D, Monaco L, Pagani C, Hillert W. Development and Characterization of Multi-Alkali Antimonide Photocathodes for High-Brightness RF Photoinjectors. Micromachines. 2023; 14(6):1182. https://doi.org/10.3390/mi14061182 .
[2] Ruiz-Osés, M.; Schubert, S.; Attenkofer, K.; Ben-Zvi, I.; Liang, X.; Muller, E.; Padmore, H.; Rao, T.; Vecchione, T.; Wong, J.; et al. Direct observation of bi-alkali antimonide photocathodes growth via in operando x-ray diffraction studies. APL Mater. 2014,2, 121101.
Sb
Chart: Evaporated thickness (nm)
Transition point
Previous XRD studies [2]

## Slide 8
Chart: Evaporated Thickness (nm)
| 0 | 0.1888456 | 0.1872587 | 0.34436559999999999 | 0.59510180000000001 | 0.79505599999999998 | 0.99501030000000001 | 1.0933999999999999 | 1.5837639999999999 | 2.4787970000000001 | 3.2802009999999999 | 3.9848020000000002 | 4.6894020000000003 | 5.3924159999999999 | 6.0954300000000003 | 6.7952690000000002 | 7.4538489999999999 | 8.1584489999999992 | 8.8598759999999999 | 9.5644770000000001 | 10.269080000000001 | 10.97209 | 11.6751 | 12.27655 | 12.977980000000001 | 13.68258 | 14.23484 | 14.939439999999999 | 15.539300000000001 | 16.24231 | 16.84694 | 17.44997 | 18.15457 | 18.754439999999999 | 19.36223 | 20.07159 | 20.720649999999999 | 21.144359999999999 | 21.24436 | 21.344360000000002 | 21.444360000000003 | 21.544360000000005 | 21.644360000000006 | 21.744360000000007 | 21.844360000000009 | 21.94436000000001
Refelcticity
Real-time Reflectivity history during Sb+K deposition (137.2 KSb-Thick,Cathode-1)
Sb deposition
K deposition
Final Reflectivity
Up to 30 nm of K evaporation, there was a marginal change in the shape of the spectral reflectivity curve (but decreased at all λ).
From 30 to 50 nm of K evaporation, in the “Reflectivity vs. Thickness” Fig., there is a change in slope in the reflectivity observed at all λ, and
the shape of the spectral reflectivity (upper plot) curve has also changed.
At 70 nm of K evaporation (transition point), a small curve has appeared (between 2.1 eV to 2.6 eV) in the spectral reflectivity Fig. (upper plot).
@30 nm of K
@50 nm of K
@88 nm of K
“Real-time” Spectral reflectivity vs. Photon energy
@70 nm of K
“Real-time” Reflectivity vs. Thickness
R(%) history during Sb+K deposition (137.2 KSb-Thick) (Cathode-1)

## Slide 9
Cathode 137.2 (K+Sb+Cs), Sb = 10 nm (Thick)
Cathode - 1
Power is used for 120 °C
K
KSb
0.4-0.6 nm/min
Cs
10 nm
KCsSb
Sb
Power is used for 140 °C
Power is used for 120 °C
0.6-0.8 nm/min
I
II

## Slide 10
“Real-time” QE & Reflectivity curve 137.2 (KSb+Cs – Thick, Cathode-1)
After 23 nm of Cs evaporation, a change in slope in the reflectivity curve for 488 nm has been noticed. At this point, the
reflectivity of red wavelengths (632 & 690 nm) starts to decrease.
After 30 nm of Cs evaporation, the reflectivity for green wavelengths (515 & 540 nm) starts to increase.
At the end of Cs evaporation, the QE of UV wavelengths (297 & 365 nm) stabilize initially and then start to increase, whereas
for the rest of the wavelengths, it starts to decrease (excess Cs evaporation!)
“Real-time” QE vs. evaporated thickness during Cs deposition
“Real-time” Reflectivity vs. evaporated thickness during Cs deposition

## Slide 11
Chart: Evaporated Thickness (nm)
| 0 | 0.1888456 | 0.1872587 | 0.34436559999999999 | 0.59510180000000001 | 0.79505599999999998 | 0.99501030000000001 | 1.0933999999999999 | 1.5837639999999999 | 2.4787970000000001 | 3.2802009999999999 | 3.9848020000000002 | 4.6894020000000003 | 5.3924159999999999 | 6.0954300000000003 | 6.7952690000000002 | 7.4538489999999999 | 8.1584489999999992 | 8.8598759999999999 | 9.5644770000000001 | 10.269080000000001 | 10.97209 | 11.6751 | 12.27655 | 12.977980000000001 | 13.68258 | 14.23484 | 14.939439999999999 | 15.539300000000001 | 16.24231 | 16.84694 | 17.44997 | 18.15457 | 18.754439999999999 | 19.36223 | 20.07159 | 20.720649999999999 | 21.144359999999999 | 21.24436 | 21.344360000000002 | 21.444360000000003 | 21.544360000000005 | 21.644360000000006 | 21.744360000000007 | 21.844360000000009 | 21.94436000000001
Refelcticity
Real-time Reflectivity history during KSb+Cs deposition (137.2 KCsSb-Thick, Cathode-1)
Sb + K deposition
Cs deposition
Final Reflectivity
@30 nm of Cs
@52 nm of Cs
@76 nm of Cs
@183 nm of Cs
“Real-time” Reflectivity vs. Thickness
“Real-time” Spectral reflectivity vs. Photon energy
Up to 30 nm of Cs evaporation, the reflectivity was increased at the 365 nm (3.39 eV) wavelength of light.
Up to 76 nm of Cs evaporation, in the “Reflectivity vs. Thickness” Fig., the reflectivity was increased in the green wavelengths
{515 (2.40 eV), 540 nm (2.29 eV)}, also a peak appeared in the spectral reflectivity curve at 2.40 eV (515 nm).
R(%) history during KSb+Cs deposition (137.2 KCsSb-Thick) (Cathode-1)

## Slide 12
Cathode 137.3 (K+Sb+Cs), Sb = 5 nm (Thin)
Cathode - 2
Decrease the power
compared to the previous K
deposition (137.2)
K
KSb
0.4-0.6 nm/min
Cs
5 nm
KCsSb
Sb
Decrease the power
compared to the previous Cs
deposition (137.2)
0.6-0.8 nm/min
II
I

## Slide 13
“Real-time” QE & Reflectivity curve 137.3 (KSb – Thin, Cathode-2)
Sb
K
During Sb deposition, the reflectivity was increased (at 1.5 nm).
There is a change in slope in real-time QE (at all the wavelengths) that has been observed after 41 nm of
K evaporation (transition point).
The rate of QE increase at 365 was higher compared to 297 nm, appeared only after 41 nm of K evaporation
(e-e scattering, if hv ≥ 2Eg).
“Real-time” QE vs. evaporated thickness during Sb & K deposition
“Real-time” Reflectivity vs. evaporated thickness during Sb & K deposition
KSb- 137.2 (Thick)
Cathode-1
Transition point
K
Sb
KSb- 137.3 (Thin)
Cathode-2

## Slide 14
Chart: Evaporated Thickness (nm)
| 0 | 0.1888456 | 0.1872587 | 0.34436559999999999 | 0.59510180000000001 | 0.79505599999999998 | 0.99501030000000001 | 1.0933999999999999 | 1.5837639999999999 | 2.4787970000000001 | 3.2802009999999999 | 3.9848020000000002 | 4.6894020000000003 | 5.3924159999999999 | 6.0954300000000003 | 6.7952690000000002 | 7.4538489999999999 | 8.1584489999999992 | 8.8598759999999999 | 9.5644770000000001 | 10.269080000000001 | 10.97209 | 11.6751 | 12.27655 | 12.977980000000001 | 13.68258 | 14.23484 | 14.939439999999999 | 15.539300000000001 | 16.24231 | 16.84694 | 17.44997 | 18.15457 | 18.754439999999999 | 19.36223 | 20.07159 | 20.720649999999999 | 21.144359999999999 | 21.24436 | 21.344360000000002 | 21.444360000000003 | 21.544360000000005 | 21.644360000000006 | 21.744360000000007 | 21.844360000000009 | 21.94436000000001
Refelcticity
Real-time Reflectivity history during Sb+K deposition (137.3 KSb-Thin, Cathode-2)
Sb deposition
K deposition
Final Reflectivity
@10 nm of K
@20 nm of K
@44 nm of K
@54 nm of K
Up to 10 nm of K evaporation, the shape of spectral reflectivity was marginally changed (shows slow reaction due to comparative low temperature).
Up to 20 nm of K evaporation, the spectral reflectivity was decreased at all the wavelengths.
Up to 54 nm of K evaporation, the shape of the reflectivity curve has changed, and a small curve formed between 1.95 eV and 2.54 eV.
“Real-time” Reflectivity vs. Thickness
“Real-time” Spectral reflectivity vs. Photon energy
R(%) history during Sb+K deposition (137.3 KSb-Thin)
Cathode-2
R(%) history during Sb+K deposition (137.2 KSb-Thick)
Cathode-1

## Slide 15
Cathode 137.3 (K+Sb+Cs), Sb = 5 nm (Thin)
Cathode - 2
Decrease the power
compared to the previous K
deposition (137.2)
K
KSb
0.4-0.6 nm/min
Cs
5 nm
KCsSb
Sb
Decrease the power
compared to the previous Cs
deposition (137.2)
0.6-0.8 nm/min
I
II

## Slide 16
“Real-time” QE & Reflectivity curve 137.3 (KSb+Cs – Thin, Cathode-2)
After 10 nm of Cs evaporation, there is a change in slope in the reflectivity curve for all the wavelengths (except 365 nm).
At the end of Cs evaporation, a small jump appeared at the QE (at all the wavelengths), but afterward, the QE was getting
decreased except UV wavelengths (297 & 365 nm) (temperature-sensitive surface layer! [1]).
“Real-time” QE vs. evaporated thickness during Cs deposition
“Real-time” Reflectivity vs. evaporated thickness during Cs deposition
[1] Mohanty SK, Krasilnikov M, Oppelt A, Stephan F, Sertore D, Monaco L, Pagani C, Hillert W. Development and Characterization of Multi-Alkali Antimonide Photocathodes for High-Brightness RF Photoinjectors. Micromachines. 2023; 14(6):1182. https://doi.org/10.3390/mi14061182 .
Cs
Cs evaporated thickness (nm)

## Slide 17
Chart: Evaporated Thickness (nm)
| 0 | 0.1888456 | 0.1872587 | 0.34436559999999999 | 0.59510180000000001 | 0.79505599999999998 | 0.99501030000000001 | 1.0933999999999999 | 1.5837639999999999 | 2.4787970000000001 | 3.2802009999999999 | 3.9848020000000002 | 4.6894020000000003 | 5.3924159999999999 | 6.0954300000000003 | 6.7952690000000002 | 7.4538489999999999 | 8.1584489999999992 | 8.8598759999999999 | 9.5644770000000001 | 10.269080000000001 | 10.97209 | 11.6751 | 12.27655 | 12.977980000000001 | 13.68258 | 14.23484 | 14.939439999999999 | 15.539300000000001 | 16.24231 | 16.84694 | 17.44997 | 18.15457 | 18.754439999999999 | 19.36223 | 20.07159 | 20.720649999999999 | 21.144359999999999 | 21.24436 | 21.344360000000002 | 21.444360000000003 | 21.544360000000005 | 21.644360000000006 | 21.744360000000007 | 21.844360000000009 | 21.94436000000001
Refelcticity
Real-time Reflectivity history during KSb+Cs deposition (137.3 KCsSb-Thin, Cathode-2)
Sb + K deposition
Cs deposition
Final Reflectivity
From 0-10 nm of Cs evaporation, in “real-time reflectivity vs. thickness” Fig., the rate of change in (slope) of reflectivity (decreasing) at green wavelengths (515 &
540 nm) was higher compared to other wavelengths.
Up to 20 nm of Cs evaporation, in “real-time reflectivity vs. Photon energy” Fig., the curve was observed to be deeper, but the shape was getting narrower.
Up to 30 nm of Cs evaporation, in “real-time reflectivity vs. Thickness” Fig., the “rate of decrease” of reflectivity was stabilized for all the wavelengths.
@10 nm of Cs
@20 nm of Cs
@30 nm of Cs
@60 nm of Cs
@85 nm of Cs
“Real-time” Reflectivity vs. Thickness
“Real-time” Spectral reflectivity vs. Photon energy
R(%) history during KSb+Cs deposition (137.3 KCsSb-Thin)
Cathode-2
R(%) history during KSb+Cs deposition (137.2 KCsSb-Thick)
Cathode-1

## Slide 18
KCsSb Thin (137.3) Cathode-2
After Sb
After K
After Cs
After Sb
After K
After Cs
Comparison of R (%) between KCsSb Thick (137.2) and Thin (137.3) cathodes
Spectral Reflectivity
Spectral Reflectivity
KCsSb Thick (137.2) Cathode-1
Summary
18

## Slide 19
Comparison between KCsSb Thick (137.2) and Thin (137.3) cathodes
Colour of the cathode
Colour of the cathode
Thick
1.05 eV
Thin
1.44 eV
1.87 eV
2.29 eV
1.22 eV
KCsSb Thick (137.2)
KCsSb Thin (137.3)

## Slide 20
Density Function Theory (DFT) study
Simulation results

## Slide 21
Electronic structure (DFT study)
Band structure calculation by HSE method
a = 8.493 angstrom
K₃Sb
(Cubic)
a = 6.025 angstrom
C = 10.690 angstrom
K₃Sb
(Hexagonal)
K₂CsSb
(Cubic)
[1] A. H. Sommer and W. H. McCarroll, “A New Modification of the Semiconducting
Compound K3Sb,” Journal of Applied Physics, vol. 37, no. 1, pp. 174–179, 062004.
[2] A. H. Sommer and W. H. McCarroll, “A New Modification of the Semiconducting
Compound K3Sb,” Journal of Applied Physics, vol. 37, no. 1, pp. 174–179, 06 2004.
[3] C. Ghosh and B. P. Varma, “Preparation and study of properties of a few alkali antimonide photocathodes,”
Journal of Applied Physics, vol. 49, no. 8, pp. 4549–4553, 08 2008

## Slide 22
n(ω) =
k(ω) =
R(ω) =
α (ω) = 4πk/λ
K2CsSb (Cubic) Optical Properties
Real & imaginary part of dielectric function
Refractive index n(ω)
Extinction coefficient k(ω)
Reflectivity R(ω)
Ground-state calculations, are implemented in Quantum Espresso and the dielectric function is calculated in epsilon.x post-processing utility.
Absorption coefficient I(ω)
Imaginary
Real

## Slide 23
Comparison of simulation with experimental results

## Slide 24
Comparison between the DFT Simulation and Experimental Data for K₃Sb
K₃Sb
(Cubic)
Comparison between the reference experimental [1] and simulated imaginary part of the dielectric function
K₃Sb
(Hexagonal)
Comparison of the peaks between reference experimental [1] and our lab-grown KSb (thin) cathodes.
Comparison between the reference experimental [1] and simulated imaginary part of the dielectric function
[1] A. Ebina and T. Takahashi, “Transmittance spectra and optical constants of alkali-antimony compounds k3sb, na3sb, and na2ksb,” Phys. Rev. B, vol. 7, pp. 4712–4719, May 1973.
Experimental [1]
Simulation
Experimental [1]
Simulation
KSb-thin
Potentially thin KSb exhibits a cubic crystal orientation!
However, the observed two major peaks in our KSb-thick cathodes do not match those of the K₃Sb hexagonal or cubic compounds.

## Slide 25
Reflectivity comparison of KCsSb compound
Simulation Spectral Reflectivity K₂CsSb (cubic)
1.49
2.13
2.93
3.67
4.39
Chart: Photon energy (eV)
| 4.1750841750841747 | 3.5428571428571427 | 3.263157894736842 | 3.0617283950617282 | 2.7555555555555555 | 2.540983606557377 | 2.407766990291262 | 2.2962962962962963 | 2.1052631578947367 | 2.0064724919093853 | 1.8787878787878789 | 1.7222222222222223 | 1.5696202531645569 | 1.441860465116279 | 1.3626373626373627 | 1.3191489361702127 | 1.2653061224489797 | 1.2277227722772277 | 1.180952380952381 | 1.1376146788990826 | 1.0782608695652174 | 1.0598290598290598 | 1.0333333333333334
R KCsSb 137.2 (Sb = 10 nm) | 24.7549 | 30.488 | 30.5114 | 30.0957 | 29.2176 | 24.8809 | 27.917 | 22.4736 | 14.8931 | 13.2297 | 11.8073 | 14.6413 | 23.7357 | 25.2788 | 18.1217 | 26.726 | 26.2835 | 32.0017 | 40.0417 | 45.0779 | 48.2182 | 49.8948 | 45.2438
R KCsSb 137.3 (Sb = 5 nm) | 13.0542 | 25.759 | 27.3282 | 28.3233 | 28.5711 | 25.9119 | 19.0903 | 19.4363 | 12.0266 | 15.6706 | 20.1223 | 22.7759 | 24.553 | 29.313 | 33.6016 | 35.3151 | 37.6077 | 37.6114 | 41.6744 | 42.1781 | 46.9411 | 46.4059 | 42.0106 | 33.6375 | 25.3428 | 20.0357 | 18.0947
2.40
3.06
Simulation Reflectivity K₃Sb
1.05 eV
1.22 eV
1.49
1.44 eV
Thin
Sb = 5 nm
Thick
Sb =10 nm
Band structure
K₃Sb
K₃Sb
1.54 eV
Experimental Spectral Reflectivity KCsSb
To arrive at a definitive conclusion, verification with photoemission spectroscopy results is necessary!!

## Slide 26
Summary & Future plan
Two cathodes have been produced with sequential deposition with QE @514 nm recorded 4-6 %.
A new “multi-wavelength” Optical Diagnostics setup has been used during the cathode deposition
  It gives information about real-time spectral response and reflectivity during cathode growth.
  The optical spectra of these semiconductors provide a rich source of information on their electronic properties.
Comparing the spectral reflectivity between two cathodes (having different thicknesses) shows that the intermediate phase, i.e., K+Sb (KSb compound), and the final phase, i.e., KCsSb compound, potentially contain different crystal structures for thick (Sb = 10nm) and thin (Sb = 5 nm) cathodes. (Further verification through photoemission spectroscopy results is required!)
By comparing with DFT simulation data, it has been found that, potentially, both the cathodes (i.e., thin and thick) have a different band gap.
By analyzing optical spectra, particularly spectral reflectivity, and comparing them with theoretical models (DFT results) offers a valuable method to predict the electronic structure of the grown compound.
Having knowledge of these real-time optical properties can further help to develop the automated growth procedure.
Future Plans:
  The next batch of green cathodes is planned to be tested at PITZ at the end of this year.
  TRAnsverse Momentum Measurement (TRAMM) device is currently being developed and planned to be integrated into the production system to measure thermal emittance.
  Photoemission spectroscopy study.
Thank You for your attention!

## Slide 27
Backup Slides

## Slide 28
R(%) history (137.2 KSb-Thick)
R(%) history (137.3 KSb-Thin)

## Slide 29
Comparison between the DFT Simulation and Experimental Data for K₃Sb
K₃Sb
(Cubic)
Comparison between the reference experimental [1] and simulated imaginary part of the dielectric function
K₃Sb
(Hexagonal)
Comparison of the peaks between reference experimental [1] and our lab-grown KSb (thin) cathodes.
Comparison between the reference experimental [1] and simulated imaginary part of the dielectric function
Comparing the transmittance data from reference experiments [1] for the cubic and hexagonal structures of K₃Sb.
[1] A. Ebina and T. Takahashi, “Transmittance spectra and optical constants of alkali-antimony compounds k3sb, na3sb, and na2ksb,” Phys. Rev. B, vol. 7, pp. 4712–4719, May 1973.
Experimental [1]
Simulation
Experimental [1]
Simulation
Not exactly match
KSb-thin
Potentially thin KSb exhibits a cubic crystal orientation!
KSb-thin
KSb-thick

## Slide 30
“New” KCsSb #8 cathode
KCsSb #8 has grown in the R&D preparation chamber
through sequential deposition method.
130 °C
120 °C
90 °C
0.2-0.4 nm/min
Sb
K
Cs
0.3-0.6 nm/min
Deposition rate has been changed compared to previous
methods (i.e., 1 nm/min) during K and Cs deposition.
Due to little elevated temp. 130 °C (before 120 °C) and
slow deposition rate (0.2-0.4 nm/min), which helped to
improve the QE (record high ~ 1.2 % at 543 nm) for KSb film.
Unfortunately, the Cs source was completely empty during the
Cs deposition, so we observe a disturbance in the QE curve.
The final QE of KCsSb #8 is
  5.1 % @543 nm (compare to 3.07 % for thin cathodes )
  8.84 %@ 515 nm (compare to 6.88 % for thin cathodes
  (the QEs are estimated by including the transmittance of the viewport)
Photocurrent and reflectivity history (not include transmittance of the viewport)
KSb
KSbCs
5nm
* Here the transmittance value of viewport is not included in QE data

## Slide 31
n(ω) =
k(ω) =
R(ω) =
α (ω) = 4πk/λ
K3Sb Cubic Optical Properties
Real & imaginary part of dielectric function
Refractive index n(ω)
Extinction coefficient k(ω)
Reflectivity R(ω)
Ground-state calculations, are implemented in Quantum Espresso and the dielectric function is calculated in epsilon.x post-processing utility.
Absorption coefficient I(ω)
Real
Imaginary

## Slide 32
n(ω) =
k(ω) =
R(ω) =
α (ω) = 4πk/λ
K3Sb Hexagonal Optical Properties
Real & imaginary part of dielectric function
Refractive index n(ω)
Extinction coefficient k(ω)
Reflectivity R(ω)
Ground-state calculations, are implemented in Quantum Espresso and the dielectric function is calculated in epsilon.x post-processing utility.
Absorption coefficient I(ω)
1.04
1.54
2.18
2.46
2.85
3.32
4.15
4.62
Real
Imaginary

## Slide 33
Reflectivity comparison of KSb compound
Chart: Energy (eV)
Chart: Photon energy (eV)
| 4.1750841750841747 | 3.3972602739726026 | 2.540983606557377 | 2.407766990291262 | 2.2962962962962963 | 1.9620253164556962 | 1.7971014492753623
R KSb- 137.3 | 27.101 | 29.8977 | 35.3271 | 27.9726 | 26.2831 | 30.3049 | 34.7553
R KSb-2 | 12.6204 | 14.808 | 13.4473 | 13.1835 | 12.6183 | 12.339 | 12.9347 | 16.657 | 17.9455 | 16.1882 | 15.1238 | 13.8761 | 12.7838 | 13.7698 | 15.3447 | 16.9449 | 17.0386 | 19.2138 | 22.624 | 24.8746 | 26.0856 | 27.0625 | 27.7504 | 28.8971 | 31.2949 | 31.5543 | 34.8612 | 36.9468 | 38.0285 | 42.7529 | 46.3855 | 47.4251 | 45.938 | 42.2894 | 40.9096 | 39.6905 | 35.7541 | 32.6244 | 30.0983 | 27.8195 | 18.5125 | 15.3282
R KSb 137.2 | 26.0711 | 23.9788 | 21.7999 | 18.6361 | 10.9865 | 9.9597
R KSb-5 | 30.8919 | 41.4401 | 41.0504 | 38.9549 | 30.551 | 32.9757 | 32.3922 | 28.1075 | 25.5718 | 22.562 | 18.5814 | 12.5291
Thin KSb
Thick KSb
Experimental Reflectivity KSb
Simulation Reflectivity KSb
Experimental Optical density for K3Sb cubic & hexagonal
findings by A. H. SOMMER
Journal of Applied Physics 37, 174 (1966); https://doi.org/10.1063/1.1707801
R &D
1.032 eV
1.54 eV
1.42 eV
2.70 eV
3.90 eV
3.37 eV
4.50 eV
2.75 eV
3.71eV
3.06 eV

## Slide 34
K + Sb
Diffusion
Evaporation
Incoming Cs
Reaction of Cs with different bulk agent
jump at the end
Bulk
Rate of diffusion α Substrate Temperature
A very temperature-sensitive surface layer
that make an equilibrium point between
inward cesium (being distributed, diffused) and
evaporated cesium.
Sudden decrease in evaporation rate
would immediately upset this balance or equilibrium
point and would impact the emission barrier via the electron
affinity.
KCsSb Photocathodes
Cathode | Temperature (°C) during Cs deposition | Δ QE (elevation)
KCsSb-3 | 60* | 1.87
KCsSb-4 | 90 | 0.86
KCsSb-5 | 90 | 0.87
KCsSb-6 | 90 | 0.86
KCsSb-7 | 110 | 0.64