## Slide 1
Photocathode Physics for Photoinjectors (P3) Workshop
Brookhaven National Laboratory, NY, October 3-5, 2023.
Electron Scattering Processes in Photoemission:
The Franck-Condon Effect
W. Andreas Schroeder
Louis Angeloni and Ir-Jene Shan
Physics Department, University of Illinois Chicago
Department of Energy
DE-SC0020387
UIC

## Slide 2
UIC
Outline
Metallized diamond(001) photocathode
 Two electron emission signals:
(i) Inner (small MTE) signal due to direct NEA emission from upper CB
(ii) Outer (large MTE) and stronger signal from optical phonon assisted emission
via the Franck-Condon effect – a momentum resonance
Near threshold MTE from ‘good’ metal photocathodes at 300K
 Sub-threshold MTE > 25meV (25-130meV measured)
 Sub-threshold MTE material (but not strongly crystal orientation) dependent
 POSTULATE: Emission via Franck-Condon effect after electron-electron scattering

## Slide 3
Photocathode characterization system
 Laser / NLO based sub-picosecond tunable UV radiation source: 3.0 – 5.3eV (235-410nm)
UIC
20 W Yb:fiber laser
400 fs, 16.7 MHz, 1030 nm
Nonlinear fiber
(SC-3.7-975)
Detector:
MCP & CCD camera;
Faraday cup
Non-collinear
sum frequency
UV generation
ΔpT measurement
LBO
LBO
LBO
LBO
LBO
6 W 515 nm
BBO
15 W
0.5 W
SHG
SHG
THG
F
OPA 2
OPA 1
-10 kV
3
s,i
Continuum
(700-950 nm)
Tunable UV (0.1-1mW)
2

## Slide 4
UIC
Prior work: N-doped diamond(001)
MTE  50meV
7.05
5.4
E
(eV)
pz
X
Γ
0
C
B
A
Evac.
ℇF
2.4eV
Δ = 1.65eV
4.7eV

Nitrogen dopant states
L.A. Angeloni et al., Phys. Rev. B 107, 165105 (2023)

## Slide 5
UIC
Metallized diamond(001)
Injection from ‘Ohmic’ metal contact
(constant metal DOS & parabolic band approximation):
Boltzmann tail emission after energy equipartition with optical phonons under acceleration in EDC/r :

... for
upper CB of diamond
CBs
ℇF
Evac.
ħω
N states
Metal Diamond Vacuum
(Au/Pt/Ti)
d = 0.5mm
e-
  0.5eV
int.
EDC

## Slide 6
UIC
Metallized diamond(001) emission
ħω = 4.54eV
Two emission signals:
Outer large MTE signal from strong optical phonon assisted Franck-Condon effect
 Emission of Boltzmann tail of electron distribution
from NEA upper CB of diamond (  1eV)
 High emission efficiency over PE barrier due to
momentum resonance (T  1)
Inner signal with MTE < 100meV from electrons
directly emitted from NEA upper CB of diamond
 Lower emission efficiency as ;
less than ~5% of total signal
BOTH with Gaussian spatial beam profiles
J.D. Rameau et al., Phys. Rev. Lett. 106, 137602 (2011)

## Slide 7
UIC
Boltzmann tail emission
Direct band emission:
Franck-Condon effect:
 Parabolic band approximation

## Slide 8
UIC
Inner signal MTE
Minimum MTE  35meV occurs when
 Initial electron cooling (by LO phonon emission)
generates same number of phonons as photo-
injected electrons
 Direct initial energy equipartition
For E > 0.41eV, initial energy equipartition maintained

... red line (ϕint.= 3.15eV, m* = 0.45m0)
Parabolic band approximation breaks down for lower CB when E > 0.8eV (ħω > 4.0eV)
MTE  35meV

## Slide 9
UIC
Outer signal MTE
Parabolic band analysis
...
 Upper CB NEA =     1.15eV
 Strong electron-phonon coupling; nav.  2

... = 165meV
QE reaches 10-6 – 10-5 for ħω > 5eV
J.D. Rameau et al., Phys. Rev. Lett. 106, 137602 (2011)

## Slide 10
UIC
Near threshold MTE in metals
‘Accepted’ idea:
Low MTE (< 50meV) readily obtained by operating close to PE threshold
At the expense of lower QE
 Order of magnitude decrease from
E = 0.15eV to 0.05eV
NOTE:
vs. ħω plot allows
extraction of work function
T. Vecchione et al., 35th Intl. Free-Electron Laser Conf., New York, NY (2013), pp. 424-426
T = Te = 300K
25meV

## Slide 11
UIC
Cu(001): Near threshold MTE
MTE  30meV > kBTe measured below threshold (E < 0) at 300K
Direct band emission simulation predicts MTE  14meV below threshold (E < 0)
... –
W.A. Schroeder & G. Adhikari, New J. Phys. 21, 033040 (2019) 033040
(eV)
T = 300K

## Slide 12
UIC
Other ‘good’ metals
Metal | MTE (meV) (E < 0)
Ag(001) Cu(001) Rh(110) Nb(001) W(001) W(111) Ta(001) Ta(111) Mo(001) | 256† 293 706 13012 839 9111 8216 10013 809
†Bulk plasmon effects
83(9)meV
T = 300K
W(001)

## Slide 13
UIC
Electron-electron scattering I
Small excess energy E
 Small
Franck-Condon effect
 PE barrier transmission T  1
Two initial electrons from occupied states; One final electron into unoccupied states
 Probability
...
 Sommerfeld free electron model; Near threshold emission
pz
pT
pF
~ kBTe

## Slide 14
UIC
Electron-electron scattering II
Two below threshold emission processes:
(i) Direct band contribution
...
(ii) Electron scattering contribution
BUT: What is M ?
 Energy dependence (neglecting DOS)
Below threshold
(E < 0)
Above threshold
(E > 0)
- - -
- - -

## Slide 15
UIC
Thermal electron mass
Specific heat of metals
Electron specific heat:
Sommerfeld free electron model gives
Measured
... M is thermal electron mass
Metal | M/m0 | NFS
Ag Cu Rh Ta W Nb Mo | 1.006 1.366 6.09 6.69 7.56 14.25 14.95 | 1 1 4 2 2 2 3 or 4
G.R. Stewart, Rev. Sci. Inst. 54, 1 (1983)
POSTULATE:

## Slide 16
UIC
MTE: Theory vs. Experiment
Theoretical MTE:
... ;
;
Emission processes not independent:
BOTH emissions from virtual excited band states
 Convolution in momentum space
 Addition of pT variances (i.e., MTEs)
... Consistent with observation of a single
Gaussian electron beam profile
MTEtheory (meV)
MTEexpt. (meV)

## Slide 17
UIC
Summary
Franck-Condon effect influences QE and MTE
(i) Metallized diamond(001): MTE > 500meV for outer signal with enhanced QE
p0 = pband + nqLO
... optical phonon assisted emission
(ii) “Good” metals: MTE > kBTe for E < 0
p0 = p1 + p2  p POSTULATE !
... electron-electron scattering near E  0
NOTE: Other possible explanations; surface states (e.g., Tamm), upper CBs ...
Clear implications for discovery of (ultra)low intrinsic emittance photocathodes – especially for operation at 300K

## Slide 18
UIC
A final note ...
 Need a better metal photocathode than copper?
Cu(001)
W(001)
Two-photon photoemission background
ħω = 4.27eV  E   0.1eV
ħω = 4.03eV  E   0.1eV
Significantly less two-photon PE in tungsten
Equivalent one-photon QE at same E
Tungsten is less chemically reactive (almost no surface oxide)
Tungsten is harder (i.e., more robust) than copper

## Slide 19
UIC
Thank You !

## Slide 20
UIC
Other work: Cu(001)
PERFORMANCE CHARACTERISATION
OF A Cu (100) SINGLE–CRYSTAL PHOTOCATHODE
L. A. J. Soomary, D. P. Juarez–Lopez, C. P. Welsch, L. B. Jones, and T. C. Q. Noakes
12th Intl. Particle Acc. Conf. (IPAC 2021), Campinas, SP, Brazil, WEPAB112

## Slide 21
Experiment: UV radiation delivery
 Laser / NLO based tunable UV radiation source: 3.0 – 5.3eV (235-410nm)
UIC
20 W Yb:fiber laser
400 fs, 16.7 MHz, 1030 nm
Nonlinear fiber
(SC-3.7-975)
Detector:
MCP & CCD camera;
Faraday cup
Non-collinear
sum frequency
UV generation
ΔpT measurement
LBO
LBO
LBO
LBO
LBO
6 W 515 nm
BBO
15 W
0.5 W
SHG
SHG
THG
F
OPA 2
OPA 1
-10 kV
3
s,i
Continuum
(700-950 nm)
Tunable UV (0.1-1mW)
2
Tunable UV (0.1-1mW)
100μm aperture
Detector:
MCP & CCD camera;
Faraday cup
ΔpT measurement
-10 kV
f = 50cm
f = 38cm
OAP
/2

## Slide 22
UIC