## Slide 1: On Chip Waveguide Integrated Photocathodes
Hyun Uk Chae, Alimohammed Kachwala (ASU), Ragib Ahsan (USC), Oksana Chubenko (NIU),
Siddharth Karkare (ASU), Rehan Kapadia (USC)
Department of Electrical and Computer Engineering
University of Southern California
Photocathode Physics for Photoinjectors (P3)

## Slide 2: Why do we care about electron emitters?
Accelerators
Vacuum Electron Devices
Bright coherent source for scientific application
High power and high frequency wave generation and amplification

## Slide 3: USC Semiconductor Photoemitters
Hot Electron Light Assisted Cathode (HELAC)

## Slide 4: USC Semiconductor Photoemitters
Hot Electron Light Assisted Cathode (HELAC)
Waveguide Integrated Hot Electron Cathode

## Slide 5: USC Semiconductor Photoemitters
Hot Electron Light Assisted Cathode (HELAC)
Waveguide Integrated Hot Electron Cathode

## Slide 6: Can we couple light into a semiconductor device to maximize the light coupling into an absorber?

## Slide 7
Rapid response Time
Key factors of good photoemitter

## Slide 8
Rapid response Time
Low Mean transverse Energies (MTE)
Key factors of good photoemitter

## Slide 9
Rapid response Time
Low Mean transverse Energies (MTE)
High Quantum Efficiency (QE)
Key factors of good photoemitter

## Slide 10: GaAs: Negative Electron Affinity
Hernandez-Garcia, Carlos, Patrick G. O Shea, and Marcy L. Stutzman. "Electron sources for accelerators." Physics today61.2 (2008): 44.

## Slide 11: Limitations; GaAs: Negative Electron Affinity
Hernandez-Garcia, Carlos, Patrick G. O Shea, and Marcy L. Stutzman. "Electron sources for accelerators." Physics today61.2 (2008): 44.
Blankemeier, L., et al., 2019.

## Slide 12: Background: Integrated Photonics
Integrated photonic circuits to manipulate, modulate and direct light on wafers are widely used in the telecommunication industry.

## Slide 13: Limitations; GaAs: Negative Electron Affinity
Blankemeier, L., et al., 2019.

## Slide 14: Integrated Photoemitter Simulation Result
Blankemeier, L., et al., 2019.
Low MTE
High Quantum efficiency (QE)
Quick response time

## Slide 15
Key factors of designing good Photocathode
Absorber

## Slide 16
Key factors of designing good Photocathode
Absorber
1. Efficient Light Coupling

## Slide 17
Key factors of designing good Photocathode
Absorber
1. Efficient Light Coupling
2. Chose Proper Light Absorber

## Slide 18: Design Grating Coupler
Lumerical FDTD simulation was used to track the transmission profile of designed grating coupler while traveling across the waveguide structure

## Slide 19: Design Grating Coupler
Micro/Nano semiconductor fabrication technique used to build a Si3N4 grating coupler with waveguide structure
Waveguide
Grating Coupler
5um
Optical Microscope image
Scanning Electron Microscope image
19

## Slide 20: Transferring GaAs epitaxial layer on waveguide
Waveguide
5um
Thin layer of p-GaAs was grown by Metal Organic Chemical Vapor Deposition (MOCVD).
Epitaxial lift-off process was processed to transfer GaAs on waveguide
Before Transfer
After Transfer
20

## Slide 21
Confined Emission using PEEM
21
Photoemission Electron Microscopy was used to observed the photoemission profile
Photoemission confinement can be found at the waveguide region
Measurement by

## Slide 22: In-situ Cs3Sb growth on top of waveguide
Instead of transferring thin epitaxial GaAs film, thin Cs3Sb was grown on top of waveguide structure in-situ.
Cs3Sb thin films were grown via co-deposition of Cs and Sb onto the substrates.
20nm of thin film was grown having ~ 1% Quantum efficiency
Measurement by

## Slide 23
Patterned Emission Using PEEM
Confined Emission using PEEM
~100 μm
PEEM image showing confined emission from a ∼20 nm thick Cs3Sb film at 𝜆 = 520 nm
The period of the beating pattern shows with ~100 um
Measurement by

## Slide 24
Patterned Emission Using PEEM
Confined Emission using PEEM
~150 μm
PEEM image showing confined emission from a ∼20 nm thick Cs3Sb film at 𝜆 = 528 nm
The period of the beating pattern shows with ~150 um
Measurement by

## Slide 25
Patterned Emission Using PEEM
Confined Emission using PEEM
~250 μm
PEEM image showing confined emission from a ∼20 nm thick Cs3Sb film at 𝜆 = 532 nm
The period of the beating pattern shows with ~250 um
Measurement by

## Slide 26
Patterned Emission Using PEEM
Confined Emission using PEEM
PEEM image showing no significant emission from a ∼20 nm thick Cs3Sb film at 𝜆 = 538 nm
Wavelength out of range where the grating coupler cannot support does not support any modes in the waveguide.
Measurement by

## Slide 27
Patterned Emission Using PEEM
Wavelength Dependent Photoemission
The period of the pattern increases as we go from 𝜆 = 520 nm to 𝜆 = 532 nm.
These transverse patterns are formed due to interference between these co-propagating modes thereby generating beating patterns with significant evanescent intensities that cause the electron emission.
Wavelength

## Slide 28
To calculate the modes, we assume that there is a symmetric SiO2/Si3N4/SiO2 waveguide where the cladding layers are infinitely thick. The asymmetry of upper and lower cladding layers in actual waveguide will modify the modes.
Then we assume that the mode profiles are not significantly altered when we have a 20 nm absorber on top of the waveguide
Si3N4
Si3N4
Cs3Sb
SiO2
SiO2
z
y
d
Simulation study on beating pattern in waveguide

## Slide 29
3rd TE and TM mode
Fundamental TE and TM modes
(3rd mode doesn’t exist)
Propagation vector decides the periodicity of the wave in z direction. For two modes with wavevectors β1 and β2, the interfered wave will have an envelope of wavevector |β1- β2|/2. This will have a spatial periodicity of
By sweeping the wavelength, it is possible to get the beating patterns by having overlapping 3rd TE and TM modes.
For higher wavelengths, we don’t get 3 modes and such a beating pattern probably cannot be observed.
Simulation study on beating pattern in waveguide

## Slide 30
Reproducing the beating patterns
Beating pattern emission was reproduced by weighting each mode by the coupling and sum them to get the emission profile
We get a periodicity of ~30 um while having 250um for the experiement. The absorber may change the modes significantly so that the propagation constants have much smaller difference and leads to a longer (250 um in experiments) periodicity.
Simulation at 532 nm
Experiment at 532 nm

## Slide 31
Future Work in experiments
Patternable Electron Emission Beam
Patterned /Split waveguide for beam shaping

## Slide 32
On Chip Waveguide Integrated GaAs / CsSb Photocathode has been introduced as a new type of photoemitter
Conclusion

## Slide 33
On Chip Waveguide Integrated GaAs / CsSb Photocathode has been introduced as a new type of photoemitter
This approach is general and proof of concept, can be improved by tuning each component of the device
Conclusion

## Slide 34
On Chip Waveguide Integrated GaAs / CsSb Photocathode has been introduced as a new type of photoemitter
This approach is general and proof of concept, can be improved by tuning each component of the device
Can be extended to other works by using other emitting material or patterning the electron emission
Conclusion

## Slide 35: Acknowledgements
Principal investigator: Prof. Rehan Kapadia
Graduate students: Hyun Uk Chae, Ragib Ahsan, Anika Tabassum Priyoti, Juan Sanchez Vazquez
ASU: Prof. Siddharth Karkare, Alimohammed Kachwala
NIU: Oksana Chubenko
Sponsors:

## Slide 36: BACK UP SLIDES

## Slide 37: Reproducing the beating patterns
We combine the decay length and propagation wavevector, exp(-(αz + j*β)z) to get the wave
Then we weight each mode by the coupling and sum them to get the emission profile
Here A is the intensity prefactor, is the coupling for the ith mode.
We change imaginary part of epsilon for absorber to fit our decay length from experiments.