## Slide 1: Development of Air Stable Silicon Photoemitter with Electronically Tunable Negative Electron Affinity
Ragib Ahsan, Hyun Uk Chae, Anika Tabassum Priyoti, Juan Sanchez Vazquez, Rehan Kapadia
Department of Electrical and Computer Engineering
University of Southern California

## Slide 2
Can we operate a negative electron affinity photocathode without ultrahigh vacuum?

## Slide 3
Pros:
High quantum efficiency
Visible photon excitation
Cons:
Requires ultrahigh vacuum
Hernandez-Garcia, Carlos, Patrick G. O Shea, and Marcy L. Stutzman. "Electron sources for accelerators." Physics today61.2 (2008): 44.
Traditional Negative Electron Affinity Photocathode

## Slide 4: Electronically Tunable NEA Photocathode

## Slide 5: Working Principle
Voltage is applied between the semiconductor and graphene, generating an electric field which mimics the surface dipole field in an NEA photocathode.
Photo-excited electrons tunnel through the barrier and introduced into graphene with higher energy than EF,Gr
VFN )
VFN )

## Slide 6
Experimental results: Emission current vs VGr-Si

## Slide 7: Experimental results: Emission current vs Anode voltage
Energy broadening by scattering
Carrier heating by electric field

## Slide 8: Stability at higher vacuum pressures

## Slide 9: Experimental results: Emission current vs Optical power
Peak EQE = 0.1%

## Slide 10: Key emission characteristics
Existence of a threshold VGr-Si to emit electrons
Energy distribution of emitted electrons is broad
Emission current shows a highly nonlinear dependence on optical power

## Slide 11: Existence of a threshold VGr-Si
The electrons tunneling into/through SiO2 must gain higher energy than the vacuum level (0.9 eV higher than SiO2 conduction band minima)
Direct tunneling of electrons through SiO2 will never allow this
Electrons must tunnel into SiO2 conduction band (FN tunneling)
These electrons must gain at least 0.9 eV energy from electric field

## Slide 12: Threshold for applied voltage
VFN )
VFN )

## Slide 13: Broad energy distribution
To have a broad energy distribution, electrons must scatter at SiO2 conduction band
Possible scattering mechanisms for SiO2
  Longitudinal polar optical phonon scattering
  Acoustic phonon scattering
  Impact ionization scattering

## Slide 14: Monte Carlo simulation: Transport at SiO2
Eox = 1 V/nm
Parabolic band approximation

## Slide 15: Monte Carlo simulation: Transport at SiO2
Eox = 1 V/nm
meff = m0
0.2 V/nm
1.0 V/nm
High energy tail heating

## Slide 16: Nonlinear emission current
Multiphoton absorption is highly unlikely in silicon for the optical power densities we have (103-104 W/m2)
There is no dominant scattering mechanism for SiO2 that is nonlinear to electron injection rate/optical power
Optical power must modify the voltage distribution within the device
  Voltage dropped at depletion region at silicon
  Voltage dropped at oxide

## Slide 17: Voltage distribution between oxide and silicon
Extremely small electron generation rate (dark/low optical power)
  No inversion layer can be formed at Si/SiO2 interface
  Majority voltage is dropped at silicon depletion layer (VGr-Si ≈ Vsi >> Vox)
Moderate electron generation rate (moderate optical power)
  Incomplete generation of inversion layer
  Appreciable voltage drop across oxide
High electron generation rate (high optical power)
  Complete inversion
  Majority voltage drop across oxide (VGr-Si ≈ Vox >> Vsi)
Poisson’s equation determines how much voltage drops across different parts of the device (VGr-Si = VSi + Vox)

## Slide 18: Voltage redistribution by optical power
VGr-Si = 26V
P = P1
P = P2
Generation current density is proportional to optical power density
Higher optical power
Higher voltage/electric field at oxide
Higher tunneling rates (Nonlinear)
Electron distribution heating (Nonlinear)
Nonlinear emission current

## Slide 19
This is a silicon photocathode
  Fabrication is easier and cheaper
NEA surface is controlled by voltage
  Can be turned on and off
  Stable at atmospheric conditions
Photons need to have energy silicon bandgap
  Visible lasers are enough for emission
Summary

## Slide 20: Acknowledgements
Principal investigator: Prof. Rehan Kapadia
Graduate students: Hyun Uk Chae, Anika Tabassum Priyoti, Juan Sanchez Vazquez, Zezhi Wu
Sponsors: