## Slide 1: Bright Electron Beams from Plasmonic Spiral Photocathode Alimohammed Kachwala Arizona State University

## Slide 2: Outline
Introduction
Reducing Emittance
Plasmonic Spiral Photocathode
FDTD Simulation
Fabrication and Characterization: Past and Present Attempts
Characterization Using Photoemission Electron Microscope
Electron Emission Spot Size
Mean Transverse Energy (MTE)
Emittance
4D-Brightness
Conclusion
Future Work

## Slide 3: Introduction
UED
Physical Review Special Topics-Accelerators and Beams 17.12 (2014): 120701.
Coherence Length
L = Coherence Length
ƛ = Reduced Compton Wavelength
𝜎e = RMS electron beam size
= Normalized Emittance
Reduce to increase

## Slide 4: Emittance
Show me the better way to reduce emittance
Reduce MTE
I said the better
Reduce
PERFECT!
Emittance

## Slide 5: Reducing
Limited by the Diffraction limit of light ~
Conventional way of focusing light
Surface Plasmon Polariton
How to focus smaller than ?
Acs Photonics 3.4 (2016): 611-619
https://en.wikipedia.org
Gold Nanotip
Gold Spiral
Structural Dynamics 9.2 (2022)
Physical review letters 110.7 (2013): 074801
Physical Review Applied 19.3 (2023): 034034

## Slide 6: Plasmonic Spiral Photocathode: FDTD Simulation
Fowler Dubridge:
Source: Circularly Polarized Gaussian; ℏω = 1.55 eV (𝜆 = 800 nm); Pulse Length = 150 fs
ΦAu ~5.4 eV; ℏω = 1.55 eV
n = 4, 𝐽4 𝛼 𝐼4
I4 Map
Physical review letters 104.8 (2010): 084801.
Nuclear Instruments and Methods in Physics Research Section A: Accelerators, Spectrometers, Detectors and Associated Equipment 601.1-2 (2009): 123-131.
Non-Linear Photoemission:
electron source size ~140 nm
Intensity(I) Map

## Slide 7: Past Attempts: Fabrication
Template Stripping Method
0.5 um
2 um
Physical Review Applied 12.5 (2019): 054057.

## Slide 8: Past Attempts: PEEM Images
PEEM Hg Lamp
Before LASER cleaning
After LASER cleaning
LASER “cleaning” for 15 hours reduces hot spots
No Emission Spot at the Center
Change Fabrication Method
Large Start Radius

## Slide 9: New Fabrication Technique
Si Substrate
185 nm PMMA 495 K
200 nm PMMA 950 K
Written with EBL
Developed in MIBK:IPA = 1:3
Treated with O2 Plasma
E beam evaporation of Cr (5 nm)/Au (120 nm)
Lift off with Remover PG
Rinsed with IPA
Spiral Fabrication Process
Si Substrate
2R0
Si Substrate
Si Substrate

## Slide 10: New Fabrication: SEM Images

## Slide 11: FDTD Simulation
4th order photoemission
For constructive interference at the center of the spiral,
Where = pitch of the spiral
Hence, interference at the center of the spiral is totally independent on the starting radius

## Slide 12: Spiral Photocathode: Study & Characterization
SEM
LASER cleaning of Hot-Spots
LASER Parameters
= 800 nm; Pulse Length = 150 fs; Rep. Rate = 500 kHz
Overnight exposure of Average Power = 0.5 mW
Hot Spots disappeared after overnight exposure (Spiral Cleaned)
PEEM Hg Lamp + LASER
LASER

## Slide 13: Spiral Photocathode: Study & Characterization
LASER Parameters
= 800 nm; Pulse Length = 150 fs Rep. Rate = 500 kHz
Photoemission Measurement: Spiral Activation
1st Activation
Faint spot
~ 5 min
ND 1.0
~ 2 mW
Low LASER power
ND 1.0
~ 2 mW
Bright spot
ND 1.5
~0.5 mW
Still bright
~ 5 min
ND 1.5
~0.5 mW
Brighter
Extremely faint spot
2nd Activation
PEEM Hg Lamp Image
10 mm
PEEM Hg Lamp+ LASER
10 mm
LASER
10 mm
LASER (Zoomed in)
200 nm

## Slide 14: Spiral Photocathode: Study & Characterization
Electron Emission spot; Average incident LASER power = 136 mW

## Slide 15: Spiral Photocathode: Order of Emission
~120 nm electron emission spot size makes sense as
Order of Emission ~5th

## Slide 16: Spiral Photocathode: Order of Emission
10-4 electrons/shot
1 electron/shot
~120 nm electron emission spot size makes sense as
Order of Emission ~5th

## Slide 17: Spiral Photocathode: Spot Size
~120 nm electron emission spot size over wide range of LASER power
Spot size increases
interaction
Effect of plasmonic fields

## Slide 18: Spiral Photocathode: MTE
MTE increases
interaction
Effect of plasmonic fields
0.5 Å-1

## Slide 19: Spiral Photocathode: Emittance
Record ~30 pm rad achieved from a flat metal photocathode without the use of any pinholes
2 pm rad from ZrO/W emitter tip in an Electron Microscope [Ultramicroscopy 176 (2017): 63-73]
700 pm rad from flat cathode in a photoinjector after the pinhole [Structural Dynamics 9.2 (2022)]
interaction could result in correlated growth so emittance could still be small
increases
interaction
Effect of plasmonic fields

## Slide 20: Spiral Photocathode: 4D-Brightness
Maximum 4-D Brightness achieved:
120 electrons/nm2
Brightness decreases
interaction
Effect of plasmonic fields
interaction could result in correlated growth so emittance could still be small and brightness higher

## Slide 21: Conclusion
Fabrication
Electron Spot Size ~120 nm
Record ~30 pm rad achieved from a flat metal photocathode
Maximum 4-D Brightness achieved:
120 electrons/nm2
B4D = 120 electrons/nm2
<60 pm rad

## Slide 22: Future Work
Explain the spiral activation process
Explain the ring like structure in images
Measure the spiral with small start radius (R0 = 0.372 mm)
Study dependence on wavelength (design for multiphoton emission closer to threshold)
Integrate these spiral cathodes with high QE (low MTE) alkali antimonide films

## Slide 23: Acknowledgement
University of Chicago
Christopher Pierce
Arizona State University
Mansoure Rizi
Siddharth Karkare (PI)
Cornell University
Jared Maxson
Lawrence Berkeley National Lab
Daniele Filippetto

## Slide 24: Thank You! Questions? Comments?

## Slide 25
Back Up Slides

## Slide 26
SEM Images: After LASER Exposure

## Slide 27
SEM Images: After LASER Exposure

## Slide 28
SEM Images: After LASER Exposure

## Slide 29
SEM Images: After LASER Exposure

## Slide 30: Spiral Tilt Compensation
θ
Δp
Δx
z
x
=
r
r+Δr
Φ = 180
Φ = 0
y
x

## Slide 31: Plasmonic Spiral: Tilt Compensation

## Slide 32: Plasmonic Spiral: Tilt Compensation
FWHM ~ 140 nm

## Slide 33: Plasmonic Spiral: Response Time
Response Time: FDTD Simulation
Incident Pulse Length: 150 fs
Polarization: Circular

## Slide 34: Brief Description of PEEM
Sample
Objective
Contrast Aperture
1st Stigmator
Transfer Lens
2nd Stigmator
Iris Aperture
1st Projective
2nd Projective
L1
L2
G1 and G2
Imaging Assembly
PEEM Column
IEF Column

## Slide 35: Density of States: Gold
Physical Chemistry Chemical Physics 17.39 (2015): 26036-26042

## Slide 36: Electron Bunch Parameters
Brightness of Electron Bunch
Charge density in phase space
B
B = Brightness of Electron Bunch
= Bunch Charge
Ɛn = Normalized Emittance
Increase Amount of Charge Extracted
Reduce Emittance/Mean Transverse Energy (MTE)
Coherence Length
Proteins: ~ 4 - 100 nm
L = Coherence Length
ƛ = Reduced Compton Wavelength
𝜎e = RMS electron beam size
Ɛn = Normalized Emittance
- Emittance
The electron beam emitted from the photocathode is contained within a phase space volume, known as the emittance
Reduce Emission Area
Reduce Mean Transverse Energy (MTE)
≥ 4 nm
≤ 200 μm
20 nm rad.