## Slide 1: Optical Near Field Electron Microscopy
John Smedley, SLAC
Guido Stam, ULEI
Sense Jan van der Molen, ULEI

## Slide 2: ONEM Goal
Optical microscopy with significantly sub wavelength resolution
Eventually fast enought to observe biological dynamics
Key inovation:
Convert scattered photons into electrons in the optical near-field
Resolution is limited by the sample to electon emitting surface distance -> need ultra-thin photocathodes!
Phys. Rev. Applied 16, 014008 (2021)

## Slide 3: Timeline ONEM
ONEM
UV-ONEM
BIPEEM
ONEM
No liquid cell
First image (nanostructure)
Signal improvement
Bio sample
Optical module installation
Low-workfunction (Graphene-Cs)
Growth and QE measurement set up
First image (nanostructure)
Image biostructure
Optimize resolution
Polarization control
Install liquid cell
Dynamic measurements
Backilluminated PEEM
https://doi.org/10.1016/j.ultramic.2023.113809

## Slide 4: Positioning ONEM in LEEM
Aberration correction

## Slide 5: UV-ONEM using LED (275 nm)
e-
Ar+
1) Create embedded Au nanostructures
Field of view: 150 μm
Scale bar: 500 nm
2) Cover with photocathode layer:
Chromium
ONEM Proof of Principle!
Illumination time: 10-35 min.
Estimated resolution: 37 nm = λ/7

## Slide 6: Vis-ONEM using laser (450 nm)
e-
Ar+
1) Create embedded Au nanostructures
Field of view: 150 μm
Scale bar: 500 nm
First visible-light ONEM!
Illumination time: 8 s
Estimated resolution: 55 nm = λ/8
(NB photocathode thickness ≈ 25 nm)
2) Cover with photocathode layer:
(amorphous) Carbon + Cs

## Slide 7: ONEM on biosamples
PEEM signal (left) UV ONEM signal (right).
(Mouse tail slice)
Large field of view: scale bar is 20 microns
hv
hv

## Slide 8: ONEM on biosamples
PEEM signal (left) blue light ONEM signal (right)
(Mouse tail slice)
Field of view: 45 μm
Notes: Right: Speckles from unwanted reflection of electron lens

## Slide 9: Growing photocathodes @Brookhaven National Lab

## Slide 10: Motivation: Develop ONEM
Concept
Illuminate sample with visible light
Photons pass through ultra-thin vacuum-liquid interface
Low-work function photocathode converts photons to electrons
Electrons are imaged with LEEM
Optical Near-field Electron Microscopy
Notes: My job is developing a crucial element of ONEM
The Low-work function photocathode converts photons to electrons

## Slide 11: Functional requirements
Good QE in the visible  or candidates
  >1% @ 530 nm for good signal
Ultra-smooth ultra-thin layer
  <10 nm film; <1 nm roughness to not degrade resolution
Suitable transparent substrate for ONEM back-illumination
  SiN, SiC, graphene
Notes: Good signal
No degradation to resolution
Must be able to grow on transparent substrate

## Slide 12: Experimental setup
Growth procedure:
Temperature
Co-deposition
Flux rates
  Cs on
  PLD freq.
Characterization:
QCM
XRD
RHEED
XRR
XRF
QE
M. Gaowei et al. Phys. Rev. Accel. Beams 22, 073401 (2019)
Feng, et al. J. Appl. Phys., 121 4, (2017)
Notes: We do this at a synchrotron, with access to hard x-rays for x-ray characterization methods
That give us insight to the thickness, roughness and chemical composition during growth so that we can optimize growth parameters
Film is grown using thermal evaporation of the Cs and pulsed laser deposition of Sb
The recipe developed at BNL uses concurrent deposition, which yields smoother photocathodes as compared to the previous sequential deposition
We can tune the growth with the temperature of the substrate and the flux rates of Cs and Sb

## Slide 13: Experimental setup
Notes: In real life the chamber looks like this:
Notably PLD laser, the chamber rotates on axis

## Slide 14: Quantum Efficiency
Very good already at very low thicknesses
Cutoff above 600 nm
Parzyck, et al., Phys. Rev. Letters 128, 114801 (2022)
New substrate - fit
New substrate
Notes: For all growths the material gives a very good quantum efficiency
As you can see, it doesn’t really matter what substrate we use for QE
Comparable to literature

## Slide 15: Film structure
XRR: Thickness & Roughness
XRD: Crystallinity
RHEED: Surface structure
XRF: Stoichiometry
New substrate
New substrate
New substrate
Notes: From the X-ray and RHEED data we can draw several conclusions about the grown films
The fact that we see the oscillations so far out means that the photocathodes are very smooth! <1nm roughness
The XRF shows the stoichiometry is spot-on
RHEED and XRD tell us more about the crystal structure of the grown film
  How ordered it is.
  The film can grow amorphous, poly-crystalline or single crystal
  What we see is that especially for the 4H-SiC-Gr substrate the films are extremely well-ordered.

## Slide 16: Conclusion @ BNL
QE of Cs3Sb is great at low thicknesses
Co-deposition method yields smooth results
Growths are crystalline,
Properties depend on (flatness) substrate
Optimal properties for a new substrate
Patent & paper in the making!

## Slide 17: In Leiden
Chromium photocathode for UV-ONEM
Cesiated Carbon for (low signal) Vis-ONEM
For high signal & high resolution Vis-ONEM:
Ultra-flat Ultra-thin Cs3Sb photocathode

## Slide 18: Leiden Outlook
Cs evaporator & PLD available, however:
Still need to optimize PLD parameters
Use the photocathode recipe developed @BNL
Complement photocathode research with LEEM
  (Surface) Crystal structure
  Homogeneity of photocathode