## Slide 1
Strained superlattice InAlGaAs/AlGaAs spin-polarized photocathodes implemented with both random and digital alloying
1Materials Dept., University of California, Santa Barbara
2Center for Injectors and Sources, Thomas Jefferson National Accelerator Facility
3Dept. of Electrical & Comp. Eng., University of California, Santa Barbara
Aaron Engel1, Marcy Stuzman2, Jason Dong1, Christopher Palmstrøm1,3
2023 P3 Workshop

## Slide 2: Outline
Applications & mechanism of spin-polarized photoemission
Benefits of InAlGaAs/AlGaAs vs. GaAs/GaAsP
Initial InAlGaAs/AlGaAs results
Improving performance with digital alloying
Wafer uniformity and progress toward integration with Bragg reflector

## Slide 3: Outline
Applications & mechanism of spin-polarized photoemission
Benefits of InAlGaAs/AlGaAs vs. GaAs/GaAsP
Initial InAlGaAs/AlGaAs results
Improving performance with digital alloying
Uniformity and progress toward integration with Bragg reflector

## Slide 4: Applications of spin-polarized photoelectron beams
In-progress electron ion collider at Brookhaven National Lab (F. Willeke)
The Jefferson Lab Qweak Collaboration. Nature 557, 207–211 (2018)
Particle physics (GeV beams)
  Studying subatomic particles via collision asymmetries
  Electron ion colliderhigh emission currents necessary
    Limited by low lifetimes
Characterization techniques for magnetic and SOC materials
  Electron microscopy/diffraction
  Inverse photoelectron spectroscopy

## Slide 5: Applications of spin-polarized photoelectron beams
Particle physics (GeV beams)
  Studying subatomic particles via collision asymmetries
  Electron ion colliderhigh emission currents necessary
    Limited by low lifetimes
Characterization techniques for magnetic and SOC materials
  Electron microscopy/diffraction
  Inverse photoelectron spectroscopy
Spin-polarized inverse photoemission spectroscopy
Elmitech LEEM3
Spin-polarized LEEM
Spin-polarized TEM
LUTECE—LPS Orsay
J. Phys.: Conf. Ser. 371 012004 (2012)

## Slide 6: Generating spin polarization with circular polarized light
1
Optical selection rules via circular polarized light
Degeneracy limits the theoretical maximum spin polarization
P3/2
S1/2
P1/2
Split-off band
Light hole band
Heavy hole band
Conduction band
mj= -3/2
mj= -1/2
mj= 1/2
mj= 3/2
mj= -1/2
mj= -1/2
mj= 1/2
mj= 1/2
3
Δmj=±1
hv ≈ Eg
I. Žutić, J. Fabian, and S. Das Sarma, Rev. Mod. Phys. 76, 323 (2004)
=
3
0
3
0
=
1
1

## Slide 7: Generating spin polarization with circular polarized light
1
=
Optical selection rules via circular polarized light
Degeneracy limits the theoretical maximum spin polarization
Confinement and epitaxial strain break heavy hole/light hole degeneracy
P3/2
S1/2
P1/2
Split-off band
Light hole band
Heavy hole band
Conduction band
mj= -3/2
mj= -1/2
mj= 1/2
mj= 3/2
mj= -1/2
mj= -1/2
mj= 1/2
mj= 1/2
3
3
0
3
0
=
Δmj=±1
hv ≈ Eg
I. Žutić, J. Fabian, and S. Das Sarma, Rev. Mod. Phys. 76, 323 (2004)
=
3
0
3
0
=
1
1
Breaking hole degeneracy…..

## Slide 8: Outline
Applications & mechanism of spin-polarized photoemission
Benefits of InAlGaAs/AlGaAs vs. GaAs/GaAsP
Initial InAlGaAs/AlGaAs results
Improving performance with digital alloying
Uniformity and progress toward integration with Bragg reflector

## Slide 9: Strained well superlattices require precise epitaxial growth
Quantum well confinement and strain break heavy hole/light hole degeneracy
Superlattice enhances hole splitting and increases quantum efficiency
Molecular beam epitaxy for precise layer control during heteroepitaxy
  MOCVD suitable alternative
Superlattice Mirror
Superlattice
active region
Very complex layer stacks
RHEED
Screen
RHEED
Gun
In
Ga
Al
Be
As
Molecular Beam Epitaxy (MBE)

## Slide 10: Current state-of-the-art strained well superlattice
Metamorphic “virtual” substrate
  Time-consuming
  Expensive
  High dislocation density
  Rough
Distributed Bragg Reflector (DBR) creates resonant cavity
  Enhances QE 2-8x
Difficult to grow (temperature sensitive)
  Group V composition control
  Uniformity issues
W. Liu, et al., Appl. Phys. Lett. 109, 252104 (2016)
GaAs0.65P0.35
GaAsP/AlAsP
DBR and window
GaAs/GaAsP superlattice
GaAs p++
EC
EV
Cs,O2/NF3
Activation
Evac
GaAs
sub.
GaAsP
graded
p-type doped throughout
FOM w/o DBR: 0.89
FOM w/ DBR: 4.52
5+2 μm
2 μm
100 nm
5 nm
Shifts lattice constant
from 5.653 Å
to 5.582 Å
Must keep ternary lattice constants matched to virtual substrate

## Slide 11: Strained well InAlGaAs/AlGaAs has more room for improvement
AlP
AlAs
GaAs
InAs
InP
GaAs0.65P0.35
No virtual substrate necessary!
Easily tunable DBRs in AlAs/AlGaAs system
No group V alloying: better uniformity?
  Better for integration with DBRs
  As/P ratio
Much more band engineering possible
  Zero conduction band offset [1]
Sample quality was not consistent, but best samples were on par with GaAs/GaAsP
  Moved to GaAs/GaAsP photocathodes grown by SVT Associates
GaP
[1] L. G. Gerchikov, et al. Semiconductors 40, 1326–1332 (2006)
Barrier
Well
Easy to lattice match
Mainly investigated by Gerchikov, Subashiev & Mamaev @ St. Petersburg State Polytechnic University

## Slide 12
InAlGaAs/AlGaAs has further benefits
Ion back bombardment induced ion damage is a main limiter of photocathode lifetime
  High emission currents necessary at EIC
T. Nishitani, et al. Jpn J. Appl. Phys. 48, 06FF02 (2009)
M. Bastani Nejad, …P. Adderley, CEBAF 200 kV inverted electron gun, Conf. Proc. C C110328, 1501 (2011).
Addition of aluminum could increase lifetimes [1]
  Higher binding energies reduce ion damage
  AlAs > GaP
V. Shutthanandan, et al. Phys. Rev. ST Accel. Beams 15, 063501 (2002)
[1] W. Wesch , et al. Nucl. Instrum. Methods Phys. Res. B: Beam Interact. Mater. At., 277, 58 (2012).;
H. H. Tan , et al. J. Appl. Phys. 77, 87–94 (1995);
E. Wendler AIP Conference Proceedings 680, 670–674 (2003)

## Slide 13: Outline
Applications & mechanism of spin-polarized photoemission
Benefits of InAlGaAs/AlGaAs vs. GaAs/GaAsP
Initial InAlGaAs/AlGaAs results
Improving performance with digital alloying
Uniformity and progress toward integration with Bragg reflector

## Slide 14: Growth optimization of photocathode structure: XRD
0
1
2
-1
-2
GaAs(004)
Superlattice X-ray diffraction
XRD indicates higher quality films grown at lower temperatures
More integer fringes and more intense satellite fringes indicate sharper interfaces
GaAs(001)
(AXT Zn-doped)
500 nm GaAs buffer
90 nm InAlGaAs/AlGaAs strained superlattice
6 nm GaAs
Undoped
Diffraction occurs from superlattice periods
0 order peak corresponds to average out-of-plane lattice constant of the repeat unit
Integer spacing corresponds to total period thickness
High frequency fringes correspond to overall superlattice thickness
5.1 nm In0.16Al0.23Ga0.61As
2.3 nm Al0.274Ga0.726As
1.1% compressive strain
12x
Higher temperature

## Slide 15: Growth optimization of photocathode structure: optical quality
RT
HH1?
LH1?
Large background from GaAs subtracted
Photoluminescence intensity has been shown to correlate to photocathode quantum efficiency
Lower temperature growth produces more intense PL from superlattice
Peak asymmetry potentially from HH/LH splitting
  ~50 meV
P3/2
S1/2
P1/2
hv > Eg
“pump”
hv ≈ Eg
“probe”

## Slide 16: Growth optimization of photocathode structure: morphology
Atomic force microscopy
Smoothest films at higher temperatures
Smoother than typical GaAsP buffers
520°C
480°C
560°C
0 nm
1 nm
1.5 nm
-1 nm
-1.5 nm
-0.5 nm
0.5 nm
RMS 0.31 nm
RMS 0.18 nm
RMS 0.20 nm
1 µm
RMS 2.45 nm
RMS 0.45 nm
Height Scale = 4 nm
Journal of Applied Physics, 109, 013708 (2011)
2 μm buffer to 20% Phosphorous
Literature GaAsP buffer
1 µm
1 µm
5 µm
…compared to our fully pseudomorphic sample
TGrowth:

## Slide 17: Spin polarization/QE measurements on 520°C sample
FOM () at 770 nm is >0.2
  Still lower than ~0.9 of GaAsP system
Unoptimized sample growth conditions
~50 meV hole splitting
GaAs(001)
(AXT Zn-doped)
500 nm GaAs buffer
AlGaAs barrier
60 nm InAlGaAs/AlGaAs strained superlattice
6 nm active layer GaAs
p-type
~4E19 cm-3 Be
p-type
~5E17 cm-3 Be
5.1 nm In0.16Al0.23Ga0.61As
2.3 nm Al0.274Ga0.726As
8x
RT
HH1
LH1
HH2
Measured w/ JLab MicroMott

## Slide 18: Outline
Applications & mechanism of spin-polarized photoemission
Benefits of InAlGaAs/AlGaAs vs. GaAs/GaAsP
Initial InAlGaAs/AlGaAs results
Improving performance with digital alloying
Uniformity and progress toward integration with Bragg reflector

## Slide 19: Approach to reduce alloy disorder and improve uniformity
Digital alloying minimizes random alloy disorder
  Broader high spin-polarization window
InAlGaAs digital alloys (near lattice matched to InP) should have
  Better optical emission than random alloys
  Better uniformity than random alloys
I. J. Fritz, J. F. Klem, M. J. Hafich, A. J. Howard Appl. Phys. Lett. 66, 2825 (1995)
C.S. Wang,…, A.C. Gossard, L.A. Coldren J. Cryst. Growth 277, 13 (2005)
D. Song,…,Y.T. Lee J. Cryst. Growth 270, 295 (2004)
Energy
LH
HH
Random alloy disorder
Energy
LH
HH
Reduced random alloy disorder
J. Appl. Phys. 125, 082514 (2019)
Digital alloy
Random alloy
Notes: Sticking coefficient of In desorption mass spec.
Frank Gruenthanger JPL 1980s early 1990s.

## Slide 20: Digital alloys preserve overall superlattice structure
Fully strained to GaAs via reciprocal space map
Extra half-period added to make each well/barrier symmetric
1
2
-2
TGrowth = 520°C
On-axis XRD
6x
5.1 nm In0.16Al0.23Ga0.61As
2.3 nm Al0.274Ga0.726As
12x
10x
0.6 ML In0.06Al0.94As
1.74 ML In0.22Ga0.78As
0.28 ML AlAs
0.59 ML GaAs
GaAs(001)
(AXT Zn-doped)
500 nm GaAs buffer
90 nm InAlGaAs/AlGaAs strained superlattice
6 nm GaAs
Undoped
-1
GaAs(004)
0
GaAs(224)
Reciprocal Space Map
GaAs(224)

## Slide 21: Digital alloy shows improved optical quality
10x
0.28 ML AlAs
0.59 ML GaAs
RT
Intensity of PL improves with both digital alloy barriers and digital alloy wells
PL asymmetry/splitting consistent with photoabsorption measurement
6x
5.1 nm In0.16Al0.23Ga0.61As
2.3 nm Al0.274Ga0.726As
12x
0.6 ML In0.06Al0.94As
1.74 ML In0.22Ga0.78As
TGrowth = 520°C
LH1?
HH1?
Large background from GaAs subtracted
Photoluminescence

## Slide 22: Outline
Applications & mechanism of spin-polarized photoemission
Benefits of InAlGaAs/AlGaAs vs. GaAs/GaAsP
Initial InAlGaAs/AlGaAs results
Improving performance with digital alloying
Uniformity and progress toward integration with Bragg reflector

## Slide 23: Digital alloys improve uniformity for cavity resonance
Uniformity essential for resonant cavity with DBR
Reflectance measures quality of DBR and resonance of photocathode w/ DBR

## Slide 24: Digital alloys improve uniformity for cavity resonance
Uniformity problematic in the past
  Essential for resonant cavity with DBR
Broader features in digital alloy well
Digital alloy well + barrier makes significant improvement to uniformity
¼ of 2” wafer
All digital alloy
All random alloy
Digital alloy barrier
Random alloy well
GaAs cap
Superlattice
RT
Uniformity is adequate… now DBRs
±8 nm
±8 nm
±3 nm

## Slide 25: Distributed Bragg reflector test successful
Average center linewidth ~755 nm vs. designed 780 nm
  Growth rate calibrations were slightly off…
50 nm bandwidth
Uniformity across wafer ~10 nm
  No substrate rotation during growth
Next step: integrate with optimized photocathode structure
AlGaAs/AlAs DBR
65 nm AlAs
57 nm Al0.34Ga0.66As
12x
p-type
~7E17 cm-3 Be

## Slide 26: Conclusions and next steps
Measure other random/digital alloys in queue
Assess lifetime of photocathodes
Best InAlGaAs photocathode (to our knowledge) in this pump range
  FOM>0.2 at 770 nm
  Future samples expected to perform better
Successfully validated digital alloyed InAlGaAs/AlGaAs photocathodes for PL and uniformity
Validated DBR growth
Future work
26
High performance random alloy InAlGaAs/AlGaAs spin-polarized photocathode
TGrowth = 520°C

## Slide 27
Thanks!
Questions?

## Slide 28
Thanks!
Questions?
Appropriate other meanings of MBE:
Mostly Broken Equipment
Massive Beer Expenditures
Mega-Buck Evaporator
Maniac Bloodsucking Engineers
Money Buys Everything
Make Believe Experiments
Many Boring Evenings

## Slide 29: Supplemental Slides

## Slide 30: Mott polarimeter: How it works
Phys. Rev. A 64, 052713 (2001)
the effective Sherman function
Calibrated with known photocathode polarization
Calculated (rather precisely)

## Slide 31: The photoemission process in a III-V photocathode
EF
EV
EC
p-type III-V
Vacuum
EVac
1
2
3
1
2
3
Transport
Emission
Photon
hν ≈ Eg
C.N. Berglund and W.E. Spicer, Phys Rev 4A, A1030 (1964)
W.E. Spicer, Phys Rev 112, 114 (1958)
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
Cs-O functionalized surface

Negative Electron Affinity

QE increased by 102-104
Excitation

## Slide 32: Photogun set up
April Cook, SULI JLAB
Nucl. Instr. Methods Phys. Res. A 618, 30 (2010)

## Slide 33: Yo-yo NEA process
April Cook, SULI JLAB
Alternating NF3 exposure and Cs exposure

## Slide 34: Record FOMs at peak wavelength
W. Liu, et al., Appl. Phys. Lett. 109, 252104 (2016)

## Slide 35
W. Liu, et al., Appl. Phys. Lett. 109, 252104 (2016)

## Slide 36: Photoluminescence shows improved optical quality using digital alloy
RT
+GaAs in DA Barrier
Superlattice
Intensity of PL improves with both digital alloy barriers and digital alloy wells
PL doublet splitting consistent with spacing in photoabsorption measurement
  Potentially HH1 and LH1 transitions
GaAs
Substrate
Buffer
Cap
TGrowth = 520°C
Notes: .

## Slide 37: DC reflectivity shows little change in uniformity with growth conditions
V/III ratio has little effect on the uniformity
Higher(lower) temperature decreases(increases) uniformity slightly
  Non-uniform indium desorption over the wafer from a non-uniform temperature profile
GaAs cap
Superlattice
520°C V/III = 2.5
485°C V/III = 2.5
560°C V/III = 2.5
520°C V/III = 1.5
RT

## Slide 38: Effect of V/III ratio
XRD shows not much of a change, higher V/III ratio is better
PL shows slight blue shift with lower V/III
  No measurable change in FWHM
Constant growth temp 520°C
0
1
2
-1
-2
GaAs(004)
RT
GaAs
Substrate
Buffer
Cap
Superlattice

## Slide 39: Clear terraces in all samples except cold grown
520 °C
V/III=2.5
520 °C
V/III=2.0
520 °C
V/III=1.5
480 °C
V/III=2.5
560 °C
V/III=2.5
2 µm
400 nm

## Slide 40: Digital alloys improve surface morphology
Unexpected improvement in sample roughness using digital alloys
  GaAs layer in DA barrier
  InGaAs layer in DA well
GaAs/InGaAs improve morphology more than AlAs/InAlAs deteriorate it
520 °C
V/III High
2 µm
520 °C
V/III High
520 °C
V/III High
All analog
DA Barrier
DA Barrier
DA Well & Barrier
0 nm
1 nm
1.5 nm
-1 nm
-1.5 nm
-0.5 nm
-0.5 nm
0.5 nm
RMS 5.1 Å
RMS 3.7 Å
RMS 1.9 Å
10x
6x
5.1 nm In0.16Al0.23Ga0.61As
2.3 nm Al0.274Ga0.726As
12x
1.8 Å In0.06Al0.94As
5.2 Å In0.22Ga0.78As
10x
0.79 Å AlAs
1.66 Å GaAs