## Slide 1: Atomic Layer Deposition (ALD) – An Enabler for Photocathodes?
Harish Bhandari, Director for Advanced Thin Films Technologies
hbhandari@rmdinc.com

## Slide 2: Spicer’s 3-Step Photoemission Model
Photocathode
Substrate
L,
escape depth
La absorption depth
Substrate
Photocathode
Photoexcitation
Transport to the Surface
Escape to Vacuum

## Slide 3: A case for conformal cathodes
photon
electron
Ultrathin conformal cathodes
Nanostructured Substrate
Nanostructured Substrate

## Slide 4: ALD – a thin film growth technique
Growth Techniques most popular for cathodes:
Thermal Evaporation
Molecular Beam Epitaxy
Pulse Laser Deposition
RF sputtering

## Slide 5: ALD – how does it work?
Case Study: Al2O3 by ALD

## Slide 6: Innovations in ALD are challenging (and rewarding)
ALD is driven by surface chemistry
  Self-limiting chemical reaction
Requires tailored chemical precursors
  Reactivity
  Predictability (reaction)
  Volatility
  Stability
ALD
Pump
Cathode handoff
Loadlock
Precursors
Source: www.moorfield.com

## Slide 7: ALD for Spin Polarized Cathodes (Group II-VI)
Source: Dr. Chubenko, P3 2023
Boutaiba et al. Phys. REV. B 89, 245308 (2014):

## Slide 9: Cross-Sectional TEM Image: CdTe/InAs
InAs
CdTe
Region used for
elemental analysis
ALD of CdTe @ 75 C
No pinholes
No cracks
No delamination
Abrupt interface
Smooth Morphology

## Slide 10
ALD @ 75 C
RMD is on the cutting edge of ALD!
Applications: Infrared detectors, X-ray detectors, Photovoltaics, Photonic integrated circuits, microelectronics, phase-change memory, etc.
High Step Coverage
16:1 Aspect Ratio

## Slide 11
ALD of ZnTe at Low Temperature (85 C)
InAs
a = 6.058 Å
ZnTe
a = 6.101 Å
Possibilities
Lattice-matched passivation InAs/GaSb
Lattice-matched CZT passivation for MCT
Epi-ready layers grown on CZT crystals for MCT growth

## Slide 12
Reciprocal Space Mapping of ZnTe (60 nm) on InAs

## Slide 13
Strained Layer Epitaxy CdTe/ZnTe
Preliminary investigation for CdTe indicate:
1.5eV bandgap permits excitation at 780nm;
~2% strain has the necessary valence band splitting (0.1eV) to realize 100% polarization;
p-type can be achieved with antimony/arsenic doping;
has excellent absorption and spin relaxation time;
negative electron affinity has been demonstrated with Cs-O surface treatments.
Cd(1-x)ZnxTe | Lattice Parameter (A) | % Strain
x=0 (CdTe) | 6.48 | 0.00
x=0.1 | 6.451 | 0.45
x=0.2 | 6.422 | 0.90
x=0.3 | 6.371 | 1.68
x=0.4 | 6.298 | 2.81
x=0.5 | 6.25 | 3.55
x=0.6 | 6.218 | 4.04
x=0.7 | 6.183 | 4.58
x=0.8 | 6.128 | 5.43
x=0.9 | 6.051 | 6.62
x=1 (ZnTe) | 6.1 | 5.86
What is needed:
DFT calculations of band structure
Monte Carlo simulations of transport properties

## Slide 14: GaAs Nanotip Activation
Swanwick, Michael E., et al. "Nanostructured ultrafast silicon-tip optical field-emitter arrays." Nano letters 14.9 (2014): 5035-5043.
ALD can be used for nanotip activation
RMD does have a proprietary Cs ALD precursor (metal organic)
On-site Cs2O surface activation is possible

## Slide 15
Mn
Te
Mn
Te
ALD MnTe @120 C
MBE (250 OC)
Bi2Te3
Te
Mn
Atomic Layer Epitaxy of MnTe at 120 OC on Bi2Te3
Sapphire
ALD Sb2Te3 @65 C
Applications: Ultra-efficient spintronic memory and transistors

## Slide 16: Some of the other ALD possibilities
Cs2Te
Cs3Sb
K3Sb
3K2CsSb  2K3Sb+Cs3Sb
ALD of capping layers for Photocathodes
Plasmonic Surface (Alimohammed Kachwala)
Grating coupler (Hyun Uk Chae)

## Slide 17: Final Thoughts…
Atomic Layer Deposition (ALD) is a versatile technique for growing high-quality thin films
  Chalcogenide-based spin polarized cathodes
  Alkali antimonide cathodes
  Surface Activation
  Capping Layers
ALD’s conformal nature can be exploited for realizing high QE cathodes
ALD’s can be a compact system that can accompany the “puck”
I am seeking collaborators on these topics
hbhandari@rmdinc.com

## Slide 18: Thank you
Sincerely thank these people for valuable discussions:
Oksana Chubenko
Sid Karkare
Luca Cultrera
Dimitre Dimitrov
Rehan Kapadia (and his students)