## Slide 1: Some ideas

## Slide 2: Truss structure
ALICE ITS2
  This design was used to define the ePIC SVT performance parameters for the outer layers
I can’t see how this will work with gas cooling
  But then, it seems to work well (low material) with liquid cooling
B Abelev et al and (The ALICE Collaboration) 2014 J. Phys. G: Nucl. Part. Phys. 41 087002
Length: 270 mm

## Slide 3: Concept for a foam-based stave
Silicon: 0.05%X0 for 50 μm thickness
FPC: For example ITS2 ~0.09%X0
Use a foam core
  For shear strength and to conduct air and heat
    Other means to maintain shear strength (ribs etc.) probably more material
  RVC (Al or SiC?)
  Typical density about 3% of bulk material
  Radiation length for SiC foam is > 3000 mm
  0.17% X0 for 5 mm thickness (this is probably overly conservative…)
Enclose to guide air flow
  Enclosing layer of Kapton foil
  Radiation length for Kapton is ~300 mm
  10-2% X0 for 25 μm
Bending stiffness from single layer of UHM fibre (K13C2U?)
  Ultra-thin plies (other fibres) down to 30 μm
  Such thin plies need very careful handling (using handling tools, elevated temperatures during lay-up, etc.) because they are likely to split
    Also, sharp corners are difficult
  Radiation length ~250 mm
  3×10-2% X0 for 70 μm

## Slide 4: Conceptual sketches
End view
Consisting of two half shells
Side view of foam core
x scale : y scale = 10:1
Top shell has complementary castellations
FPC can run underneath castellations
What would be needed next:
Verify mechanical performance with FEA
Optimise choice of foam (how low a density can we get? What is the radiation length?)
Detail joint of half shells (how do we make this gas-tight) – maybe angular Kapton strip with runny epoxy
Detail FPC underneath castellation
Is the air flow enough, or do we need to embed cooling pipes into the foam?
Possibly could co-cure the sandwich
CF coverage could be optimised

## Slide 5: Stiffness issues
Stiffness of staves might not be sufficient to work over a ~ 800 mm span
End rings
Staves
Several options:
  Intermediate support rings
    If needed for L3 this would introduce additional
    material before L4
  Link adjacent staves
    Stiffness would now be defined by the huge moment of inertia of the complete cylinder
      Effectively it means that it is defined by the buckling stiffness
      And that’s probably dominated by the distance between links
      Could be (floating) support rings as above, or something more local

## Slide 6: Solution 3: Staves under tension
End rings
Staves
Outer support cylinder
Tensioning elements could be Kevlar filaments
Want something that has high strength, but moderate modulus
Possibly also include springs to maintain tension at defined level
This could be a solution for L3 (in that case L4 would be the support cylinder, but buckling of L4 would need to be prevented…)