## Slide 1: AE-101 Optical Materials for Ultrahigh-Power​ Long-Wave Infrared Lasers Close-out report
26th ATF Users’ Meeting
2024-03-26
Misha Polyanskiy

## Slide 2
Title | Optical Materials for Ultrahigh-Power​ Long-Wave Infrared Lasers
Status | Closeout (follow-up experiment will be proposed separately)
PIs | Mikhail Polyanskiy Igor Pogorelsky
Team | BNL: M. Polyanskiy, I. Pogorelsky, M. Babzien, D. Choge UCF CREOL: K. Vodopyanov BAE Systems: P. Schunemann -> K. Zawilski, J. Jesenovec
Funding | DOE ARDAP grant Phase I (2019—2022; PI: M. Polyanskiy) DOE ARDAP grant Phase II (2022—2025; PI: M. Polyanskiy) BNL LDRD grant #20-010 (2020—2023; PI: I. Pogorelsky)
Funding Status | Received
AE-101

## Slide 3: Goals
Systematically study properties of infrared materials under the action of intense L-WIR laser irradiation
Develop a concept of nonlinear post-compression of picosecond L-WIR pulses to a sub-picosecond
Demonstrate post-compression at multi-TW level
“We propose a systematic study of the properties of a wide range of materials under the action of ultra-intense long-wave infrared (LWIR) laser pulses. The information that will be obtained during the proposed effort is critically needed for the development of the next-generation multi-terawatt LWIR lasers.”
(DOE ARDAP Accelerator Stewardship proposal, 2019)

## Slide 4: DOE ARDAP project: Team & directions
Fundamental study: Physics of interaction of IR materials with intense MWIR/LWIR optical fields
Applied science: Database of nonlinear constants, new concepts of nonlinear LWIR optical systems
Advanced materials: Fabrication methods for new types of IR crystals
BGS
BGSe
UCF (Konstantin Vodopyanov)
BNL (Misha Polyanskiy)
BAE (Kevin Zawilski)

## Slide 5
100 mm
AE-101 pre-requisite 1: beam
14 m
13 mm dia.
aperture
≤ 10 J
Energy-dependent, shot-to-shot varying beam profile
13 mm
≤ 500 mJ
Stable, near-Gaussian
beam profile
Polyanskiy et al. Opt. Lett. 46, 2067 (2021)

## Slide 6
AE-101 pre-requisite 2: Data analysis tool
Configuration tab
Results tab
Documentation
Process tab
co2amp 2020 (new interface & advanced material interaction support)
Polyanskiy Appl Opt. 54, 5136 (2015)
https://github.com/polyanskiy/co2amp

## Slide 7: Single-shot measurements
Nonlinear Refraction
Nonlinear Absorption
Non-linear absorption

## Slide 8: Nonlinear properties of LWIR materials
Nonlinear Refraction
Nonlinear Absorption
Polyanskiy et al. Opt. Mater. Express 14, 696 (2024)

## Slide 9: n2 database (now part of refractiveindex.info)
Polyanskiy. Sci. Data 11, 94 (2024)

## Slide 10: Next-generation CO2 laser: Post-compression
Self-phase modulation
Linear dispersion

## Slide 11: Proof of principle
278 mJ
In
290 fs
Autocorrelation
2 ps
Out
2 ps
5 mm dia. beam center
Whole beam
in
out
in
out
Polyanskiy et al. Opt. Express 29, 31714 (2021)

## Slide 12: 1st Prototype
measured within a central portion of the beam containing 30% of the total energy
Most powerful long-wave infrared sub-picosecond pulse ever obtained
IN
OUT
Beam center 700 fs
Model
Experiment
Pogorelsky et al. – Front. Phys. (accepted)

## Slide 13: Set-up for laser-damage characterization

## Slide 14
Optical damage experiments
Laser
Sample
Digital image of Al mirror
Optical microscope image of damaged spot for low energy shot (but above damage threshold)
Al mirror
Laser in
Sample

## Slide 15
AE-101 Results
Systematic study of nonlinear refraction and absorption properties of materials relevant for high-power LWIR lasers [✔ ✔ ✔]
n2 database [✔ ✔ ✔]
Conceptualization, proof-of-principle demonstration and 1st full-energy prototype of post-compression [✔✔]
Study of laser damage of LWIR materials and optical components [✔]
By-products: ‘perfect beam’ at reduced-energy, improved numerical modelling [🙂]

## Slide 16: Activities & Impacts Associated with this Experiment – All Years
Journal papers
  I. V. Pogorelsky, M. N. Polyanskiy, M. Babzien, A. Simmonds, M. A. Palmer, “Terawatt-class femtosecond long-wave infrared laser” – accepted for publication in Front. Phys.
  M. N. Polyanskiy, I. V. Pogorelsky, M. Babzien, K. L. Vodopyanov, M. A. Palmer, “Nonlinear refraction and absorption properties of optical materials for high-peak-power long-wave-infrared lasers” ", Opt. Mater. Express 14, 696, 2024 https://doi.org/10.1364/OME.513971
  M. N. Polyanskiy, "Refractiveindex.info database of optical constants", Sci. Data 11, 94, 2024 https://doi.org/10.1038/s41597-023-02898-2
  T. Kawamori, P. G. Schunemann, V. Gruzdev, K. L. Vodopyanov, “High-order (N=4–6) multiphoton absorption and mid-infrared Kerr nonlinearity in GaP, ZnSe, GaSe, and ZGP crystals”, APL Photonics 7, 086101, 2022 https://doi.org/10.1063/5.0089925
  M. N. Polyanskiy, I. V. Pogorelsky, M. Babzien, R. Kupfer, K. L. Vodopyanov, M. A. Palmer, "Post-compression of long-wave infrared 2 picosecond sub-terawatt pulses in bulk materials", Opt. Express 29, 31714-31725, 2021 https://doi.org/10.1364/OE.434238
  M. N. Polyanskiy, M. Babzien, I. V. Pogorelsky, R. Kupfer, K. L. Vodopyanov, M. A. Palmer, "Single-shot measurement of the nonlinear refractive index of air at 9.2 μm with a picosecond terawatt CO2 laser", Opt. Lett. 46, 2067, 2021 https://doi.org/10.1364/OL.423800
  M. N. Polyanskiy, I. V. Pogorelsky, M. Babzien, R. Kupfer, N. Vafaei-Najafabad, M. A. Palmer, "High-peak-power long-wave infrared lasers with CO2 amplifiers", Photonics 8, 101, 2021 https://doi.org/10.3390/photonics8040101

## Slide 17
Conference presentations
  I. Pogorelsky, M. Polyanskiy, W. Li, M. Babzien, M. A. Palmer, “Emerging ultra-fast multi-terawatt long-wave infrared lasers”, Optica High-Brightness Sources and Light-Driven Interactions Congress, Vienna, Austria, March 12–14 2024
  M. N. Polyanskiy, I. V. Pogorelsky, M. Babzien, W. H. Li, R. Kupfer, M. A. Palmer, N. Vafaei-Najafabadi, “Multi-terawatt, sub-picosecond long-wave infrared laser for next-generation particle accelerators”, International Particle Accelerator Conference, Venice, Italy, May 7–12 2023
  I. V. Pogorelsky, M. Babzien, W. Li, M. N. Polyanskiy, M. A. Palmer, “Opportunities for directed energy research with femtosecond long-wavelength lasers”, 2023 Annual Directed Energy Science and Technology Symposium, San Antonio, TX, 3–6 April 2023
  M. N. Polyanskiy, I. V. Pogorelsky, M. Babzien, W. H. Li, R. Kupfer, M. A. Palmer, “9.3 microns: toward a next-generation CO2 laser for particle accelerators”, 20th Advanced Accelerator Concepts Workshop, Long Island, Hauppauge, NY, November 6–11, 2022
  M. N. Polyanskiy, I. V. Pogorelsky, M. Babzien, R. Kupfer, M. A. Palmer, “The choice of materials for post-compression of high-peak-power long-wave infrared pulses”, Conference on Lasers and Electro-Optics, San Jose, CA, May 16–20 2022
  T. Kawamori, P. G. Schunemann, V. Gruzdev, K. L. Vodopyanov, “High order (N=4–6) multiphoton mid-IR absorption in GaP, ZnSe, GaSe, and ZGP and the role of free carriers”, Conference on Lasers and Electro-Optics, San Jose, CA, May 16–20 2022
  K. L. Vodopyanov, P. G. Schunemann, T. Kawamori, “Mid-IR high-order multiphoton absorption and nonlinear refraction in GaP, ZnSe, GaSe, and ZGP crystals”, Laser-Induced Damage in Optical Materials 2021 (virtual), October 12–15 2021
  M. Polyanskiy, I. Pogorelsky, M. Babzien, R. Kupfer, M. Palmer (poster presented by I. Pogorelsky), "Ultrashort-pulse, terawatt, long-wave infrared lasers based on high-pressure CO2 amplifiers", EOS Annual Meeting (EOSAM), Rome, Italy (virtual), September 13–17 2021
  I. V. Pogorelsky, M. N. Polyanskiy, M. Babzien, M. A. Palmer, "Post-compression of 9.2-μm terawatt laser pulses to femtoseconds", EOS Annual Meeting (EOSAM), Rome, Italy (virtual), September 13–17 2021
  I. Pogorelsky, M. Polyanskiy, M. Babzien, M. Palmer, “Long-wave IR terawatt laser pulse compression to sub-picoseconds”, 12th International Particle Accelerator Conference, Campinas, SP, Brazil (virtual), 24–28 May 2021
  T. Kawamori, P. Schunemann, and K. Vodopyanov, “High-order mid-IR multiphoton absorption and nonlinear refraction in GaP, ZnSe, GaSe, and ZGP crystals”. Conference on Lasers and Electro-Optics, San Jose, CA (virtual), May 09–14 2021
  I. Pogorelsky, M. Polyanskiy, M. Babzien, and M. Palmer, “Experiment on long-wave IR terawatt laser pulse compression to sub-picoseconds”. Mid-Infrared Coherent Sources 2020, Washington, DC United States (virtual), 16–20 November 2020

## Slide 18
Other
Two graduate students training (UCF)
Significantly re-factored and improved version of co2amp code with advanced support of modelling the pulse interaction with optical materials
“n2” database of nonlinear refractive indices implemented as part of the refractiveindex.info database
Method for reliably generating a reproducible high-quality beam at reduced energy for that is relevant for some user experiments

## Slide 19: COVID-19 Pandemic Impacts
There were some delays at the beginning of the project. The most significant one was the delay in the hiring of a post-doc.