## Slide 1
Sergey Mirov
University Professor of Physics
1Department of Physics, University of Alabama at Birmingham,
4100 East Science Hall, 902 14th Street South, Birmingham, AL 35294, USA
e-mail address: mirov@uab.edu
Funding:
High-power MWIR/LWIR ultrafast lasers for high-energy physics
D. Martyshkin,1 V. Fedorov,1 K. Karki,1 I. Moskalev2, S. Vasilyev2, M. Mirov2, S. Ya. Tochitsky,3 C. Joshi3, J. J. Pigeon4, Z. Cheng5, I. Pogorelsky5, M. Polyanskiy5, K. Zavilski6, J. Jesenovec6,
K. Vodopyanov7
2IPG Photonics - Southeast Technology Center, 100 Lucerne Ln, Birmingham, Al 35211, USA
3University of California,
4University of Rochester
5University of Ottawa
6Brookhaven National lab
6BAE Systems
7University of Central Florida
The work reported here partially involves intellectual property developed at the University of Alabama at Birmingham (UAB). This intellectual property has been licensed to the IPG Photonics Corporation. The UAB co-authors declare competing financial interests.
Outline
Cr:ZnSe and Cr:ZnS lasers.
Fe:ZnSe lasers.
Optically pumped CO2 systems.
Cr:ZnSe lasers pumped ZGP OPCPA.

## Slide 2: TM:II-VI laser materials: main properties
Room temperature operation
Absorption and emission spectra of Cr- and Fe-doped ZnSe
Cr2+-doped ZnSe and ZnS
Broad tuning range (1.8 – 3.3 µm)
Convenient pumping by fiber and bulk lasers, and laser diodes with up to 60% pump conversion
Excellent energy storage capabilities at 77 K
Fe2+-doped ZnSe and ZnS
Tuning range (3.5 – 5.2 µm)
Pumping at 2.7 – 3 µm
Cr:ZnS/Se and Fe:ZnSe are the “Ti:sapphires of the middle-infrared” !

## Slide 3: Cr:ZnS lasers – a unique front end for 2-10 µm high energy systems
▲ Referencing of the broadband IR frequency comb ▲
Middle IR comb is referenced with low cost near-IR detectors! Compatible with all available optical frequency standards at 1.06, 1.5 µm!
 VIS part of the continuum 
 Obtained 5-octave spectrum 
Desktop Synchrotron!
125×225×425 mm3
▲ Measured spectrum of the source ▲

## Slide 4: Ultrafast Cr:ZnS and Cr:ZnSe amplifiers: Energy amplifiers
IPG Cr:ZnSe CPA:
1-kHz, 1.5-mJ, 9.5-GW Seeded by: 12.5 nJ, 30 fs Kerr-lens mode-locked Cr:ZnS laser
1 kHz Multi-pass amplifier at CREOL
Seed pulses: 1 µJ, few-cycle pulses from BIBO-based IDFG driven by a 1.5 mJ, 30 fs Ti:Sapphire CPA
Öffner stretcher
DAZZLER
Treacy compressor
4 mJ, 44 fs (6-cycles), >90 GW output
1 kHz Multi-pass amplifier at the Ohio State
Seed pulses: 50 µJ, 80 fs pulses from BBO-based OPA driven by a 4 mJ 80 fs Ti:S CPA
Martinez stretcher
Treacy compressor
Multi-plate-like nonlinear post-compression
6.2 mJ, 39 fs (4.8-cycles), 115 GW output

## Slide 5: New Vision of Ultrafast Cr:ZnS and Cr:ZnSe Energy Amplifiers
+
+
New vision of Cr:ZnS(Se) CPAs
Pumping by Q-switched Er:YAG laser
High-gain (30 – 40 dB) single-pass preamplifier
Multi-pass main amplifier and booster (s)
Post compression
The optical layout of 1 TW Cr:ZnSe CPA

## Slide 6
MAJOR PROPERTIES
Quasi-4 level system
To minimize ground state absorption use small Er concentration ~0.5% and long ~4-5 cm crystals
Small up-conversion for low concentrated Er:YAG
Small quantum defect ~ 7%, no need for water cooling
High-brightness 1532 nm frequency stable sources are required to provide long collimated gain regions
To achieve gain the ground state absorption should be bleached – soft-aperture effect – TEM00
Hybrid (fiber-bulk) systems combine high efficiency of CW fiber lasers with high pulse energies of bulk materials
FUTURE WORK
Scale up energy of 1645 nm Er:YAG with the use of large-mode unstable cavity (see OL 2013) and the use of multimode 1532 nm Er-fiber pump.
IPG has up to 1 kW commercial 1532 nm multimode Er-fiber lasers
1.645 µm Er:YAG pump lasers for Cr:ZnSe/S CPAs. Current status and future outlook
10 ms
Er

## Slide 7
A 1-TW, Cr:ZnS-based system with a repetition rate of 1 Hz.
Combined Cr:ZnS elements to obtain high absorption of the pump laser.
TPL inside the Cr:ZnS elements was effectively suppressed by using the ink-cladding technique.
Via two stages of amplification, the pulse energy was amplified to over 200 mJ.
The pulse was compressed to 127.6 fs at an energy of 147.1 mJ.

## Slide 8
Fe:ZnSe material features and current state-of-the-art
Fe doped ZnSe – Ti-S of the infrared
Key Advantages
Access to 3.4 – 5.2 µm range
Other Features
Pumping at 2.94/2.8 µm by Er:YAG/YSGG
Pumping at 2.7 µm by HF lasers
Supports all laser regimes
cw, ms, µs at T < 220 K
ns at room temperature
mode-locked
60 s lifetime – high energy storage capability
Q-switching and amplification of ns-fs pulses in the mid-IR
Fe:ZnSe prepared via post-growth diffusion. S. Mirov et al., IEEE JSTQE 24, 1601829 (2018)
Fe:ZnSe hot-pressed ceramics
K. Karki et al., OMEX, (2020)
 40x3mm
 15x3mm
Regime of operation | Output characteristics | Reference
CW (Cr:ZnSe 2.9 µm pumping) | 9.2 W; =40%; T=77K | S. Mirov, et al., IEEE, JSTQE, 24, 1601829, 2018
Long Pulse, High Power (free running 2.94 µm Er:YAG) | 35 W, 4.1 µm, 100 Hz, 150 µs; =35%; T=77K | S. Mirov, et al., IEEE, JSTQE, 24, 1601829, 2018
Long pulse, High Energy (free running 2.94 µm Er:YAG) | 10.6J, 4.1 µm, single pulse, =53%; T=87K | V. Kozlovsky et. al., J. Physics (2016)
Gain-switched ns pumping (HF 2.7 µm laser) | 1.43J, 4.4 µm, 10 Hz, =53%; T=300K | A. Dormidonov, et al., Appl. Phys. B 122, 211 (2016)
Nanosecond MOPA (Q-switched 2.94 µm Er:YAG) | 60 mJ, 4.4 µm, 10 Hz, =30%; T=300K | D. Martyshkin, S. Mirov et. al., Opt. Express 29, 2387 (2021)
Multipass amplification of ultrashort pulses (Q-switched 2.85 µm Cr: Yb: Ho: YSGG) | 3.5 mJ, 150 fs, 4.3 µm, T=300K | E. Migal, et. al., Opt. Lett. 44, 2550 (2019)
Fe:ZnSe lasers: state-of-the-art
UAB Physics and industrial collaborator IPG Photonics are the world leaders in Cr/Fe doped II-VI materials and lasers
Room-temperature cross-sections of emission of
(i) Cr:ZnS, ii) Cr:ZnSe ; iii) Fe:ZnS, iv) Fe:ZnSe, v) Fe:Cd0.75Mn0.25Se, vi) Fe:CdTe, vii) Fe:Zn0.5Cd0.5Te, and viii) Fe:Cd0.5Mn0.5Te
Notes: Here we change gears and move to a description of Fe:ZnSe LWFA driving laser. We start with Fe:ZnSe materials properties and current state-of-the-art output characteristics. Fe:ZnSe crystals are often called Ti-sapphire of middle infrared. Fe:ZnSe provides access to a 3.4-5.2 um spectral range with cross-sections of 10^-18 cm2. It can be pumped by radiation of 3 um Er based lasersor 2.7 um of HF lasers. Fe:ZnSe supports all laser regimes of operation: cw, ms, µs at T < 220 K, ns at room temperature, as well as mode-locked regime. It features ~60 us lifetime at up to 150K and is the only available solid-state material with high energy storage capability in MWIR. It can serve as an effective MWIR amplifier at low temperatures under free-running 3 um Er laser excitation, or at room temperature under Q-switched 3 um Er laser excitation. The table depicts Fe:ZnSe lasers stat-of-the-art with 35 W of output power, in excess of 10 J of output energy in long pulse, 1.4 J short pulse lasing under ns 2.7 pump radiation of HF laser, 60 mJ nanosecond broadly tunable MOPA and 3.5 mJ, 150 fs multipass amplifier of ultrashort pulses. The technology of fabrication of Fe:ZnSe gain media is mature and ready for reaching 1TW level of power.

## Slide 9
Fe:ZnSe CPA at 4.1 mm
Fe:ZnSe gain crystal:
Large stimulated emission cross section
Long upper state lifetime at cryogenic temperature
Can be pumped by free-running Er:YAG at 2.94 µm
Current status: Z. Chang. Opt. Express 31, 13447 (2023)
4.6 mJ, 250 fs, 333 Hz at 4.1 µm
Notes: Here we show the current status of Fe:ZnSe 4.1 um CPA developed by the Zenghu Chang group. It is based on cryogenic 8 pass Fe:ZnSe CPA pumped by radiation of free running 3um radiation of diode pumped Er:YAG. Fe:ZNSe is seeded by a stretched radiation of a broadband optical parametric generator based on LGS nonlinear crystal pumped by 1 um pump from Yb KGW and broadband signal from YAG supercontinuum generator. It delivers 3.7 mJ at 247 fs, 5 mJ in 130 ps before compression at 300 Hz at 4 µm.

## Slide 10: Future RT Fe:ZnSe Terawatt System
1W Cr:ZnS@2.35 m
75MHz, 50fs
Kerr Mode-Locked laser
Pulse Picker
OPG-OPA ZGP
15 J@2.35 m, 100fs
5 J@4.0 m, 100fs
2 µJ@4.0 m, 300ps
Pulse Stretcher
Single Pass Cr:ZnSe Amplifier
Er:YAG@1.645 m
10mJ, 50 ns
Multi Pass Fe:ZnSe(S) Amplifier
Er:YSGG@2.7 m
50mJ, 50 ns
2 mJ@4.0 m, 300ps
3 stage Double Pass
Fe:ZnSe Amplifier
120 mJ@4.0 m,
300ps
Er:YSGG@2.7 m
400mJ, 50 ns
Pulse
Compressor
100 mJ@4.0 m,
100fs

## Slide 11
2.79 um, 260 mJ Pump
4.4 um, 60 mJ Fe:ZnSe
spatial profile
Cr:Er:YSGG, EO Q-switched, 100ns, MOPA
Fe:ZnSe MOPA 4.4 um
80 ns output
Fe:ZnSe MOPA 4.4 um
Pulse duration
Triggerable Fe:ZnSe gain-switched ns amplifier

## Slide 12
High-Pressure Optically Pumped CO2 Laser
Physics challenges in a gas active medium at high-pressure ≤20 atm
Goal: increase the upper-state lifetime to >1 ms and mitigate nonlinear refraction effect for the 4.3 mm pump. Gain tailoring using various CO2 isotopes to reach many THz bandwidth in a cm-scale cell.
Status
Leveraged seed funding from the DOE Accelerator Stewardship program: a 2 mJ and then 60 mJ Fe:ZnSe pump was built and used for proof-of-existence experiments at UCLA.
Collaboration between UCLA/BNL/UAB, modeling Applied Optics, 58, 5786 (2019)
Turn-key operation RT Fe:ZnSe MOPA tunable over 3.8-5.0 m (60 mJ)
The first 10 µm lasing in a ≤15 atm optically pumped CO2 cell
30% and 10% efficiencies at 1 and 7 atm cells, respectively
Notes: Here we change gears again and describe a new platform of high-pressure optically pumped CO2 lasers and amplifiers. We propose to use high pressure CO2 cells with gain tailoring using various CO2 isotopes to achieve many THz bandwidth supporting amplification of sub-ps pulses. OP CO2 multipass amplifier is seeded by radiation of 10 um 300 fs DFG and resonantly pumped to the upper 001 level by ns Fe:ZnSe laser radiation. On the right side of the slide, one can see the current status of developed at the UAB turn-key RT Fe:ZnSe MOPA tunable over 3.8-5.0 um with output energy up to 60 mJ at 200 ns pulses. At the bottom right corner, the first 10 um lasing in 15 atm optically pumped cell is demonstrated.

## Slide 13: Ultrafast CO2 amplifiers
State of the art (BNL)
Perspectives
Mixed-isotope 16O:18O High-pressure 10 atm
= Ultrafast-ready spectrum
2 ps
1) Better use of gain spectrum (9R+9P)
2 ps → 500 fs (15 TW)
Need ~10 mJ seed pulse @ 9.3 μm
2) Post-compression
500 fs → 100 fs (25 TW)
Two-bulk-material scheme [KCl+BaF2] demonstrated for longer pulses
Relies on negative GVD (typical for LWIR)
3) Optical pumping
Improved rep. rate, compactness, reliability
Need 4.3 μm (ideally) or 2.8 μm pump for CO2 pumping
5 TW
Polyanskiy et al. Photonics 8, 101 (2021)

## Slide 14
4. Er:YAG @1.6m
10 mJ , 50 ns
8. 4x Er:YAG
@1.6m 30mJ ,
50 ns
2.Pulse picker, 100 Hz
Signal Seed
@3.14 m
30 mJ Pump
@2.35 m
1.fs Cr:ZnS laser
2.35 m
30 fs, 10nJ
80 MHz
3.Cr:ZnSe
pre-amp
SC generation
(100 J, 100fs )
2-3.5 m
5. Pulse shaper
@3.14 m
7. Multi Pass
Cr:ZnS Amplifier
50mJ, 300 ps
9. Stretcher
@3.14 m 300ps
130 mJ Pump
@2.35 m
12. Multi Pass
Cr:ZnS Booster
100 Hz, 100mJ, 2.35um
11. 8x Er:YAG
@1.6m 30mJ ,
50 ns
13. ZGP
Power amplifier
9.3 m, 10mJ, 300 fs, 100 Hz
9.3 m, 3 mJ, 300 fs, 100 Hz
10. 2-stage ZGP
pre-amplifier
6. Stretcher
@3.14 m 300ps
High-energy long-wave infrared sources for seeding CO2 amplifiers
Need for ZGP e-irradiation with
integral e-beam fluence of
~ 1.5x1017 cm -2 to suppress
losses for <2.5 µm range
"Room temperature tunable color center lasers", T.T. Basiev, S.B. Mirov, Laser Science & Technology book Ser., 16, 1-160, V.S. Letokhov, C.V. Shank, Y.R. Shen, H. Walter, Eds., Gordon and Breach Science Publ./Harwood Acad. Publ. (1994).
1) OP (Fe:ZnSe or Cr:Er:YSGG) CO2 or 2) Cr:ZnSe pumped ZGP OPCPA

## Slide 15: Quad Chart
Scientific/Technical Outcomes Polycrystalline TM:II-VI is enabling laser technology Enable development of a new generation of high-power, tabletop, ultrafast infrared TW level lasers By far the best few-cycle lasing in the 2 – 5 µm By far the simplest hardware for optical frequency comb generation. Effective gateway to LWIR, THz, XUV, X-ray Promising for direct electrical excitation | Lasers/e-beam Parameters Required Need 10 MeV electron beam with pulse energy 10-20J, 10-100 Hz rep rate to improve optical quality of ZGP, ZnSe, and optical damage of the gain elements facets
ATF Facilities Upgrade Roadmap Optically pumped (4.3 µm Fe:ZnSe or 2.8 µm Er:YSGG) high-pressure multi-TW CO2 lasers Develop 10 mJ 9.2 µm seed for CO2 preamp either by OP CO2 or Cr:ZnSe pumped ZGP OPCPA. Develop mid-IR 1-3 TW level Cr:ZnS/Se (2.5 µm) and and Fe:ZnSe (4-5 µm) CPA systems at BNL and integrate them with CO2, e-beam, and Ti-S. | Beyond the Current Roadmap Need energy scaled up (1-2J) 3 µm Q-switched Er:YSGG pump laser development for pumping Fe:ZnSe or directly CO2. Need energy scaled up (0.5-1 J) 1.645 µm Q-switched Er:YAG with the use of large-mode unstable cavity and the use of multimode 1.532 µm Er-fiber pump (for pumping Cr:ZnS/Se CPA) Need J level 100 ns Fe:ZnSe development for pumping CO2.

## Slide 16
Thank you for your attention!
Dr. Sergey Mirov
University Professor of Physics
(205) 934-8088; mirov@uab.edu