## Slide 1: Update on Prototyping & Stave Structure Analysis
11/09/24

## Slide 2: Quarter Length Stave
We have all the material we need for a first prototype
Working on Kapton C channel
Currently have a couple of prototype Carbon Fibre I beams but we may try making one more
We have hand cut carbon fibre skins (2 ply 0/90) but plan to make production intent on drag knife
Stave jig parts (including K9 foam block)
Start with 2 (quarter stave)

## Slide 3: Quarter Length Stave

## Slide 4: Quarter Length Stave
3D printed stencils and resulting parts(hoping to also get drag knife versions ASAP)

## Slide 5: Module Assembly Tooling
Gap under vacuum tool looks consistent (this sets glue thickness) should be approx. 100 microns
L4 Module Installation Tooling

## Slide 6: Comparison of Flat vs. Curved stave structure
07/08/2024

## Slide 7: Introduction
Why do we curve our sensors?
  Local Stiffness argument has been presented previously
    Reduced deformation under internal pressure
    Higher internal mode of Sensor
  What about Global Stiffness?
    Curved sensors may also improve global stiffness
    Left object has higher moment of inertia should be harder to bend along the long axis
    Flat Sensor will have centre of area slightly further from neutral axis so hard to predict the difference

## Slide 8: Comparison Geometry
For fair comparison try to match radiation length
  Only components which differ are the I and C channel thicknesses
Internal volume should be equal to or higher than the curved concept we have been using so far (we don’t want to increase flow velocity)
Curved Assembly
8mm thick in centre
4mm thick at tip
Flow Area – 131 mm2
Mass - 249.4g
Flat Assembly
6.65 mm constant thickness
Flow Area – 137 mm2
Mass - 256.6 g

## Slide 9: Mode Comparison – First & Second Mode
Curved Assembly
91.581 Hz
236.44 Hz
Flat Assembly
84.57 Hz
242.33 Hz

## Slide 10: Mode Comparison – Third & Fourth Mode
Curved Assembly
274.44 Hz
379.29 Hz
Flat Assembly
254.23 Hz
338.36 Hz

## Slide 11: Sensor Internal Mode Frequencies
In previous sensor mode studies used a best-case constraint for maximising internal mode
  Fixed around outer edge,
  Equivalent to infinite stiffness structure
  Mode frequency will be lower with less stiff boundary
Internal modes in the 1-3 kHz range

## Slide 12: Sensor internal mode frequencies
745 Hz – Carbon Skins show local deformation
No modes involving substantial deformation of the LAS under 2 kHz