## Slide 1: Mirror Sample Destructive Thermal Test
Brian & Preet
October 24, 2024

## Slide 2
Test Procedure and Results
Test mirror samples 15-1 and 17-2. Both samples had carbon fiber and lexan bonded at Purdue, although in different batches
Thermal Cycle:
  Ramp to target temp at rate of 3 C / minute
  Soak at target temp for 15 minutes
  Ramp to 24 C at rate of 3 C / minute
Did 5 tests: 65 C, 70 C, 75 C, 80 C, and 90 C
After each cycle, visually inspect samples for bulk changes in reflectivity and material damage
Saw some changes in waviness of reflection after first and second thermal cycles – sample 17-2 seemed to be worse
No obvious structural changes to samples, although sample 17-2 seemed to develop a crease during last thermal cycle

## Slide 3
Next Steps
Test samples with Si02 coating (one each bonded at SBU and Purdue) at highest temp to see if coating has any influence on mechanical behavior
Perform fine-grained temperature tests on coated samples to evaluate changes to reflectivity / mirror surface flatness (do before/after reflectivity measurements and surface evaluations with dark box camera
Do temp tests on larger curved sample to see if mechanical deformation is more likely with bent substrate