## Slide 1
EIC HRPPD anode tarnish
[progress report]
Alexander Kiselev
pfRICH DSC general weekly meeting, 12/12/2024

## Slide 2
The issue: first three tiles
An apparent tarnish of unknown nature is seen on all Kyocera HRPPD anodes
It is not visible after a ~750 C brazing cycle in vacuum needed to attach HV springs, …
… but a pattern of support structure used in this iteration is clearly seen after fritting in air
It becomes apparent only after fritting of side walls in air at about 550 C
HRPPD #15
HRPPD #16
HRPPD #17
tarnish was sanded off this one

## Slide 3
The issue: HRPPD #18
This was an extreme case (first HRPPD produced in vacuum tank #2)
Could have been exposed to a higher temperature
Sanding tarnish off a ~1 mm thick gold layer may not be the best idea
Leaving it on the outer side may cause further oxidation during HRPPD use
Anode: vacuum side
Anode: air side
Air side after sanding

## Slide 4
Center for Functional Nanomaterials (CFN) @ BNL
A five-minute walk from Physics building 510
Plenty of amazing top-notch equipment
Including electron microscopes with an X-ray analysis capability
It is a user facility (free of charge for local BNL users)
Proposal -> review -> time allocation

## Slide 5
Our case
A so-called rapid access proposal "Measuring chemical composition of tarnish on HRPPD HTCC anode surface” submitted on 9/23/2024
Delays due to the SEM/FIB equipment malfunction
First half a day session on 11/26/2024

## Slide 6
Equipment used in this first study
Thermo Fisher Scientific “Helios G5 Dual Beam SEM/FIB Microscope”

## Slide 7
Equipment used in this first study
Inside view of the sample chamber
Kyocera anode mounted on a turntable
Picture from official BNL CFN site

## Slide 8
Sample
One of the old (2020) Kyocera anodes
Spot under study
tarnished area
sanded area

## Slide 9
First results [SEM & X-ray analysis]
Picture coming from vendor software
Normalization mismatch: either dead time or absorption in the tarnish layer
Filled histogram: tarnished area
Sanded area

## Slide 10
Custom analysis: overlay of two spectra
Spectra normalized by hand using Au peak and smooth “background” as a reference
Everything is the same in both cases, but Ni and O stick out

## Slide 11
Custom analysis: difference of two spectra
Full scale up to 20 KeV
Ni K-edge line @ 8.339 KeV

## Slide 12
Custom analysis: difference of two spectra
Low energy fraction
Ni L-edge lines (853 eV & 870 eV)
O K-edge line @ 530 eV

## Slide 13
Summary & Outlook
Looks like a NiO present on the surface (and nothing else?)
Ideally would like to check Ni:O proportion
Sure Ni is present in the system (right beneath a thin gold plating layer)
Whether Ni diffuses through gold plating during brazing cycle or “evaporates” off the exposed areas (and then pollutes the anode surface) is still a question
Ni diffusion through gold grains is a well-known effect, though …
… we know that obscuring / covering a fraction of pad area suppresses tarnish
There is a strong Ni signature at the very edge of gold-plated pads in the data
Have data measured between the pads; Ni presence there may give a good hint

## Slide 14
Summary & Outlook
Yet need to get access to a 2D map measurement data (next Monday)
Depth scan can be performed in January if needed using FIB functionality
Try to remove NiO by either a citric acid or ammonia in the meantime?
Consider removing Ni layer after the brazing cycle prematurely in the future (any acid would do)?
Volunteers to take this activity over?
An illustration of FIB/SEM principle (ignore -150 C note)