## Slide 1: Developments of Common Interest: Aerogel
Matt Posik & Bernd Surrow
Temple University

## Slide 2: Aerogel QA Station
Two critical QA assessments for aerogel
  Index of refraction
  Transmittance
Temple contributed available infrastructure and invested ~$25k in components/materials towards aerogel QA for the ePIC collaboration
  Build and commission LED system to measure light transmittance through aerogel tiles
  Validate Temple’s LED system using UV/VIS monochromator/spectrometer at BNL
  Measure index of refraction and validate Temple results with Aerogel Factory results
Recently expanded number of LEDs used (34) with financial support from the ePIC project/ pfRICH DSC
QA station can be used for general aerogel QA (e.g. pfRICH and dRICH)
  Temple in discussion to join dRICH DSC with focus on aerogel QA

## Slide 3: Aerogel QA Facility
LED based UV/VIS transmittance setup at Temple University
Refractive Index measurements
  Measure deflection of light passing through the corner of the aerogel

## Slide 4: QA Validation
Tile | Temple (TU) | Aerogel Factory (AF) | (TU-AF)/AF [%]
TSA120-1 | 1.0413 +/- 0.0011 | 1.0404 | 0.087
TSA120-2 | 1.0401 +/- 0.0025 | 1.0401 | 0.000
TSA114-3 | 1.0383 +/- 0.0026 | 1.0377 | 0.062
Tile |  |  | (TU-AF)/AF [%]
TSA120-1 | 1.0413 +/- 0.0011 | 1.0404 | 0.087
TSA120-2 | 1.0401 +/- 0.0025 | 1.0401 | 0.000
TSA114-3 | 1.0383 +/- 0.0026 | 1.0377 | 0.062
Temple measurements consistent with Aerogel Factory and BNL measurements
Index of refraction and transmittance measurements validated
Index of refraction measurement comparison (Temple/Aerogel Factory)
TSA120-2
TSA120-1
TSA114-3
Transmittance measurement comparison (Temple/BNL/Aerogel Factory)

## Slide 5: Aerogel QA Facility: Next Steps
Local refractive index measurements
  Measure change in light polarization to extract refractive index (via Brewster’s angle or ellipsometry)
  Equipment in hand as part of pfRICH PED
  Main effort to start in summer 2025
Laser
Linear Polarizers
Waveplate
Rotation Stage
Aerogel
Sensor

## Slide 6: Aerogel Inventory as of Jan. 24, 2025
Tiles from Aerogel Factory (Chiba University, Japan)
  Values in table provided by Aerogel Factory
Serial Number | n (405 nm) | Lateral Size [cm] | Thickness [cm]
TSA88-1 | 1.0390 | 11.11 | 2.05
TSA114-3 | 1.0377 | 10.99 | 2.51
TSA120-1 | 1.0404 | 10.94 | 2.45
TSA120-2 | 1.0401 | 11.04 | 2.48
Serial Number | n (405 nm) | Lateral Size [cm] | Thickness [cm]
TSA122-1a | 1.0215 | 10.71 | 2.03
TSA122-2a | 1.0215 | 10.72 | 2.01
TSA122-2b | 1.0215 | 10.71 | 1.99
TSA153-2 | 1.0215 | 10.75 | 2.00
TSA153-3 | 1.0223 | 10.68 | 1.99