## Slide 1: ePIC Backward EM calorimeter (EEEMCAL) status
10th EIC DAC Review
June 11th – 13th, 2025
Tanja Horn (CUA/JLab), DSL
Carlos Munoz-Camacho (IJCLab-Orsay), DSTC
for the EEEMCAL Consortium

## Slide 2: Charge Questions
10th EIC DAC Meeting
Tanja Horn

## Slide 3: EEEMCAL Major Components
10th EIC DAC Meeting, June 11th – 13th 2025
Tanja Horn
Radiator consisting of scintillating lead tungstate (PWO) crystals and a thin reflector wrapping. The physics requirements for electron identification and detection dictate the main requirements for the radiator.
Photosensors consisting of multi-pixel photon counters (MPPC) grouped into an array to maximize the surface coverage of the PWO blocks.
Mechanical structure, including installation fixtures and a cooling system providing thermal stabilization, which is important for crystal performance.
Signal Processing/DAQ providing the front-end electronics to transmit the signals to the data analysis modules.
Simulations/Software providing the software libraries and infrastructure foundation for extracting the physics from the detector.

## Slide 4: EEEMCAL Status Summary
10th EIC DAC Meeting, June 11th – 13th 2025
Tanja Horn
Status
  FDR PWO crystals – completed
  FDR MPPC – completed
  Detailed mechanical design – approaching 80%
  Front End Readout – at different stages
  Engineering article test runs – multiple prototype beam tests completed, engineering articles complete and last phase of beam tests ongoing
  CD3A QA on PWO crystals – first (140) articles passed QA
  Assembly and Installation planning - ongoing
Items for 2025
  EEEMCAL FDR – plan for this Fall after completion of further scheduled DESY and JLab beam tests
  Finalize mechanical design
    Finalize front-end electronics (FEE) and associated cooling design
    Final cooling implementation depends on final beam tests for FEE readout choice
  Continue CD3A (and in 2026+ also CD3B) QA on PWO crystals

## Slide 5
Parameter | Unit | EEEMCAL Required | Q&A Inform. Source
Light Yield (LY) at RT (for all sides polished crystals) | pe/MeV | ≥15 | Test with γ-source
LY(100ns)/LY(1μs) | % | >90 | Test with γ-source
Longitudinal Transmission at λ=360 nm at λ=420 nm at λ=620 nm | % % % | ≥35 ≥60 ≥70 | Optical Measurement
Transverse Transmission and LY uniformity along crystal | % | 10 | Optical Measurement
Inhomogeneity of Transverse Transmission Δλ at T=50% | nm | ≤5 | Optic. Measure.
Induced radiation absorption coefficient Δk at λ=420 nm and RT, for integral dose >100 Gy | m-1 | <1.5 | Irradiate with different sources
Mean value of dk | m-1 | ≤1.0 | Test
Tolerance in Length Tolerance in sides | μm μm | ≤±0,-100 ≤±50 | Measure.
Surface polished, roughness Ra | μm | ≤0.02 | Vendor
Tolerance in Rectangularity (90°) | degree | ≤0.1 | Measure.
Purity specific. (raw material) |  |  | Vendor
Mo contamination | ppm | <10 | Vendor
La, Y, Nb, Lu contamination | ppm | ? | Vendor
Smaller decay time – fast timing
  LY (100ns)/LY(1us) specification
Optimizing the light yield relies on crystal transmittance in the near UV region
  longitudinal transmittance specification
  Transmittance spectrum in agreement with photosensor curve
Require homogeneous collection of scintillation light along the crystal
  specification on transverse transmittance
Mechanical specifications important for assembly, e.g., to minimize gaps
Raw materials used impact crystal performance – QA with vendor
PbWO4 specifications are similar to those achieved for JLab Projects (NPS, FCAL)
PWO Specifications

## Slide 6
HyCal (pre-2014)
1152 PbWO4 crystals (PWO-I)
SICCAS/China
3x3 prototypes (2018/19)
9 PbWO4 (PWO-II) crystals
CRYTUR/Czech Rep.
12x12 prototypes (2019)
144 PbWO4 (PWO-II) crystals
CRYTUR/Czech Rep/
ComCal/FCAL
6
Crystal Beam Test Campaigns at JLab

## Slide 7: PWO Quality Assurance Protocol
10th EIC DAC Meeting, June 11th – 13th 2025
Tanja Horn
PWO crystals are CD3A item
First articles (140 crystals) passed QA
Additional 110 crystals arrived at JLab end of May 2025 awaiting QA
The QA builds on the process developed for NPS and consists of:
  2 step visual inspection
  mechanical dimension measurement
  light yield measurement
  Kinetics
  transmittance measurement
  induced radiation absorption coefficient.
Characterization results of CRYTUR produced crystals (2017 – present)
Chart: Crystal ID
 | 20.1
Period with focus on highest LY (PANDA, NPS)
Period with focus on new specifications (EIC, FCAL)
Chart: Crystal ID
Kinetics
EEEMCAL requirement
>90% of light in fast component
Light Yield (LY)
EEEMCAL requirement
Longitudinal Transmittance
Chart: Crystal ID
EEEMCAL requirement

## Slide 8: PWO Quality Assurance Documentation
10th EIC DAC Meeting, June 11th – 13th 2025
Tanja Horn
Crystal quality assurance results are documented in a central location with a master spreadsheet
Crystal characterization results
NPS Crystal+PMT+Cable module map
Crystal images are documented along with the numerical characteristic

## Slide 9: Mechanical Design Overview
10th EIC DAC Meeting, June 11th – 13th 2025
Tanja Horn
Physics Considerations
Distance interaction point/EEEMCal = 174 cm
Minimize the material & space between crystals
Be as close as possible to the beampipe
Optimize radiation lengths in front of the detector as possible, e.g., material budget is a consideration for the pfRICH (not shown)
Thermal Considerations
Good stability of the room temperature around 23°C
Temperature stability for crystals to within 0.1°C
About 1500 W to dissipate
Installation Considerations
Removing the detector in one block
Respect clearance between beam pipe and the DIRC

## Slide 10: Crystal Configuration
10th EIC DAC Meeting, June 11th – 13th 2025
Tanja Horn
Crystal configuration is defined
Main clearances are defined

## Slide 11: MPPC Configuration and Coupling to Crystal
10th EIC DAC Meeting, June 11th – 13th 2025
Tanja Horn
MPPC
  Active surface 3mm x 3mm
  External size: 4.35mm x 3.85mm
  Reference: S14160-3015PS
  16 MPPC per crystal  43840 MPPC
  Space between MPPC: 0.2mm
  Surface covered by MPPC: ~34%
Coupling to Crystal (Very Front End)
  4x4 MPPC coupled with optical grease
  1 PCB with the MPPC welded
  1 PCB with the output connecter plugged on the PCB MPPC
Choice of MPPC done

## Slide 12: Readout/DAQ Overview
10th EIC DAC Meeting, June 11th – 13th 2025
Tanja Horn
Work on FEE ongoing
Location of power depends on FEE

## Slide 13: DESY beam test (spring 2025)
10th EIC DAC Meeting, June 11th – 13th 2025
Tanja Horn
25 PWO crystals from CRYTUR
SiPM readout
Cooling and temp control
Two readout option tested:
Readout with H2GCROC3b chip
Preamp board & CAEN V1725S 14-bit 250MS/s digitizers
Successful readout of all 400 channels with both set of electronics
Significant noise (1/E) term in the energy resolution not yet understood:
  Likely PS instability due to large capacitance of sensors
  H2GCROC3b electronics suffered some additional issues (eg. poor grounding in some adaptor boards)
  Potential light leaks or beam energy spread (under investigation)
Upcoming 2nd campaign at DESY this Fall with improved setup
Discrete
electronics
1 – 5 GeV electron beam through a 2x2 mm2 collimator
Triggered by 2 scintillators
Typical DAQ rates: ~50-100 Hz

## Slide 14: Cooling Overview and Requirements
10th EIC DAC Meeting, June 11th – 13th 2025
Tanja Horn
Cooling environment is known
Crystal cooling
Electronics cooling

## Slide 15: Thermal Simulations
10th EIC DAC Meeting, June 11th – 13th 2025
Tanja Horn
Check impact of room temperature variation and insulation
External and internal cooling at the same temperature
Steady State
Compare two Steady States
Simple Model
Transient State
Thermal simulations with advanced design available

## Slide 16: Thermal Tests
10th EIC DAC Meeting, June 11th – 13th 2025
Tanja Horn
Room Temperature Tests
Tests with beam

## Slide 17: Mechanical Design – Internal Structure
10th EIC DAC Meeting, June 11th – 13th 2025
Tanja Horn

## Slide 18: Mechanical Design – External Structure
10th EIC DAC Meeting, June 11th – 13th 2025
Tanja Horn
Results of FEA are encouraging
Perform FEA simulation with advanced design
Choose means of production for structures (machining or foundry)

## Slide 19: Mechanical Design – Assembly
10th EIC DAC Meeting, June 11th – 13th 2025
Tanja Horn
Procedure ongoing
Depends on very front-end and FEB
Assembly test at IJCLab
Still deciding on the final assembly at JLab or BNL

## Slide 20: Mechanical Design – Installation
10th EIC DAC Meeting, June 11th – 13th 2025
Tanja Horn
Define positioning of the rails for insertion of detector
Study handling of the detector
Services depend on FEB and cooling
Backward ECAL fixed with rails to the GST (global support tube) in carbon fiber and showing the external cooling structure planned with FSW technology

## Slide 21: Software/Simulation Development
10th EIC DAC Meeting, June 11th – 13th 2025
Tanja Horn
Software builds on experience from JLab projects (e.g., HYCAL, FCAL, NPS, etc.)
Anticipated to follow a similar workflow
EEEMCAL performance
Sample pulse amplitude
Slow controls: HV monitoring
Online diagnostic plots
EEEMCAL in ePIC simulation framework

## Slide 22: Organization and Development Overview
10th EIC DAC Meeting, June 11th – 13th 2025
Tanja Horn
Item | Institutions
Crystals | CUA, UKY, JMU, MIT
MPPC | ACU, OU, Lehigh, FIU
Mechanical | IJCLab-Orsay
Signal Processing | IJCLab-Orsay, OU, ACU
Simulations and Software | AANL, UKY, AU, W&M

## Slide 23: Summary
10th EIC DAC Meeting, June 11th – 13th 2025
Tanja Horn
Design of EEEMCAL is nearing 90% completion.
Crystal first (140) articles have passed QA
Remaining technical work in FEE is progressing well and expected to reach 90% mark soon
Thermal simulations complete
Multiple prototype beam tests completed, engineering articles complete and last phase of beam tests ongoing
Last aspects of integration (FEE and associated cooling) need to be finalized after test beam completed
Still deciding on final assembly at JLab or BNL
EEEMCAL is on track to be technically ready for baselining at the end of the year

## Slide 24
10th EIC DAC Meeting, June 11th – 13th 2025

## Slide 25
In general, for high-precision electromagnetic calorimetry, the following are of relevance:
  Smaller radiation length for smaller longitudinal size
  Smaller Moliere radius allowing higher granularity
  Smaller decay time
  Better energy resolution. Larger number of photoelectrons per MeV to reach higher resolution
  Smaller constant term contribution to energy resolution, mainly due to non-uniformity and gaps, to readout and noise.  for sensitivity checks need tests with detector prototypes in beam
  Reasonable temperature dependence to light yield
  Higher radiation hardness (EM and/or hadron fluences)
PbWO4 meets the requirements of an extremely fast, compact, and radiation hard scintillator material providing sufficient luminescence yield to achieve good energy resolution.
Context for PbWO4 Specifications

## Slide 26
Crystal light yield and timing
Optical Transmittance (L/T)
Cs-137 source and calibrated 2-inch PMT (Hamamatsu R2059-01) with QE(420nm)=24%.
Radiation Hardness and recovery
Co-60 sources
Modified Varian Cary 5000 spectrometer
Perkin-Elmer Lambda 950 spectrometer
PbF2
Na-22 source and 2-inch PMT (XP2262)
x-ray irradiation system (Faxitron CP-160)
Varian Cary 5000 spectrometer
Cs-137 source and 2-inch PMT
Co-60 source, 222 TBq, simultaneous irradiation of nine crystals/water; different dose rates possible
Electrons 5.5 MeV < Ee < 16.6 MeV; adjust beam intensity to illumination with g rays (Co-60, 30 Gy)
QA facilities at Universities
26

## Slide 27
JLab crystal test facility for PbWO4 QA and prototype
Dedicated cleanroom facility for crystal characterization
  Mitutoyo QM - for mechanical dimensions measurements. Precise to 1 micron.
  Crystal Light Yield measurements
  Optical transmittance with integrating sphere
  Radiation hardness in beam
Beam test facility with tagged photon beam up to 4-5 GeV
  Technique demonstrated successfully for NPS can be adapted for EIC prototype tests
27

## Slide 28
Length uniformity of CRYTUR crystals (2017 – present)
Chart: Crystal ID
~2190 PWO crystals delivered continuously for projects at JLab since 2017
Crystals used for both NPS and FCAL-2
All 1100 NPS crystals for NPS passed the NPS quality assurance tests (similar for FCAL-2)
PbWO4 crystal production for JLab Projects
Average: 199.95 mm +0/-0.02 mm
Consistent with EEEMCAL tolerance
EIC crystals are rectangular like NPS crystals with similar tolerances
CRYTUR is a well established and tested vendor that can deliver crystals of the quality needed for EIC