## Slide 1: Air Flow Vibration Studies

## Slide 2: Setup
Use quarter stave prototypes
  For now use one flow channel (one half) of the quarter stave
  Quarter stave prototype 2 (QSP2)
    Prototype which erroneously has only one layer of CF prepreg in each skin (no transverse layer)
    To stabilize this was put into heat shrink, which makes a close air channel
  Quarter stave prototype 3 (QSP3)
    Using thin steel shim stock to replace modules, first again with shrink wrap, then glued
    Found that facesheet was damaged next to C-channel
  For now mostly proof of principle
Sensors & readout
  Flow meter (up to 100 l/min) + needle valve to adjust flow, flow measurement in DAQ
  2 capacitive displacement sensors, in DAQ
  Pressure sensor (up to 0.350 bard) – standalone, no connection to DAQ
Fixed edge
Displacement sensors

## Slide 3: Setup

## Slide 4: QSP3
Steel shim taped on, and heat shrink wrapped
Steel shim glues to stave structure with Araldite Rapid

## Slide 5: What do we need?
Target flow rates
  Still defined by coolant ΔT = 10˚C and sensor /chip power numbers from Iain @ Frascati
  for max power scenario & L4 (2×8 5-RSU LAS + AncAsic + FPC ohmic loss): Pstave = 48.2 W or 223 l/min (about 15.5 m/s)
  Nominal: Pstave = 31.4 W or 145 l/min (about 10.1 m/s)
  Per channel (one half of the stave): Max flow about 112 l/min, nominal flow about 73 l/min
RMS displacement not really known
  Needs to come from alignment and tracking studies
  Different for different directions
    Probably more demanding in-plane vs out-of-plane
    Here only measure out-of-plane displacements at worst point

## Slide 6: Single shot QSP2
fs = 5 kHz, fl = 92.9 l/min, T = 10 s
dRMS1 = 7.9 µm, dRMS1 = 8.2 µm
, for longitudinal (beam) modes
, for transverse (torsional) modes
First longitudinal mode is consistent with frequency scan on shaker table for QSP3

## Slide 7: Single shot QSP3
fs = 5 kHz, fl = 68.1 l/min, T = 10 s
dRMS1 = 4.2 µm, dRMS1 = 4.2 µm
, for longitudinal (beam) modes
, for transverse (torsional) modes
First longitudinal mode is consistent with frequency scan on shaker table for QSP3

## Slide 8: Varying flow rate QSP2
fs = 5 kHz, T = 10 s, 2000 points

## Slide 9: Varying flow rate QSP2
fs = 5 kHz, T = 10 s, 2000 points

## Slide 10: Pressure drop vs flow
Scale by 4 for full stave: nominal 0.668 bar, max 1.568 bar
Chart: flow [l/min]
| 61 | 53 | 37 | 26 | 19 | 7 | 0 | 14 | 33 | 43 | 46 | 50 | 58 | 69 | 65 | 75 | 79 | 84 | 88 | 92 | 95 | 98
QSP2 | 0.15 | 0.122 | 0.065 | 0.037 | 0.022 | 0.004 | 0 | 0.013 | 0.059 | 0.092 | 0.099 | 0.112 | 0.143 | 0.186 | 0.163 | 0.202 | 0.219 | 0.227 | 0.242 | 0.266 | 0.282 | 0.297
QSP3 | 0.065 | 0.069 | 0.095 | 0.139 | 0.146 | 0.18 | 0.045 | 0.04 | 0.025 | 0.015 | 0 | 0.082 | 0.171 | 0.252 | 0.337
Nominal
Max

## Slide 11: Conclusions and next steps
Qualitative conclusions
  The pressure drops are much more than we expected
  Containing this pressure will be challenging
  Staves are vibrating, but not shaking violently
  We can do the mechanical measurements that we planned to do
Quantitative conclusions
  None of the results shown here do have a final relevance, as the prototypes used show signs of structural damage
Next steps
  Will need to make more prototypes
  We have made a first set of simple Cu-on-Kapton heaters (incl. heat for AncASIC), use thermal camera to survey temperatures
  Also have in-flow temperature sensors
    Still need to be included into DAQ
  Mould parts for full length stave prototype are in preparation