## Slide 1: Qualifying Graphite for Reactor Applications: A Materials Perspective
8th July 2025
Presented by: Dominic Piedmont

## Slide 2: Motivation: Material Code Qualification
ASME standard required of all reactor grade materials prior commercial implementation that requires characterization of properties:
    Physical
    Mechanical
    Thermal
    Impact of relevant reactor conditions/environmental factors (oxidation, irradiation, etc.)
Last material that achieved this was Alloy 617 in 2019 (first in 30 years).
    Currently no reactor graphite grades are qualified

## Slide 3
Code Qualification
Material System Determination
Property Modeling
Material Design
Fabrication Methodology
Pristine Property Verification
Down-selection
Irradiation/Environmental Effects
Qualification Package Preparation
You are here!

## Slide 4: Climbing Tips
Consistent usage of terminology
Use the right tool for the job
Down-select as soon as possible
Eyes on the prize

## Slide 5: Experimental Model Validation

## Slide 6: Experimental Characterization and Synchrotron
Structure-property correlation
Understand the compound nature of microstructure/properties
Imperative that modeling length scale corresponds to length scale of experimental measurement
Multimodal characterization via synchrotron techniques
Mejía-Rosales, Sergio, et al. “Experimental techniques for structural characterization.” Nanoalloys, 2013, pp. 113–145, https://doi.org/10.1016/b978-0-12-394401-6.00004-7.

## Slide 7: Nanoscale Measurements: X-Ray Absorption
Resolution as low as 0.002 nm
Element-specific local structure
Coordination number
Interatomic spacing
Short range order
Model validation
Joress, Howie, et al. “Why is exafs for complex concentrated alloys so hard? challenges and opportunities for measuring ordering with X-ray absorption spectroscopy.” Matter, vol. 6, no. 11, Nov. 2023, pp. 3763–3781, https://doi.org/10.1016/j.matt.2023.09.010.

## Slide 8: E.g. X-Ray Absorption Measurements
8
Coexistence of 4- and 5-coordinate structures for Ni(II) in ZnCl2
Ab-initio MD simulations
Clear changes in electronic structure are observed as function of T in Ni (II)
X-Ray Absorption Studies
Strong dynamic heterogeneity in the coordination environments of Ni(II) may explain the lower solubility of Ni in molten ZnCl2
Simerjeet K Gill*, Frenkel A.I.* et.al. Connections between the Speciation and Solubility of Ni(II) and Co(II) in Molten ZnCl2.The Journal of Physical Chemistry B 2020, 124 (7), 1253-1258

## Slide 9: Microscale Measurements: X-Ray Tomography
Our NSUF beamline has resolution down to 5 µm
Various mechanisms for contrast
  Absorption, diffraction, fluorescence, etc.
Direct visualization of 3D morphology, structure, and density
Diffracting domain orientation mapping
Enables studies of chemical and structural changes in materials down to 5-micron resolution addressing:
Early stages of fuel life cycle
Stability of cladding and reactor containment
Stability of waste forms
Grain Orientation Mapping
[1]A. Bonnin, et al. Appl. Phys. Lett. 105, 084103 (2014)
[2]H. Palancher et al. J. Appl.d Cryst. 44, 1111 (2011).
Work on pre-irradiated UMo fuel pellets in France

## Slide 10: Structure Property Correlation
In-situ capabilities allow for bulk/environmental changes to occur while microscale properties are measured
  High temperature (> 1000 °C)
  Vapor pressure
  Electrochemical
  Loading
Data is at length scales appropriate for engineering scale model initialization and verification

## Slide 11: Structure Property Correlation Modeling

## Slide 12: Conclusion
Reaching the summit requires: clear communication, using the right tool for the job, and focused attention
Models must be experimentally validated and are only as good as the real-world data they represent
Synchrotron offers a methodology of initializing and/or validating computational models across a range of length-scales and modalities

## Slide 13: Questions?
dpiedmont@bnl.gov
Materials for Energy Applications Group