## Slide 1: Overview of Historical and New Transmission Measurements of Nuclear Graphite
Chris W. Chapman, Kemal Ramić, Iyad Al-Qasir
Oak Ridge National Laboratory
ReGra – 9 July 2025

## Slide 2: Where we are
Is this right? Is this the most accurate way to account for pores in graphite?

## Slide 3: The SANS of it all
How do pores contribute to total cross section?
Small Angle Neutron Scattering (SANS)
  Known about in graphite since at least Egelstaff (1957)
  History of potential confusion behind underlying cause e.g. Bowman (2008)
  Current consensus is that SANS manifests from porosity (e.g. Petriw (2010), Gould (2010))

## Slide 4: The SANS of it all
SANS is an effect based on the material characteristics (i.e., pores)
Previous attempts have been made to correct for SANS in total cross section measurements
If SANS is present, one of two things needs to be done in order to make a faithful comparison between processed & experimental data:
  Experimental corrections
  SANS adjustment to processed data

## Slide 5: The SANS of it all
SANS adjustments to processed data can be done IF material characteristics are well known
Needs to be done CAREFULLY

## Slide 6: The SANS of it all
Minor changes in graphite sample can lead to significantly different SANS contributions
Must be handled with EXTREME care

## Slide 7: What I Searched For – EXFOR

## Slide 8: What I Searched For – non-EXFOR
Internal
  Ramić (ISIS, 2024, preliminary)
Dissertations
  Shamasundar (Georgia Tech, 1974)
  Zhou (NC State, 2006)
Other
  Kimura (J-PARC, WONDER-2023, preliminary & digitized)
  Petriw (2010, digitized)

## Slide 9: Organization of Measurements
Measurements can be broken up into 3 categories:
  Not applicable (wrong material, too high in energy, etc.)
  SANS included
    Previously shown on slide 6
  SANS removed
    This is what we’ll show

## Slide 10: Data to Discuss
Of the 51 datasets, 5 of them contain data either without SANS or SANS-corrected below the first Bragg edge
  Palevsky (1955)
  Egelstaff (1957)
  Shamasundar (1974)
  Steyerl (1974)
  Zhou (2006)

## Slide 11: Data without SANS – Palevsky (1955)
No information provided about the sample, experimental procedure, experimental corrections (if any)
  Possible that experimental apparatus described in other publication?
This information is necessary for accurate ENDF-to-experiment comparison

## Slide 12: Data without SANS – Egelstaff (1957)
Details measurement in journal paper
Made corrections to their data to adjust for SANS
Mentions that the SANS contribution at 500 m/s [1.3 meV] is ~4 b

## Slide 13: Data without SANS – Shamasundar (1974)
Reactor-grade graphite
Details measurement in dissertation
Made corrections to their data to adjust for SANS
Acknowledges disagreement with BNL-325, but does not know why

## Slide 14: Data without SANS – Steyerl (1974)
Pyrolytic graphite (i.e., crystalline)
Agrees perfectly with Sd data
This is expected, as pyrolytic graphite contains no (or very few) pores.

## Slide 15: Data without SANS – Zhou (2006)
Two samples measured:
  Pyrolytic
  Reactor
Pyrolytic graphite measurement agrees perfectly with Sd data
Reactor graphite measurement agrees with somewhere between 20%-30%
  Made corrections to their data to adjust for SANS

## Slide 16: Conclusions
Many total cross sections are available for graphite
SANS is a material effect which manifests from porosity in materials
Careful considerations required when comparing processed ENDF files against experimental data
Pyrolytic graphite best sample for comparing with inelastic scattering cross section data (due to lack of SANS)
When SANS is not present (i.e., pyrolytic graphite), Sd shows best agreement with total cross section measurements

## Slide 17: Questions?

## Slide 18: Extra Slides
Lots of plots of total cross section measurements

## Slide 19: Cross Section Plot – Hanstein (1941)
Hanstein (1941)

## Slide 20: Cross Section Plot – Anderson (1946)
Anderson (1946)

## Slide 21: Cross Section Plot – Fermi (1947)
Fermi (1947)

## Slide 22: Cross Section Plot – Jones_1 (1948)
Jones_1 (1948)

## Slide 23: Cross Section Plot – Jones_2 (1948)
Jones_2 (1948)

## Slide 24: Cross Section Plot – Egelstaff (1952)
Egelstaff (1952)

## Slide 25: Cross Section Plot – Havens (1952)
Havens (1952)

## Slide 26: Cross Section Plot – Palevsky – 300K (1955)
Palevsky (1955)

## Slide 27: Cross Section Plot – Palevsky – 500K (1955)
Palevsky (1955)

## Slide 28: Cross Section Plot – Palevsky – 700K (1955)
Palevsky (1955)

## Slide 29: Cross Section Plot – Palevsky – 1000K (1955)
Palevsky (1955)

## Slide 30: Cross Section Plot – Sailor (1955)
Sailor (1955)

## Slide 31: Cross Section Plot – Egelstaff_1 (1957) – C12
Egelstaff_1 (1957) – C12

## Slide 32: Cross Section Plot – Egelstaff_1 (1957) – C-nat
Egelstaff_1 (1957) – C-nat

## Slide 33: Cross Section Plot – Egelstaff_2 (1957) – C12
Egelstaff_2 (1957) – C12

## Slide 34: Cross Section Plot – Egelstaff_2 (1957) – C-nat
Egelstaff_2 (1957) – C-nat

## Slide 35: Cross Section Plot – Walton (1960)
Walton (1960)

## Slide 36: Cross Section Plot – Simpson (1964)
Simpson (1964)

## Slide 37: Cross Section Plot – Neill (1965)
Neill (1965)

## Slide 38: Cross Section Plot – Rayburn_1 (1965)
Rayburn_1 (1965)

## Slide 39: Cross Section Plot – Rayburn_2 (1965)
Rayburn_2 (1965)

## Slide 40: Cross Section Plot – Iizumi (1968)
Iizumi (1968)

## Slide 41: Cross Section Plot – Harvey (1974)
Harvey (1974)

## Slide 42: Cross Section Plot – Shamasundar (1974)
Shamasundar (1974)

## Slide 43: Cross Section Plot – Steyerl_1 (1974)
Steyerl_1 (1974)

## Slide 44: Cross Section Plot – Steyerl_2 (1974)
Steyerl_2 (1974)

## Slide 45: Cross Section Plot – Harvey_1 (1977)
Harvey_1 (1977)

## Slide 46: Cross Section Plot – Harvey_2 (1977)
Harvey_2 (1977)

## Slide 47: Cross Section Plot – Harvey (1982)
Harvey (1982)

## Slide 48: Cross Section Plot – Alexandrov (1997)
Alexandrov (1997)

## Slide 49: Cross Section Plot – Zhou (2006)
Zhou (2006)

## Slide 50: Cross Section Plot – Arzumanov (2008)
Arzumanov (2008)

## Slide 51: Cross Section Plot – Bowman_1 (2008)
Bowman_1 (2008)

## Slide 52: Cross Section Plot – Bowman_2 (2008)
Bowman_2 (2008)

## Slide 53: Cross Section Plot – Petriw – Iso Pressed (2010)
Petriw – Iso Pressed (2010)

## Slide 54: Cross Section Plot – Petriw – Needle Coke (2010)
Petriw – Needle Coke (2010)

## Slide 55: Cross Section Plot – Petriw – Pitch Coke (2010)
Petriw – Pitch Coke (2010)

## Slide 56: Cross Section Plot – Liu (2019)
Liu (2019)

## Slide 57: Cross Section Plot – Teshigawara (2019)
Teshigawara (2019)
  Nano-diamonds, not graphite

## Slide 58: Cross Section Plot – Robledo_1 (2020)
Robledo_1 (2020)

## Slide 59: Cross Section Plot – Robledo_2 (2020)
Robledo_2 (2020)

## Slide 60: Cross Section Plot – Robledo_3 (2020)
Robledo_3 (2020)

## Slide 61: Cross Section Plot – Robledo_4 (2020)
Robledo_4 (2020)

## Slide 62: Cross Section Plot – Robledo_5 (2020)
Robledo_5 (2020)

## Slide 63: Cross Section Plot – Kimura – ED-4 (2023)
Kimura – ED-4 (2023)

## Slide 64: Cross Section Plot – Kimura – ET-11 (2023)
Kimura – ET-11 (2023)

## Slide 65: Cross Section Plot – Kimura – ET-34 (2023)
Kimura – ET-34 (2023)

## Slide 66: Cross Section Plot – Kimura – T-8 (2023)
Kimura – T-8 (2023)

## Slide 67: Cross Section Plot – Ramić – IG-110 1023K (2024)
Ramić – IG-100 – 1023K (2024)

## Slide 68: Cross Section Plot – Ramić – NBG-18 (2024)
Ramić – NBG-18 (2024)

## Slide 69: Cross Section Plot – Ramić – PCEA (2024)
Ramić – PCEA (2024)