## Slide 1: BIC SECTOR DEVELOPMENT Update
JUNE 26 2025
Kevin G. Bailey & Tom O’Connor

## Slide 2: This Week
First 18 layer test article back from the shops (Thank you Frank!)

## Slide 3: How’d we do…

## Slide 4: Ok, for a first try of more than 3 layers
Front lit only

## Slide 5: Missed a few
Back lit only.
The two dark rows are blocked on the other end by epoxy in the lead grooves. This should be solved now.

## Slide 6: Extrusions measured

## Slide 7: second layup on the press
Expect to have this one ready for machining by 7/4/25
Frank plans to machine it starting 7/7/25

## Slide 8: Better but not perfect

## Slide 9: New Lead

## Slide 10: Lead/Swaging Update
June 27, 2025

## Slide 11: Vulcan Prototype Lead
Lead is damaged. Some rolls are crushed and nearly all of them have some damage to the edges
Lead is dirty but we didn’t ask for degreasing or any sort of cleaning.
All lead is too thick. Specification is 0.50mm and actual is 0.59mm.
RMA in process
Alternate suppliers may be an option

## Slide 12
Last Swager Adjustment 5/13/25

## Slide 13: GLueX lead
13 rolls 10cm wide
7 rolls 11cm wide
Use 11cm roll for 2nd prototype SFIL

## Slide 14: 2nd Prototype SFIL

## Slide 15: Purdue cfrp
These two have the most voids

## Slide 16: Cfrp #2
Best pair

## Slide 17: Cfrp #3
Also some significant voids

## Slide 18
Testing Lead Fiber interface ??

## Slide 19
Tssting Lead CFRP interface ??

## Slide 20: Other
Tables arrived in 369
Pallet jack arrived in 369
works…used to move tables!
Cart arrived in 369
More tools soon.