## Slide 1: BIC Update
Kevin Bailey & Tom O’Connor
Triple I Engineering Meeting Update
July 21, 2025

## Slide 2: 2nd SFIL
Using GlueX lead 11cm wide
Using dummy fiber
No glue is fiber grooves

## Slide 3: 2nd SFIL
View of each end
18 Lead/17 Fiber = Imaging Layer
More consistent fiber layout than
1st SFIL
Day 2
Day 1

## Slide 4: 2nd SFIL Flatness/Thickness
Thickness at 1cm increments along three lines

## Slide 5: 2nd SFIL Flatness/Thickness
Chart: Position (cm)
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35 | 36 | 37 | 38 | 39 | 40 | 41 | 42 | 43 | 44 | 45 | 46 | 47 | 48 | 49 | 50
SFIL #2 Front | 4.6279 | 4.6253 | 4.6228 | 4.6203 | 4.6152 | 4.6101 | 4.6076 | 4.605 | 4.5999 | 4.5949 | 4.5898 | 4.5847 | 4.5822 | 4.5745 | 4.5695 | 4.5618 | 4.5542 | 4.5491 | 4.5415 | 4.5339 | 4.5288 | 4.5212 | 4.5161 | 4.5085 | 4.506 | 4.5009 | 4.4958 | 4.4933 | 4.4882 | 4.4856 | 4.4831 | 4.4806 | 4.478 | 4.4755 | 4.4729 | 4.4704 | 4.4679 | 4.4653 | 4.4653 | 4.4628 | 4.4602 | 4.4577 | 4.4552 | 4.4552 | 4.4526 | 4.4526 | 4.4501 | 4.4475 | 4.4475 | 4.445
SFIL #2 Center | 4.6507 | 4.6457 | 4.6431 | 4.6406 | 4.638 | 4.633 | 4.6304 | 4.6253 | 4.6228 | 4.6177 | 4.6152 | 4.6101 | 4.605 | 4.5999 | 4.5923 | 4.5872 | 4.5822 | 4.5745 | 4.5669 | 4.5618 | 4.5568 | 4.5491 | 4.5441 | 4.539 | 4.5339 | 4.5288 | 4.5263 | 4.5212 | 4.5187 | 4.5161 | 4.5136 | 4.511 | 4.5085 | 4.506 | 4.5034 | 4.5009 | 4.5009 | 4.4983 | 4.4983 | 4.4958 | 4.4958 | 4.4933 | 4.4933 | 4.4907 | 4.4907 | 4.4907 | 4.4882 | 4.4882 | 4.4856 | 4.4856
SFIL #2 Rear | 4.6812 | 4.6787 | 4.6736 | 4.6711 | 4.6685 | 4.666 | 4.6634 | 4.6584 | 4.6558 | 4.6533 | 4.6482 | 4.6457 | 4.6406 | 4.6406 | 4.6304 | 4.6228 | 4.6152 | 4.6101 | 4.6025 | 4.5974 | 4.5923 | 4.5872 | 4.5822 | 4.5771 | 4.5745 | 4.5695 | 4.5644 | 4.5618 | 4.5568 | 4.5542 | 4.5517 | 4.5491 | 4.5466 | 4.5441 | 4.5415 | 4.539 | 4.539 | 4.5364 | 4.5364 | 4.5339 | 4.5339 | 4.5314 | 4.5314 | 4.5288 | 4.5288 | 4.5263 | 4.5237 | 4.5212 | 4.5187
SFIL#1 Front | 4.6939 | 4.6939 | 4.6914 | 4.6888 | 4.6863 | 4.6838 | 4.6787 | 4.6761 | 4.6736 | 4.6711 | 4.666 | 4.6634 | 4.6609 | 4.6584 | 4.6533 | 4.6507 | 4.6482 | 4.6457 | 4.6431 | 4.6431 | 4.6406 | 4.6406 | 4.6406 | 4.6406 | 4.6406 | 4.6431 | 4.6431 | 4.6431 | 4.6457 | 4.6457 | 4.6457 | 4.6482 | 4.6482 | 4.6482 | 4.6482 | 4.6482 | 4.6482 | 4.6482 | 4.6507 | 4.6507 | 4.6507 | 4.6482 | 4.6482 | 4.6482 | 4.6457 | 4.6431
SFIL #1 Center | 4.7168 | 4.7168 | 4.7142 | 4.7117 | 4.7066 | 4.7041 | 4.7015 | 4.699 | 4.6939 | 4.6914 | 4.6888 | 4.6863 | 4.6812 | 4.6787 | 4.6761 | 4.6736 | 4.6711 | 4.6685 | 4.666 | 4.666 | 4.6634 | 4.6634 | 4.6634 | 4.6634 | 4.6634 | 4.666 | 4.666 | 4.6685 | 4.6685 | 4.6685 | 4.6685 | 4.6711 | 4.6711 | 4.6711 | 4.6711 | 4.6736 | 4.6736 | 4.6736 | 4.6736 | 4.6736 | 4.6736 | 4.6711 | 4.6711 | 4.6685 | 4.6685 | 4.6685
SFIL #1 Rear | 4.7396 | 4.7396 | 4.7371 | 4.7346 | 4.732 | 4.7269 | 4.7244 | 4.7168 | 4.7142 | 4.7117 | 4.7066 | 4.7041 | 4.699 | 4.6965 | 4.6914 | 4.6914 | 4.6863 | 4.6863 | 4.6838 | 4.6838 | 4.6838 | 4.6838 | 4.6838 | 4.6863 | 4.6888 | 4.6939 | 4.6914 | 4.6939 | 4.6965 | 4.6965 | 4.6965 | 4.6965 | 4.6965 | 4.6965 | 4.6965 | 4.6965 | 4.6965 | 4.6965 | 4.6965 | 4.6939 | 4.6939 | 4.6939 | 4.6888 | 4.6888 | 4.6863 | 4.6838
SFIL #2 F-corrected | 4.6279 | 4.6293 | 4.6308 | 4.6323 | 4.6312 | 4.6301 | 4.6316 | 4.633 | 4.6319 | 4.6309 | 4.6298 | 4.6287 | 4.6302 | 4.6265 | 4.6255 | 4.6218 | 4.6182 | 4.6171 | 4.6135 | 4.6099 | 4.6088 | 4.6052 | 4.6041 | 4.6005 | 4.602 | 4.6009 | 4.5998 | 4.6013 | 4.6002 | 4.6016 | 4.6031 | 4.6046 | 4.606 | 4.6075 | 4.6089 | 4.6104 | 4.6119 | 4.6133 | 4.6173 | 4.6188 | 4.6202 | 4.6217 | 4.6232 | 4.6272 | 4.6286 | 4.6326 | 4.6341 | 4.6355 | 4.6395 | 4.641

## Slide 6: Swaged Lead Measurements on Comparator
Horizontal Spacing 1.35mm
Overall Thickness 1mm
Vertical Spacing ~ 1.1mm (hard to focus)
Re-measure using tip/tilt platform

## Slide 7: Carbon Fiber Testing
Material is at Argonne
Two configurations for destructive testing
Fabricate test strips this week

## Slide 8: Drawer Design
Weekly Meetings with Purdue with Pau and Andy
Original plan was for 4-piece design
Single piece design now under consideration