## Slide 1: Evaluations of 155,157Gd, 95Mo, 92,94Zr
Luiz Leal1, Travis Greene1, Goran Arbanas1, Devin Barry2, and Timothy Trumbull2
  2024 CSEWG, NDAG Meeting
  Long Island, NY
  November 4−8, 2024
  1Oak Ridge National Laboratory, Oak Ridge, TN, 37831
  2Naval Nuclear Laboratory, P.O. Box 1072, Schenectady, NY 12301

## Slide 2
Evaluation of 155Gd and 157Gd Resonance
Motivation:
  Issues with benchmark calculations with Gd concentration
  Extension of the resonance region from 300 eV to 500 eV
  SAMMY R-matrix analysis;
  Transmission, capture data from RPI and n_TOF
  Improved benchmark integral representation
  Uncertainty information and resonance parameter
  Covariance generation

## Slide 3
Gadolinium Evaluation
RPI experimental data measured at the 25.59725 m flight-path
Data | Energy range (eV) | Nature
Transmission | 0.2−300.0 | Natural
Transmission | 0.3−500.0 | Natural
Transmission | 0.3−1,000.0 | Natural
Capture | 0.2−1,000.0 | 91.74% 155Gd enriched
Capture | 0.2−1,000.0 | 90.96% 157Gd enriched
Capture | 0.2−1,000.0 | Natural

## Slide 4
Gd RPI data (SAMMY Fitting): Resonance Range Extended to 500 eV for 155,1557Gd

## Slide 5
Gadolinium Evaluation (new n_TOF capture measurements)
n-TOF experimental data measured at the 183.90 m flight-path
Data | Energy range (eV) | Nature
Capture | 1.0−1,000.0 | 91.74% 155Gd enriched
Capture | 1.0−1,000.0 | 88.32% 157Gd enriched

## Slide 6
General Information
Atlas of Neutron Resonances (ANR) |  |  | 
 | Thermal cross section (b) | Capture resonance integral (b) | Westcott’s factor
155Gd | 60,900 ± 500 | 1,537 ± 100 | 0.83899
157Gd | 254,000 ± 815 | 754 ± 20 | 0.84715

## Slide 7: Benchmark Results: Issues
Zero-Energy Deuterium (ZED-II) Research Reactor
Issues with benchmark calculations with Gd concentration
Luiz Leal / IRSN – JEFF meeting - November 2017

## Slide 8: Issue:
Luiz Leal / IRSN – JEFF meeting - November 2017

## Slide 9: Keff Sensitivity to the Capture Cross Section
Luiz Leal / IRSN – JEFF meeting - November 2017

## Slide 10: SAMINT Methodology for Differential and Integral Data Treatment
SAMINT flowchart
CE TSUNAMI
MCNP-6
SAMINT
SAMMY
dk/dσ(E)
dσ(E)/dP
dk/dP
Updated
P and δP
ENDF
SAMMY
P = resonance parameters (e.g., Eλ, Γγ , Γn , Γf )
Differential data
Integral
data

## Slide 11: Resolution: Use of SAMMY and SAMINT
Luiz Leal / IRSN – JEFF meeting - November 2017

## Slide 12: 157Gd Results
Evaluation | Thermal cross section (b) | Capture resonance integral (b) | Westcott’s factor
ENDF/B-VIII.0 | 252,892.2 | 759.26 | 0.85305
RPI | 225,629.8 | 778.32 | 0.76287
ORNL | 244,071.5 | 806.62 | 0.82467
ANR | 254,000 ± 815 | 754 ± 20 | 0.84715
Luiz Leal / IRSN – JEFF meeting - November 2017

## Slide 13
95Mo Resonance Evaluation
ORELA experimental data
Data | Energy range (eV) | Nature
Transmission | 0.01−5,000.0 | 96.47% 95Mo enriched n = 0.025067 at/b L = 79.83 m
Capture | 0.01−5,000.0 | 96.47% 95Mo enriched n = 0.004591 at/b L = 38.42 m
(n, α) | 0.01−5,000.0 | 96.47% 95Mo enriched n = 0.0000317 at/b L = 8.84 m

## Slide 14
95Mo Resonance Evaluation Using SAMMY
Features:
Extension of the resonance energy range from 2,141.2 eV to 5,000 eV LRF = 7 format used (RML)
(n, α) explicitly represented via resonance parameters: ground-state and first excited–state—with energy Q-values of 6,393.55 keV and 5,458.50 keV
Resonance parameters covariance using the compact format, LCOMP = 2

## Slide 15
ORELA total and (n, α) cross-section data from thermal up to 5,000 eV

## Slide 16
Total (n, α) cross section, ground state, and first excited state

## Slide 17
 | Koehler | ORNL | ANR
Capture cross section | 13.4 ± 0.3 | 13.34 ± 0.04 | 13.4 ± 0.3
Resonance integral | 114.21 | 104.15 ± 0.33 | 118 ± 7
Capture cross section at thermal (0.0253 eV) and resonance integral

## Slide 18
Covariance

## Slide 19
LCT-106-006 and LCT-111-003: benchmark experiment dedicated to molybdenum
Benchmark Results

## Slide 20: Zirconium Evaluation at ORNL
92Zr
a) One transmission from ORELA:
b) TOF 78.2 m and thickness of 0.00455 at/b
c) 16O seems to be present in the sample!

## Slide 21: Zirconium Evaluation at ORNL
92Zr
Fit of the ORELA transmission data corrected for the normalization and background and for 16O:

## Slide 22: Zirconium Evaluation at ORNL
94Zr
a) Two transmissions from ORELA
b) TOF 78.2 m and thicknesses of 0.00565 at/b and 0.02025 at/b

## Slide 23: Zirconium Evaluation at ORNL
Some observations:
a) Whether extension of resolved resonance energy region should be examined.
b) Capture data should be included in the fitting as they become available.
c) Coherent and incoherent scattering should be included in the resonance fitting.

## Slide 24: Concluding Remarks
Lack of experimental data may hinder the task for Zr and other isotopes.
Hopefully complete the evaluation for other Mo isotopes.
The Gd evaluation will be completed using ENDF/B-VIII.1 information.
Evaluations are processed via the nuclear data processing codes.
Evaluations are tested using benchmark calculations.
Evaluations will include covariances.