## Slide 1: BIC SECTOR DEVELOPMENT Update
September 12, 2025
Kevin G. Bailey & Tom O’Connor

## Slide 2: Test SFIL #3 w/ GlueX fiber
Slice for comparator created
Small section for density created
  Density 4.76g/cc (314g, 66cc
Profile slope L-R

## Slide 3: comparing ends
Right Side = Start
Left Side = 2mm Higher

## Slide 4: Destructive Test@ CMSC
Two cases
Testing started 9/5/2025
Awaiting results
Mode 1
Interlaminar Fracture Toughness DCB
(Double Cantilevered Beam)
- normal to plane of crack

## Slide 5: Destructive tests
Mode 2
Interlaminar Fracture Toughness ENF
(End Notched Flexure)
- Parallel to crack plane – shear

## Slide 6: Degreased only samples to be tested

## Slide 7: DRAWER MOLD ARRIVES FIRST LAYUPS JUST FINISHED
ONE PIECE TRIAL
PROVES STUBORN TO REMOVE
SIDE C SHAPED FOR FOUR PIECE DRAWER

## Slide 8: Mazzella quote
Lifting beam design quote
- designed as our needs
- engineered solution design
- sign off necessary
Extra ($)
- shackles
- straps
- other hardware

## Slide 9: Forward
Agjust procedeure to reduce L-R slope in SFIL
Build a small stack to verify changes
Once corrected build a bulk layer of (2 SFIL) layers ??

## Slide 10: Build plates regrooved
Four available