## Slide 1: BIC Update
Kevin Bailey & Tom O’Connor
Triple I Engineering Meeting Update
September 22, 2025

## Slide 2: Test SFIL #3 w/ GlueX fiber
Slice for comparator created (measurements tbd)
Small section for density created
  Density 4.76g/cc (314g, 66cc)
Profile slope L-R ~2mm+
Profile slope Front to Back corrected
Fiber / lead missalignment appears to match slope error

## Slide 5: FIRST LAYUPS JUST FINISHED