## Slide 1: R&D for high intensity electron sources in support of EIC (ECA FOA)
Mengjia Gaowei on behalf of the team
Collider-Accelerator Department, BNL
C-AD Machine Advisory Committee Meeting (MAC-22),
Dec 17-19, 2025

## Slide 2
Introduction
Project timeline and task breakdown
Progress summary
Experimental results and discussion
Future plan for cathode R&D

## Slide 3
3
Electron beam for EIC Hadron Cooling
High average current
High bunch charge
Long lifetime
Low emittance
It is desirable to have flat hadron beam achieved by the hadron cooling. And may upgrade to maintain hadron emittance by using high energy hadron cooling.
Introduction
Our focus: High intensity electron source for EIC with epitaxial photocathodes.
Through epitaxial growth of photocathode, we are looking to achieve photocathode with ordered surface and low physical roughness; large grain or single crystal photocathodes with reduced grain boundaries low emittance and high QE.

## Slide 4
Project timeline
2021/8
2026/7

## Slide 5
Single crystal photocathode development
  K2CsSb (year 3)
  Na2KSb (year 4)
Upgrade growth chamber with RHEED (Year 2)
Incorporate in situ x-ray characteristics with offline technique (year 1 & 2)
Fabricate cathode transfer chamber between growth and analysis tools
  Design
  Procurement
  Modification and Fabrication
  Assembly
  Commission
High current test (in line with gun schedule)
  Lifetime test for single crystal K2CsSb
  Measure transverse emittance of the electron beam generated by the single crystal K2CsSb
  Characterize damaged cathodes and investigate recovering methods
Project tasks breakdown

## Slide 6
Custom modifications are made to the transfer chamber parts. Leak check is performed for the main compartment of the transfer chamber. Custom connections for transfer chamber are fabricated. (Figure. 1a)
Equipped the experimental chamber with new evaporator design same as the EIC HC cathode growth system (Figure. 1b), to grow the cathode material in the same deposition conditions as will be used for EIC. New evaporators are conditioned and tested, with successful growth demonstrated.
Design new sample pucks which will incorporate the mounting of lattice matched single crystal wafers.
Progress summary – hardware development

## Slide 7
Progress summary - software development
Simulation work continues for emittance measurement.
Labview based control and data requisition for emittance measurement is developed.
Figure. 2 a) Schematic of cathode emittance measurement chamber b) Schematic details of cathode-anode connection and the MCP-YAG detector c) Scatter plot and histogram of electron distribution on MCP at 5kV with MTE of 25 and 33 meV, respectively. The rms beam size on the MCP screen with respect to its beam energy for its initial MTE is obtained from Simion simulations. The rms beam size on the cathode (σx) is 60 µm. d) Interface of the Labview based control and data requisition program for photocathode emittance measurement.

## Slide 8
Progress summary - Material development
Epitaxial growth of Cs3Sb, K2CsSb and Cs2Te were performed on various lattice matched substrates. High quantum efficiency, ultrasmooth and epitaxial thin film photocathodes are achieved.
Epitaxial growth of Na2KSb with ultrasmooth surface (with EIC cathode evaporator configuration) is successfully realized.

## Slide 9: Na-K-Sb photocathode
Sodium potassium antimonide (NaKSb) photocathodes is one of the cathode choices for high-brightness applications. These materials offer high QE, fast response, and good thermal stability, making them viable candidates for high-brightness, high-average-current photoinjectors.
Thermal robustness: @100°C showed QE degradation from 7% to ~3% after 90h. QE recoverable by re-evaporating K.
Lifetime and High Current Operation: 1/e lifetime is 66 h.
Fit from MTE measurement gives a work function of ~1.95 eV;
Fit from MTE measurement gives a work function of ~2 eV.
135 meV @ 2.76 eV; 60 meV at 2.33 eV
Motivation: High current, high charge
Cathode overheating form high power laser is a concern
Possible use of NaKSb cathode is introduced as candidate that has better temperature resistance than K2CsSb.
Cultrera, L., et al. "Growth and characterization of rugged sodium potassium antimonide photocathodes for high brilliance photoinjector." Applied Physics Letters 103.10 (2013).
J. Dube, J. Kühn, C. Wang, S. Mistry, G. Klemz, A. Galdi, T. Kamps; Triple evaporation growth and photoemission characterization of bialkali antimonide photocathodes. J. Appl. Phys. 28 July 2025; 138 (4): 045704.
Notes: Added to our scope for material development

## Slide 10: In situ in operando Characterization of photocathodes @ synchrotron light source
10
Characterization:
QCM
XRD - crystal structure
XRR - surface roughness
XRF - stoichiometry
QE
RHEED
Evaporators:
Thermal Sb
PLD Sb
Alkali effusion cells
Cathode Candidates:
K2CsSb/KCs2Sb
Cs3Sb
Cs2Te
Na2KSb
11.48keV, 1.08 Å
Unique program that interfaces with the beamlines at NSLS-II to study photocathode material with the state-of-the-art synchrotron light source
Develops new tools and recipes, which benefit the broad photocathode and accelerator community in providing insight into the fundamental material research
The only active synchrotron research facility for photocathode, attracts collaborators from various Nuclear Physics facilities and from international accelerator facilities.

## Slide 11
In situ, real time XRD: Structural evolution
As K ratio increases, QE is trending up. When K reaches 1 and kept stable, QE continue to rise and eventually saturates.
At K ratio~0.4 (ideal ratio is 1); QE 0.5% another phase shows up
When K ratio reaches ~1, new phase intensity is lower than original phase
As growth continues, new phase switch intensity with original phase, as QE keeps rising and eventually saturates.
After slight annealing, original phase disappears
Slight annealing
Start
Final

## Slide 12
Na3Sb
(0002)
Na2KSb
(111)
Na3Sb
(0004)
Na2KSb
(222)
XRD: Structural evolution
Substrate
Peak
Single phase of Na2KSb
Single phase of Na3Sb
Growth
Substrate
Slight annealing
Cam 1
Cam 2
Polycrystalline

## Slide 13
Na-K-Sb photocathode – RHEED, XRR
3~ 5 nm
12 nm
18 nm
3~5nm
18nm
Thickness: 18 nm
Roughness: 0.7-0.8 nm
RHEED streaks
Azimuthal dependence
Ultrasmooth

## Slide 14
Results- QE
Sequential+ K-Sb yoyo
Spectral response gives a work function of ~1.9 eV.
530nm- QE 4.6%
450nm- QE 12.3%
Epitaxial growth
Work function estimated ~ 1.8eV
530nm- QE 2.8%
450nm- QE 7.1%

## Slide 15
@High-Average-Current, High-Brightness HVDC Electron Gun for EIC Hadron Cooling at Stony Brook University
  Lifetime test for single crystal K2CsSb
  Measure transverse emittance of the electron beam generated by the single crystal K2CsSb
  Characterize damaged cathodes and investigate recovering methods
High current test (On schedule 2026~2027)

## Slide 16
Hardware & Infrastructure Development
  Incorporate PLD laser for PLD growth.
  Upgrade growth chamber with Energy-Dispersive X-ray Spectroscopy (EDX), sharing the same electron source with RHEED.
  Design sample holders and transfer forks for the transfer chamber to interface with multiple characterization tools : XPS, ARPES.
Engineering for heterostructure photocathodes
  Grow and characterize known heterostructure systems for multialkali photocathodes: S20 and alike
  Use in situ XRR/XRF/XRD to monitor and characterize material interface
  Optimize band alignment using DFT and experimental validation
Surface engineering for enhanced stability
  DFT modelling of cathode surface + capping layer
  Evaluate protective layers (2D materials, oxide capping)
Continued High current test for cathode materials
  Lifetime test for single-crystal K₂CsSb and Na2KSb
    QE decay
    QE mapping before/after test
    Thermal load vs QE degradation
  Transverse emittance measurement
    MTE measurement at high charge
    Correlate emittance with cathode material properties
Potential Future work for cathode R&D (long term)

## Slide 17
Summary
High QE, ultrasmooth (sub-nm roughness) and epitaxial photocathodes of Cs3Sb, K2CsSb, Cs2Te and Na2KSb are achieved. The epitaxial growth of K2CsSb, Cs2Te and Na2KSb are the first demonstration in the field.
Emittance measurement is in progress.
High current test is scheduled 2026-2027.
Photocathode material | Preparation method | QE | Roughness(nm)
Cs3Sb | PLD | 3% @ 532 nm, thin | 0.3 @11 nm thickness
K2CsSb | PLD; Co-dep | >9% @ 532 nm | 0.6 @ 11 nm thickness
Cs2Te | PLD | 17~20%@270nm | 0.8 @ 22 nm thickness
Na2KSb | Co-dep | 2.8% @ 532 nm | 0.8 @ 20 nm thickness
Match or exceed the best reported results in the field!

## Slide 18: Acknowledgement
Thank you very much! Suggestions and comments are appreciated!
Work supported by Brookhaven Science Associates, LLC under Contract No. DE-SC0012704. This research used resources 4-ID (ISR) of the National Synchrotron Light Source II, a U.S. Department of Energy (DOE) Office of Science User Facility operated for the DOE Office of Science by Brookhaven National Laboratory under Contract No. DE-SC0012704.
Many thanks goes to the contributors: Kali Prasanna Mondal, Elena Maria Echeverria Mora, Yilin Yang, John Smedley, Jared Maxson, Kenneth Evans-Lutterodt, Raul Acevedo-Esteves, John Walsh, Rudy Begay

## Slide 19
(Back up slides) XRD: Heat decomposition: Na2KSb
114.5 °C
184.5 °C
162.4 °C
192.2 °C
1/e QE; 125.7 °C
108.2 °C
K ratio~ 1
K ratio~ 0.6
K ratio~ 0.4

## Slide 20
XRD of epitaxial K2CsSb cathode
Substrate
5 nm
11 nm
20 nm
Polycrystalline
Textured
Sequential growth  Polycrystalline
Co-evaporation  fiber-textured
Epitaxial growth  ordered grains/single crystal
Crystallinity

## Slide 21
Wavelength (nm) |  | Sample-3 QE (%) |  |  | 
 |  | L1 | L2 | L3 | L3 after 1 day
Green laser |  | 0.5 | 4.6 | 9.2 | --
LDLS source | 450 | 1.3 | 8.9 | 17.8 | 21.5
530 | 530 | 0.5 | 4.2 | 7.6 | 9.7
Green QE is > 9% !
Measured QE after 3-4 days of growth, no decay
Current draw is about 25 uA
Fluctuations are likely from laser power
QE of epitaxial K2CsSb cathode