## Slide 1: Technical Internal Review TOF Sensor
Satoshi YANO
(Hiroshima University)

## Slide 2: Current Status of Sensor
”Baseline” sensor fundamental parameters
  Size: 32x20 mm2
  Strip-size / Pich: 10x0.05 mm2 / 500 um
  Strip geometry: 64x2=128 ch
  Active thickness: 50 um
  Sheet resistance: 1600Ω/◻︎
  Coupling capacitance: ︎240 pF/mm2
Current best performance
  eRD112 FY23 sensor
    5x10 mm2, 10x0.05 mm2 / 500 um
  The sensor was tested at FNAL 120 GeV proton
    Timing resolution: 35 ps
    Spatial resolution: 15~20 um (depend on hit position)
20mm
32 mm
10mm
5 mm
eRD112 FY23
eRD112 FY24

## Slide 3: Upcoming Deliverable
First full-size sensor (eRD112 FY24) result
  eRD112 FY24 sensor is the first full-size sensor (32x20 mm2)
  Different strip pitches are implemented on one sensor
  Test beam results at JLab will be released soon
“Real” full-size sensor reult
  First “real” full-size sensor with 20/30/50um was received this September
  Lab-test, I/V measurement, TCT-scan, and Sr90 will start soon
  Test beam at DESY is scheduled in December-2025

## Slide 4: Unresolved Problem
Wire-bonding’s damage of sensor
  Instability of l/V curve after wire-bonding was observed in eRD112 FY24 sensor
  Oxidization film damage by wire-bonding is suspected
  Thicker oxidization film has been adopted to ”modified” eRD112 FY24 sensor
    The same sensor as the eRD112 FY24 sensor delivered to Japan in May incorporates this improvement
Solution:
  Optimization of wire-bonding is necessary
    HPK suggested us to use ball-bonding instead of wedge-bonding
  Coating bonding pad design will be used for the next production (Beginning of 2026 if possible)
After bonding
Before bonding
“Modified” eRD112 FY24 sensor
“Modified” eRD112 FY24 sensor

## Slide 5: “Baseline” Sensor R&D History
Original eRD112 FY24 sensor
  Ordered by eRD112 budget (FY24)
  The first sensor of 32x20 mm2 (full-size)
  Variable pitches 1mm, 0.75mm, 0.5mm pitches with 50um
  Observed very low-yield of 50um active thickness sensors
  Observed damage of sensor after wire-bonding
  Tested @ Jlab
Modified eRD112 FY24 sensor
  Provided by HPK as sample
  Same mask as original eRD112 FY24
  Applied improved wafer making process
  Applied thicker oxide layer than original
Real Full-size sensor
  Ordered by Japanese budget (JFY25)
  The first real sensor, 32x20 mm2, 64x2=128ch, 10x0.05 mm2, 500 um pitch
  Same parameters as Modified eRD112 FY24 sensor except geometry
  Plan to test @ DESY (December 2025)
Modified Real Full-size sensor
  Ordered by Japanese budget (JFY25)
  Same mask as original real full-size sensor
  Pad reinforcement
  Plan to test @ RARiS (March 2026)
    Only if delivered before the test

## Slide 6: Sensor R&D other than “Baseline” Plan-B
Sensors that meet the requirements under any conditions are needed
  Timing resolution of 35ps and spatial resolution of 15~20um was measured under best environment
  Performance degradation during operation due to unstable conditions can be expected
  Continuing to strive for superior performance is important
Fall back solution for the stave design is necessary
  Consideration of backup plan when the sensor's inherent performance cannot be achieved in designs using an interposer is necessary
  It is not obvious if it is possible to accurately extract tiny high-frequency analog signals from 64 parallel traces within a thin FPC
  Double-metal layer design can expand design flexibility
E.g. Double metal layer design to enable readout perpendicular to the strip direction
It is possible to mount the ASICs perpendicular to the strip direction

## Slide 7: Strategy & Schedule
“Baseline” sensor
  Solving wire-bonding’s damage on sensor is the top priority for the “baseline” sensor
    Optimal bonding condition & Pad reinforcement
  Compatibility checks with FCFD are essential
    New evaluation board is necessary (to be check)
  Plan: October ~ March 2026
    Optimal wire-bonding conditions is looked for
    Test beam @ DESY is schedules (15~21 Dec.)
      Goal: First “real” sensor test & measurement of charged particle penetrating angle effect
    Beam test @ RARiS is scheduled (2~5 Mar.)
      Goal: Modified “real” sensor test & Resolve issues identified at DESY & if possible compatible check with FCFD

## Slide 8: Strategy & Schedule
Double-metal sensor (Plan-B sensor)
  First, the performance must be measured
    Double metal effect will be extracted by comparison with “baseline” sensor
  Plan: October ~ March 2026
    Beam test @ RARiS is scheduled (2~5 Mar.)
      Goal: measurement of the performance

## Slide 9: Backup

## Slide 10: Acceptance Hole
Left-Half-Stave
Right-Half-Stave
Between half-staves, there are large acceptance holes
  2 mm at right in the middle, 10 mm at little sideways from the middle
Between modules, there are small 2 mm acceptance holes
  Due to 1 mm inactive area in a sensor
Full-Stave
Front-side
Back-side