## Slide 1: Strip-Type AC-LGAD Test, Status, and Plan
Satoshi YANO
Hiroshima University and RIKEN

## Slide 2: ”Required” Sensor Performance
hpDIRC
BTOF
dRICH
FTOF
HRPPD
pfRICH
Decay products from D-meson in ep DIS @ √s = 141 GeV
BTOF PID focuses on low-momentum particles at mid-rapidity
Continuous PID coverage requires seamless operation in conjunction with other PID detectors, avoiding PID gaps
  Minimum timing required for the sensor to eliminate the PID gap is ~95 ps
A stretch goal of sensor ~40 ps would provide substantial overlap (Δp ≈ 0.5 GeV/c) for robust cross-calibration

## Slide 3: ”Required” Sensor Performance
hpDIRC
BTOF
dRICH
FTOF
HRPPD
pfRICH
Decay products from D-meson in ep DIS @ √s = 141 GeV
BTOF PID focuses on low-momentum particles at mid-rapidity
Continuous PID coverage requires seamless operation in conjunction with other PID detectors, avoiding PID gaps
  Minimum timing required for the sensor to eliminate the PID gap is ~95 ps
A stretch goal of sensor ~40 ps would provide substantial overlap (Δp ≈ 0.5 GeV/c) for robust cross-calibration
σelec = 20ps
σT0 = 25ps
hpDIRC limit
hpDIRC limit
Overlap disappear
point
Overlap
~ 0.5 GeV/c
~95 ps
Overlap
~ 0.5 GeV/c

## Slide 4: ”Required” Sensor Performance
hpDIRC
BTOF
dRICH
FTOF
HRPPD
pfRICH
Decay products from D-meson in ep DIS @ √s = 141 GeV
σelec = 20ps
σT0 = 25ps
hpDIRC limit
hpDIRC limit
Overlap disappear
point
Overlap
~ 0.5 GeV/c
~95 ps
Overlap
~ 0.5 GeV/c
BTOF PID focuses on low-momentum particles at mid-rapidity
Continuous PID coverage requires seamless operation in conjunction with other PID detectors, avoiding PID gaps
  Minimum timing required for the sensor to eliminate the PID gap is ~95 ps
A stretch goal of sensor ~40 ps would provide substantial overlap (Δp ≈ 0.5 GeV/c) for robust cross-calibration

## Slide 5: Strip-Tyle AC-LGAD Sensor
10mm
5 mm
eRD112 FY23
SH4
1600Ω/◻︎ (E-Type)
240 pF/mm2
SiO2 50nm
SH5
1600Ω/◻︎ (E-Type)
600 pF/mm2
SiO2 50nm
SH3
400Ω/◻︎ (C-Type)
600 pF/mm2
SiO2 50nm
SH2
400Ω/◻︎ (C-Type)
240 pF/mm2
SiO2 50nm

## Slide 6: Strip-Tyle AC-LGAD Sensor
20 mm
32 mm
10mm
5 mm
eRD112 FY23
eRD112 FY24
SH4
1600Ω/◻︎ (E-Type)
240 pF/mm2
SiO2 50nm
1600Ω/◻︎ (E-Type)
600 pF/mm2
SiO2 50nm
SH5
1600Ω/◻︎ (E-Type)
600 pF/mm2
SiO2 50nm
SH3
400Ω/◻︎ (C-Type)
600 pF/mm2
SiO2 50nm
SH2
400Ω/◻︎ (C-Type)
240 pF/mm2
SiO2 50nm

## Slide 7: Strip-Tyle AC-LGAD Sensor
20 mm
32 mm
10mm
5 mm
eRD112 FY23
eRD112 FY24
20 mm
32 mm
Row1 ~ 64
col1
col2
EIC-JPN JFY25
SH4
1600Ω/◻︎ (E-Type)
240 pF/mm2
SiO2 50nm
1600Ω/◻︎ (E-Type)
600 pF/mm2
SiO2 50nm
1600Ω/◻︎ (E-Type)
240 pF/mm2
SiO2 50nm + SiN 200nm
SH5
1600Ω/◻︎ (E-Type)
600 pF/mm2
SiO2 50nm
SH3
400Ω/◻︎ (C-Type)
600 pF/mm2
SiO2 50nm
SH2
400Ω/◻︎ (C-Type)
240 pF/mm2
SiO2 50nm

## Slide 8: Strip-Tyle AC-LGAD Sensor
20 mm
32 mm
10mm
5 mm
eRD112 FY23
eRD112 FY24
20 mm
32 mm
Row1 ~ 64
col1
col2
EIC-JPN JFY25
SH4
1600Ω/◻︎ (E-Type)
240 pF/mm2
SiO2 50nm
1600Ω/◻︎ (E-Type)
600 pF/mm2
SiO2 50nm
SH5
1600Ω/◻︎ (E-Type)
600 pF/mm2
SiO2 50nm
SH3
400Ω/◻︎ (C-Type)
600 pF/mm2
SiO2 50nm
SH2
400Ω/◻︎ (C-Type)
240 pF/mm2
SiO2 50nm
✔︎ Test Beam
✔︎ Test Beam
1600Ω/◻︎ (E-Type)
240 pF/mm2
SiO2 50nm + SiN 200nm

## Slide 9: Sensor Design Strategy in JFY25
Result of eRD112 FY23
E-Type
E-Type
C-Type
C-Type

## Slide 10: Sensor Design Strategy in JFY25
E-Type
E-Type
Result of eRD112 FY23
C-Type
C-Type
No capacitance of oxide layer dependence
Thick oxide layer was preferred because we faced sensor damage by wire-bonding
Assume SiO2 50nm + SiN 200nm (240 pF/mm2) is the same performance as SiO2 50nm (600pF/mm2)
  Detector capacitance: 12 pF (240pF/mm2) v.s. 12.4 pF (600pF/mm2)

## Slide 11: Sensor Design Strategy in JFY25
E-Type
E-Type
Result of eRD112 FY23
C-Type
C-Type
No capacitance of oxide layer dependence
Thick oxide layer was preferred because we faced sensor damage by wire-bonding
Assume SiO2 50nm + SiN 200nm (240 pF/mm2) is the same performance as SiO2 50nm (600pF/mm2)
  Detector capacitance: 12 pF (240pF/mm2) v.s. 12.4 pF (600pF/mm2)

## Slide 12: Sensor Design Strategy in JFY25
No capacitance of oxide layer dependence
Thick oxide layer was preferred because we faced sensor damage by wire-bonding
Assume SiO2 50nm + SiN 200nm (240 pF/mm2) is the same performance as SiO2 50nm (600pF/mm2)
  Detector capacitance: 12 pF (240pF/mm2) v.s. 12.4 pF (600pF/mm2)
E-Type
E-Type
Result of eRD112 FY23
C-Type
C-Type

## Slide 13: Japan-Led Test Beam Campaigns JFY25+JFY26
DESY, Germany (Dec. 15–21, 2025)
  Electron beam (up to 5.6 GeV)
  Position resolution measurement using the DESY telescope
KEK PF-AR, Japan (Feb. 19–25, 2026)
  Electron beam (below 5.8 GeV)
  Timing resolution measurement of baseline sensor
RARiS, Tohoku University, Japan (Mar. 3–6, 2026)
  1 GeV electron beam
  Timing resolution measurement of alternative sensors
KEK PF-AR, Japan (June 1, 2026)
  Electron beam (below 5.8 GeV)
  Temperature dependence of timing performance (baseline sensor)

## Slide 14: Japan-Led Test Beam Campaigns JFY25+JFY26
DESY, Germany (Dec. 15–21, 2025)
  Electron beam (up to 5.6 GeV)
  Position resolution measurement using the DESY telescope
KEK PF-AR, Japan (Feb. 19–25, 2026)
  Electron beam (below 5.8 GeV)
  Timing resolution measurement of baseline sensor
RARiS, Tohoku University, Japan (Mar. 3–6, 2026)
  1 GeV electron beam
  Timing resolution measurement of alternative sensors
KEK PF-AR, Japan (June 1, 2026)
  Electron beam (below 5.8 GeV)
  Temperature dependence of timing performance (baseline sensor)

## Slide 15: Hit Position Resolution
Similar or better positioning resolution than eRD112 FY23 sensor
  Different algorithm is used
eRD112 FY23
EIC-JPN JFY25

## Slide 16: Signal Propagation Time
Leading – MCPPMT time [ps]
Strip#1
Strip#2
Δt1
Δt2
Ts1 = thit + Δt1
Ts2 = thit + Δt2
True hit time thit
Hit position accuracy connects to timing resolution via σdelay ~ σpos/veff
  σdelay = 5 ~ 16 ps @ σpos = 5 ~ 15 μm (self determination)
  σdelay = 33 ps @ σpos = 30 μm (5-bit ADC scenario)
  σdelay = 109 ps @ σpos = 100 μm (track information)
Veff ~ 0.92 um/ps
σ2total =σ2jitter + σ2Landau + σ2tw + σ2delay

## Slide 17: Signal Propagation Time
Although there is a delay in the strip direction, the signal propagates quickly
  σdelay ~ 1 ps @ σpos = 100 μm (track information)
Readout pad
Leading – MCPPMT time [ps]
Veff ~ 100 um/ps
σ2total =σ2jitter + σ2Landau + σ2tw + σ2delay

## Slide 18: Jitter
Jitter definition: σjitter = σnoise / (dV/dt)
EIC-JPN JFY25 result is the same as eRD112 FY23, 15~20 ps
Weighted
(leading & subleading)
EIC-JPN JFY25
eRD112 FY23
σ2total =σ2jitter + σ2Landau + σ2tw + σ2delay

## Slide 19: Total Timing Resolution
σ2total =σ2jitter + σ2Landau + σ2tw + σ2delay + σ2unknown
15~20 ps
~10 ps
25~30 ps
~5 ps
60~70 ps
EIC-JPN JFY25
eRD112 FY23
45~58 ps

## Slide 20: Summary of Test Beam
Hit position can be measure very precisely
  σpos ~ 7.6 μm in average
Non-negligible signal propagation time has been observed
  veff ~ 0.92 μm/ps
Accuracy of hit position estimation affects on timing resolution, but it can be controlled
  Hit position resolution of tracking O(100) μm is insufficient to get a few tens of ps timing resolution
Jitter result is the same as the previous eRD112 prototype 15~20ps, but the total timing resolution is 60~70ps due to unknown source of ~50ps
  It may come from timing reference reconstruction (MCP-PMT)
Excellent results have been measured by TCT-scan (see next presentation)
  We are investigating the “unknown” source by the new weapon

## Slide 21: Summary of Test Beam
Hit position can be measure very precisely
  σpos ~ 7.6 μm in average
Non-negligible signal propagation time has been observed
  veff ~ 0.92 μm/ps
Accuracy of hit position estimation affects on timing resolution, but it can be controlled
  Hit position resolution of tracking O(100) μm is insufficient to get a few tens of ps timing resolution
Jitter result is the same as the previous eRD112 prototype 15~20ps, but the total timing resolution is 60~70ps due to unknown source of ~50ps
  It may come from timing reference reconstruction (MCP-PMT)
Excellent results have been measured by TCT-scan (see next presentation)
  We are investigating the “unknown” source by the new weapon

## Slide 22: Summary of Test Beam
Hit position can be measure very precisely
  σpos ~ 7.6 μm in average
Non-negligible signal propagation time has been observed
  veff ~ 0.92 μm/ps
Accuracy of hit position affects on timing resolution, but it can be controlled
  Hit position resolution of tracking O(100) μm is insufficient to get a few tens of ps timing resolution
Jitter result is the same as the previous eRD112 prototype 15~20ps, but the total timing resolution is 60~70ps due to unknown source of ~50ps
  It may come from timing reference reconstruction (MCP-PMT)
Excellent results have been measured by TCT-scan (see next presentation)
  We are investigating the “unknown” source by the new weapon

## Slide 23: Summary of Test Beam
Hit position can be measure very precisely
  σpos ~ 7.6 μm in average
Non-negligible signal propagation time has been observed
  veff ~ 0.92 μm/ps
Accuracy of hit position affects on timing resolution, but it can be controlled
  Hit position resolution of tracking O(100) μm is insufficient to get a few tens of ps timing resolution
Jitter result is the same as the previous eRD112 prototype 15~20ps, but the total timing resolution is 60~70ps due to unknown source of ~50ps
  It may come from timing reference reconstruction (MCP-PMT)
Excellent results have been measured by TCT-scan (see next presentation)
  We are investigating the “unknown” source by the new weapon

## Slide 24: Summary of Test Beam
Hit position can be measure very precisely
  σpos ~ 7.6 μm in average
Non-negligible signal propagation time has been observed
  veff ~ 0.92 μm/ps
Accuracy of hit position affects on timing resolution, but it can be controlled
  Hit position resolution of tracking O(100) μm is insufficient to get a few tens of ps timing resolution
Jitter result is the same as the previous eRD112 prototype 15~20ps, but the total timing resolution is 60~70ps due to unknown source of ~50ps
  It may come from timing reference reconstruction (MCP-PMT)
Excellent results have been measured by TCT-scan (see next presentation)
  We are investigating the “unknown” source by the new weapon

## Slide 25: Future Plan
Short-term:
  Main event is the next review which will be held on Oct. to Dec. 2026
  Unknown source existing in the only test beam must be understood
    No test beam before the review
    Building a block with the test beam, TCT-scan, and Sr90 results to convince reviewers
Middle-term:
  Test beam for compatibility with FCFDv1.2 will be planned at Nov. to Dec. 2026
  EIC-JPN JFY25 sensor detector capacitance is expected to be 12 pF @ 1GHz (eRD112 FY23 sensor is 12.4 pF @ 1GHz)
Long-term:
  Strategy of sensor production in JFY26 (until March 2027) should be fixed
  The deadline for finalizing design is August to receive sensors in the JFY26
  The sensor will be used for several tests planed in 2027

## Slide 26: Future Plan
Short-term:
  Main event is the next review which will be held on Oct. to Dec. 2026
  Unknown source existing in the only test beam must be understood
    No test beam before the review
    Building a block with the test beam, TCT-scan, and Sr90 results to convince reviewers
Middle-term:
  Test beam for compatibility with FCFDv1.2 will be planned Nov. to Dec. 2026 @ KEK
  EIC-JPN JFY25 sensor detector capacitance is expected to be 12 pF @ 1GHz (eRD112 FY23 sensor is 12.4 pF @ 1GHz)
Long-term:
  Strategy of sensor production in JFY26 (until March 2027) should be fixed
  The deadline for finalizing design is August to receive sensors in the JFY26
  The sensor will be used for several tests planed in 2027

## Slide 27: Future Plan
Short-term:
  Main event is the next review which will be held on Oct. to Dec. 2026
  Unknown source existing in the only test beam must be understood
    No test beam before the review
    Building a block with the test beam, TCT-scan, and Sr90 results to convince reviewers
Middle-term:
  Test beam for compatibility with FCFDv1.2 will be planned Nov. to Dec. 2026 @ KEK
  EIC-JPN JFY25 sensor detector capacitance is expected to be 12 pF @ 1GHz (eRD112 FY23 sensor is 12.4 pF @ 1GHz)
Long-term:
  Strategy of sensor production in JFY26 (until March 2027) should be fixed
  The deadline for finalizing design is August to receive sensors in the JFY26
  The sensor will be used for several tests planed in 2027

## Slide 28
Extra

## Slide 30: Signal Strength
Readout board designed by FNAL and UCSC was used
EIC-JPN JFY25 sensor should be the same as SH4/5 but it looks similar to SH2/3
EIC-JPN JFY25
HV= - 185 V
eRD112 FY23
EIC-JPN JFY25 signal strength is about half the height of the eRD112 FY23
EIC-JPN JFY25
HV= - 185 V
- 204 V
- 200 V
- 180 V
- 190 V

## Slide 31: Risetime（10 - 90%）
EIC-JPN JFY25 sensor’s risetime is faster than eRD112 FY23 by ~50 ps
  Due to small signal strength?
eRD112 FY24は極端に短い400ps @ ストリップ直上
  TCTを用いているのでLandau揺らぎがないことが原因か
EIC-JPN JFY25
eRD112 FY23
eRD112 FY24