## Slide 1: Zr-96 and Ru-96 Preparation
D. Raparia
August 9, 2017
RHIC Retreat

## Slide 2: Outlines
Requirements
Zirconium-96
Ruthenium-96
Conclusion

## Slide 3: Acknowledgements
E. Beebe, S. Ikeda, T. Kanesue, M. Okamura
C. Carlson, D. Steski, P. Thieberger
C. Gardner, W. Fischer

## Slide 4: Requirements for Zr-96 and Ru-96
1.3E9 ion per bunch at the beginning of the store, with this bunch intensity we can have >~10 h stores with L(t) > 22E26 cm-2s-1 for the whole store and thereby filling the STAR bandwidth completely (Wolfram)
=> 1.5E9 ions per bunch out of the AGS for both Zr-96 and Ru-96 (Wolfram)

## Slide 5: Sources for Zr-96 and Ru-96
=> 0.625E9 ion per pulse for Zr-96 at booster input from EBIS1 with 12-6-2 bunch merge scheme (Gardner)
=> 1.1E9 ion per pulse for Ru-96 at booster input from Tandem2 with 8-4-2 bunch merge scheme (Gardner)
1 Zr-96 will be provided by LION-EBIS
2 Ru-96 will be provided by Tandem

## Slide 6: Natural Abundance of Zr and Ru
Zirconium | Abundance (%) | Ruthenium | Abundance (%)
Zr-90 | 51.45 | Ru-96 | 5.54
Zr-91 | 11.22 | Ru-98 | 1.87
Zr-92 | 17.15 | Ru-99 | 12.76
Zr-93 | trace | Ru-100 | 12.60
Zr-94 | 17.38 | Ru-101 | 17.06
Zr-96 | 2.80 | Ru-102 | 31.55
 |  | Ru-104 | 18.62
Q/M: 96Zr16 = 90Zr15
96Ru12= 104Ru13

## Slide 7: Zirconium E. Beebe, S. Ikeda, T. Kanesue, M. Okamura
~ns
Laser
Target
~ a few ns
20~30 deg.
~ms
z
x
z
x
z
Plasma formed
Plasma expands
Extraction field
Ion beam
Drift length
x
Primary ions are provided by laser ion source (LION)
Target must be 96Zr.
EBIS
RFQ
IH
ETB
LION

## Slide 8
Laser for NSRL
Laser for RHIC
NASA target – Array of flat targets
(B, Ca, Au, O, Si, Ti, Fe, Ta, C ..)
RHIC target – Spinning gold disk
Laser Ion Source (LION)

## Slide 9: Zr-90 Test EBIS/ Booster
 | (16:28) | (16:36) | (17:05) | Au (6/6 13:05)
Target | Zr metal | ZrO2 | ZrO2 | Au from rotary
M/Q | 90, 16+ | 90, 16+ | 90, 16+ | 197, 32+
Laser P (mJ) | 270 | 270 | 120 | 240
XF 14 | 13.2 nC | 7.7 nC | 6.4 nC | 17.2 nC
XF 108 | 4.8 nC | 2.7 nC | 2.0 nC | 6 nC#
# Ions | 1.9E+9 | 1.1E+9 | 7.8E8 | 1.2E+9
Required | 0.625e9 | 0.625e9 | 0.625e9 | 
Booster early | 1.2e+09 | 7.8e+08 | 6.9e+08 | 1.4e+10 (12p) = 1.2e+9 (per 1p)
Booster late | 4.2e+08 | 2.6e+08 | 2.6e+08 | 1.3e+10 (12p) = 1.1e+9 (per 1p)
(1) Zr and ZrO2 of natural abundance were used. 51.45% of Zr is mass 90.
(2) For Au 1.25E9 ion per pule gives about after bunch merge about 3.E9 ions per bunch at AGS extraction and 2.6E9 per bunch at RHIC collision

## Slide 10
Acceleration test using 90Zr (not 96Zr) with natural abundance metal sheet – Confirmed good performance
Laser irradiation condition survey within current setup – 240 mJ laser energy with high enhancement of solenoid
Laser polarization test – No significant effect
Target scanning optimization – in progress
Laser spot size optimization – in progress
Target consumption measurement using metal sheet – 0.15 mg/shot (140 mJ), 0.53 mg/shot (385 mJ)
Enriched 96Zr sheet test – Only 12 shots at a spot
Compressed powder target test (ZrO2 and ZrH2) – ZrO2 failed, ZrH2 OK.
Sintering at 1000 ℃ and 1300 ℃ (at RIKEN)– Need 1300C at least
Sintering ZrO2 (round shape at RIKEN) – Sintering procedure established
Zirconium Tests at EBIS

## Slide 11: Zirconium Tests at EBIS
Sintering ZrO2 (strip shape at RIKEN) – Successful
Sintering on site - Oven and dies to be procured
Recycling process for used sintered ZrO2 –Successful in RIKEN, trying to be done on site
Target consumption measurement using sintered ZrO2 – 1.6 mg/shot (240 mJ)
Reduction of ZrO2 consumption– Need more time
Sintering metal powder – More investment, no vender
High temperature sintering – to be tested
Collecting sputtered ZrO2 – to be tested
Design of new XY movement mechanism – Necessary for compatible operation for NSRL and RHIC, in progress

## Slide 12
Natural ZrO2 power
Die , ~ $2000, need to be polished
after several ten of presses
Programmable press machine 1.6 ton
The target temperature was set to 1300C.
It was programmed to take 5 hour
from room temperature to 1300C and
hold for 2 hours and take 5 hours to
cool down. Furnace ~ $3000
1, 2 and 3 mm, 15 mm
of diameter. The sintered sample were measured as from 12.27 to 12.39. Almost no weight loss.
Sintering ZrO2

## Slide 13: Target after Laser Irradiation
Target ID: 3mm-1R
Laser1
Total 8861 shots
11.5 microgram/shot
Target ID: 3mm-1
Laser1 and Laser2
Total 73178 shots
1.8 microgram/shot

## Slide 14
Recycling of ZrO2 Target
1.1891 g
20 cc HCL + 4 g H3BO3
150 CC water + NH3
Heating over night
6 Hrs

## Slide 15: Zr-96 Schedule
Target |  |  | July | Aug | Sep | Oct | Nov | Dec | Jan | Feb
 | ZrO2 |  |  |  |  |  |  |  |  | 
 |  | 1300C sintering. | Done |  |  |  |  |  |  | 
 |  | 1700C sintering. | Test | Test & mea |  |  |  |  |  | 
 |  | Recycle process. | Test | Establish in BNL |  |  |  |  |  | 
 |  | Target shape. | Test | Mea |  |  |  |  |  | 
Laser irradiation condition survey. |  |  |  |  |  |  |  |  |  | 
 |  | Laser intensity. | Done |  |  |  |  |  |  | 
 |  | Spot size. | Test | Test |  |  |  |  |  | 
 |  | Scanning speed. | Test | Test | Test |  |  |  |  | 
 |  | Overwrap of the spots. | Test | Test | Test |  |  |  |  | 
 |  | Polarization. | Done |  |  |  |  |  |  | 
 |  | Laser angle and scanning | Done |  |  |  |  |  |  | 
Final test |  |  |  |  |  | Test & Mea |  |  |  | 
Stage develop |  |  |  | Design | Order | Fabri |  | Install |  | 
Enriched target |  |  |  |  |  |  | Order | Fabri |  | 

## Slide 16
For 30 days of operation for 2 rings,
From Run-16 data, 2.0 M + 41000*30 = 3.2M shots 5.1 g
From Run-17 data, 0.5 M + 52800*30 = 2.1M shots  3.4 g
 | Shots before first P store | From | To | Shots after first physics | From | To | Day | Shots per day | Store length
 | M shots |  |  | M shots |  |  |  | shots | 
Run-16 Au-Au at 100 GeV/nucleon | 2.0 | 20151123 | 20160207 | 2 | 20160207 11:15 | 20160627 | 49 | 41000 | 6
Run-17 Au-Au at 27.2 GeV/nucleon | 0.5 | 20170411 | 20170603 | 0.95 | 20170603 10:50 | 20170621 08:18 | 18 | 52800 | 3.5
Estimated Zr Target Consumption
Measured average target consumption for ZrO2: 1.6mg/shot
Estimated target weight is from 7 to 10 g

## Slide 17: Estimated Target Cost
Less consumption mode is being searched.
Pilot species may reduce the cost dramatically. (90Zr15)
Efficient machine tuning also reduce the cost a lot.
Recycle process is being examined.
In case of 10 g
150K USD

## Slide 18: Ruthenium C. Carlson, D. Steski, P. Thieberger

## Slide 19: Source
IS Chabber
Target Changer
Cs
Extractor

## Slide 20: Ruthenium from Tandem
Enriched Ru-96 is not available commercially
We will get about 500 mg Ru-96 (79%) from ORNL,

## Slide 21: Ruthenium Tests at Tandem
Dec 2015: Analyzed 102Ru12 and 96Ru12 from Natural RuO
-102Ru 29.2 μA (7.7e9) and 96Ru 5.7 μA (1.5E9)
March 2016: Using natural RuO, eight pulses per SC of 96Ru12 were delivered to Booster. The SC length was 5.4 sec and pulse width was 600 us. Single pulse at 11/30 FC was 1E9 & 0.76E9 ion per pulse at booster input and 1.07E9 ion per bunch at extraction of AGS, with 8-4-2 merge scheme in AGS.
Feb 2017: Compared Natural RuO 100%, 50/50% and 25/75 % with Ag
- 102Ru; 100% 18 μA (4.7E9), 50/50% 15.8μA (4.1E9), 25/75 % 15.2 μA (4.0E9)

## Slide 22: Ru Tests at Tandem (Cont.)
June 17: Compared natural Ru Metal 100%, 50/50% and 20/80% with Al.
-102Ru 100% - 26.8 μA (7 E9), 50% - 16 μA(4.2E9), 25% - 15.2μA (4.0E9)
July 2017: Ru metal target analyzed. The analyzed beam intensity from the Ru metal was slightly better than 50% of the intensity from RuO targets. ORNL claim to convert Ru to RuO , 40-50 % material will be lost. The decision to go with Ru metal was based on ample intensity for the run as the enriched isotope is made in the metal form and material losses would occur during the oxide process. It appears at this time that the metal targets have a longer lifetime.

## Slide 23: Ru Metal with Different Percentage of AL
 | Ru 100% |  |  | Ru 50% Al 50% |  |  | Ru 20% Al 80% |  | 
Mass | 102 Ru | 118 RuO | 16 O | 102 Ru | 118 RuO | 16 O | 102 Ru | 118 RuO | 16 O
Le Cup μA | 88 | 132 | 472 | 108 | 118 | 740 | 60 | 70 | 608
11/30 FC μA | 18 (4.7E9) | 26.8 (7E9) |  | 16 (4.3E9) | 24 (6.3E9) |  | 13 (3.4E9) | 10.5 | 

## Slide 24: Ru tests at Tandem
July 2017: Target lifetime tests are ongoing with 25%Ru 75% Al using 6 pulses 600 μsec wide every 2.5 sec. The source runs 24 hour/day with analyzing being done during the day in MP6 bypass line.
Aug 2018: Will continue to evaluate target life times, and optimize target sample volume, size and shape. Investigate best dilution material and percentage. This work will probably continue through to the end of year.
Jan 2018: When available try enriched 96Ru at determined percentage to see if intensities correspond to results from 102Ru.

## Slide 25: Summary
We have established that tandem and EBIS can satisfy RHIC requirements for Ruthenium-96 and Zirconium-96.
Zirconium and NSRL ion species compete for same physical space in LION => schedules conflicts.
Life time test and cost minimization will continue till end of the year.