## Slide 1: 9MHz System Performance & Update
Salvatore Polizzo
FY17 RHIC Retreat
8/8/17

## Slide 2: Presentation Overview
  New 9MHz Systems
    Cavity Design Basics (Visual Overview)
    FY17 Performance Review (Polarized Proton Operation Mode)
    Current Efforts (Extending the high end voltage margin)
    Conclusions

## Slide 3: 9MHz Cavity Design Overview
  Cavity Length ≈ 3m
  Cavity Radius = .45m
Coarse Tuning
Fine Tuning
Drive Loop
Air
Gap Cap
60kV
The resulting gap capacitor assembly is the product of an ongoing collaboration between BNL and Comet Technologies.

## Slide 4: 9MHz Cavity Design Overview
Internal Beam Pipe View
Bell Housing Installed

## Slide 5: 9MHz Cavity Performance Review (Polarized Proton Operation Mode)
  Cavity Voltage
    32kV Peak
    60kV Max Design Voltage (53.4kV LEReC Design Requirement)
  Frequency
    9.376MHz – 9.384MHz
    8.7MHz – 9.8MHz (LEReC Design Requirement)
  Drive Power
    ≈ 8.2kW Peak for ≈ 32kV (Acceleration ø =33°, βfpc ≈ 2)
    ≈ 5.4kW Peak for ≈ 32kV (Acceleration ø =16.5°, βfpc ≈ 2)
    ≈ 7kW for 60kV (LEReC Design Requirement βfpc ≈ 1)

## Slide 6
  Making voltage is not the challenge in the PP operation mode
  The challenge is to provide enough power to the beam during acceleration (max()) while maintaining sufficient power margin to fight transients.
  Fast Ramp (øacc @ max() = 33°)
    Fill Number = 20595
    Bunch Intensity ≈ 2e11 protons
    Ramp Time ≈ 4.5 minutes
    Gap Voltage = 32kV
    Drive Power ≈ 8.2kW
  Slow Ramp (øacc @ max() = 16.5°)
    Fill Number = 20865
    Bunch Intensity ≈ 2.07e11 protons
    Ramp Time ≈ 9 minutes
    Gap Voltage = 32kV
    Drive Power ≈ 5.4kW
Real(Ig)
Real(Ib)
Ib
Ig
ø =33°
Real(Ig)
Real(Ib)
Ib
Ig
ø =16.5°
Simplified post transition phasor plots
9MHz Cavity Performance Review

## Slide 7: 9MHz Cavity Performance Review
  Assuming we were able to push the beam intensity to peak FY15 levels (≈ 2.6e11 protons/bunch)
    Estimated Drive Power > 10kW
    Estimated Reflected Power > 1.2kW
  We may have wanted a bigger stick
    Leverage the configurability of the cavity design to
    further optimize βfpc thus minimizing Preflected @ max()
    Peak Forward Power Reduction ≈ 10%

## Slide 8: New 9MHz System Current Efforts
  Before ordering the balance of the gap cap devices we are working to improve the cavities high voltage margin by replacing the inner ceramic RF window with a higher performance alumina.
Dielectric loss profile inside alumina window
Thermal image taken through CaF2 window
Max calibrated internal temp ≈ 70C @ 55kV
End result of window heating is cavity Q degradation and thermal runaway above 72kV

## Slide 9: New 9MHz System Current Efforts
  Dielectric Material Test Cavity (50MHz)
Chart: tanδ VS Temperature
| 351 | 344 | 319 | 315 | 308 | 301 | 299 | 292 | 284 | 279 | 273 | 264 | 257 | 248 | 238 | 227 | 218 | 208 | 198 | 189 | 180 | 169 | 160 | 149 | 139 | 128 | 119 | 108 | 98.6 | 87.7 | 77.599999999999994 | 68 | 58.6 | 48.8 | 38.299999999999997
RF860 Sample 1 | 0.0010741 | 0.00096248 | 0.00086731 | 0.00085689 | 0.00085182 | 0.00082698 | 0.00082298 | 0.00078464 | 0.00077033 | 0.00074723 | 0.00071899 | 0.00070412 | 0.00068062 | 0.00066605 | 0.00064662 | 0.00061973 | 0.00060533 | 0.00060224 | 0.00057551 | 0.00054918 | 0.00052641 | 0.00053326 | 0.00050617 | 0.00051107 | 0.00049898 | 0.00047174 | 0.00047812 | 0.00045401 | 0.00044584 | 0.00045533 | 0.00045221 | 0.00043457 | 0.00042407 | 0.00043148 | 0.00042847
RF1080 Sample 1 | 0.0025416 | 0.002488 | 0.0024436 | 0.0023504 | 0.0022893 | 0.0021903 | 0.0021233 | 0.0020574 | 0.0020184 | 0.0018897 | 0.0018529 | 0.0017875 | 0.0017605 | 0.0016886 | 0.0016043 | 0.0015853 | 0.0015189 | 0.0014876 | 0.0014975 | 0.0014458 | 0.0013534 | 0.0012936 | 0.0012389 | 0.0011987 | 0.0011648 | 0.0011549 | 0.0011047 | 0.0010885 | 0.001046 | 0.001009 | 0.0009788 | 0.00094979 | 0.00092041 | 0.00084107 | 0.00081001 | 0.00076324 | 0.00073469 | 0.00069267 | 0.00069317 | 0.00065334 | 0.00062733 | 0.00061432 | 0.00056263 | 0.00052435 | 0.00049751 | 0.00052518 | 0.00049825 | 0.00049039 | 0.00047096 | 0.00047807
Cap Inner Sample Test2 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.0017754 | 0.0016529 | 0.0016226 | 0.0014969 | 0.001454 | 0.0013684 | 0.0013137 | 0.0012329 | 0.0011702 | 0.0011362 | 0.001059 | 0.0010322 | 0.00096875 | 0.00094452 | 0.00092969 | 0.00088763 | 0.00085646 | 0.00081657 | 0.00076507 | 0.00073803 | 0.00070138 | 0.0006972 | 0.00066786 | 0.00063922 | 0.00060908 | 0.00060557 | 0.0006036 | 0.00054623 | 0.00057888 | 0.00055667 | 0.00055632 | 0.00053884 | 0.0005206 | 0.00051746 | 0.0005044 | 0.00050136 | 0.0004812 | 0.00048167 | 0.00046862 | 0.00046186
PFC_Sample2_NoGap_(AL995) | 0.0001446 | 0.00014446 | 0.00018019 | 0.00018038 | 0.0001939 | 0.00015536 | 0.00014532 | 0.00021859 | 0.00019222 | 0.00018699 | 0.0001626 | 0.00014214 | 0.00017455 | 0.0001692 | 0.00016581 | 0.00019503 | 0.0001753 | 0.00018158 | 0.00015095 | 0.00016896 | 0.00016644 | 0.00015586 | 0.00015112 | 0.00015046 | 0.00015452 | 0.0001533 | 0.00015681 | 0.00014552 | 0.0001712 | 0.00019163 | 0.0002147
PFC_Sample2_Gap_(AL995) | 0.00014202 | 0.00010336 | 0.00015081 | 0.00014827 | 6.903e-05 | 8.7734e-05 | 0.00013056 | 0.00016505 | 0.00017033 | 0.00021079 | 0.00018497 | 0.00014135 | 0.00012108 | 0.00012271 | 0.00016973 | 0.00019116 | 0.00022057 | 0.00021476 | 0.00019609 | 0.0001796 | 0.00018371 | 0.00018826 | 0.00022214 | 0.00023269 | 0.00025641 | 0.00030136 | 0.00026832 | 0.00028392 | 0.00032014 | 0.0004395
New 99.7% | 0.01679 | 0.018605 | 0.019693 | 0.020174 | 0.019095 | 0.018096 | 0.014176 | 0.012079
Temperature (°C)
tanδ

## Slide 10: New 9MHz System Current Efforts
  Dielectric Material Test Cavity (50MHz)
Bare Cavity (Picture)
Pertinent Parameters

## Slide 11: New 9MHz System Current Efforts
  Dielectric Material Test Cavity (50MHz)
Testing RF1080 Sample 2 (Video)
Pertinent Parameters

## Slide 12: New 9MHz System Conclusions
  Summary
    Overall the new 9MHz systems performed reliably during the FY17 PP run
    High intensity fast ramping fills provided a good test of system design margins
    Current efforts are focused on the enhancement of peak voltage margin
      LEReC CW Voltage Requirement = 53.4kV (160kV per ring)
      Current CW Voltage Limit ≈ 72kV CW (Goal = 80kV)

## Slide 13: New 9MHz System Conclusions
  Summary
    Overall the new 9MHz systems performed reliably during the FY17 PP run
    High intensity fast ramping fills provided a good test of system design margins
    Current efforts are focused on the enhancement of peak voltage margin
      LEReC CW Voltage Requirement = 53.4kV (160kV per ring)
      Current CW Voltage Limit ≈ 72kV CW (Goal = 80kV)
    This is for if when we find ourselves in a bind.

## Slide 14: Thank you