## Slide 1: OB stave prototyping

## Slide 2: EIC-LAS thermal specifications
2 power scenarios: typical/max
  Chip design still evolving
  Power depends on temperature
Requirement | LEC | RSU | AncASIC
Maximum T [◦C] | 65 | 40 | 80
Maximum T variation [◦C] | 10 | 1 over 3 mm 10 over full length | 10
 |  | Typical | Max
LEC | Power [mW] | 160 | 208
 | P density [mW/cm2] | 182 | 236
per RSU | Power [mW] | 146 | 208
 | P density [mW/cm2] | 34 | 48
5-RSU LAS (L4) [mW] |  | 890 | 1246
6-RSU LAS (L3) [mW] |  | 1036 | 1454
AncASIC |  | 35% of LAS | 45% of LAS
FPC |  | 20% of LAS | 30% of LAS
L3 Stave (8×6-RSU LAS) [W] |  | 12.8 | 16.9
L4 Stave (16×5-RSU LAS) [W] |  | 22.1 | 34.9
114.330
4.500
19.564
LEC
RSU
RSU
RSU
RSU
RSU
4.5
Temperature requirements

## Slide 3: Stave manufacture – internal mould
Pre-cure the central I-beam
Assemble internal parts on internal mould parts
  Internal mould for less challenging tolerances and assembly
  Moulds are segmented into two halves with 3 parts each (wire-EDM)
    Clamp around the central I-beam
    Skewered onto two silver steel rods for straightness
Add FPCs on the sides (positioned by dowel pins)
Cover with pre-cut CF pre-preg (K13C2U/EX1515 0/90
Cover with release film, breather and vacuum bag for autoclave cure
⌀ 3 mm Silver Steel rods
K9 foam heatsink

## Slide 4: L4 prototype manufacture – issues encountered
We used expired CF pre-preg left over from other projects
  Reduced tackiness caused movement of narrow sections during cure
  Bond between I-beams and facesheet detached – tried to fix with Araldite, but not clear how reliable
We did not have enough K9 for all cross-ribs so used foam with poor thermal conductivity for M1 and M2
Resin seepage into the gaps between the mould parts
  This made removal, especially of the outer parts, difficult and some damage to the thin facesheet was incurred – this was repaired by gluing 25 µm Kapton over the damage
All these caused weaknesses of the structure, resulting in leaks that were patched with 25 µm Kapton glued on with Araldite
  In particular, the poor adhesion of some I-beam sections resulted in bulging out of facesheets under pressure with subsequent bursting
K9 cross-ribs
Non-conductive cross-ribs
M1
M2
LEC
LEC
LEC
LEC
LEC
LEC
LEC
LEC
M3
M4
M5
M6
M7
M8

## Slide 5: Dummy heater modules
Use dummy modules made of 50 µm steel shim stock, covered with Kapton/Cu heater circuits
Heater circuits have three different areas to replicate AncASIC, LEC and RSUs with their different power densities
Dimensionally similar to modules (2×5-RSU LAS + 2×AncASIC), but steel has larger CTE and higher modulus than silicon
Power density ratio inspired by LAS but not exact (LEC/RSU: heater 17.4, final typical 4.9)
Full dummy module | AncASIC | LEC | RSUs
R [Ω] | 0.88 | 0.90 | 1.53
A [mm2] | 112 | 132 | 3959
R/A [mW/mm2A2] | 7.86 | 6.79 | 0.39
RSUs
LEC
AncASIC
40 mm (2 LAS)
121 mm (for 5-RSU LAS + AncASIC)

## Slide 6: Test setup
TI camera
fixed
constraint
fixed
constraint
heater
heater
heater
4 more heaters on backside
(interleaved)
heater
capacitive
displacement
sensors
Air
in
Air out (to atmosphere)
M7
M5
M3
M1
LEC
LEC
LEC
LEC
Fixed-fixed support conditions

## Slide 7: Pressure drop vs air flow
Input pressure is measured in feed line
Stave is venting to atmosphere
No power, but makes little difference
Pressure drop depends (mildly) quadratically on flow mostly laminar
Biggest obstruction are cross-ribs
  Central hole for the steel rods during assembly, but also to facilitate air flow
  Might add more holes for that
Leaks pop at 150 l/min (~0.4 bar)

## Slide 8: Module temperatures – Module 7
Parallel flow from module 1 end
Module temperature measured with thermal imaging camera
  AncASIC, LEC and RSU temperature quoted is hottest temperature in component area
Affected by natural convection and proximity
  For example, hottest point on RSU is always close to LEC
T [°C]

## Slide 9: Output air temperatures
Air out temperature is measured by TC in exhaust line
Significant difference (~factor 1.5) between power supplied to stave and power removed by air flow (heat capacity of air J/kg/K, density 1.2 kg/m3)
  must have gone to natural convection
Surprising: Higher airflow (which keeps stave colder) results in higher fraction removed by natural convection?...

## Slide 10: Displacements
Displacements measured with capacitive sensors at centre of stave
Sampled in 1 s windows at 5 kHz
RMS displacements smaller than expected
  Little variation with flow
  RMS is dominated by macroscopic deformations due to
    Internal air pressure
    Temperature (power)
Top view
Sensor 3
Sensor 1 & 2
Front view
Sensor 1
Sensor 3
Sensor 2

## Slide 11: Gradual deformations - pressure
All sensors move in the same direction (out)
Stave core expands with pressure
This could be enhanced due to poor bonding of facesheet with I-beam
No power

## Slide 12: Gradual deformations – temperature
We do expect some temperature-dependent deformations due to CTE mismatch
Expect this to be much smaller for silicon modules
  Steel CTE ~12 µm/m°C, E ~200 GPa
  Silicon CTE ~2.6 µm/m°C, E ~160 GPa
Observe about 30 µm/3 °C variation of the LEC temperature
This is in the centre of the stave, could be larger locally
  Future investigations
Pressure increase all sensors move out
Temperature variation Sensors 1&2 move in the same absolute direction to 3

## Slide 13: Module temperatures – Module 5
Heat removal capability (ΔT/P) worse than M7
  Still within specs (TLEC < 65°C, TRSU < 40°C) at 150 l/min
  Possibly more significant internal damage
Interestingly also higher ΔT/P for air out temperature

## Slide 14: Module temperatures – Module 2
Moved stave with all instrumentation to allow access from rear
M2 does not have a K9 cross-rib
  So we expected to do worse than M5/7 in the AncASIC/LEC area
  We see the opposite
  RSUs have been so cold that temperature data were dominated by reflections from the environment
It appears from the TI that the two halves of the module saw different cooling
Air flow cooling power vs input power looks more sensible and much better than for the runs for M7
  But: this data is not module-specific (relies on stave power and air outlet temperature)???

## Slide 15: Counterflow measurements
We wanted to investigate counter-flow of air
  But we were concerned whether the central I beam still acts as a barrier
  So, we connected air flow to one half of the stave and measured flow in and out, and indeed the flow out was only a small fraction, so counterflow likely would turn around immediately
  So, we gave up on this – will investigate with future stave

## Slide 16: Conclusions
Stave manufacture
  Good: Stave manufacture with internal moulds
  Bad: Removal of outer mould sections is too difficult, causing damage to facesheets will try covering mould surface with low-tack tape
  Bad: Poor adhesion of face sheets (due to expired material?)
Mechanical performance
  Good: Low air flow-induced vibrations
  Bad: Pressure drop in the stave is too high, causes mechanical damage additional holes into cross-ribs for future designs
  Need to understand better: Outward push of stave surfaces due to internal air flow (could be due to internal damage)
Thermal performance
  Good: AncASIC/LEC/RSU temperatures are within specifications (on the better modules we could operate with much lower air flow)
    It appears that heat conductivity of cross-ribs is not that relevant
  The large fraction of heat removed by natural convection, and the strange behaviour for one stave needs further study
Thermo-mechanical performance
  Need to understand better: stave movement with power/temperature variations: Is the magnitude as expected? Can we stabilise temperatures sufficiently?
We still need to
  Learn how to build modules (in particular curved)
  Study temperature uniformity within RSUs
  Investigate the effect of counter-current flow
  Design the end supports to maintain stave stiffness, while allowing for tolerances, and couple in air-flow

## Slide 17: Further material

## Slide 18: MOSAIX/EIC-LAS

## Slide 19: OB layout parameters
19
Baseline is castellated layout
Nominal is original SVT specification, design is optimised for sensor size, overlaps, overall integration (disks)
Layer | radius [mm] |  | length [mm] |  | # of staves | target X/X0
 | nominal | design | nominal | design |  | 
L3 | 270 | 262/268 | 540 | Overall 550 (active 503) | 44 | 0.25%
L4 | 420 | 417/423 | 820 | Overall 840 (active 793) | 70 | 0.55%

## Slide 20: OB layout

## Slide 21
Modules are small units that can be tested before integration into staves
2 EIC-LAS + 2 AncASICs
Glued to Kapton module carrier
  Contains trace layers to allow to act as bridge FPC
EIC-LAS and AncASIC connections wire-bonded to bridge FPC
Modules need to be assembled on jig and stay on there for protection until they get glued onto stave
  Jigs will be used during transport from module production to module loading site
Currently prototyping flat modules as a first step
  Curved modules will require assembly on a curved jig
  Challenge for curved modules will be bonding
    Sensor will be curved, AncASIC flat

## Slide 22: Module – FPC electrical interface
Modules will be glued to the stave core to close the air channel and contribute to the stave stiffness
Electrical connections between the module and the stave FPC will be made using sp-TAB
  Requires stave FPC to bridge FPC alignment of ±0.025 mm
  Module will be aligned based on local reference features on the FPC instead of a global module alignment
Stave FPC
Bridge FPC

## Slide 23: Stave mounting
Support off L4
Support IB
Support D0
Air supply duct
Inlet
Diffused Outlet
L3 stave
Inlet CSA of 30 mm2 (equivalent to ⌀6 mm)
  Flow velocity at inlet will be approx. 4× internal flow velocity

## Slide 24: Preformed components
  Carbon Fibre I-beam pre-cured in a 2-part mould
  Flexible Printed Circuits (FPC) preformed (with heat and pressure) into C channel

## Slide 25
Based on old geometry with minimum overlap between modules
  Up to date L4 stave would be shorter (by approx. 50 mm)
New tooling for FPC & I-beam manufacture tested
  Kapton thermal forming tooling works well, alignment holes are very effective
  I-beam tooling may need refinement, very difficult to remove
6 of 18 K9 foam blocks replaced with Rohacell 110
  Low thermal conductivity, closed cell foam, holes added to allow airflow
Redesigned stave ends for vibration & flow testing
CF Trimming Tool
Kapton FPC Forming Tooling
Stave End Supports

## Slide 26: L4 prototype co-curing
End pieces with optimised air flow
K9 cross-ribs
Non-conductive cross-ribs

## Slide 27: Post-Cured Stave Assembly (quarterstave)