## Slide 1
Thermal Neutron Scattering in Graphite
Ayman I. Hawari
Nuclear Reactor Program
Department of Nuclear Engineering
North Carolina State University
Raleigh, North Carolina, USA
US National Nuclear Data Week 2017
November 6 – 10, 2017 • Brookhaven National Laboratory, Upton, NY, USA

## Slide 2: Graphite
Hexagonal Structure
4 atoms per unit cell
a = b = 2.46 Å
c = 6.7 Å
Density = 2.25 g/cm3
Ideal “crystalline” graphite consists of planes (sheets) of carbon atoms arranged in a hexagonal lattice. Covalent bonding exits between intraplaner atoms, while the interplaner bonding is of the weak Van der Waals type. The planes are stacked in an “abab” sequence.
Nuclear Graphite (SEM at NCSU)
Density = 1.5 – 1.8 g/cm3
Reactor graphite consists of ideal graphite crystallites (randomly oriented) in a carbon binder. It is highly porous structure with porosity level ranging between 10% and 30%.

## Slide 3: Thermalization in Graphite TREAT Reactor
Highlighted values are calculated using ENDF/B-VII.1 type S(a,b) libraries

## Slide 4: Thermalization in Graphite

## Slide 5: Thermalization in Graphite

## Slide 6: Methods
A. I. Hawari, “Modern Techniques for Inelastic Thermal Neutron Scattering Analysis,” Nuclear Data Sheets, Vol. 118, 172, 2014.

## Slide 7: Graphite TSL 2016-2017
Material | Method | Comments
Beta4 crystalline graphite | DFT/LD | NJOY inelastic + hexagonal coherent elastic model
Beta4 reactor graphite (10% porosity) | MD | NJOY inelastic + hexagonal coherent elastic model
Beta5 crystalline graphite | DFT/LD | NJOY inelastic + hexagonal coherent elastic model (supersedes Beta4)
Beta5 reactor graphite (10% porosity) | MD | NJOY inelastic + hexagonal coherent elastic model (supersedes Beta4)
Crystalline graphite | DFT/LD | NJOY (inelastic + elastic cubic approximation)
Reactor graphite (10% and 30% porosity) | MD | NJOY (inelastic + elastic cubic approximation)

## Slide 8: Graphite TSL 2016-2017
Material | Method | Comments
Beta5 crystalline graphite | DFT/LD | NJOY inelastic + hexagonal coherent elastic model (supersedes Beta4)
Beta5 reactor graphite (10% porosity) | MD | NJOY inelastic + hexagonal coherent elastic model (supersedes Beta4)
Crystalline graphite | DFT/LD | NJOY (inelastic + elastic cubic approximation)
Reactor graphite (10% and 30% porosity) | MD | NJOY (inelastic + elastic cubic approximation)

## Slide 9: Graphite Thermal Scattering Cross Sections

## Slide 10: Experimental Setup – NIST NG #6

## Slide 11: Graphite Thermal Scattering Cross Sections

## Slide 12: Graphite Thermal Scattering Cross Sections

## Slide 13: Summary - Graphite
Graphite is not a unique material
  Ideal “crystalline” graphite density = 2.25 g/cm3
  “Reactor” graphite density = 1.5-1.8 g/cm3
The total thermal scattering cross section of graphite depends on the specifics of graphite manufacturing
Transmission measurements below the Bragg cutoff (E < 0.002 meV) are useful to test various types of graphite

## Slide 14: Graphite AILD Model
VASP and PHONON codes
4 × 4 × 4 supercell (256 atoms)
4× 4 × 2 k-mesh
650 eV plane wave cutoff
GGA density functional
VDW interactions

## Slide 15: Graphite Thermal Scattering Cross Sections

## Slide 16: Graphite Thermal Scattering Cross Sections

## Slide 17: SANS in Graphite
SANS is an experimental artifact
Must be removed (by design) to measure the true total (inelastic) thermal scattering cross section below the Bragg cutoff
If not removed, it will artificially inflate the total cross section below the Bragg cutoff
Its impact is reduced as the neutron wavelength increases

## Slide 18: Graphite Thermal Scattering Cross Sections

## Slide 19: Graphite Thermal Scattering Cross Sections

## Slide 20: Graphite Thermal Scattering Cross Sections

## Slide 21: Reactor Graphite Model
Construct an atomistic model of a carbon structure that contains a porosity concentration consistent with “reactor graphite”
  Molecular dynamics ideal graphite supercell
  Removed single vacancies randomly to reach various porosity levels
  Obtained velocity autocorrelation function (VACF)
  From VACF obtained the density of states (i.e., phonon spectrum)
  Used phonon spectrum in NJOY/LEAPR and/or FLASSH to calculate TSL, inelastic cross section, and elastic cross sections

## Slide 22: Reactor Graphite MD Models
8000 atoms
300 K
10%-30% porosity
Notes: .

## Slide 23: SNS Measurements
Notes: .

## Slide 24: Graphite Thermal Scattering Cross Sections

## Slide 25: Graphite Thermal Scattering Cross Sections

## Slide 26: Graphite Thermal Scattering Cross Sections

## Slide 27: Graphite Thermal Scattering Cross Sections

## Slide 28: Benchmarks
Material | Method | Comments
Beta5 crystalline graphite | DFT/LD | NJOY inelastic + hexagonal coherent elastic model (supersedes Beta4)
Beta5 reactor graphite (10% porosity) | MD | NJOY inelastic + hexagonal coherent elastic model (supersedes Beta4)
Crystalline graphite | DFT/LD | NJOY (inelastic + elastic cubic approximation)
Reactor graphite (10% and 30% porosity) | MD | NJOY (inelastic + elastic cubic approximation)

## Slide 29
Notes: The focusing effect is because the high energy neutron will have more collision v*Sigma than the low energy neutron, therefore high energy neutrons will be slowed down faster than low energy neutrons.
Only the no absorption xsec and almost constant elastic xsec moderator will have this effect.

## Slide 30: ORELA TSL Benchmark – Top Detector

## Slide 31: ORELA TSL Benchmark – Top Detector

## Slide 32: ORELA TSL Benchmark – Top Detector

## Slide 33: ORELA TSL Benchmark – Back Detector

## Slide 34: ORELA TSL Benchmark – Back Detector

## Slide 35: ORELA TSL Benchmark – Back Detector

## Slide 36: Summary ORELA TSL Benchmark
Use of “reactor graphite” libraries improves the agreement between calculated and measured detector responses in the ORELA experiment.
The improvement is most noticeable when 30% porosity cubic data is used.
  No hexagonal 30% porosity model TSL library was generated!
For the 10% porosity data, the hexagonal version seems to shift the predicted detector response towards lower energies.
  Correlates with trend in the total cross section

## Slide 37: LEU_COMP_THERM_060 Benchmark

## Slide 38: LEU_COMP_THERM_060 Benchmark

## Slide 39: LEU_COMP_THERM_060 Benchmark

## Slide 40: HEU_COMP_THERM_016 Benchmark

## Slide 41: HEU_COMP_THERM_016 Benchmark

## Slide 42: HEU_COMP_THERM_016 Benchmark

## Slide 43: TREAT M2 Experiment

## Slide 44: TREAT M2 Experiment

## Slide 45: TREAT M2 Experiment

## Slide 46: Benchmarks Summary
For the LEU Benchmark, the Beta5 and cubic graphite TSL libraries show improvement relative to ENDF/B-VII.1.
For the HEU Benchmark, the Beta5 reactor graphite library falls above the uncertainty band. However, the cubic libraries fall in the band or are close to it.
For TREAT M2 experiment model, the Beta5 and cubic graphite TSL libraries yield larger keff relative to ENDF/B-VII.1.

## Slide 47: UO2
3.21E-3 | 0 | 0
0 | 3.21E-3 | 0
0 | 0 | 3.21E-3
Cubic Approximation
Debye-Waller Matrix ()
Tetragonal System

## Slide 48: UO2
3.19E-3 | 1.62E-6 | 9.03E-7
1.62E-6 | 3.19E-3 | -3.48E-7
9.03E-7 | -3.48E-7 | 3.22E-3
3.21E-3 | 0 | 0
0 | 3.21E-3 | 0
0 | 0 | 3.21E-3
-0.62% | - | -
- | -0.62% | -
- | - | +0.31%
Tetragonal Analysis
Debye-Waller Matrix ()
Cubic Approximation
Debye-Waller Matrix ()
Difference
Tetragonal System

## Slide 49: Beryllium Oxide
4.14E-3 | 0 | 0
0 | 4.14E-3 | 0
0 | 0 | 4.14E-3
Cubic Approximation
Debye-Waller Matrix ()
Hexagonal System

## Slide 50: Beryllium Oxide
4.22E-3 | -7.88E-5 | -1.22E-5
-7.88E-5 | 4.12E-3 | 1.75E-7
-1.22E-5 | 1.75E-7 | 4.42E-3
4.14E-3 | 0 | 0
0 | 4.14E-3 | 0
0 | 0 | 4.14E-3
+1.93% | - | -
- | -0.48% | -
- | - | +6.76%
Difference
Hexagonal Analysis
Debye-Waller Matrix ()
Cubic Approximation
Debye-Waller Matrix ()
Hexagonal System

## Slide 51: Summary
Graphite TSL investigation at NCSU has been an intensive computational and experimental effort.
Graphite is an a complex material. Its thermal neutron scattering depends on its manufacturing details (e.g., porosity).
  Total cross section (transmission) measurements especially below the Bragg cutoff may help.
Slowing down experiments (without fuel) are very useful in isolating thermalization effects.
In the current situation, the outcome of transmission measurements, ORELA slowing down measurements, and the computational benchmarks, seem to correlate best for the “cubic” treatment of crystalline and reactor graphite TSL libraries.

## Slide 52: Summary
Motivated the development of modern predictive methods for thermal neutron cross section calculations based on the use of atomistic simulations
  Ab initio lattice dynamics
  Molecular dynamics (ab initio and classical)
Many TSL evaluations contributed to ENDF/VIII
  Many are coming
Motivated FLASSH: a new thermal scattering analysis platform that uses a generalized theoretical approach for TSL calculations.