## Slide 1: Photocathode production, transport and use
Erdong Wang on behalf of photocathode team
Brookhaven National Laboratory

## Slide 2: Outline
Overview of photocathode systems for LEReC
Achievements
Upgrades of cathode growth system and cathode transport
To do list
Questions and answers
Summary

## Slide 3: Photocathode growth systems
K
K
e e
Mo
Sb
KxSb
CsK2Sb

## Slide 4: Cathode transport system
2 Ferris wheels are in use.
Third one is in assembly.

## Slide 5: Progress in this run_cathode growth I
We switched Na2KSb to CsK2Sb which we have many years experience.
- Quickly get into production mode.
The homemade Effusion cells have been changed to Commercial SAES alkali source.
    - Reliable and sufficient for growing 12 cathodes.
The co-evaporation has been changed to sequential evaporation.
    - Controllable and simplified recipe; Better uniform.
Total: 31
Tested in gun:10

## Slide 6: Progress in this run_cathode growth II
X-Y stage for cathode uniformity measurement are available.
  -Fast QE scan, save couple hours.
Pre-heating chamber has been installed.
  -Heat two pucks together, save a half day.
Developed a detail procedure.
  -Reproducible and reliable
LEDs replace lasers in cathode preparation
-For small and off-center cathode preparation avoid time consuming laser alignment

## Slide 7: Upgrade on 1st deposition system
Fix damaged parts
-Two 30 years valves; leaked wobble stick;
Off-center mask installation
- Fixed 6 mm diameter ,off-center 4mm, Ti mask
Improve the vacuum
-Install a NEG cartridge in growth chamber.
Replace the borrowed RGA.
Three to four weeks upgrade. In progress.

## Slide 8: Cathode transport at 2017
 | Material | Suitcase | Lab QE | In Gun QE (est)
Cath#1 | Na2KSb | #2 | 1.7% | 0.1%
Cath#2 | Na2KSb | #1 | 7% | 0.3%
Cath#3 | Na2KSb | #2 | 4% | 1.2 %
Cath#4 | CsK2Sb | #1 | 5% | 0.7%
Single cathode transport is not work due to cathode cold gas trap…
We were in trouble at 2017…

## Slide 9: Progress in cathode transport at 2018
Load lock has been baked for 52 hrs, no QE drops!
Change valve and seal
Very well bake
8 Cathodes were prepared in 10 days. All survive with good QE in transport.
Problem solved !

## Slide 10: Lessons we learned
Not well bake : leaking, virture leak, spray seal…
Pucks exposed to bad vacuum for long time.
Not only bad initial QE, also very short lifetime

## Slide 11: Next step
The second cathode deposition chamber has been designed and in fabrication.(schedule into production mode by mid-Nov.)
  Movable off-center mask
  Evaporation efficiency design, could grow more cathodes and quickly.
Ferris wheel
Exchange chamber
Puck exchange equipment has been designed and will be available next year.
  Avoid multiple bakes on FW
  Quick turn around, save weeks.
Study NaK2Sb recipe in shutdown
  May increase lifetime
Clean room setup at Bldg 535
Puck cooling device: Shorten the time for growing cathodes.
Dual puck pre-heating chamber-manipulator design: Convince to transfer puck.
Providing capability to hold two pucks in the deposition chamber.
Providing short evaporation distance for the sources on the cathode deposition chambers: Save alkali material.

## Slide 12: Questions and answers
Will off cathode area help with constant requirement to re-condition the Gun after CW running?
Answer: Yes and no. Cathode material may drop to the electrodes and reduce the work function…
However, both JLab and Cornell don’t need re-conditioning; QE increasing on discolor spots also not support cathode material peel off, it may be caused by crystal annealing.
Go to higher voltage and stay there for more than 24 hrs.
Many hours
My opinion: The gun may not be fully conditioned. The radiation must be exactly zero after HV conditioning.

## Slide 13: Summary
The cathode deposition system has been commissioned and demonstrated its capability of producing high QE and uniform bi-alkali antimonide photocathodes repeatedly.
We will provide off-center and small area cathode after deposition system upgrade.
The cathode transportation and storage system works very well. Recent results show that all 8 cathodes has no QE decay in cathode transport, load-lock bake and cathode transferring.
Second deposition system, puck exchange chamber, third Ferris wheel will be ready for next year run.

## Slide 14: Photocathode team
Joe Tuozzolo
Mengjia Gaowei
CJ Liaw (with all designer support)
John Walsh
Robert D Lehn
Donald Vonlintig
Mike Mapes (all techs support)
John Smedley
Zenggong Jiang

## Slide 15
Thanks for your attention!

## Slide 16: Cathodes
Second cathode production system, timeline?
Production of cathode with off center active area.
Looks like we have established reliable cathode production with very good QE.
Cathode delivery and baking procedure is also established.
Will off cathode area help with constant requirement to re-condition the Gun after CW running?