## Slide 1: Next Steps for CO2 System at B820 Igor Pogorelsky (ATF)
21st ATF Program Advisory Committee and Users’ Meeting
November 14-16, 2018

## Slide 2: History of ATF CO2 laser upgrades
1995-2015
10x power increase every 7 years
Reached saturation at <2 TW due to fundamental limitations of short-pulse amplification (B-integral)
2016-2017
Regrouped to implement new concepts
R&D to make new concepts productive
2018 and after
Continue initial trend of power increase
2020
2025
30 TW

## Slide 3: Scientific Needs Workshop 2017
Research Thrusts identified in SNW report:
Sub-ps, TW, mid-IR pulses: Pushing the CO2 laser technology into new paradigms of pulse duration and peak power is an important goal of the ATF. Accessing the sub-picosecond regime, while maintaining terawatt peak power, would be a major milestone for mid-IR laser development.
Mid-IR materials research: The availability of high peak power 10 micron pulses opens up many possibilities for important mid-IR materials research. Apart from characterization of perturbative nonlinearities, damage thresholds in the mid-IR are not well known.
Novel CO2 amplifier concepts: An example of a concept that might evolve in the near future is an optically pumped CO2 amplifier.
Enabled Priority Research Directions:
LWFA: The size of the wakefield structure is much larger than that driven by a MIR laser for the same intensity. This presents two significant opportunities: diagnosis of the wakefield acceleration process and controlled injection. Self-modulated 1 TW, 2ps; blowout 7 TW, 0.5 ps; bubble 25 TW, 0.5 ps.
Ion acceleration: Extend hole-boring radiation pressure ion acceleration to higher energy (10-20 MeV with 10 TW, 100 MeV with > 25 TW).
DLA, ICS, Laser Filamentation and Propagation in Atmosphere, IFEL, Electron Beam Phase Space Manipulation…

## Slide 4
CPA regime
Purpose: extract and transport beam from laser amplifier without nonlinear distortions
Recently completed upgrade thrusts
OPA
Ti:Al2O3
Amplifier 1
Stretcher
20 µJ
350 fs
5 µJ
80 ps
Amplifier 2
30 mJ
60 ps
Compressor
20J
~1 TW
4ps
Plasma
Shutter
YAG
Isotopic amplifiers
Purpose: produce a single 2ps pulse at elevated peak power
Plasma shutter
Purpose: block parasitic reflection from laser/plasma interaction point
ATF CO2 laser system a year ago

## Slide 5
OPA
Ti:Al2O3
Amplifier 1
Stretcher
20 µJ
350 fs
5 µJ
60 ps
Amplifier 2
30 mJ
40 ps
Compressor
20J
30 ps
YAG 2
Plasma Shutter
Efficiency 50%
10J
4 ps
2.3 ps
Energy
Pulse
In-vacuum transport to user experiments (prevents filamentation at high power)
Present-day laser configuration and planned upgrades
Upgrade R&D thrusts:
Reduce pulse expansion via stronger pulse stretching, reducing amplifier window thickness, beam profile control (apodizing, adaptive mirror)
Energy increase by improving compressor efficiency, stronger pulse stretching, implementing a bigger amplifier and window (long term)
Femtosecond regime with NLPC
        Variable polarization
        Material studies
Work on improving:
Rep. rate (faster HV switches, optical pumping)
Beam quality
Energy/power stability
System reliability
YAG 1
ps
fs

## Slide 6: Pulse expansion due to self-phase modulation
-integral
Known for CPA lasers since 1994
Increase pulse stretching
Reduce window thickness
Flatten beam profile
Ways to reduce B-integral:

## Slide 7: Reduce pulse expansion
via stronger pulse stretching
29 ps
62 ps
75 lines/mm
100 lines/mm
Stronger stretching results in significant reduction of the pulse expansion due to SPM
In addition, groove profile optimization for our compressor configuration may improve the compressor efficiency from the present 50% to >70%
12
14
16
~5 TW
CPA compressor
New matching gratings will be needed for both stretcher and compressor
Producing compressor gratings is more challenging due to bigger size and energy fluence
Experiment with 75 lines/mm
Expected with 100 lines/mm
@50% efficiency
Expected with 100 lines/mm
and 70% efficiency
2-2.5TW
3-4TW

## Slide 8: Reduce pulse expansion
reducing amplifier window stresses and thickness
10 atm
10 atm
local stresses cause cracking
chamfer removes local stresses
=2.72” compared to 4” used in present window design
1.5 reduction in B-integral
keeping 4” thickness allows to increase the window diameter to 6”

## Slide 9: Reduce SPM by beam expansion
gain
saturation
active beam
profile control
(apodization,
adaptive mirror)
0
R
-R
sin2
24 J
Expanded Gaussian beam subject to diffraction
after amplifier
10m distance
100
200
300
400
500
600
Maximum capability with the current final amplifier

## Slide 10: Approach to NLPC
2.5 J
1.7 J
0.7 J
0.9 J
1.3 J
0.5 J
75 mm
Self-focusing of a 4-ps pulse in 10-cm NaCl amplifier window (15 m from the amplifier)
No self-focusing
Self-focusing (2.5 J)
75 mm
No self-phase modulation
SPM (2.5 J, beam integral)
1 THz (~0.3 µm)
Now we are going to use this “parasitic” effect productively by compressing a self-chirped component and spatially filtering it out it via self-focusing with properly selected optical elements
n = n0 + n2I
Compressible portion of the pulse
Amplifier Output
SPM Focused Spatial Filtered
Recompressed
1.7 ps
100 fs
We already observed Kerr effect on the amplifier’s output window that leads to the beam’s spectral self-chirping and spatial self-focusing
)

## Slide 11
Subscale NLPC test using a fraction of the laser output
160 fs
0.3J
4.5 m
7.5 m
FWHM = 2 ps
1J
0.5 TW
1.5 TW
ZnSe
12mm
NaCl
60mm
Upon completion of this test, we will plan the full-scale implementation where NLPC is imbedded into the ATF transport line.
Starting with 5 TW, compressing to 15 TW might be feasible.

## Slide 12: Flexible polarization
16”
11.3”
11.3”
9”
8”
8”
12”
A circular polarizer
using a mirror with
a quarter-wave
coating
axis of rotation
3 mirrors on a platform rotating around the beam axis will be arranged to preserve the beam direction
Rotation of the platform by 450 off the initial plane of polarization makes the polarization flip by 900 after three reflections
Replacing the first Cu mirror with a mirror having a l/4 coating provides circular polarization
900 polarization
rotation

## Slide 13: Material studies
One of the scientific challenges in handling the extreme laser peak power at 9-10 mm wavelengths is that the behavior of optical materials remains largely unexplored in this spectral domain and regime.
We will continue detailed studies of:
  Damage thresholds and damage mechanisms of materials and structures generally used for both reflective and transmissive optics at the CO2 wavelength, including various coating/substrate combinations. Specific example: choosing the best substrate and coating for compressor gratings.
  Nonlinear optical properties (nonlinear refraction and absorption) of a broad range of semiconductor and dielectric materials. Specific example: study towards NLPC.
This effort is co-aligned with user interests.
See DLA proposal from Stanford/STIOptronics/Technion.
0.53 J/cm2
2.4 J/cm2
100 μm
10 J/cm2
Cu-Cu grating
3 J/cm2
9.7 J/cm2
Cu mirror
5 J/cm2
l/4 Si mirror
Examples from optical damage studies conducted at ATF

## Slide 14: Improving beam quality, laser stability and reliability
32 mm FWHM achieved at the focus of F#=2 off-axis parabola at M2=2.
We will continue dedicated efforts in analyzing the beam parameters, identifying sources of their degradation, and improving beam handling. A new design of a plasma shutter and in-vacuum beam transport are the examples.
Equal efforts will be directed towards providing the pulse format desirable for users and improving the energy reproducibility <10%.
An ongoing rigorous program of creating large inventory of critical spares aims to reduce downtime and improve system reliability.
Measuring M2 at different energy levels

## Slide 15: Higher repetition rates
Front end (including regen) operates at linac’s repetition rate and up to 5 Hz, while the final amplifier is presently at 0.03 Hz.
Marx generator’s spark gaps are capable to 0.1 Hz. We will explore the possibility moving to 0.1 Hz by faster capacitor charging and gas circulation.
Thyristors are identified as faster switches for use in Marx generators. We team with STI Optronics to develop the first version of a high-repetition (potentially up to 300 Hz) power amplifier used in intra-cavity pulse circulation experiments (high-duty ICS and high-duty IFEL)
Optical pumping:
High-repetition solid state lasers can be configured to pump a high-pressure CO2 gain vessel.
4.3mm
10mm
An additional benefit is in expanding the active medium choices (e.g., carbon isotopes, CO2/N2O) and using higher pressures (e.g., 30 atm) to increase gain and allow fs pulses. We team with Univ. of Alabama and UCLA in demonstrating CO2 optical pumping with a Fe:ZnSe laser.

## Slide 16: Keeping eye on safety
Implementing radiation fault studies at each incremental increase of the laser power
OAP
target
sphere
lens
IR camera
Plasma Shutter
Optical transport
Interaction Chamber
TLDs
Test sphere 6” diam.; windows are for placing TLDs around a target
laser
TLD
TLD
TLD
TLD

## Slide 17: Laser experimental requirements by topical area from the report of Scientific Needs Workshop 2017
Experiment | Entry Level Requirements | ATF Laser Upgrade
Nonlinear Kerr effect | 1 TW | Yes
Non-linear LWFA | ~2 TW | Yes
Blow-out LWFA | 5 TW, 0.5 ps | Yes, near term upgrade
Bubble LWFA | 25 TW, 0.5 ps | Possible, long term upgrade
Ion acceleration | 25 TW, circ. polar | Possible, long-term upgrade
IFEL | 25 TW | Possible, long term upgrade
DLA | 10 GW | Yes
ICS | 2 TW | Yes
Phase space manipulation | ~1 TW | Yes
ATF CO2 upgrade is matched to the scientific needs identified in SNW report

## Slide 18: Summary
Completed milestones including full CPA and isotope regimes, plasma shutter and in-vacuum transport open a path to further improvements in our service to users
FY2019 might see:
  power increase through a better control of B-integral with new gratings, smarter windows and apodizing mirrors
  first results from proof-of-principle NLPC
  polarization state control
FY2020-21:
  Design and implementation of a full-scale NLPC to allow access to the “blow-out” LWFA regime and other groundbreaking applications.